## Slide 1: Results of MQXF tests in SM18, FNAL, and BNL
Paolo Ferracin
on behalf of the MQXF collaboration
21st HL-LHC Technical Coordination Committee (TCC) meeting
CERN
24 Novemeber, 2016

## Slide 2: Acknowledgments
CERN
  A. Ballarino, H. Bajas, M. Bajko, B. Bordini, J.C. Perez, S. Izquierdo Bermudez, P. Fessia, C. Fichera, P. Grosclaude, M. Guinchard, P. Hagen, F. Lackner, H. Prin, E. Rochepault, S. Sequeira Tavares, E. Todesco, G. Vallone
BNL
  M. Anerella, A. Ghosh, J. Muratore, J. Schmalzle, P. Wanderer
FNAL
  G. Ambrosio, R. Bossert, G. Chlachidze, L. Cooley, E. Holik, S. Krave, F. Nobrega, I. Novitsky, S. Stoynev, T. Strauss, M. Yu,
LBNL
  D. Cheng, D.R. Dietderich, R. Hafalia, M. Marchevsky, H. Pan, I. Pong, E. Ravaioli, G. Sabbi, X. Wang
CEA Saclay
  H. Felice
LASA
  V. Marinozzi, M. Sorbi
Tampere Univerisity of Technology
  T. Salmi

## Slide 3: Outline
MQXFS1 and MQXFS1b
MQXFS3 and MQXFS3b
MQXFPM1

## Slide 4: Overview of magnets under test
MQXF1 (test at FNAL)
MQXF3 (test at CERN)
MQXFPM1
(test at BNL)

## Slide 5: …where we were
MQXFS1a
  Tested at FNAL in April 2016 with coils 3,5,103,104
  Exceeded ultimate current
  Demonstrated temperature margin and excellent memory
  Quenches distributed on the pole turn (end and straight section)
    Training was stopped to increase azimuthal preload

## Slide 6: Increase of pre-load of MQXFS1 MQXFS1b and assembly of MQXFS3
Unloading shifted
  Check impact on training
    trained magnet (MQXFS1b)
    virgin magnet (MQXFS3)
MQXFS1: 80 MPa
MQXFS1b: 100 MPa
MQXFS3 100 MPa

## Slide 7: A previous similar case
HQ02b: Much faster training up to 95% SSL after pre-load increase

## Slide 8: MQXFS1b Training
Re-loaded at LBNL in summer 2016, test in progress and FNAL
Again, good memory
Stably above ultimate
  Only 1 quench below
Slower training than MQXFS1a
Temperature margin
All quenches in the ends
88% of Iss at 1.9 K
95% of Iss at 4.5 K

## Slide 9: Outline
MQXFS1 and MQXFS1b
MQXFS3 and MQXFS3b
MQXFPM1

## Slide 10: MQXFS3
Tested at CERN in October 2016 with coils 105,106,107,7
Same azimuthal pre-load as MQXFS1b
At nominal in 7 quenches
Most of quenches in coil 105, ends of the inner layer
Slower training than MQXFS1b

## Slide 11: MQXFS3
Detraining after quench 19
Plateau
  coil 7, end region
    Same

## Slide 12: MQXFS3
Ramp-rate quenches
  Full recovery to initial maximum current
  Last 3 quenches in 105, straight section

## Slide 13: MQXFS3
Full recovery to initial maximum current

## Slide 14: MQXFS3
Again, temperature margin
81% of Iss at 1.9 K
89% of Iss at 4.5 K

## Slide 15: MQXFS1b vs. MQXFS3
MQXFS1b vs. MQXFS3
  Very similar axial and azimuthal pre-load
    wrt MQXFS1, same axial, +20 MPa azimuthal
  Similar training slope
    Although at different current level
      …but 1b not virgin
    Slower than MQXFS1a
  Similar quench locations
    End region, I3I4 segment

## Slide 16: Plans for MQXFS1 and MQXFS3 (I)
Analysis in progress
  More detailed analysis with quench antenna in MQXFS1b
    Adjusted quench antenna to pinpoint quench locations
  Comparison of HQ03 and MQXF pre-loading levels
    Strain gauges measurements
      Pole strain plateau levels
    Finite element model
      Ratio between axial load and e.m. forces
      Contact pressure between coil and end parts
      Model of the LE
  Check for differences between MQXFS1a/1b/3a

## Slide 17: Plans for MQXFS1 and MQXFS3 (II)
MQXFS3b
    Retest with axial pre-load increased
      Pre-load increased by about a factor two at cold
        No need of disassembly
    Insertion of a new quench antenna with 40 mm long coils
    Test expected in December 2016

## Slide 18: A previous similar case
From HD1 to HD1b, improved axial loading

## Slide 19: Plans for MQXFS1 and MQXFS3 (III)
MQXFS3c
  Full disassembly and coil visual inspection
  Reassembly and re-loading with higher azimuthal pre-stress
    Depending on 3b test and visual inspection
MQXFS1c (currently stainless steel shell test)
  Increase of axial pre-load under consideration

## Slide 20: Field quality
Good agreement with expected on saturation, allowed harmonics and persistent currents.
The dominant source of field errors is the coil geometry and its initial assembly in the collared coil  coil shimming
Magnetic shimming:
  Demonstrated the capability to correct 3 units of b3 and a3 in MQXFS1b
Successfully corrected 3 units of b4 in MQXFS3a.
Still work to do on a4 and b5

## Slide 21: Quench protection
Quench heater powering scheme was adapted to have conditions as close as possible to the full length magnet for the given constrains in SM18.
Outer layer heaters perform as expected.
Two inner layer heater strips were lost. Investigations needed to understand the source of the problems.
Quench integral studies indicate that the heaters effectively quench the magnet.
CLIC test in progress in MQXFS1b (first time on an MQXF model)
  As expected, a significant reduction of the quench load is achieved with respect to O-QH only

## Slide 22: Outline
MQXFS1 and MQXFS1b
MQXFS3 and MQXFS3b
MQXFPM1

## Slide 23: MQXFPM1 assembly

## Slide 24: MQXFPM1 test
Vertical Test Facility @ BNL commissioned in September-October 2016
Test results at 1.9 K
  First quench: 14387 A, 65% of Iss (22.1 kA)
    Outer layer mid-plane block
  Second quench: 16040 A, 73% of Iss
    Inner layer pole turn straight section
Replacement of IGBT blown at discharge of quench 2 in progress
Training resuming this week

## Slide 25: Appendix

## Slide 26: MQXFS1b Quench locations
aa