## Slide 1
Alexander V. Zlobin
US-EuroCirCol video meeting
18 October 2016
15 T Dipole Demonstrator: design parameters and work status

## Slide 2: US Magnet Development program
FNAL 15 T Dipole demonstrator is the program key milestone for FY17

## Slide 3: Coil Design Study [1]
Coil aperture: 60 mm
Coil cross-section: 4 layers, graded
Design parameters: Bmax, an/bn, coil volume, coil stress, quench protection
4L-1
4L-2
4L-3
4L-4
4L-5
Parameter | Cable 1 | Cable 2
Number of strands | 28 | 40
Strand ID, mm | 1.0 | 0.7
Mid-thickness, mm | 1.870 | 1.319
Width, mm | 15.10 | 15.10
Keystone angle, deg | 0.805 | 0.805

## Slide 4: Mechanical Structure [2], [3], [5]
Thin coil-yoke spacer (no collar)
Mechanical structure:
  Design 1: SS C-clamps and 20-mm thick skin
  Design 2: Al I-clamps and 12-mm thick skin
  Design 1: 50-mm thick Al shell
Axial support: thick SS rods and end plates
Cold mass OD<610 mm (VMTF Dewar limit)

## Slide 5: Magnet Design Specifications

## Slide 6: Strands and Cables [4]
Magnet short sample estimated based on the cable test data:
  11.1 kA (Bap=15.3 T) at 4.5 K
  12.2 kA (Bap=16.7 T) at 1.9 K
RRP150/169
RRP108/127

## Slide 7: 15 T Dipole Demonstrator Status
Magnet design study phase is complete
Magnet (design 2) and tooling engineering design is complete
  Engineering design of design 3 is planned for Q1 FY17
Tooling and parts procurement is in progress
L1-L2 cable was developed, fabricated and tested
L3-L4 cable is available from the 11 T dipole program
Outer (L3 and L4) and inner (L1 and L2) practice coils are complete
Coil fabrication has started
Magnet assembly and first tests are planned for summer 2017

## Slide 8: Publications
A.V. Zlobin, N. Andreev, E. Barzi, V.V. Kashikhin, I. Novitski, “Design concept and parameters of a 15 T Nb3Sn dipole demonstrator for a 100 TeV hadron collider”, IPAC2015, Richmond, May 2015.
V.V. Kashikhin, N. Andreev, E. Barzi, I. Novitski, A.V. Zlobin, “Magnetic and structural design of a 15 T Nb3Sn accelerator dipole model”, CEC/ICMC2015, Tucsan (AR), June 2015.
I. Novitski, N. Andreev, E. Barzi, J. Carmichael, V. V. Kashikhin, D. Turrioni, M. Yu, A.V. Zlobin, “Development of a 15 T Nb3Sn Accelerator Dipole Demonstrator at Fermilab”, IEEE Trans. on Appl. Supercond., Vol. 26, Issue 3, June 2016.
E. Barzi, N. Andreev, P. Li, V. Lombardo, D. Turrioni, A.V. Zlobin, “Nb3Sn RRP® Strand and Cable Development for a 15 T Dipole Demonstrator,” IEEE Trans. on Appl. Supercond., Vol. 26, Issue 3, June 2016.
I. Novitski, A.V. Zlobin, “Development and Comparison of Mechanical Structures for FNAL 15 T Nb3Sn Dipole Demonstrator”, NAPAC2016, Chicago, Oct 2016.