## Slide 1: 15T Demonstrator: mechanical design, analysis and optimization
Igor Novitski
Video Meeting
18 October 2016

## Slide 2: Outline
Magnet concept evolution
Models and Materials
Design 1: C-Clamp
Design 2: IC-Clamp
“HD-2” structure optimization
Design 3: AL Cylinder
Summary

## Slide 3: Magnet Concept Evolution
I-Clamp Magnet
Al Shell Magnet
C-Clamp Magnet

## Slide 4: Geometry Comparison
15T Dipole
D20
VMTF Dewar

## Slide 5: FEA Models
Coils in “HD2” Structure
C-Clamp Magnet
I-Clamp Magnet

## Slide 6: Material Properties
Structural element | Material | Thermal contract. (300-2 K), | Elasticity modulus, GPa |  | Yield stress, MPa | 
 |  | mm/m | warm | cold | warm | cold
Coil (rad/azim) | Nb3Sn composite | 2.9/3.3 | 35/20 | 40/40 | n/a | n/a
In.coil pole blocks | Ti-6Al-4V | 1.7 | 115 | 125 | 650 | >900
Out.coil pole blocks | St St | 2.9 | 195 | 215 | 230 | 500
Wedges | Bronze | 3.2 | 110 | 120 | 280 | 350
Coil-yoke spacer | St St | 2.9 | 190 | 210 | 230 | 500
Clamp | Aluminum | 4.1 | 70 | 81 | 500 | 700
Yoke | Iron | 2.0 | 205 | 225 | 220 | 500
Skin | St St 316 | 2.9 | 190 | 210 | 290 | 580

## Slide 7: Design 1: C-Clamp+20mm Skin, FEA Results
Inner Pole Gap=0.002mm
Seqv=120MPa
Seqv=158MPa
Seqv=179MPa
Seqv=725MPa
Seqv=850MPa
Seqv=880MPa
4K+15T
300K
4K

## Slide 8: Design 2: IC-Clamp+12mm Skin, FEA Model
X1
X2
Y2
Y1
d Skin and skin thickness
Clamp-Yoke
angle and
interference
Pole slot
Mid-Plane shims
Shell-Yoke Rad
interference
Clamp-Skin Rad
Yoke-Skin Rad
interference
Coil-Coil Rad
interference
Yoke-Yoke
gap taper
R
Step

## Slide 9: Design 2: IC-Clamp+12mm Skin, FEA Results
4K+15T
300K
4K
Inner Pole Gap=0mm
Seqv=133MPa
Seqv=176MPa
Seqv=168MPa
Spole=472MPa
Sskin=280MPa
Spole=724MPa
Sskin=404MPa
Syoke=448MPa
Sskin=428MPa

## Slide 10: Design 2: IC-Clamp+12mm Skin, FEA Results
4K+15T
300K
4K
Seqv=115MPa
Seqv=353MPa
Seqv=448MPa
Seqv=118MPa
Seqv=280MPa
Seqv=292MPa

## Slide 11: AL Shell Design
HD2
15 T Alternative

## Slide 12: Parametric Model of the Structure
1
2
3
4
Al Shell: 50 and 70 mm thick
Iron Pad: 2 or 4-piece
Iron Yoke: 2 or 4-piece

## Slide 13: Design 3: 50mm AL Cylinder, FEA Results
4K+15T
300K
4K
Seqv=118MPa
Seqv=190MPa
Seqv=165MPa
Inner Pole Gap=0.3um

## Slide 14: Design 3: 50mm AL Cylinder, FEA Results
4K+15T
300K
4K

## Slide 15
October 18, 2016
Alternative
Baseline
15 T Demonstrator Support Structures
Igor Novitski | Mechanical analysis

## Slide 16: Comparison of Baseline and Alternative Designs
Baseline at 15T:
Inner Pole Gap =0um
Layer 3 pole Gap=7um (20%)
Al Shell at 15T:
Inner Pole Gap=0.3um (30%)
Layer 3 pole Gap=4um (15%)
Contact gaps at poles

## Slide 17: Summary
  Several concepts of mechanical structure have been analysed and compared.
  Mechanical designs with IC-Clamps (Baseline) provides the required coil prestress and restricts turn radial, azimuthal and longitudinal motion for the operating current range up to 15T.
  Alternative magnet support structure based on a 50 mm thick aluminum shell, 4-piece iron yoke and 2-piece iron pad behave likewise.
  Both structures allow keeping the stresses in the coil and support structure within acceptable limits during magnet assembly and operation.