## Slide 1
Flattop quenches in MB magnets in the LHC until 15 July 2015
LHC quench behavior team
Meeting 16-07-2015
By Gerard Willering

## Slide 2
Hardware commissioning 2015
Training to 11.08 kA, plateau of 1 – 5 minutes
CFB test, 2 hours at 10.98 kA
Additional test at 11.08 kA for 2 hours (only 30 minutes for A34 and up to 5.5 hours for A45)
Operation at 10.98 kA
The quenches in the training cycle are not included in the flattop quenches.
For overview of MB training during HWC, see presentation in the LMC 8 April 2015

## Slide 3
# |  | Date | magnet | Current | Total time of the circuit at training current 11.08 (kA) (h) | Total time of the circuit at nominal of 10.98 kA (hours) | Flattop quench time (s) | Training cycle? | comment
 | RB.A23 |  | 2063 | 11080 | 0.0 | - | 5 | Y | 
 | RB.A34 |  | 2196 | 11080 | 0.0 | - | 95 | Y | 
1 | RB.A78 | 13/03/2015 | 2017 | 10980 | 0.1 | 0.2 | 310 | N | 
2 | RB.A56 | 08/02/2015 | 3358 | 11080 | 0.4 | 0.4 | 21 | N | 
3 | RB.A56 | 08/02/2015 | 3334 | 11080 | 0.4 | 0.4 | 1 | N | 
4 | RB.A78 | 14/03/2015 | 2014 | 10980 | 0.1 | 0.8 | 3000 | N | 
5 | RB.A34 | 03/04/2015 | 2067 | 11080 | 0.6 | 5.2 | 1860 | N | 
6 | RB.A78 | 25/03/2015 | 3264 | 11077 | 0.1 | 16.2 | 0 | N | 
7 | RB.A56 | 18/03/2015 | 3355 | 11080 | 1.6 | 19.3 | 5400 | N | 
8 | RB.A67 | 01/04/2015 | 3300 | 11038 | 2.2 | 95.3 | 8 | N | 
9 | RB.A34 | 14/05/2015 | 2092 | 10975 | 0.6 | 106.0 | 5640 | N | 
10 | RB.A34 | 11/06/2015 | 2101 | 10975 | 0.6 | 329.0 | 43200 | N | 
11 | RB.A34 | 09/07/2015 | 2172 | 10979 | 0.6 | 443.5 | 1020 | N | at the start of ramp down during precycle
Overview all Flattop quenches
The first 2 in the table were during the training cycle: I don’t count them in.
11 flattop quenches
6 quenches at training current level
  Magnets 2067, 3264, 3300, 3334, 3355 and 3358)
5 quenches at nominal current level
  2014, 2017, 2092, 2101 and 2172.
3 quenches during operation
  2092, 2101, 2172.
  All in RB.A34, the circuit that stayed the shortest time at training current level. Possible correlation?

## Slide 4
5 Flattop quenches at nominal current
Discussion
Quench origin: Mechanical or electrical?
Is there a correlation with flattop quenches and the short stay at training current, or are we just unlucky?
Followup
Train S34 longer at Itraining?
Check quenches during OSQAR tests (continuous current during)

## Slide 5
Year | Bench B | Bench E
2009 | MB2431 | MB2868
2010 | MB2431 | MB2868
2011 | MB2431 | MB2868
2012 | MB2111 | MB2102
2013 | MB2111 | MB2102
2014 | MB2111 | MB2102
2015 | MB2111 | none
What can we learn in SM18?
No specific plateau tests are performed. Standard test duration at ultimate current is 1 hour.
However, during the OSQAR tests MB magnets have been powered to ultimate for up to 17 days almost continuously at 12.85 kA
For future tests, a plateau at ultimate or at nominal current could be used to see if magnets quench.

## Slide 6
Magnet 2011 |  |  |  |  |  |  | 
Year | Type | Current | Location | Plateau time (h) | Total time at ultimate (h) |  | Comments
2006 | Training | 12115 | D2L | - |  | quench | 
2006 | Training | 12850 |  |  | 1 | No quench | 
2010 | Training | 11320 | D2U | - |  | quench | 
2010 | Training | 12850 |  |  | 1 | No quench | 
2012 | Training | 12406 | D1U | - |  | quench | 
2012 | Flattop | 12850 |  |  | Many short cycles | No quench | 
2013 | Training | 12850 |  |  |  | No quench | 
2013 | Flattop | 12850 |  |  | 380 | No quench | 
2014 | Flattop | 12851 | D1U | 5 seconds | 5 seconds | quench | 
2014 | Flattop | 12852 | D2L | 19 | 49 | Quench | 
2014 | Flattop | 12850 |  |  | 200 | No quench | Note: 200 consecutive hours at 12.85 kA
Magnet 2011 test overview

## Slide 7
Magnet 2102 |  |  |  |  |  |  | 
Year | Type | Current | Location | Plateau time (h) | Total time at ultimate (h) |  | Comments
2004 | Training | 11467 | D1U |  |  | Quench | 
2004 | Training | 12188 | D2L |  |  | Quench | 
2010 | Training | 11977 | D1U |  | 1 | quench | 
2010 | Training | 12647 | D1U |  |  | Quench | 
2010 | Training | 12850 |  |  |  | No quench | 
2010 | Training | 12850 | D2L |  |  | No quench | After thermal cycle
2010 | Training | 12716 | D2L |  |  | Quench | After thermal cycle
2010 | Training | 12850 |  |  |  | No quench | 
2012 | Training | 12850 |  |  |  | No quench | 
2013 | Training | 12850 |  |  |  | No quench | 
2013 | Flattop | 12850 | D2L | 10 | 20 | Quench | 
2013 | Flattop | 12850 | D2L | 1 | 180 | Quench | 
2013 | Flattop | 12850 |  |  | 70 | no quench | 
2014 | Training | 12850 |  |  |  | No quench | 
2014 | Flattop | 12850 | D2U | 9 | 28 | Quench | 
2014 | Flattop | 12850 |  |  | 400 | No quench | 
Magnet 2102 test overview
The OSQAR tests show that flattop quenches occur (at training current level of 12.85 kA), even after 20 or 180 hours.
How this relates to flattop quenches at nominal current is difficult to say.

## Slide 8
Conclusions
These are new data gathered for discussion.
Flattop quenches have occurred 3 times during operation, all in 2000-series magnets, all-in S34.