## Slide 1: TEST OF 3000 SERIES MAGNETS
E. Todesco
CERN, Geneva Switzerland
CERN, 16th March 2015
QBT meeting

## Slide 2: 2015 DATA
Analysis of G. Willering: batches of 10
  Until 3130 perfect performance
  Slow rise, reaching a max of 1.2 quenches/magnet at 3180
  Back to normal between 3310 and 3350

## Slide 3: 2015 DATA
Available spares: 3096, 3100, 3409
  3096 (good batch) tested in May 2010, 1st Q at 11826 A, 2nd at12850 A
  3100 (good batch) tested in May 2013, 1st Q at 12143 A, 2nd at12800 A
  3409 (bad batch) tested in Jan 2010, 1st Q at 11348 A, 2nd at12850 A
  So these data are consistent with training in the tunnel

## Slide 4: TENTATIVE COMPARISON BETWEEN 2015 and VIRGIN TRAINING
The degradation of the quench performance appears in the virgin data much earlier
  See plot below with running average of 50 magnets