## Slide 1: Transient Thermal Electromagnetic Behaviour of HL-LHC SC-Link Global Analysis and Experimental Studies
Y Yang, I Falorio, J Pelegrin, E A Young
University of Southampton, UK
S Giannelli, A Ballarino
CERN, Switzerland

## Slide 2: Outline
Background
Quench load and safe circuit discharge upon cable quench
Transient magnetic field imposed on neighbouring cables upon fast discharge of a circuit
AC loss measurements
Quench by local disturbances in helium gas

## Slide 3
A. Ballario, EUCAS 2013, Genova
20 kA
Six cables,  = 19.5 mm
Concentric  3 kA
Seven cables,  = 8.4 mm
0.4 kA
Four cables
0.12 kA
Eighteen cables
ext  65 mm
Layout of SC Link at LHC P1 and P5
18 MgB2 wires
 = 6.5 mm
Cu
MgB2 ,  = 1 mm

## Slide 4
Superconducting Material: State-of-the-art
Use of Nb barrier
wire = 1 mm
37 MgB2 filaments
Twisted filaments (LT=100 mm)
eq_MgB2 = 56 m
ACu  5 % Awire (th=30 m)
Cu plating
Sn coating of Cu surface
Ic(25 K, 0.9 T) > 186 A
Launched procurement of 80 km of wire
Unit lengths  500 m
20 km at CERN
60 km delivered before end 2015
Launched development of MgB2 round wire
A. Ballario, EUCAS 2015, Lyon

## Slide 5: Self-Fields and Inductances
Cables/Link layout
6x20kA , 7x3kA, 4x0.4kA, 8x.12kA
65mm
Lines of force Magnetic field
6x20kA fully powered
Main Characteristics
Maximum Field:
1x20kA: Bmax=0.47 T
(±)20kA: Bmax=0.90 T
3x(±)20kA: Bmax=0.75 T
Inductances
(±)20kA: L = 0.19 μH/m
3x(±)20kA: L = 0.32 μH/m
Insignificant compared to those of the magnets in circuit
3kA coaxial cables have minimum impact on the overall field distribution within the link, hence not considered.
0.12/0.4kA cables not exposed to the 20kA fields , hence not considered.

## Slide 6: Thermal Transients: Quench Load of Cables
Heating dynamic upon the quench of a cable
Assume that the normal zone has exceed the minimum propagation zone (MPZ) and longitudinal propagation has started.
Neglect the retardation due to (a) heat diffusion to un-quenched section and (b) cooling by GHe.
Assume a (sufficiently) small thermal/electrical contact resistance to the stabilizer.
The relevant calculation is the quench load (QL):
  is the superconductor fill factor.
  The stabilizer with a low resistivity shares total current.
  The specific heat (Jkg-1K-1) and density include both the superconducting wire and the stabilizer.
18-wire sub-cable and 20kA cable are thermal/electrically equivalent:
The inner layer of the 3kA coaxial cable is equivalent to 18-wire sub-cable and the outer layer is under-stabilized

## Slide 7: Thermal Transient: Quench of Cables
Quench load of 20kA cable
With a nominal Cu RRR=100 for the stabiliser:
The cable heats up to ~90K in 1 s at 17kA;
Room temperature is reached in approximately 3.5 s.
Little influence by the initial temperature and the contribution of monel.
Stabilizer RRR has a significant impact at low/medium temperature (55K in 1s) and a moderate improvement at high temperature (230K in 3.5 s)
When discharged at is matched by
Discharging at τ < 2 s virtually ensures that the maximum temperature will not exceed 100K.
Problem eliminated with a even faster discharge, but will likely be without energy extraction from magnets.

## Slide 8
Measurement performed at 15 K, 3000 A
Max hot-spot temperature reached Ths~340 K with no degradation of cable performance
25 K, 3 kA, 100 mV detection threshold  15 MIITS of “quench capital” before detection  final Tmax  150 K with 3 s time constant of the circuit
Hot spot temperature lower than QL: not fully propagated
Recent results at CERN:
consistent with QL calculation
A. Ballarino, 27/10/2015

## Slide 9: Electromagnetic Transient: Field imposed by a circuit discharge
Response of neighbouring cables upon a fast discharge of a magnet circuit
The net field change within the link is the same as the field produced by the fast discharging cable.
For a discharging current , the field change rate imposed on the link is , proportional to the field produced at .
+17kA
-17 kA

## Slide 10: Electromagnetic Transient: Field imposed by a circuit discharge
Imposed , electrical field and induced current
The maximum imposed field change is at immediate adjacent wires (30o and 150o) in the neighbouring cables.
At 20kA, at these locations is about 0.3T, or 40mT/s at .
About 4 wires are exposed at any longitudinal location. The sub-cable twist pitch of 400mm means that each wire is exposed for about 90mm.
0.3T @17kA

## Slide 11: Electromagnetic Transient: Field imposed by a circuit discharge
Coupling loops, induced current and dissipation
Two distinct coupling loops
  Intra-wire coupling among the filaments within individual wires
  Inter-wire coupling among the wires within a sub-cable across the copper stabilizer
  Coupling between the sub-cables unlikely
Intra-wire coupling depends on twist pitch of the filaments an.
Inter-wire coupling is complex due to asymmetric across the sub-cable, uncertainty in the contact resistance between the wires and stabiliser.
The voltages for the induced current depend on the size of the coupling loop , i.e.
Intra-wire: , a
Inter-wire: , a
The voltage is sufficiently high that the induced current will reach critical current and give a dissipation at

## Slide 12: Electromagnetic Transients: AC Loss Measurements
Bac
MgB2 wire
Resistive matrix
Ci
Co
MgB2 wire
Focus on the coupling among the wires in a sub-cable
A simpler arrangement: two wires soldered to the long edges of a metal shim of 6mm wide and 0.5mm thick
Cu, Cu braids and brass shims were used
Applied sinusoidal field
  B0 ≤ 0.2 T
  5Hz ≤ f ≤ 2kHz
Measurements
  3K ≤ T ≤ 100K
  Single-turn saddle pick-up coil
  Sample length L ≤ 100mm

## Slide 13: Electromagnetic Transients: AC Loss Measurements
Losses in the assembly is 1000x of a single wire;
Losses in superconducting state is 10x of normal state;
Coupling transition field higher at low temperature;
Losses are eddy current like (Q ~ B2 and Г ~ constant) in decoupled regime;
Losses vary with matrix resistivity as expected: reduced coupling and shorter time constant at higher ρ;
Decoupled regime has a longer time constant;
High coupling current losses with Cu matrix quite high;

## Slide 14: Electromagnetic Transients: AC Loss Measurements
Sharp coupling transition at high field/frequency , leading in significantly higher losses;
Higher coupling frequency with higher matrix resistivity;
There are scopes for compromise between stability and coupling losses;
Losses from a single pulse can be measured directly using a thermometer;
Coupling

## Slide 15
Quench of MgB2 by Local Disturbances, adiabatic
Quench measurements:
Temperature 36 K, 34.5 K, 32.5 K
V0 = 20 mm
V1 = 70 mm
Heater
VR
VL
Steep dIc/dT = 50A/K

## Slide 16
Higher MQE at lower operating current
MPZ voltage:
Relative slow increase with decreasing current for MgB2: fasting weakening of the power law index
increases of ~9 times from 99%Ic to 87%Ic in YBCO
Quench by Local Disturbances, adiabatic

## Slide 17
Quench by Local Disturbances, adiabatic
Difference in voltage observed between YBCO and MGB2 correspond to a difference in n-number
Faster drop in n-number in Mgb2 where quench voltage remains very low at all currents
Novel methodology to calculate n-number from normal zone temperature and voltage, by using power-law equation
Increasing n-number with decreasing temperature, expected change of slope of MgB2 n-number as temperature further lowered

## Slide 18: Quench by Local Disturbances in Helium gas
Flow change D = 3mm
Helium in
Helium out
MgB2 wire
Heater
Flow channel formed using 3d-prited artefacts;
Flow rate up to 270mg/s covering laminar and turbulent regimes;
Outer surfaces insulated, negligible heat loss to He gas during pulses;
Helium gas cooling increases the minimum quench energy (MQE) and leads to much higher MPZ voltage:
Better stability and easier detection

## Slide 19: Quench by Local Disturbances in Helium gas
He flow MQE deviates from (1-j) reduction of the critical state;
Enhancement MQE by helium flow encouraging, but seemed higher than expectation as small ΔT of the MPZ is small;
Natural convection also results in higher MQE with smooth dependence on He pressure;

## Slide 20: Conclusions
Quench calculation confirmed by experiments
Transient magnetic field scenario outlined
Significant ac loss in simple cable assembly observed experimentally
Quench by local disturbances in helium gas studied experimentally, higher MQE and MPZ voltages confirmed
Thank You
Funded by
HILUMI Design Study (EU FP7 2011-2015)
HL-LHC-UK (CERN/STFC 2016-2020)