## Slide 1: High-gradient test of a structure built from halves
T. Argyropoulos
On behalf of the XBOX team at CERN
CLIC Workshop 2017
CERN 06/03/2017

## Slide 2: Outline
Introduction
Xbox-2: T24-OPEN
  Conditioning
  Performance
  High-gradient studies
Summary

## Slide 3: Introduction
Recent developments in design and production of normal-conducting RF structures raised the achievable accelerating gradient of 20-100 MV/m.
High-Gradient technology could be exploited in certain applications (Linear Colliders, FEL, hadron therapy etc).
For the Compact Linear Collider (CLIC) 10ths of thousands accelerating cavities are needed on pulse mode operation with the requirements:
  100 MV/m on axis accelerating RF field (tens of MW) , ~180 ns pulse length
High-power RF fields can lead to a vacuum arc formation (Breakdown) inside the structure  degrades beam transmission and acceleration  loss of Luminosity
  CLIC specification on the Breakdown rate (BDR): 3x10-7 BD/pulse/m
Main Linac Accelerating Structure: CLIC-G prototype (TD26CC), Travelling-Wave at 11.994 GHz

## Slide 4: High-gradient testing
The High-Gradient performance needs to be tested in advance at high-power test stands
Different CLIC prototypes of accelerating structures have been tested so far at CERN, KEK and SLAC , and high gradients above 100 MV/m have been achieved at low breakdown rate.
At CERN: three X-band (12 GHz) klystron-based test stands (Xboxes)
  support the development of high-gradient accelerating structures and high-power, 50-100 MW range, and RF components for the CLIC project.(N. Catalan-Lasheras et al, IPAC14)

## Slide 5: The Xbox-2 test stand at CERN
The Xbox-2 is the second generation of CLIC high-power klystron-based test stand at CERN.
Same infrastructure design as Xbox-1.
Close access to the bunker where the accelerating structure is tested.
RF Power capabilities: up to 150 MW 250 ns
Scandinova Modulator
Klystron
(50MW, 1.5us)
LLRF
TWT (~1 kW)
Pulse compressor, (250ns, ~3 x power)
BUNKER:
Acc. Structure under test

## Slide 6: T24-OPEN
H. Zha, A. Grudiev, V. Dolgashev, IPAC2015
W. Wuensch et al., LINAC2016
A new prototype, CLIC-G “OPEN”, was designed and built by CERN and SLAC.
Milled structure built in two halves and brazed together potential advantages compared to traditional structures (individual cells are brazed together):
Only two pieces per structure  significantly decrease in surface area to be machined.
Free choice of joining since no RF currents between halves: brazing, welding…
Overall reduction of the total fabrication cost of the structure.
What about the structure performance?
T24-OPEN installed at Xbox-2
24 regular cells (20cm-long) and two matching cells.
Same dimensions of irises as CLIC-G
No HOM damping

## Slide 7
T24-OPEN Full history
200 ns
155 ns
100 ns
4-Sep-2015
14-Nov-2016
Structure being well conditioned towards 100 MV/m at BDR below 1x10-6 BDs/pulse
Operation was restricted by radiation in the test area (bunker shielding issue)
Improved shielding  conditioned to 100 MV/m
BDR falls during flat E run

## Slide 8
Last run @ 45 MW peak INC power
Run at constant peak power continuously for 2 months
Structure was conditioning to 1E-6 bpp
No obvious reason for this high rate

## Slide 9: T24-OPEN Conditioning
The T24-OPEN structure follows the same conditioning trend as previously tested structures with different design.
Previously tested
T24OPEN
Data scaled at 200 ns and 1e-6 bpp

## Slide 10: T24-OPEN Conditioning
Unlike other CLIC designs, the T24-OPEN presents 20% higher surface E fields Esurf  Esurf rises faster in time
Modified Poynting vector, Sc fits better with conditioning curves of previous tests in other disk-based structures. (A. Grudiev, S. Calatroni, W. Wuensch, PRSTAB 12, 102001 (2009))
Data scaled at 200 ns and 1e-6 bpp

## Slide 11: Breakdown positioning
When breakdown occurs:
Transmitted power drops
Reflected power rises
Edge method: Trip time delays, combined with RF group velocity vg, gives the onset position of the breakdown.
Diagnostics of where the breakdown is triggered inside the structure during the testing can be done by analysing the RF signals  Directional couplers to read the RF signals
Trip time delay:

## Slide 12
More BDs in the beginning of the structure (started after Dec 2015)
Not hot cell development  BDR was decreasing
Phase distribution of the BDs spaced by ~120 degrees.
Combination of timing and phase information  better accuracy in breakdown localization
In the structure
Breakdown positioning
Aug 2016
Nov
2016

## Slide 13: BDR dependence on Power
Measurements for constant power: many interruptions due to interventions for Xbox-3 installations  idle periods in between  possible effect on the statistics.
BDR calculated only for the last 5M pulses of each constant power run.
Fit follows the empirical scaling low for a pulse length of 200 ns.

## Slide 14: Dark current measurements
Dark Current is measured: Faraday Cups, Beam Loss Monitors (BLM) (M. Kastriotou and now T. Geoffrey Lucas), Radiation Monitors (CERN Radioprotection group)
Measurements with BLM (March 2016) Exponential fit function as in the theoretical model
Linear relation to the radiation monitor placed downstream of the structure

## Slide 15
β = 29.1
β = 33.4
Fowler-Norheim plot gives a β = 29, similar to the β for the disk-based structures. Similar values obtained also from FC and Radiation monitor.
Field enhancement factor
Blue points are the number of electrons inside the cavity estimated by FLUKA simulations.

## Slide 16: Pulse shape dependence on BDR
Two pulse shape configurations are used: with and without Pulse compressor (PC)
Pulse surface heating increased with PC  higher effective field  higher BDR is expected (F. Wang, C. Adolphsen, C. Nantista, PRSTAB 14, 010401 (2011))
Solid= with pulse compressor
Dashed= without pulse compressor

## Slide 17: Pulse shape dependence on BDR
Measurements showed that BDR with the PC is larger than without PC
Fit follows the empirical scaling, for the same pulse length (200 ns)

## Slide 18
Conditioning summary
T24-OPEN
Empirical scaling :

## Slide 19: Summary
Milled structures have potential advantages - cost, treatment, materials
T24-OPEN built in halves was installed at Xbox-2 test stand at CERN for checking its performance with respect to the disk-based structures
  Structure conditioning: similar trend as the other structures
  Breakdown localization: more BDs in the beginning but not hot cell developed
  Field emission: similar enhancement field factor β as the other structures
High-gradient studies of the pulse shape effect on the structure performance : Pre-pulse due to the PC increased the BDR