## Slide 1: DVM Summary and Acoustic Microscopy Imaging of Cu Sample
Antti Meriläinen1,2, Robin Rajamäki3, Ivan Kassamakov1,2, Markus Aicheler2, Walter Wuensch3, Kenneth Österberg1,2 and Edward Hæggström1
1) Department of Physics, University of Helsinki
2) Helsinki Institute of Physics
3) CERN

## Slide 2: Summary of DVM 2016
Lamp On
Spark
~40 000x Larger than Lamp
After Glow
→ No. of Atoms?
O III
Cu I, II
C IV
O II
(Cu I)
O I, O II
(Cu I, II)
(C IV)
O II
C II
Cu I
19.2.2016
Absorption
Emission
Light in
Light out?
PMT

## Slide 3: Why Acoustic Microscope
Optical methods do not measure elasticity
Tapping mode AFM is not easy to calibrate for elasticity
µCT Does not see elasticity close to the surface
10 mm
Ultrasound transducer
Tilt stage
XY Stage
Sample holder

## Slide 4: Pulse Echo Measurements
Time-of-Flight
Single Pixel
Echo Amplitude
Time-of-Flight: Surface Topography
Amplitude: Mechanics

## Slide 5: Math of Acoustic Reflection
Time-of-Flight
Echo Amplitude

## Slide 6: Lateral Resolution
Amplitude
Time-of-Flight
2.76 µm
2.46 µm
2.19 µm
3.10 µm
Step Height: 85 nm (White-light-interferometer: WLI)

## Slide 7: Copper Sample ID5 #495
1 mm
1 mm
0.1 mm

## Slide 8: Scanning Acoustic Microcopy
10 mm
Frequency range: 240 – 480 MHz
Pixel-by-Pixel Imaging
Areas 1 mm * 1 mm
  ~Stepping 2 µm
Focus size: less than 3 µm
Imaging time: ~1 hour/mm2

## Slide 9: Results: Copper Sample
TOF
Amplitude
Microscope
0.1 mm

## Slide 10
Results: Copper Sample

## Slide 11: Future Work
Surface Elasticity (GPa)
  Acoustic Impedance Calculations
  Scattering from non-flat surface
Surface Wave-Velocity
  Another acoustic parameter
  V(z) -Technique
  Young’s Modulus
Look Under the Surface
  Hard with Focused Transducer
  Time-Reversal -Techniques?

## Slide 12: Questions and Comments
Thank You!

## Slide 13: Pulse Compression Cross Correlation
dt descript depth resolution
dt depends on bandwidth
dt

## Slide 14: Coded Signal and SNR
SNR =0.1
SNR =1