## Slide 1: OVERMOS CMOS HR detector for HEP applications
E. G. Villani STFC Rutherford Appleton Laboratory
on behalf of OVERMOS project collaboration

## Slide 2
Overview
OVERMOS1 description
First test results of irradiated / non –irradiated OVERMOS1
TCAD simulation
Conclusions and next steps
1

## Slide 3
CMOS MAPS detectors solutions are and are going implemented in HEP
Further improvements needed for more challenging HEP use
1
  Introduction – CMOS MAPS & HEP
HSTD11 – Okinawa, Japan - Dec 2017
STAR at RICH
ALICE-LHC
ILC
ATLAS
 | ATLAS HL LHC | ATLAS | ILC | ALICE | STAR
TID[Mrad] | 103 | 80 | 0.4 | 0.7 | 0.3
Fluence[neq cm-2] | 1016 | 1015 | 1012 | 1013 | 1012
P.Rate[kHz mm-2 | 104 | 103 | 2.5102 | 15 | 102
Timing[ns] | 25 | 25 | 350 | 2104 | 2105

## Slide 4
To improve the CMOS MAPS radiation hardness a drift component needs adding, as the diffusion based charge collection drastically reduces their CCE past ~ 1013 cm-2 1 MeV neq
As the depletion region ~ one can either increase the resistivity  (HR CMOS) and / or the biasing Vbias (HV CMOS)
Ultimately the sought end result is the same, i.e. a depleted CMOS MAPS (DMAPS)
2
HSTD11 – Okinawa, Japan - Dec 2017
Small collection well
Small capacitance = low noise, low power Electronics shielded by DPW,
Longer drift distance and relatively low field region
Large collection well
Larger capacitance = higher noise, higher power
Short drift distances, high field
Possible Xtalk from RO to sensor, as electronics inside the DNW
  Introduction – CMOS MAPS & HEP

## Slide 5
OVERMOS is a RAL project, in collaboration with IHEP, aimed at investigating and modelling performances of HR CMOS MAPS fabricated using:
TJ 180 nm Hi-res 18 μm thick epitaxial layer 1kOhm –cm
Small ( 4 x 4 μm2) 4 collecting nodes within each pixel
CMOS DPW or INMAPS, originally proposed TPAC for DECAL of ILC
3
  OVERMOS description
N++
P-Epi
P++-Sub
DPW
SiO2
HSTD11 – Okinawa, Japan - Dec 2017
18 μm

## Slide 6
4
  OVERMOS1 description
ACTIVE
PASSIVE
The ASIC logically consists of PASSIVE and ACTIVE structures, i.e. without and with in-pixel electronics respectively;
HSTD11 – Okinawa, Japan - Dec 2017

## Slide 7
5
  OVERMOS1 description
The PASSIVE pixels consist of arrays of pixels with different arrangements of the 4 collecting nodes (of the same size) within each pixel
The ACTIVE pixels, i.e. with in-pixel electronics, all allow analogue readout of the pixels
5: Basic Active: 5x5 of 40 x 40 um
6: Basic Active AC Large 5x5 of 40 x 400 um independent diode biasing AC coupled
1: Symmetric Passive: 5x5 of 40 x 40 um
2: Basic Passive: 5x5 of 40 x 40 um
1
2
3
4
3: Basic Passive Large: 5x5 of 40 x 400 um merged
4: Basic Passive Large: 5x5 of 40 x 400 um
5
6
7
8
7: Basic Active Large Merged 5x5 of 40 x 400 um
8: Basic Active Large 5x5 of 40 x 400 um
ACTIVE
PASSIVE
HSTD11 – Okinawa, Japan - Dec 2017

## Slide 8
6
  OVERMOS1 description
The ACTIVE pixels include a charge amplifier, shaper and Voltage follower with each output being routed out
Some flavours feature AC coupling to the RO, allowing for relatively high voltage biasing to the pixels
HSTD11 – Okinawa, Japan - Dec 2017
charge amplifier
shaper

## Slide 9
7
All the pixels in the OVERMOS1 include an p++ region around each diode to isolate them from neighbouring ones, an issue that plagued previous version of OVERMOS
The OVERMOS1 ASIC ‘basic passive’ has been tested before and after n-irradiation for DC and charge collection
Pixel 4
  OVERMOS1 description
P++
N++
40um
40um
HSTD11 – Okinawa, Japan - Dec 2017

## Slide 10
8
  OVERMOS devices have been irradiated at Ljubljana in October 2017 to 1E13, 5E13,1E14 and 5E14 n fluence
  Estimated around 30% of fluence consisting of high energy neutrons (> 100keV)
  OVERMOS1 irradiation
HSTD11 – Okinawa, Japan - Dec 2017

## Slide 11
9
  OVERMOS1 Charge collection
Charge collection studies performed using Laser injection:
1: Amptek A250CF calibrated using mV voltage pulses injected through (measured) 1.2 pF capacitor to get V(Q). RMS Noise ≈ 76 e- @ OVERMOS capacitance
2: Trilite Laser 1064 nm calibration using a 300 um Si sensor, 1um top passivation. Laser beam size 5 x 5 um2 (measured with beam profiler), 4.1 ns FWHM (measured with FEMTO 2 GHz optoreceiver ), 50 Hz repetition rate. Up to 5 points measured on sensor to calculate average injected charge
HSTD11 – Okinawa, Japan - Dec 2017

## Slide 12
10
  3: the calibrated Laser was used to inject <Q injected> = 541.66 fC or 1.805 fC/um (corresponding to the Laser attenuation settings which gave the minimum error %)
  (not taking into account IR reflection on ASIC’s top)
OVERMOS
In metal box to reduce EMP noise
OVERMOS
Under Laser 100x optics
HSTD11 – Okinawa, Japan - Dec 2017
  OVERMOS1 Charge collection

## Slide 13
11
  =1E14
  =0
  =1E13
  A
  B
  C
  =0
  =1E13
  =1E14
  =1E14
  =0
  =1E13
  Total collected charge vs. Vbias , points A,B,C. Integration time 400 ns
  <Q injected> = 1.805 fC/um
  HVbias =10V provided through the A250CF, via a 400 Meg resistor chain
  T = 21C in all tests
  4.04fC ±29.7%
  3.14fC ±36.3%
  2.31fC ±5.4%
HSTD11 – Okinawa, Japan - Dec 2017
  OVERMOS1 Charge collection

## Slide 14
12
Laser injection test results (1064 nm, 5 x 5 um2 beam size)
Vbias = 10V
<Q injected> = 1.805 fC/um
  =0
HSTD11 – Okinawa, Japan - Dec 2017
  OVERMOS1 Charge collection
  Q[fC]

## Slide 15
13
  =1E13
Laser injection test results (1064 nm, 5 x 5 um2 beam size)
Vbias = 10V
<Q injected> = 1.805 fC/um
HSTD11 – Okinawa, Japan - Dec 2017
  OVERMOS1 Charge collection
  Q[fC]

## Slide 16
14
  =1E14
Laser injection test results (1064 nm, 5 x 5 um2 beam size)
Vbias = 10V
<Q injected> = 1.805 fC/um
HSTD11 – Okinawa, Japan - Dec 2017
  OVERMOS1 Charge collection
  Q[fC]

## Slide 17
15
  Collected charge vs. time, points A,B,C Vbias = 10V,  = 0
  <Q injected> = 1.805 fC/um
  AMPTEK A250CF
  RAMP= 15 ns
  Fs  sqrt((Ftot )2 - (RAMP )2 ) 
  A: 123 ns
  B: 151.4 ns
  C: 165.5 ns
  FtotA= ~ 123.9 ns
  FtotB= ~ 152.18 ns
  FtotC= ~ 166.2 ns
  A
  B
  C
HSTD11 – Okinawa, Japan - Dec 2017
  OVERMOS1 collection time

## Slide 18
16
  DC test results of leakage currents test of single pixel 4 with substrate and other pixels floating
  Linear increase with fluence, as expected
Vbias
Ipix4 (A)
Vbias (V)
K = 1.121e-24 ± 3.52e-26
Fluence( cm-2)
HSTD11 – Okinawa, Japan - Dec 2017
  OVERMOS1 DC test

## Slide 19
Individual doping profiles for OVERMOS were obtained using SPROCESS, to simulate a (simplified) CMOS fabrication by using TJ foundry process information
These (1D) doping profiles were then implemented in SDE
  Huge reduction in mesh size (O(3e5) points) and computation time
Epi-Bulk
NW
PW
sub
epi
epi
epi
sub
sub
17
  Synopsys TCAD simulations
HSTD11 – Okinawa, Japan - Dec 2017
B sucking from 8 nm SiO2

## Slide 20
18
  TCAD DC initial results Leakage currents
  Leakage current for tested non irradiated pixel and TCAD results differ by ~ 3 max
  Surface Recombination velocity SRV=1e4
  SiO2/Si trap density 1e11
  R ~2.85 Max
‘1D’ profiles from SPROCESS
Vbias
GND
  =0
HSTD11 – Okinawa, Japan - Dec 2017

## Slide 21
Conclusions and next steps
First test results of OVERMOS1 basic flavor were presented
Measured with Laser injection, initial increase in CCE observed for irradiated device
Charge collection drops by tenfold at  = 1e14 w.r.t  = 0
DC tests showed expected leakage increase with n-fluence
Initial TCAD simulations for DC only off by ~ 3
Next step: to fully characterise the remaining sensors, both passive and active and TCAD simulations comparisons
THANK YOU
19

## Slide 22
I
~
  Backup slides Mott-Gurney currents
Vss
P++
Sub - P++
Epi- P
Leakage current is measured between P wells ( top and substrate)
For constant current and assuming only drift component
HSTD11 – Okinawa, Japan - Dec 2017

## Slide 23
II
  Backup slides - Leakage currents
  =0
  =5E13
  =5E14
Vss(V)
Iss
Iss
Iss
Vss(V)
Vss(V)
  =0: IV2.72
  =5E13: IV2.02
  =5E14: IV1.86
Fitting @ 5E13 shows a nearly ideal V^2 dependence
The power coefficient depends on the fitting
Only one device/ each radiation level
Asymmetry w.r.t. Vss may be due to conductive glue at the substrate
HSTD11 – Okinawa, Japan - Dec 2017

## Slide 24
Some approximations as a result but more affordable for big 3D simulations:
No B sucking
No lateral spread doping information
Coarser doping profiles
III
SiO2
Epi
B sucking from 8 nm SiO2
TJ
SPROCESS
PW
TJ
SPROCESS
NW
NW
BSG
M1
SiO2
HSTD11 – Okinawa, Japan - Dec 2017

## Slide 25
IV
  BACKUP slides – Laser beam width
Laser beam size vs. focusing – Measured beam size with beam profiler
HSTD11 – Okinawa, Japan - Dec 2017

## Slide 26
V
  OVERMOS next steps
  Determine Neff by measuring depletion width vs. bias
  We use the Trilite Laser (~ 3 um minimum b.w. @ 1064 nm) to sample the OVERMOS1 along the edge
Laser (IR or GREEN)
OVERMOS1
top
bottom
XY table
HSTD11 – Okinawa, Japan - Dec 2017