## Slide 1
Radiation Hardness of
Silicon-on-Insulator Pixel Devices
- Ten years of struggle -
Project supported by
JSPS Grant-in-Aid for Scientific Research on Innovative Areas
K. Hara (Univ. Tsukuba)
Wataru Aoyagi (University of Tsukuba) Shun Endo (University of Tsukuba) Hiroki Yamauchi (University of Tsukuba) Ryuhei Abe (University of Tsukuba) Shikie iwanami (University of Tsukuba) Shunsuke Honda (University of Tsukuba)
Toru Tsuboyama (KEK) Ysuo Arai (KEK) Ikuo Kurachi (KEK) Toshinobu Miyoshi (KEK) Miho Yamada (KEK)

## Slide 2
OUTLINE
SOI Pixel and Radiation Damage
TID Damage and Compensation
- First Results
- BPW
  - Double SOI
  TrTEGs
  INTPIXh2
  FPIX2
  FPIX3
Conclusions

## Slide 3
SOI PIXEL
SOI: Silicon-On-Insulator
Material budget
S/N
power dissipation
single event effects
latch up
Operation temp. (0.3K～570K)
speed
cost
Pixel size
CMOS circuitry fabricated on buried oxide(BOX)
LAPIS 0.2um FD-SOI
Features:
monolithic (no metal bumps)
SOI-CMOS (FETs fully isolated)
Can choose* substrate of optimum resistivity (fully depleted CMOS sensors possible)
*SOITEC SmartCutTM
many excellent features

## Slide 4
In summary…already
OK
OK
Not needed
OK
Notes: norbert

## Slide 5
Rad-damage in SOI
strong against SEE*
(thin active layer in SOI)
*SOI is a standard in space application
40nm
~O(10)um
Contribution from BOX is larger
- affected by TID caused by accumulation of holes in insulator
Surrounded by insulator

## Slide 6
IEEE2008
NMOS
PMOS
The threshold shifts are significant (Vcc~1.8V)
Proton-induced damage ~ γ damage (TID)
200nm
350um
Back-gate biasing is
a clue to compensation
but the detector back is for sensor biasing…
BOX
Hole accumulation
⇒smaller Vgate required for turn-on
⇒VBG can null the Vth shift

## Slide 7: BPW (buried p-well)
HSTD9(2010)
BPW(V=0) no effect for rad-damage
BPW(V<0) should improve, but
BPW tied to the pixel node … ⇒ nested structure
BOX
BPW
N-sub
FET
BPW suppresses the back-gate effect
Back-gate effect suppressed
~10kGy

## Slide 8: Double SOI wafer since 2011
Courtesy of Lapis semiconductor
SOITEC
nCz(0.6ｋΩｃｍ）
Shin-etsu
Oxy-Cz p (1ｋΩｃｍ）
pFZ (>5ｋΩｃｍ）

## Slide 9: Double SOI
VS=0
VD=1.8
VS=-1.8
VD=0
IEEE2013
Vth Compensable by VSOI2 !

## Slide 10: Double SOI
IEEE2013
However…
Substantial reduction of gm for PMOS…. ⇔ reason understood and solved
But, SOI works up to 100 kGy, good enough for ILC vertex

## Slide 11: Double SOI PIXEL
HSTD10(2015)
Single VSOI2 control (INTPIXh2)
Response after 100kGy observed
though
VREST response not fully recovered
Proportional to depl. thick (IR laser)

## Slide 12: Double SOI PIXEL
HSTD10(2015)
Signal Shape (INTPIXh2)
The amplifier is not optimized for fast signal, but radiation-induced degradation in charge collection time seems small.

## Slide 13: DouBLE SOI – 3 VSOI2 controls
VRESET response almost recovered
preirrad
VSOI2(0V,0V,0V)
VSOI2(-5V,-10V,-21V)
200kGy
VSOI2=(VSOI2 IO ,VSOI2 pix , VSOI2 dec)
500kGy
VSOI2(0V,0V,0V)
preirrad
VSOI2(-12.5V,-15V,-29V)
SOI2 I/O
SOI2 DECORDER
SOI2 PIXEL
FPIX2
JPS (2016)
VRESET response partially recovered
PIXEL … signal integration
DEC … voltages for gain control
IO … FET functioning for ESD
TID most critical on :

## Slide 14: FNAL test beam
FTBF: 120GeV protons from Main Injector
Trigger generated by a SEABAS2 board using Scint.(5mm-sq) and ATLAS FE-I4 (2mmx1.75ｍｍ ROI)
Data of 4 FPIX2 and 2 SOFIST sensors acquired per TLU request.
All R/O boards (SEABAS2) implemented with same TimeStamp firmware
Last FPIX2 made accessible for exchanging to irradiated DSOI
scint.
(view from downstream)
SEABAS2（Soi EvAluation BoArd with Sitcp): 16ch 12bit 40MHz ADCs, Giga-bit Ethernet
4.2s beam spill every 1 minute
DAQ~1.2k/spill
R.Nishimura et al. “high speed DAQ system…”
Jan (2017)

## Slide 15: TID Damage compensation
Chart: 
| 5 | 12.24744871391589 | 14.142135623730951 | 10 | 7.0710678118654755 | 10.954451150103322 | 8.9442719099991592 | 11.401754250991379 | 12.649110640673518
irrad | 193.4 | 404.3 | 472.6 | 332.7 | 246.3 | 363.6 | 303.2 | 376.4 | 416.2
non irrad | 489.8 | 337.1 | 234.4
100
200
5x5 cluster charge [ADC]
5x5 cluster charge about the maximum charge pixel in an event
Non-irrad (200V)
VSOI2=0
100kGy (200V)
VSOI2 : I/0=-4V ,
Pixel=-8V , Dec=-12V
Innovative double-SOI allows operation of SOI devices @ 100kGy
~150um/300
depleted
FNAL TB : FPIX2 100kGy
TIPP (2017)
Noise:1.8±0.1 ⇒5.4±0.5＠RT

## Slide 16: More compensation…
PMOS TID in sidewall: LDD loses control
(LDD: lightly doped drain)
increasing LDD by x10 (FPIX2-.>FPIX3),
Trans-conductance recovered significantly
I/O
DECODER
PIXEL
chip layout (3mm-sq)
p/n
p/n
FPIX3
FPIX2
Vth shift compensable by applying negative volts to SOI2: optimum volts differ for n/p as dose ~1MGy
Separate n/p SOI2 controls in FPIX3

## Slide 17: Compensation tuning
IO outputs are clipped
due to always “ON” ESD
ESD protection
Wide range of VSOI2_IO
VSOI2_IO
STEP-1 tune IO
STEP-2 tune DECODER
V RESET
ADC
dynamic range
Typical V RESET response (non-irrad)
For VRESET=100mV, tune to minimize the output
VSOI2_decP
VSOI2_decN
200kGy
STEP-3 tune PIX to maximize the dynamic range and linearity

## Slide 18: TID damage compensation
FPIX2:500kGy
FPIX3:500kGy
FPIX3:1MGy
Response to pulsed IR-laser
V(IO)=-6
V(DecN/P)=-20/-30
V(PixN/P)=-9/-11
V(IO)=-6
V(DecN/P)=-26/-30
V(PixN/P)=-10/-11
V(IO)=-12.5V
V(Dec)=-29V
V(Pix)=-15V
Test pulse
(test circuit only)
Response fully recovered at 500kGy
Expect linear response at 1MGy

## Slide 19: FPIX3 Pixel layout
FPIX2
FPIX3
8um
9um
PIXEL NMOS FETs (N1+N2) located at a corner
One VPIX_n for a group of 2×2 pixels
Rolling shutter R/O resets the signals in next row…
Pre-irrad
No response
from odd-row
OK w/ singleSOI

## Slide 20: conclusions
TID identified as main concern for SOI applications in high-radiation environment
Innovative Double SOI solved many issues including TID. LDD profile revisited to enhance radiation tolerance
TID tolerance up to 500 kGy is achieved and good performance is expected also at 1 MGy (FPIX3)
SOI pixel (SOFIST) is being developed for the ILC.
SOI applications to wider area are encouraged.
Ten years of struggle …..

## Slide 21
SLUM DUNK
By M. Inoue

## Slide 22: spares

## Slide 23
Fine-pixel detector: FPIX2
I/O
DECODER
PIXEL
Pixel size: 8μm□
#Pixels: 128×128
Handle wafers:
>single SOI
25kΩ・cm p, 500 umt >double SOI
1kΩ・cm p, 300 umt
Rolling shutter RO
8 parallel outputs
chip layout (3mm-sq)
In Development:
to demonstrate excellent spatial resolution achievable with SOI technology (=>tracker for SOFIST TB)
as demonstrator of TID tolerance (FPIX2 equipped with three middle-SOI regions)
On-pixel circuit
TID: hole accumulation in BOX/GOX
Middle-SOI: compensate TID effects by applied negative voltages
Analog signals are digitized (2ms) by external SEABAS2 12-b ADCs (8 parallel)