## Slide 1
Hiroshima Conference HSTD 11
Okinawa, Dec 10 – 15, 2017
Norbert Wermes
University of Bonn
Pixel Detector Overview
Pixel Detectors ... where do we stand ?
in my very subjective opinion ... w/ apologies

## Slide 2
~1997
Hybrid pixel detectors
HEP tracking
Imaging
2017
Monolithic pixel detectors
LHC
HI
ALICE ITS
ATLAS CMOS
HEP tracking
Imaging
LHC
HI, B-FAC
ATLAS/CMS
MEDIPIX
AGIPD
biomedical
photon science
DSOI pixels
Notes: DLTS = Deep level transient spectroscopy
TSC = Stimulated Current technique
n in p-type sensors provide cost efficient single sided processing

## Slide 3
Some early prejudices
... e.g. about HL-LHC radiation levels
Tough for planar sensors ... !?
There is no alternative, though ... !?
Diamond will never become a pixel detector ... !?
You have to use p-type material ... !?
...

## Slide 4
Radiation
Readout at n+ electrodes (e- collection)
Operate at high bias voltages
Carefully plan the annealing scenario
Provide proper electrode design and guard rings
Use p-substrates (rather than n-in-n) ... why?
HL-LHC fluence =>every Si lattice cell sees about 50 mips
Recipe
evidence
but more complex
for pixels
Q trapping
structured weighting fields
E-field after irradiation
talk by G. Kramberger
Notes: DLTS = Deep level transient spectroscopy
TSC = Stimulated Current technique
n in p-type sensors provide cost efficient single sided processing

## Slide 5: What is actually different for p vs n bulk?
e- trap
positive space charge
higher conc. after proton
than neutron irradiation
depends on oxygen content
BD=bistable donor (e- trap)
positive space charge
strongly produced
in oxygen rich DOFZ material
triple vacancy, small cluster
negative space charge
-> high leakage current
V2O complex (?)
negative space charge
causes leakage current, strongly produced in oxygen lean STFZ
extended acceptor defects produced equally by n,p
negative space charge
-> reverse annealing
moves
with changes
to Neff
EF
most defects show linear fluence dependence
cooling helps to keep Ileak and rev. annealing smaller
Neff changes
Radu et al., J. Appl. Phys. 117, 164503 (2015)
RD50, M. Moll et al., PoS (Vertex 2013) (2013) 026
Notes: defecte become effective for N_eff when charged
this depends on Fermi-level which depends itself on the doping concentration and on N-eff

## Slide 6: Donor removal/acceptor increase <-> acceptor removal
Junkes, E. Donegani, C. Neunbüser, IEEE TNS (2014)
10.1109/NSSMIC.2014.7431260
E. Donegani, Thesis U Hamburg (2017)
oxygen enriched silicon
radiation induced vacancy
(mobile even below RT)
harmless
VOi defect
donor (P) removal
decreases pos. ρ
+
[O] ≫[P]
=>
radiation induced oxygen interstitial
+
Bi
Ps
BiOi
acceptor (B) removal
decreases negative ρ
Cure? C-enrichment?
(donor)
(E-center)
n – bulk
p - bulk
Notes: mobile radiation induced vacancy defects can catch a Phosphorus atom (i.e. a donor) to form a VP complex and the donor is gone.
Wheras if we make it more likely that the vacancy hits an oxygen atom (e.g. by MCz grown ingots) ... a rather harmless VO complex is formed instead.
Furthermore, reverse annealing, i.e. activating lattice defects after some time, is hindered at low temperatures.

## Slide 7: Radiation hard Si sensors -> (thin) planar pixel sensors
7×1015
1.4×1016
best (100-150 µm)
4-5 x 1015 neq/cm2
1016 neq/cm2
Macchiolo, Nisius, Savic, Terzo, NIM A831:111–115, 2016.
Terzo, Andricek, Macchiolo, Nisius et al, JINST 9 (2014) C05023
K. Kimura et al., NIM A831 (2016) 140-146
Y. Unno et al.,NIM A699(2013)72–77.
6000 – 7000 e- for 100 - 200 µm sensors @ 300 V – 600 V bias
hit efficiencies are still reasonable at Φ > 1016
thin n+ in p sensors after high fluences (neutrons)
talk by K. Nakamura
Notes: Wenn man die Guardring structure auf die Unterseite bringen will, benötigt man eine doppelseitige/teure Prozessierung.

## Slide 8: Radiation hard Si sensors -> 3D-Si sensors
Development for
HL-LHC:
thin (100 µm)
6” wafers
electrodes thin (5µm) & narrowly spaced
slim or active edges
50 µm
S. Parker, C. Kenney , J. Segal, ICFA Instr.Bull. 14 (1997) 30
C. Da Via, et al., NIM A49 (2005) 122-125, NIM A 699 (2013) 18
particle path (signal) different from drift path
high field w/ low voltage
-> radiation tolerance -> Q still 50% @ 1016 cm-2
slightly larger Cin (noise)
now also in diamond, CdTe
3D sensors have been put to reality in ATLAS IBL detector since 2015 -> so far reliable and well performing
talk by C.B. Martin
FBK design
G.F. Dalla Betta et al., NSSMIC.2015, arXiv:1612.00608,
J. Lange et al., arXiv:1707.01045
talks by H. Oide, J. Lange
ATLAS
Notes: A thin, highly resistive (p-type) sensor wafer is supported by a low ohmic (p++ ) handle wafer
that can be backside thinned after processing. While the p+ columns are deep
etched through to the handle wafer where they receive their electric potential,
the n+ columns stop about 15µm short from the handle wafer. Besides for
technical reasons (i.e.wafer-to-wafer bonding), studies have shown that also for
single-sided 3D-Si sensors the trade-off between signal efficiency and breakdown
performance favors non-passing-through n-columns

## Slide 9: Radiation hard Si sensors -> 3D-Si sensors
Development for
HL-LHC:
thin (100 µm)
6” wafers
electrodes thin (5µm) & narrowly spaced
slim or active edges
50 µm
S. Parker, C. Kenney , J. Segal, ICFA Instr.Bull. 14 (1997) 30
C. Da Via, et al., NIM A49 (2005) 122-125, NIM A 699 (2013) 18
particle path (signal) different from drift path
high field w/ low voltage
-> radiation tolerance -> Q still 50% @ 1016 cm-2
slightly larger Cin (noise)
now also in diamond, CdTe
3D sensors have been put to reality in ATLAS IBL detector since 2015 -> so far reliable and well performing
talk by C.B. Martin
FBK design
G.F. Dalla Betta et al., NSSMIC.2015, arXiv:1612.00608,
J. Lange et al., arXiv:1707.01045
talks by H. Oide, J. Lange
CNM
d = 230 µm
98%
after 1016
ATLAS
Notes: A thin, highly resistive (p-type) sensor wafer is supported by a low ohmic (p++ ) handle wafer
that can be backside thinned after processing. While the p+ columns are deep
etched through to the handle wafer where they receive their electric potential,
the n+ columns stop about 15µm short from the handle wafer. Besides for
technical reasons (i.e.wafer-to-wafer bonding), studies have shown that also for
single-sided 3D-Si sensors the trade-off between signal efficiency and breakdown
performance favors non-passing-through n-columns

## Slide 10: Diamond ...
... has been made into a radhard “quasi” tracker
ATLAS
DBM
beam monitor
(3 layer telescopes)
mean efficiency 87.6%
Kononenko et al., Diamond and Relat. Mater 18 (2009) 196
mpv ~13600 e-
3D Diamond
talks by
H. Kagan N. Venturi
3D Diamond
F. Bachmair, RD42-Coll., doi.org/10.1016/j.nima.2016.03.039

## Slide 11
You cannot use CMOS (technologies for) sensors.
They do not have the same properties as “good” silicon sensors ... !?

## Slide 12: ... passive CMOS sensors
can have in-pixel AC coupling
fancy RDL possibilities by metal layers
cheap large feature size technology possible
no extra bumping step, because bumps (C4) come with CMOS fabrication
do flip-chipping in-house (large pitch)
large sensors possible ( reticule stitching)
may be even wafer based flip-chipping (8“)
D.-L. Pohl et al., JINST 12 (2017) no.06, P06020

## Slide 13: Performance of passive CMOS sensors
noise
116 e-
131 e-
DC
AC
IV curves of all samples ok (bias 120 V -> 500 V)
about 220 µm depletion depth
leakage current 20 µA / cm3 (IBL: 15 µA/cm3)
noise as in standard sensors - planar sensors (CD = 117 fF): ENC = 120 e-
- 3D-Si sensors (CD = 180 fF): ENC = 140 e-
high efficiency after irradiation (1 x 1015 neq/cm2)
3.2 GeV e-
before
irradiation
after
irrad
3.2 GeV e-
D.-L. Pohl et al., JINST 12 (2017) no.06, P06020

## Slide 14
FE chip
A complex chip (o(109) transistors) in general can only be done by industry and needs many years of development ... !? ... and is too expensive ... !?
250 nm technology was radhard => 65 nm technology is even better ... !?

## Slide 15: Pixel R/O-Chip for HL-LHC rates (and radiation)
250 nm technology
pixel size 400 × 50 µm2
3.5 M. transistors
130 nm technology
pixel size 250 × 50 µm2
70 M transistors
FE-I3
FE-I4
FE-65
65 nm technology
pixel size 50 × 50 µm2
~ 1000 M transistors
hit rate 2-3 GHz/cm2
< 1 MHz trigger @12µs
3.5 mW/mm2
rad hard: 2x1016/cm2 1 Grad
Effort and costs so large that joint approach (cross experiments) is needed -> RD53 (20 Institutes)
High hit rate (not smaller pixel size) requires high logic density -> 65nm TSMC
FE-65 prototypes (2016) -> RD53A (full size chip) -> back from foundry
Deep submicron (250 nm & 130 nm) saved LHC pixel R/O chips
65 nm has its own – geometry induced – radiation effects to deal with
Requires long and tedious study program ...
RINCE = Radiation Induced Narrow Channel Effects
RISCE = Radiation Induced Short Channel Effects
hit rate < 400 MHz/cm2
1.8 mW/mm2
rad hard: 5x1015/cm2 200 Mrad
< 100 MHz/cm2
< 100 Mrad
talk by F. Faccio ... “radiation strikes back”

## Slide 16: RD53A alive ... (received last Wednesday)
image produced by selective injections

## Slide 17: Pixel R/O philosophy changes -> better architectures
column drain R/O
FE-I3 like
4-pixel region logic
efficient for clusters
FE-I4 like
region architectures with grouped logic -> regional hit draining
surrounded by synthesized logic (“digital sea”)
RD53A like
1st generation
2nd generation
3rd generation
“analog islands in digital sea”
... complex designs can be made much faster now than in the early LHC days.
talk by M. Garcia-Sciveres
Notes: In the classic column drain architecture of 1st generation chips (fig. 29 (a) ), all pixels in a column share a data bus that only one pixel at a time can use.

## Slide 18: Current favorite large system layouts ...
strips
outer
pixel
depl. CMOS pixels
inner
pixel
innermost
pixel
cost driven
radiation
driven
n in p
strip modules
large modules planar n in p pixels / CMOS?
3D silicon
dedicated
rad.-hard
detectors
1.0
0.5
0.0
R (m)
talks by
L. Rossi
J. Schwandt
B. Agkun

## Slide 19: LHCb - Vertex Locator Upgrade (2019-2020)
bla
Vertex detector surrounding collision region
  In vacuum
  5.1 mm from beam
change from strips to pixels + VeloPix chip
~41 Mpix, 55 x 55 µm2 pixels
triggerless R/O (~2.9 Tbits/s)
microchannel cooling (a first !)
talk by
K. Cavalho Akiba

## Slide 20
Monolithic pixel modules
Monolithic pixels will never stand the LHC rates and radiation environment ... !?
SOI pixel technology is fine, but it is difficult to get around the many challenges ... !?

## Slide 21
Hybrid Pixel Detectors
  PROs (split functionality)
    complex signal processing in readout chip
    zero suppression and hit storage during L1 latency
    radiation hard chips and sensors to >1015 neq/cm2
    high rate capability (~MHz/mm2)
    spatial resolution ≈10 – 15 µm
    NEXT: 3D integration (TSVs) ... from C2W to W2W assemblies
  CONs
    relatively large material budget: >1.5% X0 per layer
    sensor + chip + flex kapton + passive components
    support, cooling (-10oC operation), services
    resolution could be better
    complex and laborious module production
    bump-bonding / flip-chip
    many production steps
    expensive
  hence: Monolithic pixels relying on commercial CMOS processes have come in focus (first outside LHC-pp -> also for HL-LHC)
STAR
MAPS
2014
0.16 m2
ALICE upgrade
MAPS
2021
10 m2
ILC
DEPFET
MAPS SOIPIX
20??
Belle II
DEPFET
2018
0.014 m2
talks by W. Snoeys. H. Pernegger, I. Peric, T. Hirono, B. Hiti, D. Dannheim

## Slide 22: What is needed to realize (radhard) depleted CMOS pixels?
from: www.xfab.com
“High” Resistivity Substrate
Wafers (100 Ωcm – kΩ cm)
Backside Processing
(for thinning and back bias contact)
“High” Voltage add-ons
to apply 50 – 200 V bias
Multiple (3-4) nested wells
(for shielding and full CMOS)
kΩcm
~100 Ωcm
~10 Ωcm
I. Peric, NIM A582 (2007) 876-885
I. Mandic et al., JINST 12 (2017) no.02, P02021
1
2
3
4

## Slide 23: The question of the fill-factor / electrode geometry
Electronics outside charge collection well
Very small sensor capacitance (~5 fF)  noise low, speed high, power low
on average longer drift distances and low field regions  radhard?
also full CMOS with addn’l deep-p implant
Electronics inside charge collection well
Collection node with large electrode  no low field regions  on average short(er) drift distances  more radhard
Full CMOS with isolation between NW&DNW
Large (> 100 fF) sensor capacitance (due to DNW/PW junction!)  noise & speed or power penalties  x-talk possible (from digital to sensor) needs dedicated IC design

## Slide 24: TJ Process modification of small electrode design
W. Snoeys et al., NIM A871 (2017) 90 – 96.
TowerJazz 180 nm CMOS CIS
deep PW full CMOS in pixel
epi thickness: 18 – 40 µm
Design derived from ALICE development
Modified process to improve depletion & lateral E
Pixel dimensions:
36 x 42 µm2 pixel size
3 µm diameter electrodes
Measured capacitance <5fF
3 µm
36 µm

## Slide 25: Large (~1 cm2) full CMOS chips (=modules) w/ readout
ATLASPix
MuPix
LF-MONOPIX
LFoundry 150 nm
substrate ρ > 2 kΩcm
ams 180 nm
substrate ρ ~ 0.08 - 1 kΩcm
TowerJazz 180 nm epitaxial (25 µm) substrate ρ > kΩ cm
talks by W. Snoeys. H. Pernegger, T. Hirono, I. Peric, D. Dannheim
MALTA
TJ
Monopix

## Slide 26: Large (~1 cm2) full CMOS chips (=modules) w/ readout
ATLASPix
MuPix
LF-MONOPIX
LFoundry 150 nm
substrate ρ > 2 kΩcm
ams 180 nm
substrate ρ ~ 0.08 - 1 kΩcm
TowerJazz 180 nm epitaxial (25 µm) substrate ρ > kΩ cm
talks by W. Snoeys. H. Pernegger, T. Hirono, I. Peric, D. Dannheim
MALTA
TJ
Monopix
LF Monopix
ATLASpix

## Slide 27: Results extremely encouraging
radiation hardness
LFoundry
  1.5e15neq/cm2
gain
noise
TID 1 MGy
efficiency
timing
LFoundry
Timing [25ns bins]
ams180 after 1 x 1015 neq/cm2
w/o jitter reduction
I. Mandić et al., JINST 12 (2017) no.02, P02021
99.7%
ATLASpix
98.9%
LF-Monopix
before irrad
after 1015 neq cm-2
full depl.
100 µm
after 2x1015
talks by H. Pernegger, T. Hirono, I. Peric
with jitter reduction

## Slide 28
SOI pixels
Note again dedicated workshop included in this conference

## Slide 29: SOI monolithic pixels
FD CMOS on SOI
fully depleted SOI (thin film) @ Lapis / KEK
issues
  back gate effect
  coupling of sensor to circuit
  radiation (TID) issues due to BOX
cures developed in recent years
  buried p-well, nested wells
  “double SOI” structures
  => TID hard to 10 Mrad
talks Y. Arai, K. Fukuda, S. Kawahito + SOI workshop
FPIX, SOFIST | particle tracking
INTPIX | X-ray
XRPIX, SOIPIX-PDD | X-ray astro
SOPHIAS | synchrotron rad.
cryogenic | far infrared
CNTPIX | counting -> biomed
MALPIX | ion spectroscopy
H. Kamehama et al., Sensors 2017
SOIPIX-PDD
Notes: There are a large number of applications spun off from this development whcih I have listed here.
I would like to emphasize here a new development to reduce the input capacitance.
SOIPIX-with pinned depleted diode structure .
-HV at backside -> depleted substrate.
BPW on backside of BOX for pinning the back-gate voltage of the SOI transistors and acting as shielding layer between the charge sensing node and the SOI circuits: against noise, coupling and dark current generation.
A BNW formed under the BPW is depleted and this layer acts as a buried channel to gather carriers generated in the pixel into the sensing node (n+) and to improve charge correction efficiency, because lateral electric field is created in this channel.
Like Tower Jazz moduified process.

## Slide 30: SOI monolithic pixels
FD CMOS on SOI
fully depleted SOI (thin film) @ Lapis/KEK
issues
  back gate effect
  coupling of sensor to circuit
  radiation (TID) issues due to BOX
cures developed in recent years
  buried p-well, nested wells
  “double SOI” structures
  => TID hard to 10 Mrad
H. Kamehama et al., Sensors 2017
SOIPIX-PDD
0.65 µm
FPIX
Notes: There are a large number of applications spun off from this development whcih I have listed here.
I would like to emphasize here a new development to reduce the input capacitance.
SOIPIX-with pinned depleted diode structure .
-HV at backside -> depleted substrate.
BPW on backside of BOX for pinning the back-gate voltage of the SOI transistors and acting as shielding layer between the charge sensing node and the SOI circuits: against noise, coupling and dark current generation.
A BNW formed under the BPW is depleted and this layer acts as a buried channel to gather carriers generated in the pixel into the sensing node (n+) and to improve charge correction efficiency, because lateral electric field is created in this channel.
Like Tower Jazz moduified process.

## Slide 31: SOI monolithic pixels
FD CMOS on SOI
fully depleted SOI (thin film) @ Lapis/KEK
issues
  back gate effect
  coupling of sensor to circuit
  radiation (TID) issues due to BOX
cures developed in recent years
  buried p-well, nested wells
  “double SOI” structures
HV-SOI (thick film)
a promising alternative
doped, non-depleted P- and N-wells prevent back gate effect and increase the radiation tolerance
Hemperek, Kishishita, Krüger, Wermes, NIM A796 (2015) 8-12
Notes: There are a large number of applications spun off from this development whcih I have listed here.
I would like to emphasize here a new development to reduce the input capacitance.
SOIPIX-with pinned depleted diode structure .
-HV at backside -> depleted substrate.
BPW on backside of BOX for pinning the back-gate voltage of the SOI transistors and acting as shielding layer between the charge sensing node and the SOI circuits: against noise, coupling and dark current generation.
A BNW formed under the BPW is depleted and this layer acts as a buried channel to gather carriers generated in the pixel into the sensing node (n+) and to improve charge correction efficiency, because lateral electric field is created in this channel.
Like Tower Jazz moduified process.

## Slide 32
Time measurement with Si detectors
  Sub-ns timing with Si detectors is not possible ...!?
  Not with pixel detectors ...!?
4D tracking ... Δt = 30 ps <-> Δx = 1cm

## Slide 33: Exploit charge amplification
  in “Geiger Mode” fashion (like in gas RPCs or in SiPMs) => σt governed by avalanche fluctuations
  OR .... in “linear mode” fashion -> Low Gain Avalanche Detectors (LGADs)
talks by N. Cartiglia, H. Sadrozinski, G. Pellegrini
arrival
fluct.
distortion
low w-field
Separate the “collection” of charge from the signal gain
Figure of merit for σt is the “slew rate” dV/dt ≈ Signal/τrise
  thin (!!)
  HV
  intr. amplification
  (small electrodes)
  broad-band amplifier
Need: fast drift + large S/N
H. Sadrozinski et al., NIM A730 (2013) 226-231, NIM A831 (2016) 18-23
N. Cartiglia et al., NIM A796:141–148, 2015; NIM A845 (2017) 47-51
H. Sadrozinski, A. Seiden, N. Cartiglia, arXiv:1704.08666
Notes: How would one go about getting in to the 10 ps range with (structured) Si detectors?
typ. charge collection ~5 ns range and CSA rise time of several 10 ns?
ok, the induced current is immediately there, even though small pixel effect (weighting field) prevents from seeing much of it before the charge arrives at the pixel
use in-Si amplification (like APDs or in SiPMs) ?
Die 1.4 kommen von dem Sigma der landauartigen Zeitverteiilung (siehe Riegler)

## Slide 34: LGAD – successes so far ... and current challenges
CNM LGADs
LGAD
pad (~1 mm2)
detectors
G. Pellegrini et. al, NIM A 765 (2014) 12–16.
G. Pellegrini et al., HSTD 2015, arXiv:1511.07175
H. Sadrozinski et al., NIM A730 (2013) 226-231, NIM A831 (2016) 18-23
N. Cartiglia et al., NIM A796:141–148, 2015;
NIM A845 (2017) 47-51
main problem: gain variation with fluence (due to high doping of amplification region)
(especially annoying in varying radiation fields)
also: amplification no longer in metallurgical p-n junction only (so what!)
current directions:
    (1) substitute B with Ga as acceptor dopant -> ?
    (2) Carbon-enriched p-silicon wafers ... ?
Ultimate Goal: simultaneous space (~10µm) AND time resolution (< 50 ps) ... no pixels yet !
Concrete application: ATLAS (HighGranularityTimingDetector; Forward) -> pile-up killer
CMS-TOTEM (in Roman Pots)

## Slide 35
Pixel Imaging SYSTEMS (!!)

## Slide 36: Hybrid Pixels for SLS @ PSI
talk by G. Carini
dynamic gain switching (1-104)
for swissFEL (exp. just started)
PILATUS successor
high frame rates
23 kHZ
smallest pixels
low noise => low eneries

## Slide 37: Hybrid Pixels for SLS @ PSI
100 µm
EIGER 500k
75 µm pixels
Photon Counting
MÖNCH 0.3
25 µm pixels
Charge Integrating
JUNGFRAU 1M
75 µm pixels
Charge Integrating
interpolated image with Mönch
(~1 mm resolution after interpolation)
25 x 25 μm2 bumped (!) pixels
320 eV energy resolution FWHM -> interpolation possible -> 1 µm res.
Large dynamic range
mask made from photo

## Slide 38: AGIPD (adaptive gain) ... EU XFEL Pixel Detector
First XFEL Light
addressing >104 dynamic range @ EU XFEL
by “adaptive gain stages” (as JUNGFRAU)
first XFEL Light has been seen ...

## Slide 39: X-ray imaging with Monolithic SOI Pixels
Image taken with single SOI pixel detector 17 x 17 µm2 pixels, 500 µm bulk thickness
Double SOI pixel detector
with > 10 Mrad TID tolerance
Notes: DSOI = repeating the layer transfer step twice during wafer production

## Slide 40: Conclusions
Silicon detectors remain the working horse for tracking and imaging detectors, especially in high rate and/or high radiation environments.
This HSTD11 (2017) Conference is an excellent forum presenting the current state of the art.

## Slide 41
BACKUP

## Slide 42: Radiation effects in 65 nm CMOS small channel devices
W = moderate size
W = minimum size
cartoons: F. Faccio, TWEPP2015
heating
trap release
L = moderate size
L = minimum size

## Slide 43: Performance of sensor fabricated in CMOS
noise
116 e-
131 e-
DC
AC
compare IBL
- planar sensors (CD = 117 fF): ENC = 120 e-
- 3D-Si sensors (CD = 180 fF): ENC = 140 e-
110 V
D.-L. Pohl et al., JINST 12 (2017) no.06, P06020
before
irradiation
after
irrad
before
irradiation
3.2 GeV e-
IV curves of all samples ok (bias 120 V -> 500 V)
about 220 µm depletion depth
leakage current 20 µA / cm3 (IBL: 15 µA/cm3)
noise as in standard sensors - planar sensors (CD = 117 fF): ENC = 120 e-
- 3D-Si sensors (CD = 180 fF): ENC = 140 e-
high efficiency after irradiation (1 x 1015 neq/cm2)