## Slide 1: WP4 Meeting, ALBA Cryogenic SEY measurements 7/11/2016
Taaj Sian
Reza Valizadeh, Oleg Malyshev

## Slide 2: Outline
We need to measure the SEY of materials at Cryogenic temperatures
To do this we will need to cool the samples to these temperatures
We will also need to desorb gas onto the samples

## Slide 3: Particle Counts
Measurements taken with 0.5 bar of filtered N2 onto sample 50 mm away from the sample
The measurements were taken for 1 minute and the counts were averaged over 3 measurements

## Slide 4: Particle Counts
Largest particle size measured was 1 micron
The sample prepared in Ar had the lowest counts
Polished and untreated samples were used as reference
The detector could measure particles up to 25 microns
Chart: Particle counts between 0.3 and 0.5 microns
| 5mm Air | 30mm Air | 5mm Ar | Polished | Untreated
 | 7239 | 2436 | 1519 | 318 | 177
Chart: Particle counts between 0.5 and 1 micron
| 5mm Air | 30mm Air | 5mm Ar | Polished | Untreated
 | 1801 | 706 | 636 | 136 | 106

## Slide 5: Current SEY system
350
225
60
125
Current bellows go from 120 to 65 mm during normal operation
85
35
100
8
10
150
Electron gun

## Slide 6: Un upgrade to current system for cooling sample to 77 K
CO2 injection via leak valve
Flexible hose
LN
350
225
60
125
120 - 65
85
150
35 mm
100
8
10
Electron gun

## Slide 7: A new system with sample temperature between 3.5 and 80 K Option 1:
Injecting gas to the test chamber at a pressure Ptc for a period of time tinj
20
200
8
Electron gun
s[mbarl/cm2] =Ptc S tinj /Asample (1)
Pg, Vg
A flow of injected gas q:
q [mbarl/s] = Vg dPg/dt
Pumping speed:
S [l/s] = Q / Ptc
then concentration of cryosorbed gas s on the sample surface:
Ptc
s[mbarl/cm2] =  Ptc v(M,T) Asample tinj (2)
A less accurate method:
flow of gas q to the surface Asample is
q = v(M,T) Asample Ptc
then
Sticking probability should  me measured or use literature data.
Since  ≤ 1, then  = 1 gives maximum possible s.

## Slide 8: A new system with sample temperature between 3.5 and 80 K Option 2:
Fill with a set amount of gas
from a defined volume Vg
at known pressure Pg.
Majority of gas should cryosorb to the sample as it is the only part of that is cold besides the gap which has low conductance.
Pg, Vg
20
200
8
Electron gun
s[mbarl/cm2] =PgVg/Asample
Ptc
This method is more precise, the total amount of cryosorbed gas Q can be checked by heating the sample and measuring Ptc
Q [mbarl] = PtcVtc
and
s[mbarl/cm2] =PtcVtc/Asample

## Slide 9: A new system with sample temperature between 3.5 and 80 K Option 2: accuracy
d
D
For d = 20 mm and D = 21 mm
Area ratio is 10 thus maximum uncertainty in the total amount of cryosorbed gas Q is 10%
Gap
Sample
D
d

## Slide 10: Thanks Questions?