## Slide 1
Comparison of Silicon, Germanium and Diamond sensors for Using it in HEP Detector Applications
Advanced Detectors for Nuclear, High Energy and Astroparticle Physics
Bose Institute Kolkata
Shyam Kumar1 , Raghava Varma1, K.Das Gupta1, Pradeep Sarin1, S.K. Deb2
Department of Physics, IIT Bombay, Mumbai1
CRNTS, IIT Bombay, Mumbai2
Email: shyam055119@gmail.com
Thanks for ALICE Utilization and Upgrade Project and IRCC, IIT Bombay for Support
15-17 February 2017

## Slide 2: Outline
Important properties of HEP detectors
Simulation for Charge created by MIP
Comparison of Radiation damage
Particle Identification capabilities
MPCVD System designing
Growth of diamond film and Characterization
Summary and Future Plan

## Slide 3: Important properties of HEP detectors
pb-pb collision in ALICE @5.02 TeV
Particle colors:
Blue: Electrons
Green: Muons
Red: Pions
Yellow: Kaons
Orange: Protons
PMD
AliAOD.root
High precision tracking=> Semiconductor detectors
Typical choice of semiconductors are Si, Ge and Diamond
Material should have following properties:
High signal to noise ratio for good position resolution
2. Low material budget for less multiple scattering
3. Fast pulse timing for less pile up
4. Low radiation damage
5. Particle Identification capabilities
In this talk we will compare Si, Ge and Diamond and will try to figure out the suitable material for High energy and high luminosity experiments

## Slide 4
40 cm
60 cm
Geometry used for Simulation
Double sided strip sensors
Simulation for Charge created by MIP
Simulation and Digitization in
PANDA Root
Diamond (has low material budget than Si ( and Ge ( for same thickness i.e. diamond will have less
Ref: “Particle Detectors”, C. Grupen and B. A. Shwartz
Diamond has low multiple scattering

## Slide 5
Signal to Noise ratio for Sensors
MIP
Thickness=0.3 mm
for Intrinsic material
Material | MPV Signal |  |  |  | Noise (e)
Silicon | 22680 | 640 | 1450 | 505 | 
Germanium | 57070 | 0.46 | 3900 | 1800 | 
Diamond | 9645 |  | 1800 | 1600 | 0.013
Material | MPV Signal |  |  |  | Noise (e)
Silicon | 22680 | 640 | 1450 | 505 | 
Germanium | 57070 | 0.46 | 3900 | 1800 | 
Diamond | 9645 |  | 1800 | 1600 | 0.013

## Slide 6
Signal to Noise ratio for intrinsic Si, Ge are very small so we can not use them intrinsic material but diamond can be used as intrinsic material
The intrinsic noise can be reduced by increasing some how resistivity=> p-n junction in reverse bias condition
Silicon sensor reverse biased:
Material | Voltage | Current |  | Noise (e) | Signal/Noise
Silicon | 300 V |  |  | 9591 | 2.365
Silicon | 300 V |  |  | 10 | 2268
Material | Voltage | Current |  | Noise (e) | Signal/Noise
Silicon | 300 V |  |  | 9591 | 2.365
Silicon | 300 V |  |  | 10 | 2268
Just rough numbers
Diamond
Si and Ge same detector concept

## Slide 7
Signal to Noise Ratio: Expressed in terms of ENC (Equivalent Noise Charge)
1. Shot Noise due to :
2. Parallel thermal noise:
3. Series thermal noise from metal strip resistance:
4. Preamplifier noise:
, a and b preamplifier design parameters
For making the small noise design follow the below specification:
Small load capacitance =
(∼ depends on strip dimension) to minimize and
low leakage current to minimize
high parallel resistance to minimize
small series resistance to minimize
Ref: Evolution of Silicon sensor technology in Particle Physics: pages: 27-28
Frank Hartmann

## Slide 8
Impact Parameter IP: for short lives particles , If life time is => Impact parameter 30-3000
Binary Readout:
Limited position resolution or
Analogue Readout:
Nonlinear Eta Algorithm- For small track angles where diffusion is large
Simple linear Analogue Head Tail algorithm- For large angle tracks
Charge Centre of gravity method- For middle range of angles
Best Position resolution
ENC Silicon: (DELPHI microvertex)
s, , , ,
,
ENC Diamond: (Estimation)
s, , , ,
161 e
Ref: First measurements with a diamond microstrip detector, NIM, Research A 354 (1995) 318-327
Ref: “Spatial resolution of silicon microstrip detectors”,
R. Turchetta, Nuclear Instruments and Methods in Physics

## Slide 9: Comparison of Radiation damage
Surface damage: Ionizing energy loss due to electron stopping=> Not present in diamond sensors as no oxide layer
Bulk damage: Non-Ionizing energy loss due to Nuclear stopping
DOSE Equivalent: For real experiments
Both types of damage reduces Signal to Noise ratio 10 is critical value
(Si)
(Ge)
(Di)
of incident particles in eV
Fluka Simulation

## Slide 10
Si1MeVNeutronEquivalent: For real experiments
In diamond, there will be no surface damage , bulk damage will be smallest and also less number of Single Event Upset (simple concept of detector as compared to Si, CMOS, LGAD)
Bulk damage
Particles
thick material
SEU: Single Event Upset (Random in time) may cause loss of data but temporary most of the time
Diamond has low radition damage than others
Thanks to Michael Moll (RD50), CERN
and Moritz Guthoff, CMS (CERN)

## Slide 11: Particle Identification capabilities
Particle Identification: Determination of mass and charge of the Particle
dEdX vs Momentum method => Band merging due to Landau distribution and MIP
Time of Flight=> Measurement of time of flight
and vs momentum plot, band merging due
to time resolution of detectors
S
S
Diamond can be used as dEdX detector

## Slide 12
Diamond can also be used as ToF detector
L= 6.4 m
3. Cherenkov PID:
Refractive Index n= 2.417 ??????

## Slide 13
MPCVD : Microwave Plasma Chemical Vapour Deposition System & Resonant Cavity
MPCVD System designing
TE11 mode
TE10 mode
Computer Simulation Technology
Used also in accelerator designing
Real System in Lab

## Slide 14
Range of G Band ~ 1500-1600 Range of D Band ~ 1300-1400
2D Band ~ 2650-2700
Raman Spectroscopy
Diamond Picture
1 mm thick diamond
Growth of diamond film and Characterization
Diamond looking yellow due to Nitrogen content
Electronic grade diamond has N in Parts per billion level (ppb)
Thanks to Aman Bajaj, Sushant Raniwala, Krishna Chaitanya and Nilormi (summer student)
Growth Parameters of Diamond film:
HPHT diamond (100) substrate
Hydrogen=250 sccm and Methane=2.0 sccm
Pressure 90-91 torr (atmospheric pressure=760 torr)
Temperature =916-938
Power Input = 0.7 kW
Power reflected = 0 kW
Deposition time=198.5 hrs
Thickness of film 1 mm (grown)

## Slide 15: Characterization techniques
C-DLTS: Capacitance Deep Level Transient Spectroscopy
XPS (X-ray photoelectron spectroscopy): For elemental composition
I-DLTS: Current Deep Level Transient Spectroscopy
TSC: Thermally Stimulated Currents
RL: Recombination Life-time Measurements
PC: Photo Conductivity Measurements
PL –Photoluminescence
Raman Spectroscopy
IV-CV Characteristics: For leakage current and capacitive noise determination
Atomic Force Microscopy (AFM)
Transient current technique (TCT): For electron and hole mobility determination
HRXRD: High Resolution X-ray Diffraction
N-V Center reduces CCE
Ref. Diamond nitrogen vacancy impurity ppt, April 2013, physics 6530, Stefan Thonnard

## Slide 16
Diamond peak
at
Diamond peak
at
High Resolution XRD @ Department of Physics IIT Bombay
Raman Spectroscopy @ CRNTS, IIT Bombay
2 119.443
2 119.443
Diamond film shows the good XRD and Raman spectrum

## Slide 17
Ohmic Contact: Thermal Evaporation (Both side)
Cr/Au: 20 nm/100 nm
Slow Annealing of the sample up to 605 K
Sample 407 :
Sample 407
Thick film
Resistance =
Resistance =
I-V done at BARC, Thanks to Amit and Dr. Anita Topkar (Electronics division BARC)
Contact made @ CEN, IIT Bombay
Diamond peak
at
Red Laser =632.8 nm
I-V looking promising

## Slide 18
Transient Current Technique (TCT) measurement for diamond
- source of energy, 5486 KeV (85%), 5443 KeV (13%) and 5388 KeV (1%)
Range of in Material: Fluka simulation (Ionizing Energy Loss (IEL))
Bragg’s Peak
Curve highly useful in cancer treatment (Medical Applications)
Diamond
IEL 5485.9 KeV
NIEL KeV
Signal=5485900/13.6
=403375 e-h pairs
thick material
Experimental measurement:
3.5 3.5 0.4 diamond (IIA technologies)
will stop with in of diamond
Silicon
IEL 5485.9 KeV
NIEL KeV
Signal=5485900/3.6
= 1523861 e-h pairs
Germanium
IEL 5485.8 KeV
NIEL KeV
Signal=5485800/2.96
= 18,53311 e-h pairs
Gain of cividec amplifier= +40 dB =>
Ref: Electron-Hole-Pair Creation Energies in Semiconductors , PRL, Volume 35, Number 32

## Slide 19
100 = 100
Cividec Amplifier CERN, used for testing
Timing of diamond pulse of the order of ns

## Slide 21: Summary and Future Plan
Diamond has good signal to noise ratio, fast timing, low material budget, low radiation damage and good particle identification capabilities, so it will be a good choice for HEP experiments
Diamond has large e-h pair creation energy so less disturbance in charge center of gravity
Diamond can also be used for the detection of slow and fast neutrons
We have grown diamond film up to 1 mm thickness it has nitrogen, I will do cutting and polishing and will test again
We have also tested good quality diamond from IIA technologies
The only problem with diamond we don’t have large area high quality diamond
Still working on growing high quality diamond in Lab
Thank You !!!
FLUKA Simulation used Ref : "FLUKA: a multi-particle transport code" A. Ferrari, P.R. Sala, A. Fasso`, and J. Ranft, CERN-2005-10 (2005), INFN/TC_05/11, SLAC-R-773

## Slide 22
n
9Be
Fast neutrons
Tritium (2.73 MeV) and emitted at
14.1 MeV n, with and 9
Ref: CVD Diamond Neutron Detectors, Arnaldo Galbiati
Diamond as Neutron detectors
Diamond Pulse time Estimation at E field = :
Experimental

## Slide 23: Comparison of Material budget [For geometry in Slide 4]
1000000 Geantino particle with multiplicity 5 of 0.1- 0.5 GeV/c

## Slide 25
Diamond peak
at
Raman Spectra taken as a function of depth

## Slide 26: Atomic force Microscopy (AFM) [Polishing of 407 is compared to thick film]
407 film
407 film
Thick film
Thick film
AFM @ Department of Physics IIT Bombay

## Slide 27
Single Port – reflection coefficient,
For two Ports
Frequency= 2.45 0.020 GHz
S parameter -50 dBW = -20 dBm=10
Decibel-milliwatts (dBm)= Decibel watt (dBW) +30
MPCVD : Advantages
Electrode less process=> No Plasma sheath
formation take place
Plasma density is high
Stability of Plasma up to many days
Ability to scale up the process over large substrates
Quality of film grown is high
TE10 to TE11 mode converter simulation

## Slide 28
Energy loss vs momentum up to order of
Energy loss vs momentum up to order of

## Slide 29
Energy loss vs momentum up to order of

## Slide 30
Silicon
Diamond
dEdX band separation is good in diamond

## Slide 31
small
large
Large and Small Trapezoid used for Simulation in PANDAROOT

## Slide 32
Energy deposited in thick sensors (Geant3) PANDA Root

## Slide 33
Frankel Pairs distribution for 1 GeV proton in 300 Si

## Slide 34
Frankel Pairs distribution for 1 GeV proton in 300 Si