## Slide 1: Measurements of passive structures on irradiated HV-CMOS detectors
Bojan Hiti, Vladimir Cindro, Andrej Gorišek, Gregor Kramberger, Igor Mandić, Marko Mikuž, Marko Zavrtanik
On behalf of ATLAS Strip CMOS collaboration
Jožef Stefan Institute, Experimental Particle Physics Department (F9)
Ljubljana, Slovenia
12th Trento Workshop, 21.02.2017

## Slide 2: Outline
CHESS 2 chip introduction
Edge-TCT measurements
Acceptor removal parameters
90Sr measurements
Summary

## Slide 3: CHESS 2 chip
Developed by the ATLAS Strip CMOS collaboration as a candidate for HVCMOS strip detector for ATLAS Phase II upgrade
Design by UCSC, SLAC and KIT, produced in AMS H35 process, max. bias 120 V
  H. Grabas, Chess2 front end readout of the multi-segmented HV CMOS sensors, FEE 2016
Reticle size demonstrator chip, follow up of CHESS 1
  3 striplet arrays with fully digital encoding and readout
  1 pixel array with an in-strip amplifier and analog readout
  Several passive arrays for material studies – subject of this talk
18.6 mm
24.3 mm
digital
analog
passive

## Slide 4: Passive test structures on CHESS 2
Edge-TCT arrays, 3 x 3 pixels, pixel size: 630 x 40 μm2 (six 90.2 μm x 24.3 μm nwells in each pixel)
Large Passive Array, 1.3 x 1.3 mm2 for 90Sr measurements, implants ganged together (Large n-well, not used here)
Chips produced on four different substrate resistivities
  20 Ω·cm, 50 Ω·cm, 200 Ω·cm, 1 kΩ·cm
Irradiation study:
  Samples irradiated with neutrons in Ljubljana
  Fluences: 0, 1e14, 3e14, 5e14, 1e15, 2e15 neq/cm2
  Total 24 chips (4 x 6)

## Slide 5
Edge-TCT

## Slide 6: Edge-TCT setup
Edge TCT setup
HV
scope
GND
Substrate (p-type)
Pixels (n-well)
Beam direction
Detector connection scheme:
x
y
TCT measurements with passive pixels (no amplifier in the n-well)
 collecting electrode connected to the amplifier
( more details: www.particulars.si )
25 ns integr. time

## Slide 7: Edge-TCT measurements
depth
Chip surface
beam
FWHM
surface
depth
Sensors only partially depleted
Edge-TCT allows to study the depletion depth dependence on voltage/fluence
Charge collection width = FWHM of the charge collection profile
projection

## Slide 8: 20 Ω·cm Edge-TCT charge collection profiles
Charge collection width at 120 V changes with irradiation
  Increase at fluences above 5e14 neq/cm2 – initial acceptor removal
Low substrate resistivity  late acceptor removal
surface
depth
Preliminary!
20 Ω·cm
charge collection width

## Slide 9: 50 Ω·cm Edge-TCT charge collection profiles
Charge collection width increases up to 1e15 neq/cm2, then reducing
Acceptor removal finished earlier than with 20 Ω·cm substrate
surface
Preliminary!
50 Ω·cm

## Slide 10: 200 Ω·cm Edge-TCT charge collection profiles
variations of charge collection width are small
Maximal width reached around 5e14 neq/cm2
surface
Preliminary!
200 Ω·cm

## Slide 11: 1000 Ω·cm Edge-TCT charge collection profiles
Unirradiated sample could not be biased (breakdown)
Initially large charge colleciton width > 100 μm
Charge collection width monotonously falling with irradiation
High resistivity  acceptor removal completed below 1e14 neq/cm2
surface
Preliminary!
Vbias = 110 V
Φ = 1e14 neq cm-2
1000 Ω·cm

## Slide 12: 20 Ω·cm charge collection width vs. bias voltage
Preliminary!
Extract value of Neff from fit
0 V offset
20 Ω·cm
At Ф = 0:
Neff = 6.7e14 cm-3  20 W∙cm
Good agreement with nominal resistivity

## Slide 13: 50 Ω·cm charge collection width vs. bias voltage
Preliminary!
50 Ω·cm
At Ф = 0:
Neff = 2.3e14 cm-3  58 W∙cm
Preliminary!
200 Ω·cm
Neff(0) = 0.65e14 cm-3
 205 W∙cm
Preliminary!
1000 Ω·cm
neq cm-2
1000 Ω·cm best material in terms
of depletion depth
But sensitive breakdown behaviour

## Slide 14: Neff vs. fluence
Preliminary!
Removal completed below 1e14 neq/cm2
acceptor removal
radiation induced deep acceptors (gC = 0.02 cm-1 fixed)
Neff evolves differently for different initial wafer resistivities
Behaviour converges for fluences above 1e15 neq/cm2

## Slide 15: Acceptor removal constant vs. initial doping
Blue marker – charged hadron irradiated
Red marker – neutron irradiated
High resistivity fast acceptor removal (finished at low fluence)
Low resistivity slow acceptor removal (finished at high fluence)
CHESS2 (partly) fits in this picture
Removal constant for CHESS2 1kOhm-cm still not measured
Measurements by Edge-TCT in Ljubljana
LFoundry,
Mandić et al.,
arXiv 1701.05033
X-Fab
B. Hiti et al.,
arXiv 1701.06324
HVFEI4, CHESS 1,
G. Kramberger et al., JINST 2016
CHESS 2

## Slide 16: Charge collection width vs. fluence in CHESS 2
Chart: Φ (1014 neq/cm2)
| 0 | 1 | 3 | 5 | 10 | 20
20 Ω·cm | 13.899 | 16.421 | 17.5548 | 20.1115 | 30.4057 | 53.6307
50 Ω·cm | 23.7222 | 38.3511 | 46.0633 | 47.6521 | 65.6839 | 61.6993
200 Ω·cm | 44.6234 | 48.9579 | 54.2367 | 62.6271 | 56.8839 | 57.6086
1000 Ω·cm | 103.8554 | 80.446 | 75.0163 | 67.9893 | 53.6307
Charge collection width at 100 V for different wafers/fluences
Calculated from Neff measured with Edge-TCT using formula

## Slide 17
90Sr measurements

## Slide 18: 90Sr setup
HV-CMOS: small signals, large noise  S/N very low
  clean sample of events needed (no hits missing DUT)
  require a large detector (trigger rate), good collimation, small scintillator
Measurement:
  Calibration with a 300 µm thick Si pad detector
  1) Record N ( = 2500) waveforms
  2) Average over all waveforms and determine time of the signal peak
  3) Sample waveforms at the peak
  4) Fill spectrum
detector
ORTEC 142 charge sensitive amplifier + custom made shaper (25 ns)
+ digital oscilloscope
ampl.
90Sr
PMT
cooling jig
DUT

## Slide 19: 20 Ω·cm, 90Sr
Chart: Bias (V)
| 0 | 20 | 40 | 60 | 80 | 100 | 120
W1, not irr | 1236.2196 | 1488.8073 | 1855.7067 | 1947.4315 | 2160.9052 | 2362.8101 | 2595.8408
CHESS1 | 1351.787 | 1271.866 | 1632.77 | 1590.176 | 1783.223 | 2111.151 | 2189.24
W1 1e14 | 413.175 | 605.99 | 826.35 | 936.53 | 1101.8 | 1101.8 | 1267.07
W1 3E14 | 275.45 | 413.175 | 633.535 | 743.715 | 964.075 | 964.075 | 1129.345
W1 5E14 | 192.815 | 385.63 | 523.355 | 661.08 | 881.44 | 908.985 | 1129.345
W1 1E15 | 220.36 | 413.175 | 661.08 | 1019.165 | 1019.165 | 1211.98
W1 2E15 | 220.36 | 771.26 | 936.53 | 1432.34 | 1652.7 | 2010.785 | 2093.42
Diffusion contribution of approx. 1000 e- vanishes after irradiation
Signal increase due to acceptor removal at high fluences
Minimal mean charge at 100 V: 1000 e- (but would expect > 1600 el from Neff )
not irr.

## Slide 20: 50 Ω·cm, 90Sr
Chart: Bias (V)
| 0 | 19.813500000000001 | 39.968510000000002 | 59.963679999999997 | 79.939989999999995 | 99.854799999999997 | 119.4588
w7 not irrad. | 1416.136 | 2099.014 | 2391.676 | 2749.832 | 2828.608 | 2851.05 | 3430.649
w7, 1e14 | 628.605 | 828.293 | 1261.103 | 1466.287 | 1899.326 | 2114.586 | 2439.537
w7, 3e14 | 328.8873 | 587.8103 | 1010.0752 | 1397.3579 | 1525.993 | 1815.7664
w7, 5e14 | 268.2883 | 582.8522 | 796.6014 | 1148.0756 | 1249.7167
w7, 1e15 | 257.5457 | 726.9126 | 1288.2796 | 1581.6339 | 1896.7487 | 2132.8093
w7, 2e15 | 210.4438 | 452.5643 | 611.7745 | 917.2485 | 1137.6085 | 1179.2015
Minimal mean charge at 100 V: 1300 e- (extrapolated)

## Slide 21: 200 Ω·cm, 90Sr
Chart: Bias (V)
| 0 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 110 | 120
W13, not irrad. | 1759.636 | 2017.032 | 2425.797 | 2658.919 | 3041.578 | 3341.339 | 3566.904 | 3667.435 | 3926.663 | 4098.184 | 4205.814 | 4325.352 | 4595.572
w13 1e14 | 393.193 | 847.758 | 1171.106 | 1586.283 | 2001.231 | 2343.128 | 2644.034
w13 3e14 | 331.363 | 914.397 | 1471.096 | 1993.216 | 2347.937 | 3132.949
w13 5e14 | 374.415 | 945.999 | 1530.636 | 1882.38 | 2438.85 | 2864.332
w13 1e15 | 179.536 | 888.978 | 1421.174 | 1876.197 | 2392.821 | 2376.562
w13 2e15 | 155.491 | 673.031 | 993.631 | 1330.261 | 1654.067 | 1915.585
Minimal mean charge at 100 V: 2000 e- (extrapolated)

## Slide 22: 1000 Ω·cm, 90Sr
Chart: Bias (V)
| 0 | 19.563600000000001 | 39.362699999999997 | 59.187899999999999 | 79.006100000000004 | 98.769000000000005 | 116.461
1e14 not ann. | 256.9948 | 1646.6401 | 2625.0385 | 3641.7245 | 4404.7209 | 5499.9101 | 6304.2242
1e14 | 2681.2303 | 4096.4924 | 5247.0471 | 6427.0748 | 7480.9465
3e14 | 280.959 | 1329.0463 | 2101.1326 | 2889.7459 | 3432.6579 | 4220.1695
5e14 | 213.4737 | 1022.4704 | 1620.1969 | 2138.5938 | 2748.1646 | 2901.3149
1e15 | 199.4258 | 982.2547 | 1431.7891 | 1906.6649 | 2356.7502 | 2601.3498
2e15 | 252.0368 | 626.3733 | 1007.8715 | 1312.2438 | 1584.1129 | 1846.3413
Minimal mean charge at 100 V: 2000 e- (extrapolated)

## Slide 23: 90Sr comparison for different substrates
Preliminary!
CHESS 1 vs. CHESS 2 (20 Ω·cm) : trend is similar, but mean charge differs
could be due to a different wafer composition  different acceptor removal
More than 2000 el in whole fluence range for 200 Ohm-cm and 1 kOhm-cm
Measured charge after irradiation smaller then expected from depleted depth calculated from Neff

## Slide 24: Summary
Completed measurements of charge collection on passive structures on CHESS 2
  4 wafer resistivities 20 – 1000 Ω·cm, each wafer 6 neutron fluences up to 2e15 n/cm2
  Edge-TCT and 90Sr MIPs
Edge-TCT:
  Study of charge collection width for different substrates / irradiation levels
  Charge collection width may increase with irradiation  acceptor removal
  Determined parameters of the acceptor removal model
90Sr
  Mean collected charge at least 1000 electrons for any substrate and fluence
  Collected charge roughly follows the behaviour from Edge-TCT (increase due to acc. removal)
  Mean signals more than 2000 e- in whole fluence range for 200 Ω·cm and 1000 Ω·cm
  200 Ω·cm: smallest changes over whole fluence range

## Slide 25
BACKUP

## Slide 26: I-V characteristics
Measured on a TCT array
(3 x 3 pixels, pixel size 630 x 40 μm2)
At room temperature
not all measurement are good
20 Ω·cm
50 Ω·cm
200 Ω·cm
1000 Ω·cm

## Slide 27: Depletion zone shape at large depths
Large peak at the back side of charge collection profiles is commonly observed (especially with high resistivity samples)
This is due to an expansion of the depletion zone along the direction of the beam (pear shape)
Extra charge is due to an increased path of the beam in the sensitive region
This occurs for depleted depth ≥ structure width and on narrow structures (few neighbours)
chip surface
FW @ 30 %
Case A: depleted depth << structure size
no back peaks
Case B: depleted depth ≈ structure size
pear shape

## Slide 28: 2d Edge-TCT scan
depth
Chip surface
beam
Good response uniformity – no gaps between n-wells
200 Ω·cm, 3e14 neq/cm2

## Slide 29: Comparison of results from Edge-TCT and 90Sr
From Edge-TCT (Neff) calculate depleted depth W
assume 1000 e from diffusion before irradiation
Simulate charge collection in a pad detector of thickness W to estimate trapping loss
Observation: with 90Sr less charge is collected than expected from Edge-TCT
The reason is not understood: maybe simple pad detector approximation not correct, hints: different behaviour of border vs. central pixels (see backup)

## Slide 30: Top TCT 1
On irradiated samples charge from 90Sr measurements systematically less than expected for the depletion depth measured by Edge-TCT
Investigation with top TCT
  IR light – 980 nm, absorption depth in Si 100 μm  no reflections from back plane
W19 5e14
Large pass. array for 90Sr
(1.3 mm x 1.3 mm)
Gaps between pixels due to metalization on top of the chip
But on the large scale intensity in central pixels less than on edges !

## Slide 31: Top TCT 2
Difference in the collected charge indicates a larger depletion depth on the edges of the 90Sr array.
Edge-like pixels also measured in Edge-TCT. This may be a reason for discrepancy between the measurements.
W19 5e14

## Slide 32: Q-TCT calibration 1
Sr90 calibration procedure
using epitaxial diodes with known thickness (d = 50 and 100 μm) – similar thickness to CHESS 2, well known response
after epi-layer is fully depleted extract scaling factor A = d x 100 pairs/μm / Vsig
Only n-type diodes could be biased highly enough for calibration
p-type breaks down at 60 V, before full depletion

## Slide 33: Q-TCT calibration 2
Results:
calibration with n-type epi diodes
unirradiated CHESS 2 devices are compatible with the calibration
irradiated CHESS 2 devices (different wafers) have less charge than expected:
* Depleted depth for CHESS 2 is determined from the formula:

## Slide 34: 90Sr spectra 1000 Ω·cm
1e14 100 V
– Noise
– Signal
3e14 100 V
– Noise
– Signal
High resistivity wafer - Relatively good separation between signal and noise
No peak around 0 in signal spectrum  misalignment does not seem to be the main factor for smaller charge