## Slide 1: Status of 1st and 2nd ASIC prototype
Inge Diehl
Measurement results of 1st ASIC with flower device
Inspection of 24 chips, assembled with 30-µm solder balls, delivered by PacTech, end of October
Status 2nd ASIC
Next steps and questions

## Slide 2: Results of 1st ASIC with flower device of dSiMPl
Test set-up
Measurements with separate device
Measurements with device connected to ASIC pixel

## Slide 3: Test set-up
PG3 HG10 connected to resistor and oscilloscope
PG4 HG8 connected to ASIC pixel #31

## Slide 4: I-V measurements on PG3 HG10
Chart: I-V curve for 25°C
| 30 | 31 | 32 | 33 | 34 | 34.5 | 34.6 | 34.700000000000003 | 34.799999999999997 | 34.9 | 35 | 35.01 | 35.020000000000003 | 35.03 | 35.04 | 35.049999999999997 | 35.06 | 35.07 | 35.08 | 35.090000000000003 | 35.1 | 35.11 | 35.119999999999997 | 35.130000000000003 | 35.14 | 35.15 | 35.159999999999997 | 35.17 | 35.18 | 35.19 | 35.200000000000003 | 35.25 | 35.299999999999997 | 35.35 | 35.4 | 35.5 | 35.6 | 35.700000000000003 | 35.799999999999997 | 35.9 | 36 | 36.200000000000003 | 36.4 | 36.6 | 36.799999999999997 | 37 | 37.1 | 37.200000000000003 | 37.299999999999997
no LED | 8.44e-06 | 8.38e-06 | 8.44e-06 | 8.26e-06 | 8.58e-06 | 8.64e-06 | 8.54e-06 | 8.6e-06 | 8.88e-06 | 8.96e-06 | 9.02e-06 | 9.26e-06 | 9.1e-06 | 8.92e-06 | 8.6e-06 | 8.74e-06 | 9.8e-06 | 1.8e-05 | 4.88e-05 | 8.76e-05 | 0.00012 | 0.0001422 | 0.0001584 | 0.0001716 | 0.0001846 | 0.0001968 | 0.0002094 | 0.0002216 | 0.000233 | 0.000245 | 0.000258 | 0.000322 | 0.000386 | 0.000452 | 0.000516 | 0.00065 | 0.000784 | 0.000918 | 0.001052 | 0.001184 | 0.001322 | 0.001586 | 0.001844 | 0.002098 | 0.002344 | 0.002588 | 0.002706 | 0.002824 | 0.002942
blue LED | 8.64e-06 | 8.66e-06 | 8.66e-06 | 8.88e-06 | 9.04e-06 | 9.3e-06 | 9.44e-06 | 9.94e-06 | 1.016e-05 | 1.162e-05 | 1.498e-05 | 1.676e-05 | 1.79e-05 | 2.05e-05 | 2.98e-05 | 4.76e-05 | 6.94e-05 | 9.14e-05 | 0.0001144 | 0.0001312 | 0.0001458 | 0.000159 | 0.0001736 | 0.0001868 | 0.000199 | 0.0002112 | 0.0002246 | 0.0002362 | 0.000248 | 0.0002604 | 0.0002744 | 0.00034 | 0.0004046 | 0.0004704 | 0.0005376 | 0.0006708 | 0.0008052 | 0.0009402 | 0.001072 | 0.0012054 | 0.0013358 | 0.001602 | 0.001862 | 0.002112 | 0.0023616 | 0.002604 | 0.002722 | 0.00284 | 0.002956
IR LED | 8.92e-06 | 8.98e-06 | 9.18e-06 | 9.18e-06 | 9.22e-06 | 9.38e-06 | 9.5e-06 | 9.58e-06 | 9.88e-06 | 1.04e-05 | 1.316e-05 | 1.346e-05 | 1.466e-05 | 1.69e-05 | 2.184e-05 | 2.974e-05 | 4.16e-05 | 5.82e-05 | 8.02e-05 | 0.0001002 | 0.0001164 | 0.0001318 | 0.0001472 | 0.0001604 | 0.0001734 | 0.000186 | 0.0002 | 0.0002122 | 0.0002246 | 0.0002372 | 0.0002512 | 0.000304 | 0.00038 | 0.0004462 | 0.000513 | 0.000647 | 0.00078 | 0.000914 | 0.001048 | 0.00118 | 0.0013192 | 0.001582 | 0.001844 | 0.002098 | 0.002348 | 0.00259 | 0.002712 | 0.00283 | 0.002946
Chart: Breakdown voltage versus temperature
| -35.5 | -15.1 | 0.5 | 15.3 | 24.7 | 34.200000000000003
V_bd (V) | 33.3 | 33.91 | 34.38 | 34.82 | 35.1 | 35.37
Vbd = 35.09 V
Vbd
Rin = 50 Ω
Cin = 16 pF
in good agreement with Stefan’s results

## Slide 5: DCR measurements on PG3 HG10
RQ = 510 kΩ
Rin = 1 MΩ
Cin = 16 pF
Chart: DCR, single dSiPMl on RQ = 333 kΩ
| 33.299999999999997 | 33.32 | 33.35 | 33.369999999999997 | 33.4 | 33.5 | 33.6 | 33.799999999999997 | 34 | 34.5
-35.4°C | 89 | 93.18 | 109.07 | 116.23 | 145.35 | 187.7 | 241 | 325.5 | 390.6 | 462.8
0.5°C | 48.13 | 77.95 | 93.13 | 103.74 | 108.3 | 122.45 | 146.36 | 191.9 | 260 | 299.6 | 328.1 | 478 | 513.1 | 561.1 | 578.9
24.5°C | 23.05 | 46.08 | 75.28 | 88.65 | 102.83 | 142.33 | 184.8 | 280.5 | 325.6 | 398.8 | 512.5 | 628
Chart: DCR, single dSiPMl on RQ = 333 kΩ
| 9.9999999999980105E-3 | 3.0000000000001137E-2 | 6.0000000000002274E-2 | 7.9999999999998295E-2 | 0.10999999999999943 | 0.21000000000000085 | 0.31000000000000227 | 0.50999999999999801 | 0.71000000000000085 | 1.2100000000000009
-35.4°C | 89 | 93.18 | 109.07 | 116.23 | 145.35 | 187.7 | 241 | 325.5 | 390.6 | 462.8
0.5°C | 48.13 | 77.95 | 93.13 | 103.74 | 108.3 | 122.45 | 146.36 | 191.9 | 260 | 299.6 | 328.1 | 478 | 513.1 | 561.1 | 578.9
24.5°C | 23.05 | 46.08 | 75.28 | 88.65 | 102.83 | 142.33 | 184.8 | 280.5 | 325.6 | 398.8 | 512.5 | 628
Rres = 333 kΩ

## Slide 6: Connection scheme of ASIC and sensor
hit counter
0…3
infrared LED
LED pulse length
adjustable
ASIC pixel frontend
frame length: 1 µs
# of frames: 1000
Test result: # of hits in one frame
Vsupply = Vex
according to prior agreement with Stefan

## Slide 7: Measurements on PG4 HG8, Hit-counting with ASIC, 25°C
Chart: Dark counts at different Vex, 25°C
| 35.6 | 35.61 | 35.619999999999997 | 35.630000000000003 | 35.64 | 35.65 | 35.659999999999997 | 35.67 | 35.68 | 35.69 | 35.700000000000003 | 35.71 | 35.72 | 35.729999999999997 | 35.74 | 35.75 | 35.76 | 35.770000000000003 | 35.78 | 35.79 | 35.799999999999997 | 35.81 | 35.82 | 35.83 | 35.840000000000003 | 35.85 | 35.8599999999999 | 35.869999999999898 | 35.879999999999903 | 35.889999999999901 | 35.899999999999899 | 35.909999999999897 | 35.919999999999902 | 35.9299999999999 | 35.939999999999898 | 35.949999999999903 | 35.959999999999901 | 35.969999999999899 | 35.979999999999897 | 35.989999999999903 | 35.999999999999901 | 36.009999999999899 | 36.019999999999897 | 36.029999999999902 | 36.0399999999999 | 36.049999999999898 | 36.059999999999903 | 36.069999999999901
1.4 | 0 | 0 | 0.005 | 0.047 | 0.264 | 0.848 | 1.832 | 2.421 | 2.821 | 2.971 | 2.997 | 3
1.65 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.014 | 0.183 | 0.713 | 1.547 | 2.119 | 2.698 | 2.944 | 2.99 | 3 | 3
2 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.015 | 0.095 | 0.435 | 1.303 | 1.858 | 2.16 | 2.608 | 2.912 | 2.996 | 2.998 | 3 | 3
2.5 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.003 | 0.092 | 0.441 | 1.293 | 1.509 | 1.533 | 1.927 | 2.45 | 2.855 | 2.955 | 2.999 | 3
3.3 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.001 | 0.008 | 0.146 | 1.102 | 1.531 | 1.489 | 1.538 | 1.435 | 1.523 | 1.928 | 2.267 | 2.73 | 2.947 | 2.993 | 3
Chart: 1 LED pulse (100 ns) at different Vex, 25°C
| 35.450000000000003 | 35.46 | 35.47 | 35.479999999999997 | 35.49 | 35.5 | 35.51 | 35.520000000000003 | 35.53 | 35.54 | 35.549999999999997 | 35.56 | 35.57 | 35.58 | 35.590000000000003 | 35.6 | 35.61 | 35.619999999999997 | 35.630000000000003 | 35.64 | 35.65 | 35.659999999999997 | 35.67 | 35.68 | 35.69 | 35.700000000000003 | 35.71 | 35.72 | 35.729999999999997 | 35.74 | 35.75 | 35.76 | 35.770000000000003 | 35.78 | 35.79 | 35.799999999999997 | 35.81 | 35.82 | 35.83 | 35.840000000000003 | 35.85 | 35.86 | 35.869999999999997 | 35.880000000000003 | 35.89 | 35.9 | 35.909999999999997 | 35.92 | 35.93 | 35.94 | 35.950000000000003 | 35.96 | 35.97 | 35.979999999999997 | 35.99 | 36 | 36.01 | 36.020000000000003 | 36.03 | 36.04 | 36.049999999999997 | 36.06 | 36.07
1.4 | 0 | 0 | 0 | 0 | 0.004 | 0.118 | 0.763 | 0.984 | 1 | 1 | 1 | 1 | 1 | 1 | 1.002 | 1.033 | 1.444 | 1.932 | 2.007 | 2.058 | 2.309 | 2.491 | 2.9 | 2.997 | 3 | 3 | 3
1.65 | 0 | 0 | 0 | 0 | 0 | 0.03 | 0.419 | 0.972 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1.051 | 1.502 | 1.919 | 2.014 | 2.118 | 2.201 | 2.236 | 2.803 | 2.998 | 3 | 3 | 3 | 3
2 | 0 | 0 | 0 | 0 | 0 | 0.003 | 0.374 | 0.997 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1.023 | 1.402 | 1.944 | 2.035 | 2.156 | 1.793 | 2.164 | 2.718 | 2.99 | 3 | 3 | 3 | 3 | 3
2.5 | 0 | 0 | 0.007 | 0.574 | 1.169 | 1.082 | 1.049 | 1.01 | 1.008 | 1.015 | 1.005 | 1.007 | 1.182 | 1.816 | 2.085 | 2.039 | 1.832 | 2.093 | 2.491 | 2.897 | 2.995 | 3 | 3 | 3
3.3 | 0 | 0.004 | 0.229 | 1.603 | 1.633 | 1.415 | 1.409 | 1.36 | 1.297 | 1.264 | 1.391 | 1.727 | 1.523 | 1.648 | 1.86 | 2.11 | 2.224 | 2.41 | 2.872 | 2.989 | 2.999 | 3 | 3
Chart: 2 LED pulses at different Vex, 25°C
| 35.35 | 35.36 | 35.369999999999997 | 35.380000000000003 | 35.39 | 35.4 | 35.409999999999997 | 35.42 | 35.43 | 35.44 | 35.450000000000003 | 35.46 | 35.47 | 35.479999999999997 | 35.49 | 35.5 | 35.51 | 35.520000000000003 | 35.53 | 35.54 | 35.549999999999997 | 35.56 | 35.57 | 35.58 | 35.590000000000003 | 35.6 | 35.6099999999999 | 35.619999999999898 | 35.629999999999903 | 35.639999999999901 | 35.649999999999899 | 35.659999999999897 | 35.669999999999902 | 35.6799999999999 | 35.689999999999898 | 35.699999999999903 | 35.709999999999901 | 35.719999999999899 | 35.729999999999897 | 35.739999999999903 | 35.749999999999901 | 35.759999999999899 | 35.769999999999897 | 35.779999999999902 | 35.7899999999999 | 35.799999999999898 | 35.809999999999903 | 35.819999999999901 | 35.829999999999899 | 35.839999999999897 | 35.849999999999902 | 35.8599999999999 | 35.869999999999898 | 35.879999999999903 | 35.889999999999901 | 35.899999999999899 | 35.909999999999897 | 35.919999999999902 | 35.9299999999999 | 35.939999999999898 | 35.949999999999903 | 35.959999999999901 | 35.969999999999899 | 35.979999999999897 | 35.989999999999903 | 35.999999999999901 | 36.009999999999899 | 36.019999999999897 | 36.029999999999902 | 36.0399999999999 | 36.049999999999898 | 36.059999999999903 | 36.069999999999901
1.4 | 0 | 0 | 0 | 0 | 0 | 0 | 0.262 | 0.525 | 0.526 | 0.976 | 1 | 1 | 1 | 1 | 0.999 | 0.998 | 1.318 | 1.954 | 2 | 2 | 2 | 2 | 2 | 2 | 2.001 | 2.085 | 2.999 | 2.972 | 2.936 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3
1.65 | 0 | 0 | 0 | 0 | 0 | 0.008 | 0.304 | 0.998 | 1 | 1 | 0.997 | 1.157 | 1.809 | 1.998 | 2 | 2 | 2 | 2 | 2 | 2 | 2.009 | 2.416 | 2.992 | 2.996 | 2.905 | 2.991 | 3 | 3 | 3 | 3 | 3 | 3 | 3
2 | 0 | 0 | 0 | 0 | 0.526 | 1.063 | 1.062 | 1.56 | 2.017 | 2 | 2 | 2 | 2 | 2 | 2 | 2.004 | 2.167 | 2.811 | 2.967 | 2.77 | 2.401 | 2.371 | 2.772 | 2.994 | 3 | 3 | 3 | 3 | 3
2.5 | 0 | 0 | 0.001 | 0.215 | 1.753 | 2.107 | 2.07 | 2.047 | 2.026 | 2.013 | 2.012 | 2.004 | 2.018 | 2.219 | 2.761 | 2.569 | 2.279 | 2.243 | 2.719 | 2.98 | 3 | 3 | 3 | 3
3.3 | 0 | 0 | 0.168 | 1.361 | 1.728 | 2.006 | 2.121 | 2.161 | 2.166 | 2.212 | 2.254 | 2.127 | 2.055 | 1.878 | 2.073 | 2.504 | 2.697 | 2.813 | 2.95 | 2.999 | 3 | 3 | 3
Chart: 3 LED pulses at different Vex, 25°C
| 35.299999999999997 | 35.31 | 35.32 | 35.33 | 35.340000000000003 | 35.35 | 35.36 | 35.369999999999997 | 35.380000000000003 | 35.39 | 35.4 | 35.410000000000103 | 35.420000000000101 | 35.430000000000099 | 35.440000000000097 | 35.450000000000102 | 35.4600000000001 | 35.470000000000098 | 35.480000000000103 | 35.490000000000101 | 35.500000000000099 | 35.510000000000097 | 35.520000000000103 | 35.530000000000101 | 35.540000000000099 | 35.550000000000097 | 35.560000000000102 | 35.5700000000001 | 35.580000000000098 | 35.590000000000103 | 35.6000000000002 | 35.610000000000198 | 35.620000000000203 | 35.630000000000202 | 35.6400000000002 | 35.650000000000198 | 35.660000000000203 | 35.670000000000201 | 35.680000000000199 | 35.690000000000197 | 35.700000000000202 | 35.7100000000002 | 35.720000000000198 | 35.730000000000203 | 35.740000000000201 | 35.750000000000199 | 35.760000000000197 | 35.770000000000202 | 35.7800000000002 | 35.790000000000198 | 35.800000000000303 | 35.810000000000301 | 35.820000000000299 | 35.830000000000297 | 35.840000000000302 | 35.8500000000003 | 35.860000000000298 | 35.870000000000303 | 35.880000000000301 | 35.890000000000299 | 35.900000000000297 | 35.910000000000302 | 35.9200000000003 | 35.930000000000298 | 35.940000000000303 | 35.950000000000301 | 35.960000000000299 | 35.970000000000297 | 35.980000000000302 | 35.9900000000004 | 36.000000000000398 | 36.010000000000403 | 36.020000000000401 | 36.030000000000399 | 36.040000000000397 | 36.050000000000402 | 36.0600000000004 | 36.070000000000398
1.4 | 0 | 0 | 0.003 | 0.357 | 0.525 | 0.495 | 0.509 | 0.528 | 0.632 | 0.994 | 1 | 1 | 1 | 1.011 | 1 | 1 | 1 | 1 | 1 | 1.027 | 1.786 | 2.789 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3
1.65 | 0 | 0 | 0.016 | 0.572 | 0.987 | 1 | 1.159 | 1.088 | 1 | 1 | 1.012 | 1.531 | 2.672 | 2.999 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3
2 | 0 | 0 | 0 | 0.001 | 0.89 | 1.441 | 1.059 | 1.552 | 2.777 | 2.999 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3
2.5 | 0 | 0 | 0 | 0.139 | 1.409 | 1.934 | 2.566 | 2.756 | 2.941 | 2.981 | 2.985 | 2.99 | 2.989 | 2.691 | 2.636 | 2.944 | 2.817 | 2.612 | 2.774 | 2.981 | 3 | 3 | 3 | 3
3.3 | 0 | 0 | 0.01 | 0.331 | 1.471 | 1.269 | 1.189 | 1.341 | 1.448 | 2.174 | 2.573 | 2.509 | 2.358 | 2.319 | 2.195 | 2.534 | 2.841 | 2.878 | 2.986 | 3 | 3 | 3 | 3
Vrecharge = Vquench = 1 V

## Slide 8: Dark measurements on PG4 HG8, Hit-counting with ASIC
Chart: Temperature (°C)
| -35.200000000000003 | -25.3 | -15.2 | 0.7 | 15.3 | 24.7 | 34.200000000000003
1 Hit | 33.94 | 34.21 | 34.51 | 34.97 | 35.39 | 35.65 | 35.92
V_bd (V) | 33.3 | 33.91 | 34.38 | 34.82 | 35.1 | 35.37
Chart: dark measurements
Vex = 1.4 V instead of 3.3 V, to decrease Vthreshold of FE-Inverter
→ Vbias 1 Hit = Vbd + Vov (Vthreshold+ Vx)
Vrecharge = Vquench = 1 V
Vbd

## Slide 9: Measurements on PG4 HG8, Hit-counting with ASIC, Vex = 1.4 V
Chart: Vquench = Vrecharge = 0.57 V
| 35.450000000000003 | 35.46 | 35.47 | 35.479999999999997 | 35.49 | 35.5 | 35.51 | 35.520000000000003 | 35.53 | 35.54 | 35.549999999999997 | 35.56 | 35.57 | 35.58 | 35.590000000000003 | 35.6 | 35.61 | 35.619999999999997 | 35.630000000000003 | 35.64 | 35.65 | 35.659999999999997 | 35.67 | 35.68 | 35.69 | 35.700000000000003 | 35.71 | 35.72 | 35.729999999999997 | 35.74 | 35.75 | 35.76 | 35.770000000000003 | 35.78 | 35.79 | 35.799999999999997
1-LED pulse | 0 | 0 | 0 | 0 | 0.006 | 0.296 | 0.984 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1.05 | 1.272 | 1.671 | 2.152 | 2.53 | 2.751 | 2.934 | 2.988 | 2.996 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3
2-LED pulses | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.669 | 0.982 | 0.78 | 0.996 | 1 | 1 | 1 | 1 | 0.999 | 1.052 | 1.524 | 1.952 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2.006 | 2.074 | 2.254 | 2.509 | 2.63 | 2.775 | 2.938 | 2.988 | 2.998 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3
3-LED pulses | 0 | 0 | 0.019 | 0.783 | 0.999 | 0.959 | 0.608 | 0.516 | 0.934 | 1.188 | 1.052 | 1 | 1.002 | 1.359 | 1.685 | 1 | 1 | 1 | 1 | 1.012 | 1.662 | 2.636 | 2.735 | 2.995 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 2.998 | 2.996 | 2.98 | 2.908 | 2.677 | 2.5 | 2.74 | 2.937 | 2.992 | 2.999 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3
good range: Vbias = 35.52 V … 35.62 V
Chart: Vquench = Vrecharge = 1 V
dark | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.005 | 0.047 | 0.264 | 0.848 | 1.832 | 2.421 | 2.821 | 2.971 | 2.997 | 3
100-ns IR-LED pulses, frame rate = 1 MHz
BUT: In this range, the sensor doesn’t work in Geiger mode, but in proportional mode!
Dark events produce too small signal → no detection.
In Geiger-mode range, DCR too high.

## Slide 10: Measurements on PG4 HG8, Hit-counting with ASIC, Vex = 1.4 V
Chart: DCR, Frame rate = 1 MHz, Vex = 1.4 V
| 35.6 | 35.61 | 35.619999999999997 | 35.630000000000003 | 35.64 | 35.65 | 35.659999999999997 | 35.67 | 35.68 | 35.69 | 35.700000000000003 | 35.71 | 35.72 | 35.729999999999997 | 35.74 | 35.75 | 35.76 | 35.770000000000003 | 35.78 | 35.79 | 35.799999999999997 | 35.81 | 35.82 | 35.83 | 35.840000000000003 | 35.85 | 35.86 | 35.869999999999997 | 35.880000000000003 | 35.89 | 35.9
Vq = Vr = 1.4 V | 0 | 0 | 2 | 16 | 154 | 675 | 1415 | 2275 | 2712 | 2927 | 2993 | 2998 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000
Vq = Vr = 1 V | 0 | 0 | 2 | 33 | 149 | 761 | 1596 | 2222 | 2790 | 2965 | 2996 | 2998 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000
Vq = Vr = 0.57 V | 0 | 0 | 0 | 21 | 144 | 587 | 1229 | 1891 | 2343 | 2717 | 2906 | 2967 | 2994 | 2996 | 2998 | 2999 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000 | 3000
DCR very high and the increasing very fast.
Maybe we should increase the threshold again, to be sure that the sensor works in Geiger mode.
More investigation in measurements.
DCR measurement limited by the hit-counter depth.

## Slide 11: Measurements on PG4 HG8, Hit-counting with ASIC, Vex = 3.3 V
Chart: 25°C, 100-ns LED pulse, FR = 1 MHz, Vquench = Vrecharge = 1 V
| 35.6 | 35.61 | 35.619999999999997 | 35.630000000000003 | 35.64 | 35.65 | 35.659999999999997 | 35.67 | 35.68 | 35.69 | 35.700000000000003 | 35.71 | 35.72 | 35.729999999999997 | 35.74 | 35.75 | 35.76 | 35.770000000000003 | 35.78 | 35.79 | 35.799999999999997 | 35.81 | 35.82 | 35.83 | 35.840000000000003 | 35.85 | 35.8599999999999 | 35.869999999999898 | 35.879999999999903 | 35.889999999999901 | 35.899999999999899 | 35.909999999999897 | 35.919999999999902 | 35.9299999999999 | 35.939999999999898 | 35.949999999999903 | 35.959999999999901 | 35.969999999999899 | 35.979999999999897 | 35.989999999999903 | 35.999999999999901 | 36.009999999999899 | 36.019999999999897 | 36.029999999999902 | 36.0399999999999 | 36.049999999999898 | 36.059999999999903 | 36.069999999999901
dark | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.001 | 0.008 | 0.146 | 1.102 | 1.531 | 1.489 | 1.538 | 1.435 | 1.523 | 1.928 | 2.267 | 2.73 | 2.947 | 2.993 | 3
LED 1 Puls | 0 | 0.004 | 0.229 | 1.603 | 1.633 | 1.415 | 1.409 | 1.36 | 1.297 | 1.264 | 1.391 | 1.727 | 1.523 | 1.648 | 1.86 | 2.11 | 2.224 | 2.41 | 2.872 | 2.989 | 2.999 | 3 | 3
LED 2 Pulses | 0 | 0 | 0.168 | 1.361 | 1.728 | 2.006 | 2.121 | 2.161 | 2.166 | 2.212 | 2.254 | 2.127 | 2.055 | 1.878 | 2.073 | 2.504 | 2.697 | 2.813 | 2.95 | 2.999 | 3 | 3 | 3
LED 3 Pulses | 0 | 0 | 0.01 | 0.331 | 1.471 | 1.269 | 1.189 | 1.341 | 1.448 | 2.174 | 2.573 | 2.509 | 2.358 | 2.319 | 2.195 | 2.534 | 2.841 | 2.878 | 2.986 | 3 | 3 | 3 | 3
Chart: 25°C, 50-ns LED pulse, FR = 1 MHz Vquench = Vrecharge = 1 V
| 35.85 | 35.86 | 35.869999999999997 | 35.880000000000003 | 35.89 | 35.9 | 35.909999999999997 | 35.92 | 35.93 | 35.94 | 35.950000000000003 | 35.96 | 35.97 | 35.979999999999997 | 35.99 | 36 | 36.01 | 36.020000000000003 | 36.03 | 36.04 | 36.049999999999997 | 36.06 | 36.07 | 36.08 | 36.090000000000003 | 36.1
dark | 0 | 0 | 0 | 0 | 0.002 | 0.002 | 0.183 | 0.835 | 1.55 | 1.559 | 1.589 | 1.436 | 1.536 | 1.881 | 2.245 | 2.834 | 2.913 | 2.987 | 2.998 | 3 | 3 | 3 | 3 | 3 | 3 | 3
1 pulse | 0 | 0 | 0 | 0.005 | 0.086 | 0.981 | 1.291 | 1.198 | 1.474 | 1.58 | 1.523 | 1.486 | 1.667 | 1.659 | 1.851 | 2.029 | 2.647 | 2.95 | 2.994 | 2.998 | 3 | 3 | 3 | 3 | 3 | 3
2 pulses | 0 | 0 | 0 | 0.021 | 0.23 | 1.332 | 1.892 | 2.099 | 1.928 | 1.506 | 1.596 | 1.702 | 1.985 | 2.066 | 2.291 | 2.198 | 2.533 | 2.933 | 2.999 | 3 | 3 | 3 | 3 | 3 | 3 | 3
3 pulses | 0 | 0 | 0.001 | 0.049 | 0.654 | 1.452 | 1.43 | 1.624 | 1.541 | 1.514 | 1.912 | 2.069 | 2.053 | 2.236 | 2.498 | 2.863 | 2.995 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3
Vex = 3.3 V
More investigation in measurements.

## Slide 12: 30-µm bumping at PacTech
delivered end of October
24 chips with 30-µm solder balls
  Inspected by Keyence Digital Microscope VHX-5000
  2 chips with homogenous ball size: 22 – 24 µm
  8 chips with 1 – 5 Macro balls, in order of 27 – 31 µm
  2 chips with few missing bumps and Macro balls
  5 chips with solder bridges, 2 maybe useable
  2 with burnings, 1 maybe useable
  1 with some flat balls, usable
  4 not usable, setup, no balls on IO pads
  16 useable

## Slide 13: Bumping inspection: chip #g1
Chip with 3 macro balls and 1 missing bump

## Slide 14: Bumping inspection: chip #g1
Keyence Digital Microscope VHX-5000
Keyence 3D-Laserscanning Microscope VK-X
Chip with 3 macro balls and 1 missing bump
Standard IO balls: 21.7 µm* (σ = 0.3 µm)
Standard Matrix balls: 23.2 µm* (σ = 0.6 µm)
Macro balls: 25.9 µm* (IO), 32.1 µm*, 29.4 µm*
Empty pad: 3.2 µm*
*height in respect to top metal layer

## Slide 15: Bumping inspection: chip #sb1
Chip with 9 solder bridges, 1 macro ball, 2 displaced balls, and 39 free pads

## Slide 16: Bumping inspection: chip #sb1
Keyence Digital Microscope VHX-5000
Keyence 3D-Laserscanning Microscope VK-X
Chip with 9 solder bridges, 1 macro ball, 2 displaced balls, and 39 free pads
Standard IO balls: 23.3 µm* (σ = 0.6 µm)
Standard Matrix balls: 23.6 µm* (σ = 0.5 µm)
Solder bridges: 23.2 µm* (σ = 0.3 µm)
Macro ball: 29.2 µm* (IO)
Empty pads: 3.5 µm* (σ = 0.03 µm)
*height in respect to top metal layer

## Slide 17: Bumping inspection: #b2
Chip with 3 macro balls
Standard ball: 22 – 25 µm
Huge macro balls: 43 – 47 µm
burnings of PI in Matrix
Residual metal on pad
3 rows without bumping
IOs good

## Slide 18: Status 2nd ASIC
“Tape out”: 15. August
Number of prototypes: 40
Die size: 1918 x 2118 µm² (design: 1850 x 2015 µm²)
Die thickness: 256 µm (10 mils)
Parts already shipped to CERN: 11. November
Expected at DESY: this week

## Slide 19: Readout ASIC - components
16-by-16 matrix of pixel readout electronics
  active quenching and recharging circuit
  hit-counting and –serializing
  masking
fast trigger via wired-OR
slow trigger for validation, returns valid-event signal
  16 slow row-triggers as pre-stage, with 4 adjustable ref. voltages as threshold condition (1…4 or more pixels in 1 row)
  2nd-stage with 2 adjustable ref. voltages (1…2 or more row-triggers)
12-bit TDC (7-bit coarse, 5-bit fine TDC)
21-bit bunch counter
16:1 multiplexing scheme
clock generator
control register for static signals
  pixel masking
  counting depth (1 or 2 Bit)
  reference voltages for validation
  process-corner settings for validation and TDC
pad ring with LVDS TX/RX
separate test-circuits
  LVDS RX/TX
  TDC
34-bit serial output timing data
valid: 1 bit
bunch-counting value: 21 bit (bunch<20:0>)
fine-TDC: 5 bit (fine<4:0>)
coarse-TDC: 7 bit (coarse<6:0>)
256-bit serial output hit data
interleaved
pxl<0,4,8,12,1,5,9,13,2,6,19,14,3,7,11,15, 16,20,24,28,17,21,25,29,18,22,26,30,19,23,27,31,…>
265-bit serial input data
“H” followed by 264 input control bits

## Slide 20: 2nd ASIC prototype – final layout
16x16 pixel matrix
bunch counter
TDC
serializer
control register
20-µm pads
LVDS IOs
test circuit (LVDS) with wire-bond pads
validation logic
fast trigger
clock generator
test circuit (TDC) with wire-bond pads
16:1 multiplexer

## Slide 21: Next steps and questions
Bumped 1st ASIC to Munich for ball reflow test and bonding
Status of corresponding tests of dummy structures?
2nd ASIC can be send to PacTech
Status measurements for result comparison in Munich? (before visit of Stefan)
Test-board design for flipped 1st ASIC with sensor and 2nd ASIC with sensor in preparation
  Connection to DAQ-system
  Test at test beam
Test preparation of test-circuits on 2nd ASIC

## Slide 23: Measurements on PG4 HG8, Hit-counting with ASIC
Chart: Vex =3.3 V, 25°C Vquench = Vrecharge = 1 V
| 35.6 | 35.61 | 35.619999999999997 | 35.630000000000003 | 35.64 | 35.65 | 35.659999999999997 | 35.67 | 35.68 | 35.69 | 35.700000000000003 | 35.71 | 35.72 | 35.729999999999997 | 35.74 | 35.75 | 35.76 | 35.770000000000003 | 35.78 | 35.79 | 35.799999999999997 | 35.81 | 35.82 | 35.83 | 35.840000000000003 | 35.85 | 35.8599999999999 | 35.869999999999898 | 35.879999999999903 | 35.889999999999901 | 35.899999999999899 | 35.909999999999897 | 35.919999999999902 | 35.9299999999999 | 35.939999999999898 | 35.949999999999903 | 35.959999999999901 | 35.969999999999899 | 35.979999999999897 | 35.989999999999903 | 35.999999999999901 | 36.009999999999899 | 36.019999999999897 | 36.029999999999902 | 36.0399999999999 | 36.049999999999898 | 36.059999999999903 | 36.069999999999901
dark | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.001 | 0.008 | 0.146 | 1.102 | 1.531 | 1.489 | 1.538 | 1.435 | 1.523 | 1.928 | 2.267 | 2.73 | 2.947 | 2.993 | 3
LED 1 Puls | 0 | 0.004 | 0.229 | 1.603 | 1.633 | 1.415 | 1.409 | 1.36 | 1.297 | 1.264 | 1.391 | 1.727 | 1.523 | 1.648 | 1.86 | 2.11 | 2.224 | 2.41 | 2.872 | 2.989 | 2.999 | 3 | 3
LED 2 Pulses | 0 | 0 | 0.168 | 1.361 | 1.728 | 2.006 | 2.121 | 2.161 | 2.166 | 2.212 | 2.254 | 2.127 | 2.055 | 1.878 | 2.073 | 2.504 | 2.697 | 2.813 | 2.95 | 2.999 | 3 | 3 | 3
LED 3 Pulses | 0 | 0 | 0.01 | 0.331 | 1.471 | 1.269 | 1.189 | 1.341 | 1.448 | 2.174 | 2.573 | 2.509 | 2.358 | 2.319 | 2.195 | 2.534 | 2.841 | 2.878 | 2.986 | 3 | 3 | 3 | 3
Chart: Vex =3.3 V, 25°C Vquench = Vrecharge = 1 V