## Slide 1: DESIGN FOR ARC QUADRUPOLE
E. Todesco
CERN, Geneva Switzerland
C. Lorin
CEA, France
CERN, 9th December 2015
Future Circular Colliders – Other magnets

## Slide 2: CRITICAL CURRENT
Data from D. Tommasini
  1400 A/mm2 at 16 T, 4.5 K (red curve)
  At 1.9 K, 2250 A/mm2 at 16 T (black curve)
For the scaling laws I use an hyperbolic fit (dots in the fig)
  with b=23.5 T
  and s=4800 A/mm2

## Slide 3: Gradient VS COIL THICKNESS
Using the scaling laws I find the following relation width/gradient

## Slide 4: TWO LAYER DESIGN 30 STRAND CABLE
Two layers, 30 strand cable, 1 mm diameter strand, no grading [M. Karppinen]
  29 mm coil eq. width
    Current 26.1 kA, peak field 10.5 T, 380 T/m, at 75% of short sample
  At 80% can reach 400 T/m, with 27.4 kA
  Very large jov=780 A/mm2

## Slide 5: TWO LAYER DESIGN 40 STRAND CABLE
Two layers, 40 strand cable, 1 mm diameter strand, no grading [C. Lorin]
  35.8 mm coil eq. width
  Current 32.2 kA, peak field 11.4 T, 413 T/m, at 80% of short sample
  Large jov=720 A/mm2

## Slide 6: FIVE BLOCKS DESIGN
Three layers, 40 strand cable, 1 mm diameter strand, no grading
  46.2 mm coil eq. width,
  Current 27.5 kA, peak field 12.2 T, 423 T/m, at 80% of short sample
  Much less effective but more reasonable jov=620 A/mm2

## Slide 7: LOADLINES
Coil width larger than 35 mm is not needed for larger gradient but to lower the current density

## Slide 8: Gradient VS COIL THICKNESS
Coil width larger than 35 mm is not needed for larger gradient but to lower the current density at 600 A/mm2

## Slide 9: TWO LAYER DESIGN 30 STRAND CABLE: PROTECTION
Two layers, 30 strand cable, 1 mm diameter strand, no grading [M. Karppinen]
  Time margin 21 ms – too small
  To get to 40 ms, lowering current to 23.5 kA and increasing copper to 1.8: gradient reduces to 345 T/m

## Slide 10: TWO LAYER DESIGN 40 STRAND CABLE
Two layers, 40 strand cable, 1 mm diameter strand, no grading [C. Lorin]
  Time margin 24 ms – too small
  To get to 40 ms, lowering current to 29 kA and increasing copper to 1.7: gradient reduces to 370 T/m

## Slide 11: FIVE BLOCKS DESIGN
Three layers, 40 strand cable, 1 mm diameter strand, no grading
  Time margin 35 ms – a bit small
  To get to 40 ms, lowering current to 27.0 kA, gradient reduces to 415 T/m

## Slide 12: LOADLINES
Coil width larger than 35 mm is not needed for larger gradient but to lower the current density

## Slide 13: CONCLUSIONS
The target of 400 T/m for a 50 mm aperture quadrupole is feasible within the current hypothesis, including protection
  20% margin on the loadline, 40 ms of time margin for protection
A large coil is required to lower the current density and make protection possible
  The 45 mm equivalent coil width size allows to gain 15% gradient w.r.t. the compact (and simple) two layer, 15 mm cable width
    We pay with 80% more cable, we get 1 m shorter quad, 1% more filling factor, ie. 1% more margin in the dipoles
    Global optimization (including cell length, phase advance, etc) needed to see if this is worth or not
  There are proposals to operate with 20 ms time margin with CLIQ (Sabbi at EUCAS) – is this reasonable? For the moment I consider more conservative parameters, but this options should be explored