## Slide 1: Impedance of a laser-treated beamscreen
A few kHz < < a few GHz
Measurements: classical wire measurement lacks sensitivity and repeatability.*
Low frequency:
f< 1 MHz
Eddy-current testing
High frequency:
f=multiple GHz
Measuring Q-factor of a sample in a cavity
Medium frequency
Resonance method with a pipe made of laser treated sheets, several meters long
* Personal communication with F. Caspers
Frequency range of interest:
Alternatives:

## Slide 2: Eddy-current testing
Sigma meter by Förster: frequency range 60 kHz <f< 960 kHz
We need a model to extrapolate data to other frequencies and to convert eddy-current measurements to wake impedance.

## Slide 3: Theoretical model for laser-treated copper surface. A naïve approach: two-layer model.
Impedance “felt” by a wave incident on the two-layer structure:

## Slide 4
Boundary condition between the layers:
Final answer for surface impedance:
Quantity measured by the sigmameter:
Characteristic impedance of metal 1
Propagation constant in metal 1

## Slide 5: Two-layer model check: LHC beamscreen (copper + stainless steel)
LHC beamscreen stripe: copper-coated stainless steel

## Slide 6: Two-layer model check: laser-treated copper stripe
Conclusion: for eddy-current measurements to be useful, a better theoretical model is necessary.

## Slide 7: Proposal for a future experiment with the resonator method
Figure from F. Caspers and T. Scholz 1995 - Resonator method for impedance determination
Can we make a pipe of laser-treated stripes a few meters long?

## Slide 8: Proposal for a future experiment with the resonator method
F. Caspers and T. Scholz 1995 - Resonator method for impedance determination
Q-factor deviations from the case of untreated sample are used to find the real part of impedance.
T. Kroyer, F. Caspers, E. Gaxiola - Longitudinal and Transverse Wire Measurements for the Evaluation of Impedance Reduction Measures on the MKE Extraction Kickers
Papers:
Shifts in resonance frequency are used to determine the imaginary part of impedance.

## Slide 9
Done. See FCC impedance database.
Done. Oleg is willing to conduct more experiments in his laboratory if there is interest.
In progress
In progress