## Slide 1: Ion microbeam facility at RBI as a tool for detector characterization
N. Skukan, M. Jakšić, I. Bogdanović-Radović, T. Tadić, S. Fazinić, Z. Siketić, I. Zamboni, I. Božičević Mihalić, I. Sudić, D. Španja, Ž. Periša, A. Kovačević
(Veljko Grilj)
Ruđer Bošković Institute, Bijenička c. 54, 10000 Zagreb, Croatia

## Slide 2: Outline
1. Facility
2. Statistics in brief
3. Ion Beam Induced Charge
4. Some AIDA runs

## Slide 3: WP12 -Detector Characterization Facilities WP12.1. – RBI Accelerator Facility
RBI | User Projects |  | Total users | TA units
 | Submissions | Selected |  | 
M1-M22 | 8 | 8 | 17 (11 supported) | 280
M1-M48 | 16 |  | 24 | 640
8 TA projects have been already approved
7 TA access have been completed by 30th March 2017
( on schedule –completed)
Users from 6 countries supported

## Slide 4: WP12 .1 : RBI Accelerator Facility
4-4
AIDA-2020 2nd Annual Meeting
Mar 30th 2017
4-5

## Slide 5: WP12 .1 : RBI Accelerator Facility
5-4
AIDA-2020 2nd Annual Meeting
Mar 30th 2017
5-5

## Slide 6: WP12 .1 : RBI Accelerator Facility
PUBLICATIONS
  4 Oral contributions to conferences :
  Jerzy Pietraszko at al., “Radiation damage in scCVD diamond material measured with relativistic Au ions for future CBM/HADES experiments at FAIR“ 4th ADAMAS Workshop at GSI , December 4, 2015, GSI Helmholtzzentrum für Schwerionenforschung,, Germany
  Jerzy Pietraszko at al., DPG Spring Meeting, Darmstadt, 14 - 18 March 2016 “Systematic study of radiation hardness of single crystal CVD diamond material investigated with an Au beam and IBIC method.”
  Veljko Grilj at al., 15. ICNMTA 2016, 31. Jul-5. Aug 2016 “Radiation hardness study on multi-strip diamond sensor ”, invited
  Alex Oh "3D diamond detectors for particle tracking and dosimetry", invited talk, European Materials Research Society Symposium Materials for electronics and optoelectronic applications, Warsaw, Poland, 19-22 September 2016.
  1 paper publication
  M. Erich et al, EBS/C proton spectra from a virgin diamond crystal, NIMB 381 (2016)96-102.
  3 papers in preparation
  + several posters
6-4
AIDA-2020 2nd Annual Meeting
Mar 30th 2017
6-5

## Slide 7
1.0 MV HVE Tandetron accelerator
6.0 MV EN Tandem Van de Graaff accelerator
Laboratory for ion beam interactions
Accelerator facility

## Slide 8
1.0 MV HVE Tandetron accelerator
6.0 MV EN Tandem Van de Graaff accelerator
IAEA beam line
TOF-ERDA
PIXE/RBS
Dual-beam irradiation
Ion microprobe
Nuclear reactions
In-air PIXE
PIXE crystal spectrometer
Dual beam,
Detector
testing

## Slide 9
Ion Beam Induced Charge
Ouput signal Vout
Deposited energy
Free charge generation and transport
-
+
Vout = F (deposited energy, free carrier transport)
Gunn’s
Theorem:

## Slide 10
What is needed for IBIC?
 POSITION
- Focusing and scanning
 RATE
- 0 - 106 p/s
100 pA current –
620 ions in 1 s
0.1 fA current –
620 ions/second
250 nm
 IONS
- p, , Li, C, O,..
 RANGE
- 1 to 1000 m
signal
ion beam
+V

## Slide 11: Nuclear microprobe

## Slide 12
IBIC imaging
Configurations:

## Slide 13
IBIC imaging
Configurations:
2 MeV p+
2 MeV He+

## Slide 14
Lateral damage creation
frontal IBIC defect mapping
Bragg peak clearly visible
Examples – defects mapping
http://www.unito.it/

## Slide 15
Examples – radiation hardness tests
An ion microprobe allows for:
selective damage introduction
on-line monitoring of CCE degradation and total fluence

## Slide 16: Charge transient spectroscopy (QTS) setup (similar to DLTS)
CoolFET preamplifier +WaveMaster 8500A oscilloscope
Target temperatures: -100°C to +700°C
Achieved: -40°C to 600°C
Stability ± 0.5°C
NDT sample mounted on QTS setup

## Slide 17: QTS trace analysis- NDT HPHT sample
Traps in whole sample:
  = 0.53 eV ±0.1 eV
  is lower
  Boron? Arsenic?
Traps close to the edge:
  = 0.43 eV ± 0.04eV
  is higher
  Boron? Arsenic?
Heating

## Slide 18: Time resolved IBIC (AKA mapped TCT)
TCT gives different information about physical parameters of the sample depending on the beam and energy chosen
Coupled with beam scanning, possible to characterize the sample spatially
scCVD diamond
Ideal case
)
If no plasma effect
and L=0

## Slide 19
  AIDA-2020-RBI-2015-4
  3D diamond, Alexander Oh, University of Manchester, UK
  CCE maps for different biases and geometries
  TRIBIC (TCT) amplitude maps

## Slide 20
  AIDA-2020-RBI-2016-1
  IBIC characterization of single crystal diamond based Shottky diodes for microdosimetry application, Claudio Verona, ‘Tor Vergata’ University, Italy
  AIDA-2020-RBI-2016-2
  Microbeam tests of silicon telescope for clynical dosimetry, G. Magrin, Austron, Austria

## Slide 21
a instead of b
particles
  AIDA-2020-RBI-2015-2
  Diamond Membranes for Radioisotope Batteries BATDiαm, Michal Pomorski, CEA, LIST, France

## Slide 22
Number of traps:
Au / p4.5MeV / p24GeV = 1 / 30 / 2430
p4.5MeV / p24GeV = 81
AIDA runs
Correlating fluences from different sources and detector degradation scCVD diamond strip detector
  AIDA-2020-RBI-2015-1
  Systematic study of radiation damage in scCVD diamond material irradiated with relativistic Au beams, Jerzy Pietraszko, GSI Darmstadt, HADES, Germany

## Slide 23: To conclude:
RBI accelerator facility hosts microbeam line used for IBIC and semiconductor modification among other uses
Ion Beam Induced Charge/Current is efficient method for mapping basic properties of semiconductor and insulator detector materials
Several different setups of IBIC exist: Lateral, Frontal, TRIBIC (TCT), Temperature dependent…
So far 7 (+1 in the following month) different characterizations carried out through AIDA transnational access program

## Slide 24
Thank you for attention!

## Slide 25: WP12 .1 : RBI Accelerator Facility
TA completed:
  AIDA-2020-RBI-2015-1
  Systematic study of radiation damage in scCVD diamond material irradiated with relativistic Au beams, Jerzy Pietraszko, GSI Darmstadt, HADES, Germany.
  AIDA-2020-RBI-2015-2
  Diamond Membranes for Radioisotope Batteries BATDiαm, Michal Pomorski, CEA, LIST, France
  AIDA-2020-RBI-2015-3
  Investigation of channeling depth profiles of high energy carbon and silicon ions implanted in diamond and SiC crystals for detector characterization, Michael Kokkoris, National Technical University of Athens, Greece
  AIDA-2020-RBI-2015-4
  3D diamond, Alexander Oh, University of Manchester, UK
  AIDA-2020-RBI-2016-1
  IBIC characterization of single crystal diamond based Shottky diodes for microdosimetry application, Claudio Verona, ‘Tor Vergata’ University, Italy
  AIDA-2020-RBI-2016-2
  Microbeam tests of silicon telescope for clynical dosimetry, G. Magrin, Austron, Austria
  AIDA-2020-RBI-2016-3
  Investigation of channeling depth profiles of high energy carbon and silicon ions implanted in SiC /Si crystals for detector characterization, University of Athens, Greece
25-4
AIDA-2020 2nd Annual Meeting
Mar 30th 2017
25-5

## Slide 26: WP12 .1 : RBI Accelerator Facility
The last TA proposal submitted and approved in March 2017:
  AIDA-2020-RBI-2017-1
  Diamond Membrane Microdosimeter, Michal Pomorski, CEA, LIST, France
  expected two users; one or both supported by the project
  Realization expected before the end of April (although there is high possiblity to delay
  the experiment due to some problems in the sample preparation as reported recently by the PI).
26-4
AIDA-2020 2nd Annual Meeting
Mar 30th 2017
26-5

## Slide 28: Ion beam analysis
Molecular Desorption
→ Secondary Ion Mass Spectrometry-SIMS