## Slide 1
The CSOI approach for integrated micro channels
L. Andricek1, J. Dingfelder2, I. Garcia3, C. Lacasta3, G. Liemann1, C. Marinas2,
D. Markus2, J. Ninkovic1, E. Scheugenpflug1, M.A. Villarejo3, M. Vos3
1MPG Halbleiterlabor Munich, 2Bonn University, 3IFIC Valencia

## Slide 2: Processing thin detectors - the SOI approach
The sensor thickness becomes a free parameter, adjustable to the needs of the experiment!
Key Process Modules:
:- Wafer Bonding and thinning of top layer (external)
:- Sensor fabrication on SOI
:- Etching of the Handle Wafer
Top Wafer
Handle <100> Wafer
a) oxidation and back side implant of top wafer
b) wafer bonding and grinding/polishing of top wafer
c) process  passivation
open backside passivation
d) anisotropic deep etching opens "windows" in handle wafer
Custom made SOI Wafer
DEPFET for Belle II PXD (75µm)
Direct electron detectors (30 and 50 µm)
SiPMs - SiMPL (down to ~14 µm)
ATLAS ITk (150 and 100µm)

## Slide 3: Direct Wafer Bonding in "Micro-Cleanroom"
picture from: www.mpi-halle.mpg.de
Q.-Y. Tong and U. Gösele “ Semiconductor Wafer Bonding ”
John Wiley & Sons, Inc.

## Slide 4: Direct Wafer Bonding
qlso native

## Slide 5
integrated silicon frame

## Slide 6: thin DEPFETs
full DEPFET technology in thin area
thin area supported by a monolithically integrated silicon frame

## Slide 7: introducing a Cu layer on the DEPFET module
three metal layer system in periphery
  Copper as third metal
  low-k dielectric to Alu2
  UBM for flip chip
  landing pads for passives
  Solder connection to kapton

## Slide 8: Belle II Module 0
X/X0 = 0.21%

## Slide 9: Thermal management and material
8W DCD&DHP
1W sensor & SWB  gas cooling
Belle II
  9W/half ladder, 8W at EOS
  Active (CO2) cooling at EOS, cooling block outside acceptance
difficult for experiments with larger acceptance region
at EOS still high power density, active cooling would be good
   How about silicon integrated cooling channels there ????

## Slide 10: Integrated micro-channels
A spin-off of SOI approach : thinned all-silicon module with integ. cooling
:- idea: integrate channels into handle wafer beneath the ASICs
:- channels etched before wafer bonding  cavity SOI (C-SOI)
:- full processing on C-SOI, thinning of sensitive area
:- micro-channels accessible only after cutting (laser)

## Slide 11: Prototypes with resistive heating and micro channels
~350 µm
DRIE etching of handle wafer
CSOI wafer with integrated ressistors
Module after cutting
Detail: inlet for the cooling fluid

## Slide 12: IR movie – just for entertainment
:- silicon particles in water
:- low flow 300µl/s

## Slide 13: 2nd round

## Slide 14: 2nd round: Profiles before wafer bonding

## Slide 15: Summary
Active pixel sensors for Belle II are already fabricated on SOI wafers
  Convection cooling in thin sensitive region, “aggressive” CO2 at the end-of-stave (EOS)
Natural next step is the introduction of integrated cooling channels at the EOS
  Cavity SOI
Feasibility studies done, look promising
Concept can be extended to any kind of sensors on SOI, in particular hybrid pixel sensors as in ATLAS/CMS
  Would of course require re-design of the module ..

## Slide 16: Module Assembly – overview
Flip Chip of ASICs (~240°C):
  Bumped ASICs have the same solder balls (SAC305)
    DHP bumping at TSMC, DCD bumping via Europractice
    So far SWB bumping on chip level
  Flip Chip of PXD modules on custom made support plates
SMD placement (~200°C):
  Passive components (termination resistors, decoupling caps)
  Dispense solder paste/jetting of solder balls, pick, place and reflow
    PbSn 37/63 solder
Kapton attachment (~170°C), wire bonding:
  Solder paste printing on kapton,
    SnBi solder
  Wire-bond, wedge-wedge, 32 µm Al bond wires