## Slide 1
CERN seminar
January 20, 2017
Lucio Pancheri
DII, University of Trento & TIFPA-INFN, Italy
State of the art and perspectives of CMOS avalanche detectors

## Slide 2
INFN-TIFPA
FBK
Clean room
UniTN
Dept. Industrial
Engineering
UniTN
Dept. Physics
Research on silicon detectors in Trento

## Slide 3
TIFPA
FBK
UniTN
Proton therapy

## Slide 4: Outline
Introduction
CMOS-integrated single-photon detectors: an overview
APiX: Geiger-mode avalanche pixel detectors for ionizing particles
Conclusion and future perspectives

## Slide 5: Geiger-mode avalanche detectors
RQ
VBIAS > VBD
VSPAD
VB
VBIAS
Avalanche
triggering
Quenching
Recharging
ISPAD
SPAD
a.k.a. Single-Photon Avalanche Diodes (SPADs), SiPM cell
VEX

## Slide 6: Geiger-mode avalanche detectors
RQ
VBIAS > VBD
time
Vout
SPAD
Vout
events
1 primary generated electron-hole pair:
very large current pulse ~105 - 106 electrons
VEX

## Slide 7: CMOS SPAD characteristics
Features:
Single-photon sensitivity → shot noise limited
Excellent timing resolution: ~100 ps FWHM
Monolithic integration of SPAD and processing electronics
Arrays → single-photon imaging
CMOS:

## Slide 8: Outline
Introduction
CMOS-integrated single-photon detectors: an overview
APiX: Geiger-mode avalanche pixel detectors for ionizing particles
Conclusion and future perspectives

## Slide 9: CMOS SPADs: early example at EPFL
A. Rochas et al., Proc. SPIE 2003
Process: CMOS 0.8μm
Area: 30μm2
Peak PDE: 20%
DCR: 300 Hz
Timing resolution: 50 ps FWHM

## Slide 10: CMOS SPADs: deep submicron
J. Richardson et al., IEEE Trans. Electron Dev. 2011
Process: CMOS 130 nm
Area: 50μm2
Peak PDE: 33%
DCR: 40 Hz
Timing resolution: 237 ps FWHM

## Slide 11: CMOS SPADs: high efficiency
Process: CMOS 350nm
Imaging with custom implantation
Area: 700μm2
Peak PDE: > 50%
DCR: 50 Hz
Timing resolution: 142 ps FWHM
D. Bronzi et al., Proc. IEEE ESSDERC 2012

## Slide 12: Summary and comparison with SiPM
With customization, CMOS can approach SiPM performance
SiPM:
For major manufacturers
PDE > 70% (single cell, not
considering FF)
DCR ~ 50 kHz/mm2
For a complete overview, see D. Bronzi, et al., IEEE Sensors J. 2016

## Slide 13: SPAD array applications
Time-Of-Flight optical ranging, LIDAR
Fluorescence spectroscopy
Raman spectroscopy
Gamma ray detection (PET)
Quantum cryptography
…

## Slide 14: Time-of-Flight optical ranging
C. Niclass et al., IEEE J. Solid-State Circuits, 2013
Automotive LIDAR developed by Toyota
180nm CMOS
SPAD array with integrated TDCs
70% array Fill Factor
Distance range: 100 m

## Slide 15: Fluorescence microscopy
M. Popleteeva et al., Opt. Expr, 2015
Label-free imaging of unstained liver tissue excised from a tumorogenic murine model
Intensity
Color
Lifetime
Multi-parametric fluorescence imaging
350nm CMOS (AMS)
4-line SPAD array
Sub-ns gated counters
36% Fill Factor

## Slide 16: Digital SiPMs for PET
L. Braga et al., IEEE J. Solid-State Circuits, 2014
SPADNET project (EU FP7)
130nm CMOS process
Large pixels including 180 SPADs (Mini-SiPM)
integrated TDCs
42.6 % pixel Fill Factor

## Slide 17: First consumer products: ST ToF sensor
Proximity sensor based on SPAD array and pulsed VCSEL
Presented in 2014
Mobile applications (mounted on iPhone7)
Low power
Short range (15 cm)

## Slide 18: SPAD image sensor
C. Veerappan et al., ISSCC 2011
MegaFrame EU project (FP6)
160 x 128 pixel array
Technology: 130nm CMOS
In-pixel Time-to-Digital Conv.
140ps timing resolution
Pixel pitch: 50um
Fill factor: 1%

## Slide 19: Improving the Fill Factor
I. Gyongy et al., IEDM 2016
16μm x 16μm pixel
65nm CMOS
binary pixel (7 transistors)
SPAD deep nwell sharing
Improved SPAD GR
61% Fill Factor

## Slide 20: Deep APD
Panasonic project
110nm CMOS
Backside illumination
Avalanche multiplication region below electronics
Pixel pitch 3.8μm
4 transistors / pixel
Linear and binary mode
M. Mori et al., ISSCC 2016

## Slide 21: 3D integration
High density interconnections successfully demonstrated for image sensors
electroiq.com
Sony 13 Mpixel stacked image sensor (2013)

## Slide 22: 3D-integrated SPAD image sensor 1
MIT Lincoln Laboratory
25μm pitch
180nm CMOS + custom (APDs)
7-bit counter/pixel
Backside illumination
10 - 20% detection efficiency (limited by optical cross-talk)
B. Aull et al., IEEE Sensors J., 2015

## Slide 23: 3D-integrated SPAD image sensor 2
T. Al Abbas et al., IEDM 2016
7.83μm pitch
65nm CMOS (top) + 40nm CMOS (bottom)
2 6-bit counters/pixel
Backside illumination
45% Fill Factor

## Slide 24: Outline
Introduction
CMOS-integrated single-photon detectors: an overview
APiX: Geiger-mode avalanche pixel detectors for ionizing particles
Conclusion and future perspectives

## Slide 25: APiX particle detector concept
Two Geiger-mode avalanche detectors in coincidence:
DCR = DCR1 x DCR2 x 2DT
In-pixel coincidence: integrated electronics is needed: CMOS avalanche detectors
Discriminators
Coincidence detector
Quenching
Particle
detection
Dark counts
V. Saveliev, US Patent. 8,269,181, 2012 N. D’Ascenzo et al., JINST 2014

## Slide 26: SPADs in 150nm CMOS process
Type2:
Deep graded junction
Active thickness ~ 1.5μm
Type 1:
Shallow step junction
Active thickness ~ 1μm
L. Pancheri, D. Stoppa, ESSDERC 2011
Standard CMOS process – no modifications
Avalanche diodes in deep nwell: isolated from substrate

## Slide 27: Photo-Detection Efficiency
L. Pancheri et al., J. Selected Topics in Quantum Electron, 2015
Type 2: pwell/niso
Type 1: p+/nwell
Shallower junction:
better NUV – Blue efficiency
Wider depletion region:
Better red-IR efficiency

## Slide 28: Single-photon timing resolution
Measured on 10-μm devices, with blue laser (470nm), 70ps FWHM
Type 1: 60ps FWHM Type 2: 170ps FWHM

## Slide 29: Proof-of-concept demonstrator
2-layer pixel cross section:
Electronic readout on both layers
Metal shielding from optical cross-talk
Vertical interconnection by bump bonding

## Slide 30: Pixel architecture
High voltage VbSPAD applied at nwell
Maximum voltage at node A: Vov = VbSPAD – VBD
Small capacitance at node A
Passive quenching with constant current recharge

## Slide 31: Pixel architecture
Front-end transistors: 3.3V  Maximum overvoltage 3.3V
Digital circuitry: 1.8V compact – fast – low-power

## Slide 32: Pixel architecture: enable register
Pixels can be individually disabled:
M2 disables recharge
Output and gate blocks output pulses

## Slide 33: Pixel architecture: coincidence
Coincidence with top-layer pixel

## Slide 34: Pixel architecture: coincidence
Accidental coincidence
Real coincidence

## Slide 35: Pixel architecture: monostable
Pulse shortening: reduces the rate of accidental coincidence
Programmable pulse width: 750ps, 1.5ns, 10ns

## Slide 36: Pixel architecture: storage
Global shutter operation:
  Fast transfer from memory to output register
  Simultaneous accumulation and data output

## Slide 37: 2-level pixel schematic
Top pixel: subset of bottom pixel

## Slide 38: Sensor architecture: row-wise OR
Test output outOR:
combination of all the active
(enabled) pixels in the row

## Slide 39: Row-wise coincidence circuit
Test coincidence in the sensor plane
m and n can be arbitrarily selected

## Slide 40: Sensor floorplan
Wire bonding pads on chip 2: pre-integration test.
Final assembly
Bottom chip
Top chip
Bottom chip
Top chip

## Slide 41: Pixel array
Pixels with different detector area
(unshielded)
Pixels with shielded detectors
16 x 48 pixel array
Pixel size: 50μm x 75μm
Splittings in detector type and area
Bump bonding pad
43μm x 45μm
40μm x 40μm
35μm x 35μm
30μm x 30μm

## Slide 42: Bottom chip - Micrographs
Shielded
Unshielded

## Slide 43: Sensor micrographs
Bottom chip
Top chip

## Slide 44: Experimental results - summary
Characterization of single-layer sensors:
Core supply current (at 1.8V): 8mA
Breakdown voltage uniformity
Dark count rate
In-plane coincidence
Timing resolution
Cross-talk
Vertically integrated sensors with bump bonding (IZM):
Coincidence dark counts
Test with beta source
Test beam

## Slide 45: Breakdown voltage uniformity
Measurements on 5 sample chips x 2 types x 196 devices per chip
Very good uniformity on-chip (s < 20mV)
Large difference (1V) between different chips for type 1

## Slide 46: DCR distribution
DCR distribution spans 2 orders of magnitude at RT
Median value at 20°C: 2.8kHz - MHz/mm2
Active area: 43μm x 45μm

## Slide 47: DCR temperature dependence
Trap-assisted tunneling: EA < EG/2
Devices with 43μm x 45μm active area, but different DCR
Measurements from -30°C to 50°C with 10°C steps
Overvoltage: VOV = 3.3V

## Slide 48: DCR temperature dependence
SRH generation EA ~ EG/2

## Slide 49: DCR temperature dependence
Injection from neutral regions: EA ~ EG

## Slide 50: DCR temperature dependence
Band – to – band tunneling: EA  0

## Slide 51: Coincidence detection
Count rate in coincidence between
two pixels in the same column
Normalized rate:
1 2 3 4 5 6 7
Cross-talk
Cross-talk

## Slide 52: Timing resolution
VEX = 1V
208ps FWHM
IR laser (780nm)
50ps FWHM
Timing histogram between laser trigger and sensor coincidence output
N.B. Design not optimized for timing
Row coinc.
output
Diffuser
Sensor
2 pixels enabled

## Slide 53: Crosstalk characterization
Crosstalk coefficient
CRm = DCRe ∙ DCRd ∙ 2∆T + K ∙ ( DCRe + DCRd )
Emitter (fixed)
Detector (scan)
Crosstalk map – Type 1, 25µm thickness

## Slide 54: Crosstalk vs substrate thickness

## Slide 55: Dark Count Rate and cross-talk
Die thickness: 280 µm
Median DCR increase of 70% due to cross-talk:
from 2.8kHz to 4.8kHz
Large detectors
T = 20°C
VEX = 3.3V
A. Ficorella, et a., Proc. IEEE ESSDERC, 2016

## Slide 56: Vertically-integrated assembly
Dark Count Rate vs. coincidence time DT
DCRCOINC = DCR1 x DCR2 x 2DT
DT = 10ns
DT = 1.5ns
DT = 0.75ns
T = 20°C
DCRCOINC = 27 counts/s mm2

## Slide 57: b-source measurements
90Sr β source – 37kBq at 2mm distance from sensor
b count rate ~10,7 Hz/mm2
VEX = 2V T = 5°C Dt = 0.75ns
~ 40 mHz/pixel

## Slide 58: Test beam at CERN
Test at CERN SPS north area facility (H4 beam line)
Two APIX under test + auxiliary Beam Tracker detector
Positrons and π+ beams at 50, 100, 150, 200 and 300 GeV

## Slide 59: Test beam – hit maps
Noisy pixel disabled
Unshielded pixels disabled

## Slide 60: APiX - Summary
Strengths:
Can be thinned to a few microns: low material budget
Timing resolution
Low power consumption
Early signal digitization
Weaknesses:
Radiation tolerance (still to be assessed)
Efficiency: guard ring and in-pixel electronics
Cost and availability of 3D integration technologies

## Slide 61: Current - future work
Current prototype:
  Test beam data analysis (in progress)
  Radiation hardness studies
Design of new prototype:
  Improved fill factor
  Larger array
  Optimized timing
  Optimized power consumption

## Slide 62: Summary
Higly parallel SPAD systems require high-density digital circuit for high efficiency
SPAD technology in deep sub-micron processes is evolving driven by consumer applications: investments
Maximum efficiency: 3D integration. Optical cross-talk is still an issue in systems with very high FF
Concept of charged-particles direct detection with Geiger-mode detectors in coincidence is feasible
Efficiency is still an issue, but timing can be very good
Development in deep-submicron SPADs and 3D integration can the key for a full exploitation of this concept

## Slide 63: Acknowledgements
APiX2 project
“Development of an Avalanche Pixel Sensor for tracking applications”
Funded by INFN – CSN5
Project coordinator: Pier Simone Marrocchesi, INFN Pisa and University of Siena
Partners:
TIFPA and University of Trento,
INFN Pavia and University Pavia,
INFN Padova and University of Padova,
Laboratoire APC, Université Paris-Diderot/CNRS