## Slide 1
Accelerators and Technology Sector Seminar

## Slide 2: Nanostructured materials for particle beams: the example of ISOLDE targets
Accelerators and Technology Sector Seminar
PhD Public Defense
João Pedro Ramos
26th of January, 2017
PhD supervisors: Prof. Paul Bowen, Dr. Thierry Stora
http://www.joaopedroramos.com

## Slide 3: Structure
ISOLDE at CERN
Production of isotopes at ISOLDE
Overview target materials
Nanomaterials at ISOLDE
Outlook

## Slide 4: at CERN
Isotope Separator OnLine Device
Produces Radioactive Ion Beams (RIB)
Approved by the CERN council in 1964
  Supplied by the SC with 600 MeV protons
  Then by the PSB in 1992 with 1.0 GeV (later 1.4 GeV)
RIBs are used for studies in:
  Nuclear physics
  Atomic physics
  Solid state physics
  Astrophysics
  Life sciences

## Slide 5: How many isotopes?
Predicted
~6000
Discovered
~3000
ISOLDE
~1000
Elements
74
t1/2
>tens of ms
*nuclide chart from Nucleonica
*J. Ballof, ISOLDE database yields

## Slide 6
LINAC2
PSB
PS
ISOLDE
~50 staff – maintain/operate the facility
A few students and fellows
~450 users for physics in more than 90 experiments
Operates ~8 months/year, 24/7
at CERN
ISOLDE takes ~50% of CERN protons

## Slide 7: Facility
*picture courtesy of M. Delonca
Protons (1.4 GeV)
Pulsed protons (1.2 s)
1.4 GeV
3.3x1013 protons per pulse
GPS
General Purpose Separator
HRS
High Resolution Separator
High energy RIBs (up to 10 MeV/u – A/q=4.5)
Low energy RIBs (up to 60 keV)
High Energy RIB
Target area
MEDICIS
Radioactive laboratory Class A
Route Einstein
Route Democrite
Low energy RIB

## Slide 8: Beam interaction with target
A&T Sector Seminar | Public Defense
João Pedro Ramos | 26/01/2017
2.3 μs
230 ns
Beam power deposition – pulsed beams!
Thermomechanical stresses and shockwaves
Booster pulse pictures from PhD Thesis, R. Wilfinger

## Slide 9: Target Unit – Heart of
*pictures courtesy of M. Delonca and J. Montano
ISOLDE Frontend Target station
20 cm
Transfer line
Target
Ion Source

## Slide 10: Target Unit – Heart of
Ions
Radioisotopes
Primary beam
*picture and animation courtesy of M. Delonca
Vacuum
Air
1.4 GeV proton
fragmentation
fission
spallation
238U
142Cs
11Li
201Fr
X
Y
Beam power
2.8 kW in average
1.2 GW (pulse length 2.3 μs)
  ~10% deposited
What is the sound of proton impact on target?

## Slide 11: ISOL Isotope Separation
Pulsed
Protons
+/- 8V
500 A
+/- 9 V
1000 A
Ion Source
Proton
Transfer line
4. Ionization
3. Effusion
2. Diffusion
1. Production
– Nr of exposed atoms [dim]
– Proton flux [cm-2]
– Cross section [mb]
– Efficiency [%]
5. Mass Separation
6. Transport
Extraction optics
Mass separator
Target unit
OnLine
Extraction electrode
up to 2300 °C
Chart: t1/2 (s)
| 0.01 | 0.02 | 0.03 | 0.04 | 0.05 | 0.06 | 7.0000000000000007E-2 | 0.08 | 0.09 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 200 | 300 | 400 | 500 | 600 | 700 | 800 | 900 | 1000 | 2000 | 3000 | 4000 | 5000
 | 0.00054957 | 0.0018729 | 0.0036522 | 0.0057048 | 0.00792 | 0.010229 | 0.012586 | 0.014963 | 0.017341 | 0.019706 | 0.041777 | 0.06095 | 0.078054 | 0.093714 | 0.10831 | 0.12207 | 0.13516 | 0.14767 | 0.15969 | 0.26076 | 0.33869 | 0.4014 | 0.45312 | 0.49656 | 0.53358 | 0.56552 | 0.59335 | 0.61782 | 0.76137 | 0.82651 | 0.86371 | 0.88777 | 0.90462 | 0.91706 | 0.92663 | 0.93423 | 0.94039 | 0.96924 | 0.97927 | 0.98437 | 0.98745 | 0.98952 | 0.991 | 0.99212 | 0.99299 | 0.99369 | 0.99683 | 0.99789 | 0.99841 | 0.99873
Radioisotopes have finite half-lives!
20 cm
Target heating (1 – 2kW), <~10% beam power

## Slide 12: ISOLDE target materials
Material requirements
  High production cross section of the isotope(s) of interest
  Stability at high temperatures
  Chemically stable and inert
  Resistance to radiation damage
  Rapid diffusion and effusion rates of the element(s) of interest
Operation temperature limitations:
  Sintering (preserve target microstructure)
  Limited reactivity with surrounding materials
  Reduced stable beam contaminants (chemical impurities)
  Moderate equilibrium vapor pressure compatible with ion source (10-2 Pa)
Chart: 
| Metal | Oxide | Molten | Carbon based | Others
 | 0.22647 | 0.15588 | 0.061765 | 0.54412 | 0.012
Sn, Pb,...
CaO, ZrO2,…
UC2-2C, SiC,…
Ta, Ti,…
Powders, pellets or liquid form
Number of targets in the last 16 years at ISOLDE:
Metals – 23%
Oxides – 16%
Molten – 6%

## Slide 13: Target Materials
In squares – currently used at ISOLDE
Underlined and Bold – had some kind of material development
120 Materials (possibly more) were tested and/or used as ISOL targets!
J.P. Ramos, PhD Thesis, EPFL/CERN (2017)

## Slide 14: What is sintering?
Temperature - time
Sintering temperature (densify):
Defined in function of the material melting point (Tm)
0.5 to 0.8Tm
0.2 to 0.4Tm
Main reason why nanomaterials were discarded in the past for ISOL target application
Micrometric materials
Nanomaterials
The smaller the particle size (larger surface area) the higher the sintering driving force
!
!
Sintering can be affected by irradiation (defect creation)

## Slide 15: Target material influence on beam intensity?
Melting/Sublimation
Sintering
Grain size increase
Reduction of porosity
Targets are traditionally operated at very high temperatures (close to the materials melting point)
Chart: Target Temperature
| 24.699999999999989 | 102 | 202 | 301.99999999999994 | 401.99999999999994 | 451.99999999999994 | 501.99999999999994 | 552 | 602 | 652 | 702 | 752 | 802 | 852 | 902 | 952
 | 0.42573 | 114.082 | 10631.9017 | 204812.0561 | 1642873.545 | 3751666.0785 | 7701734.9507 | 14491200.7639 | 25366333.3837 | 41795805.1335 | 65429100.1916 | 98045046.8083 | 141496257.8747 | 197654319.9033 | 268359307.4753 | 355375928.474
31Ar (15.1 ms)
32Ar (98 ms)
35Ar (1.78 s)
Arrhenius dependance of effusion and diffusion with temperature
However during operation
Target material degradation
or even low from the beginning
Very often
Expected beam intensity

## Slide 16
Time
In most cases limit by far the yields.
Operation T
Grain size/Porosity
Assess microstructure stability
r /10
Diffusion limited release:
x10
Chart: t1/2 (s)
| 0.01 | 0.02 | 0.03 | 0.04 | 0.05 | 0.06 | 7.0000000000000007E-2 | 0.08 | 0.09 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 200 | 300 | 400 | 500 | 600 | 700 | 800 | 900 | 1000 | 2000 | 3000 | 4000 | 5000
 | 0.00054957 | 0.0018729 | 0.0036522 | 0.0057048 | 0.00792 | 0.010229 | 0.012586 | 0.014963 | 0.017341 | 0.019706 | 0.041777 | 0.06095 | 0.078054 | 0.093714 | 0.10831 | 0.12207 | 0.13516 | 0.14767 | 0.15969 | 0.26076 | 0.33869 | 0.4014 | 0.45312 | 0.49656 | 0.53358 | 0.56552 | 0.59335 | 0.61782 | 0.76137 | 0.82651 | 0.86371 | 0.88777 | 0.90462 | 0.91706 | 0.92663 | 0.93423 | 0.94039 | 0.96924 | 0.97927 | 0.98437 | 0.98745 | 0.98952 | 0.991 | 0.99212 | 0.99299 | 0.99369 | 0.99683 | 0.99789 | 0.99841 | 0.99873
Target material influence on beam intensity?
1 μm
1
2
3
4
t1/2 = 1 s
1s – 50%
2s – 25%
3s – 12.5%
4s – 6.25%
10x smaller!
Porous nanomaterials campaign started ~10 years ago (ISOLDE is 50 years old)
  Shorter diffusion lengths
  Higher porosity
Chart: Target Temperature
| 24.699999999999989 | 102 | 202 | 301.99999999999994 | 401.99999999999994 | 451.99999999999994 | 501.99999999999994 | 552 | 602 | 652 | 702 | 752 | 802 | 852 | 902 | 952
 | 0.42573 | 114.082 | 10631.9017 | 204812.0561 | 1642873.545 | 3751666.0785 | 7701734.9507 | 14491200.7639 | 25366333.3837 | 41795805.1335 | 65429100.1916 | 98045046.8083 | 141496257.8747 | 197654319.9033 | 268359307.4753 | 355375928.474
Diffusion/Effusion
Can we stabilize porous nanostructures at high temperatures?
Not found in the literature
Needed R&D
100 nm
Same T!
Nano materials sinter faster
Reduce operation temperature to stabilize
Diffusivity
(rate of diffusion)
Diffusion lengths

## Slide 17: What about the material microstructure?
Electron microscope of the EN-MME-MM group, at CERN
0.67 mm
100 μm
20 μm
2.0 μm
660 nm
200 nm
As Feynman said: “There is plenty of room at the bottom”!
31 x
200 x
1 000 x
10 000 x
30 000 x
100 000 x

## Slide 18: Nanomaterials
Identifying suitable target nucleus and chemical compound
Stabilizing microstructure at high temperature and high-power irradiation
Engineering desired microstructure
Studying diffusion and release properties
Post-irradiation material analysis
Online tests
2-5 years per material
A&T Sector Seminar | Public Defense
TiC+CB – J.P. Ramos, et al.
Nov- 2014
Nov- 2014
LaC2 + 2C – J. Guillot, et al.
Nov - 2014
UC2 + 2C – A. Gottberg, et al.
Apr- 2015
MWCNT – C. Seiffert, et al.
SiC - S. Fernandes, et al.
2010
*submicron
*1st nanomaterial at ISOLDE
Reactive sintering and microstructure stabilization
Microstructure stabilization
Synthesis
Acquired and tested
2011
CaO – J.P. Ramos, et al.

## Slide 19: TiC nanocomposite – from A to Z
Mixture done in isopropanol with 5 wt.% pyrrolidone as dispersant
TiC
(80 – 120 nm)
Graphite
(~16 µm)
Carbon Black
(~40 nm)
C Nanotubes
(~10 nm x 1.5 μm)
+
or
or
Co-milling
Deaglomeration and pressing
Polymer (PVP) decomposition
Drying
Thermal treatment
Characterization
TiC
TiC
TiC
TiC
TiC
TiC
TiC
TiC
TiC
TiC
TiC
TiC
C
C
C
C
1800 °C
J.P. Ramos, PhD Thesis, EPFL/CERN (2017)

## Slide 20
A&T Sector Seminar | Public Defense
João Pedro Ramos | 26/01/2017
TiCm
29.1 m2 g-1
48 nm
2.3 m2 g-1
107 nm
0.3 m2 g-1
122 nm
0.1 m2 g-1
277 nm
32.8 m2 g-1
43 nm
13.0 m2 g-1
59 nm
10.2 m2 g-1
64 nm
7.7 m2 g-1
134 nm
36.6 m2 g-1
43 nm
22.1 m2 g-1
52 nm
19.7 m2 g-1
58 nm
16.7 m2 g-1
76 nm
49.4 m2 g-1
46 nm
23.0 m2 g-1
52 nm
17.4 m2 g-1
47 nm
12.0 m2 g-1
138 nm
50 vol.% Graphite
50 vol.% C Black
75 vol.% CNT
TiC milled
as produced
1500 ºC
1650 ºC
1800 ºC
TiC crystallite < 100 nm
for isotope release
Carbon very successfully hinders the sintering of TiC
In most cases nanometric TiC is stable at high temperatures

## Slide 21: TiC – release testing
A&T Sector Seminar | Public Defense
João Pedro Ramos | 26/01/2017
Be: probable reaction with C
Na, Mg and K: well released
Sc: not released, carbide formation
Protons

## Slide 22: Prototype
A&T Sector Seminar | Public Defense
João Pedro Ramos | 26/01/2017
Material scaled up to make a full target
500nm
J.P. Ramos, PhD Thesis, EPFL/CERN (2017)

## Slide 23: Prototype – Online results
A&T Sector Seminar | Public Defense
João Pedro Ramos | 26/01/2017
Na (1.07 s)
Pulsed
Protons
Proton
Target tested online at ISOLDE at 4 different temperatures, from 1300 to 2000 °C
Beams extracted:
Li (high)
Na (very high)
K (similar)
Ca (much lower)
Very stable beam intensities over time.
(unlike current Ti-based targets)
Probable chemical reaction with carbon black
New
Proton impact
Ti metal foils
TiC nanocomposite

## Slide 24: Calcium Oxide
800oC – 2 h
Vacuum (base P=10-3 mbar)
Pseudomorphous reaction
J.P. Ramos, et. al., Ceramics International 41 (6) (2015), 8093-8099.
J.P. Ramos, et al., NIMB 320 (2014), 83-88
J.P. Ramos, Master Thesis, Univ. Aveiro/CERN (2012)
650 nm
CaCO3
CaO
Operation temperature reduced to keep nanostructure!
Grain size ~40 nm
Chart: Operation time (h)
| 4.6833333332324401 | 8.71666666661622 | 17.150000000023283 | 54.149999999965075 | 83.150000000023283 | 96.149999999965075
NewTarget | 35283018.8679 | 27924528.3019 | 22941935.4839 | 39615639.8104 | 36678082.1918 | 28684210.5263
Old Target | 9000000 | 1900000
35Ar
Grain size ~1 μm

## Slide 25: CaO – Beams from a cold target
FLUKA
Recoil energy of 35Ar
9.23±1.77 keV
10 nm 35Ar+ average range in CaO
CaO particles are around 40 nm
J.P. Ramos, et al., NIMB 376 (2016), 81-85.
New release mechanism
thanks to the nanomaterial
Release doesn’t follow the classic diffusion-effusion
35Ar beam intensity (/μC)
*only possible with volatile elements

## Slide 26: Carbon Nanotubes – Boron Beams
Area 7140 m2 (68 x 105 m) – FIFA recommendation
Melting point 2070 °C
Reacts with other elements to form refractory compounds
14.85 g of MWCNT
4352.1 m2
> 60% Football field
Specific Surface Area
293.1 m2/g
C. Seiffert, et al., to be published.
C. Seiffert, PhD Thesis, CERN-THESIS-2014-332.
Source of F - Injection of SF6 in the target container
Boron reacts promptly with fluorine forming a volatile molecule BFx

## Slide 27: Uranium based materials
A&T Sector Seminar | Public Defense
João Pedro Ramos | 26/01/2017
and with K. Novoselov
PhD of M. Nazarova
Graphene on Ta
  Uranium carbide targets are the most used at ISOLDE (>60% of beam time).
  Very porous structure (75%)
  Much less prone to sinter than conventional UC2 targets (micrometric UC2 + Graphite)
  Release rates on many isotopes improved.
𝑈𝑂2+6𝐶→𝑈𝐶2+2𝐶+2𝐶𝑂
  Uranium Oxide (120 nm)
up to 1800oC
Uranium Oxide (micron sized)
milled
+CNT
500nm
*similar (not nanoUCx)
Uranium Oxide (micron sized)
+Graphite
𝑈𝑂2+6𝐶→𝑈𝐶2+2𝐶+2𝐶𝑂
up to 1800oC
Standard
nanoUCx
Grow graphene in metal surfaces
Ultimate goal – grow it on U foils (oxidation protection and avoid adsorption of other atoms/molecules)

## Slide 28: Outlook
A&T Sector Seminar | Public Defense
João Pedro Ramos | 26/01/2017
Target materials investigation brings high output for physics
More beam! More isotopes! Less waste!
Good stability of nanomaterials is probably related with their ability to self heal the irradiation induced defects
Application in other beam intercepting devices
ISOL nanomaterials are a niche research topic:
Can be applied to other ISOL facilities
Similarities to fusion reactor blanket technology
Nuclear reactors - release know-how
G. Ackland, Science (80-. ). 327 (2010) 1587–1588

## Slide 29: Thank you! Merci! Obrigado!
CERN | EPFL | Thierry Stora | Paul Bowen | Ana Senos | Alexander Gottberg | Wonjoo Hwang | Tânia Mendonça | Michal Czapski | Jochen Ballof | Julien Guillot | Melanie Delonca | Yisel Martinez-Palenzuela | Ricardo Augusto | Christoph Seiffert | Silvain Badie | CERN Library | Carlos Morais | Jacques Lemâitre | Heinrich Hofmann | Fabien Sorin | Marijana Mionic | Yves Leterrier | David Geissbϋhler | Zhangli Hu | LTP Laboratory | Universidade de Aveiro | Cristina Fernandes | Maria João Bastos | Carla Pinho | Célia Miranda | Artur Sarabando | Manuela Fernandes | Isabel Antunes | Filipe Oliveira | STI-RBS Section | Richard Catheral | Bernard Crepieux | Michael Owen | Matteo Vagnoni | Ermanno Barbero | Ana Paula Bernardes | Camille Lemesre | Ans Pardons | Joachim Vollaire | Alexandre Dorsival | Uli Köster | ISOLDE Operation | ISOLDE Physics | RILIS | MME-MM Section | Stefano Sgobba | Floriane Leux | Barbora Bartova | Dora Rio | Filipe Martins | Gabriel Ribeiro | Luís Alberty | Paulo Marques | Vitor Gouveia | Monika Stachura | Silvia Aguilera | Elvis Fournasiere | Sérgio Pina | Rogério Roque | André Santos | Francisco Duarte | Evangelina Neves | João Riço | Virgílio Pinto | Olinda Pinto | Tiago Ramos | Tânia Viegas | Paulo Ramos | Mariana Graça Ramos | Elsa Ramos | João Margaça Ramos | Diana Pinto Ramos
A&T Sector Seminar | Public Defense
João Pedro Ramos | 26/01/2017