## Slide 1: Preparation of post mortem analysis of HiRadMat experiment 31
V. Raginel, K. Kulesz, D. Wollmann

## Slide 2: HiRadMat Experiment 31
In the HiRadMat facility shooting 440 GeV protons at:
  LHC Nb-Ti Cable stacks to study degradation of cable insulation
  Nb-Ti and Nb3Sn strands to study degradation of superconducting properties
  Stainless steel plate to study mechanical stability of steel (input for the design of our next beam experiment at cryogenic temperature)
  Samples were within an inert atmosphere.
Nb-Ti & Nb3Sn strands
Steel plate
30 Nb-Ti cables
~ 5 cm
~ 10 cm
~ 7 cm
~ 15 cm

## Slide 3
Second Picture with the tank open
Inside the tank
Nb-Ti cable stacks
in steels moulds
Nb-Ti and Nb3Sn strands fixed on a steel plate
p+
Nb-Ti strands
Nb-Ti & Nb3Sn strands

## Slide 4: Samples extractions in control area (b 867)

## Slide 5: Some samples after beam impact

## Slide 6: High-voltage measurements
  Aim is to compare the breakthrough voltage cable to cable of our irradiated samples to non irradiated ones and furnace experiment.
  The tests consist of rising the voltage between 2 adjacent cables until breakthrough (electric arc)
  Special precautions have to be taken since the sample are activated (up to 130 μSv/h): limited duration, no destructive test, protection of the sample surrounding,…
Supervised Area
RF Group – Klystron section
HV Power Supply (up to -60 kV)
Faraday cage

## Slide 7: High-voltage measurement setup
To Power Supply
Test Cable 1 to Cable 2
Current Transformer
(current readout)
HV Relay
HV Probe (voltage readout)

## Slide 8: Measurement example
The scope is triggered on the rising flange of the voltage
Voltage divided by 1000
Current divided by 2
Electric arc!
~ -20 KV
Recharge of the system
~ 1 A

## Slide 9: How do a breakthrough look like?

## Slide 10: Next steps
The HV tests on the irradiated sample will take place next week (25th to 27thJanuary)
After the tests, the cable stacks will be sent back to radioactive storage
Questions ?