## Slide 1: First Experimental Results on Damage Limits of Superconducting Accelerator Magnet Components due to Instantaneous Beam Impact
V. Raginel, D. Kleiven, K. Kulesz, M. Mentink, R. Schmidt, A. Siemko, A. Verweij, A. Will, and D. Wollmann

## Slide 2: Beam – matter interaction
Damage experiment on solid copper
Burkart, F., et al. Journal of Applied Physics 118.5 (2015): 055902.
The fast (μs) interaction of an high energy beam with matter leads to:
  Temperature rise Ieading in the worst cases to phase transition (melting, vaporization, plasma ….).
  Dynamic stresses that can lead to extended mechanical damage - deformations, cracks.
  In an particle accelerator such as LHC, energy stored in beam = 362 MJ
  Uncontrolled loss of <1% of this energy into accelerator equipment lead to extended damage!
  Slow beam losses Active protection Fast beam losses  Passive protection

## Slide 3: Example of one of the most critical LHC beam loss
Injection kicker magnet
Injection absorber
Superconducting magnet
particle shower
Quench ! Damage ?
One such event per year in today’s LHC. No damage.
With an increase of beam intensity (HL-LHC), will the magnet survive?
What are the damage mechanisms and limits of superconducting magnets ?
LHC BEAM
Injection Failure LHC
Notes: Will the magnet survive? = Will it be still operational after beam impact?

## Slide 4
Polyimide insulation
10 cm
Reduction of the Jc induced by:
  High temperature
  Mechanical stress, deformation and cracks
Magnets most sensitive parts
Nb3Sn RRP type (HL-LHC triplet)
Nb-Ti strands (LHC dipole)
200 μm
200 μm
Decomposition of the polyimide when expose to high temperature
  Reduction of the dielectric strength
Nb-Ti and Nb3Sn superconducting cables
Vivien Raginel
Fessia, P., et al. IEEE Transactions on Applied Superconductivity 20.3 (2010): 1622-1625.

## Slide 5
10 cm
Experimental road map
Vivien Raginel
Polyimide insulation degradation due to heating over hours [1]
  Cable stacks heated over hours in furnace between ~460 K and ~860 K.
  Polyimide dielectric strength measured with high voltage.
Jc degradation of Nb-Ti and Nb3Sn due to heating over seconds [2]
  Nb-Ti and Nb3Sn single strands heated up between ~640 K and ~1250 K using a capacitive discharge.
  Strand were in air at room temperature.
  Jc degradation measured via magnetization measurements
  Microscopic Analysis
Degradation of polyimide insulation and of Nb-Ti & Nb3Sn critical current density induced by interaction with 440 GeV proton beam pulses
[1] V. Raginel, et al, “Degradation of the insulation of the LHC main dipole cable when exposed to high temperatures”, IPAC’16
[2] V. Raginel, et al, “Change of critical current density in Nb-Ti and Nb3Sn strands after millisecond heating”, IPAC’17

## Slide 6: Beam Experiment: Samples
At CERN HiRadMat facility shooting 440 GeV proton beam pulses on:
Samples at room temperature within an inert atmosphere (Argon).
30 Nb-Ti cables
~ 5 cm
Nb-Ti & Nb3Sn strands

## Slide 7: Experimental setup
Second Picture with the tank open
Nb-Ti cable stacks
in steels moulds
Nb-Ti and Nb3Sn strands fixed on a steel plate

## Slide 8: Experimental setup
Second Picture with the tank open
6x1011 p+
2.6x1012 p+
1.3x1012 p+
p+
933 K 1026 K
1035 K
823 K
445 K
706 K
882 K
960 K

## Slide 9: Polyimide insulation degradation
beam impact
Side view of a Nb-Ti cable stack after beam impact
Degradation due to chemical decomposition as function of temperature and exposure time.
No degradation measured after beam impact – temperature up to ~1050 K for few ~ms
  Weakening of the insulation at the point of the beam impact was observed for T>~850 K.

## Slide 10: Jc degradation of Nb-Ti
ΔM ∝ Jc x df
Fp = Jc x B
b = B / Bc2(T)
@ 6 K
@ 6 K
@ 6 K
@ 6 K
Capacitive discharge
Beam impact
Capacitive discharge, ΔM degradation (∝ Jc) above 651 K
After beam impact, ΔM degradation above 878 K
Fp decrease and Fpmax shifts toward lower b.
Change of pinning behaviour
Decrease of Bc2(T) for T ≥ 916 K in discharge case. No decrease for beam case.
Variation of Ti content in filaments

## Slide 11: Jc degradation of Nb-Ti
* C. Scheuerlein et all., Journal of Physics: Conference Series, vol. 234, no. 2. IOP Publishing, 2010
*
@ 4 K and 5 T
At T=1157 K (discharge case), filament merging is observed
For same temperature, ΔM goes down with increasing exposure time.
Diffusion process
+ change of pinning behaviour
Degradation of Jc caused by variations of α-Ti precipitates size and spacing
If higher temperature or longer exposure time, Ti diffuses outside filaments to form Cu-Ti compound => Bc2(T) reduction, filament merging
Ref
1157 K

## Slide 12: Jc degradation of Nb3Sn
Capacitive discharge, ΔM degradation for T > 823 K
All samples degrade after beam impact ,T ≥ 699 K
Fp decrease and no shift of Fpmax
No change of pinning behaviour
No grain growth observed (SEM analysis)
Decrease of Bc2(T) not observed, however Tin content measurements are planned
Capacitive discharge
Beam impact
@ 15 K
@ 15 K
@ 15 K
@ 15 K
Ref.
1264 K

## Slide 13: Jc degradation of Nb3Sn
@ 4 K and 5 T
Contrary to Nb-Ti, for same temperature, ΔM goes down with decreasing exposure time.
Indication degradation due to beam impact is dominated by stresses and potentially cracks caused by fast heating and high thermal gradients
Further investigations to identify the origin:

## Slide 14: Conclusions and outlook
Identification of the damage mechanisms and damage limits of critical magnet components due to instantaneous beam impact is essential for future increase of beam energy (HL-LHC, FCC)
Polyimide insulation
  Chemical decomposition due to exposure to high temperature
  No degradation induced by beam up to 1050 K, however observation of a weakening for T>850 K
  For long exposure time, degradation for temperatures above 728 K
Nb-Ti strand
  Degradation dominated by diffusion processes.
  Jc degradation for peak temperatures above 900 K in case of beam impact
Nb3Sn strand
  Most probable causes are stresses and cracks induced by the fast heating and high thermal gradient
  Grain growth is excluded. Further investigations to identify degradation mechanism
  Jc degradation due to beam impact observed in all samples – lowest peak temperature ~700 K
  For second long heating, Jc degradation for temperatures above 823 K
Experimental validation of results with beam at liquid Helium temperature scheduled for mid-2018

## Slide 15
Thank you for your attention

## Slide 16
Spare slides

## Slide 17: Insulation degradation due to hours heating
~7 hours
Insulated cable stacks heated over hours in furnace between 461 K and 864 K in inert atmosphere (Argon).
Dielectric strength is measured via cable-to-cable breakdown voltage measurement after heat treatment.
Vivien Raginel
Stack of 6 Nb-Ti cables
25 cm