## Slide 1: Update on irradiation test results at GSI and correlations to material damage simulation activity
M. Tomut

## Slide 2: Team
Micromechanical and resistivity measurements:
Ph. Bolz, TU Darmstadt/GSI
C. Porth, TU Darmstadt / GSI
Microstructural & morphological characterization:
K Bunk, Frankfurt University/GSI
                F. Kopietz, TU Darmstadt/GSI
                W. Bolse & group, U. Stuttgart
DPA calculations-FLUKA: E. Skordis, CERN
MD simulations: K. Kupka, TU Darmstadt / GSI
A. A. Leino, W. Ren, E. H.Ahlgren,K. Nordlund, F. Djurabekova University of Helsinki

## Slide 3: Summary
Micromechanical characterization of pristine MoGR samples
  contribution to D11.4 “Results on characterisation of new materials and composites” M46
Update on characterization of MoGr samples irradiated at GSI
  contribution to D11.3 “Irradiation test results” M46
FLUKA DPA calculations for irradiations at GSI and integration with experimental results
  contribution to MS72 “Present results on material damage from simulation and compare to experiments” due by M45 (delayed to after this meeting)

## Slide 4: Microindentation depth controlled: 5 µm 20-30 indents Berkovich indenter
Pristine MoGR characterization-
micromechanical properties

## Slide 5
Damping constant (Dc):
Dynamic hardness (DH):
Indenter accelerated 2 µm towards
the surface with 15 mN
‘Bouncing` on the surface measured
20 repeats
Single impact nanoindentation characterization

## Slide 6
Pristine MoGR characterization-
dynamic mechanical response

## Slide 7: Characterization of MoGr samples irradiated at GSI

## Slide 8: Overview of irradiation tests on MoGr
Feb. 2014
mid 2013
July 2014
2016
BNL (p+, n)
3th generation
MG 1110-E
(3.7 g/cm3)
NOT fully molten
20%v Mo
40%v C-fibers (long+short)
5th generation
MG 5200-S
(2.65 g/cm3)
Fully molten
7.2%v Mo
46.4%v C-fibers (long+short)
2 annealing cycles:
1150°C
1300°C
4th generation
MG 3110-P
(2.67 g/cm3)
Fully molten
20%v Mo
40%v C-fibers (long+short)
6th generation
MG 6400-U
(2.63 g/cm3)
Fully molten
4.5%v Mo
NO C-fibers
Annealing 1800˚C
MG 6530-Aa
(2.5 g/cm3)
Fully molten
4.5%v Mo
5%v C-fibers (long only)
Annealing 1900°C
MG 6541-Aa
(2.5 g/cm3)
Fully molten
4.5%v Mo
0. %v Ti
5%v C-fibers (short only)
Annealing 1900°C
GSI (238U, 209Bi, 197Au, 152Sm, Ca, C ions)
7th generation
MG 6403-Aa
(g/cm3)
Fully molten
4.5%v Mo
%v Ti
NO C-fibers
mid 2015
BNL (p+, n)
E. Quaranta, CERN
Notes: MG 6400U was also irradiated with high-energy Sm beam, however (at date of WP11 meeting in Dec 2014) samples were still to radioactive…

## Slide 9: Irradiation of novel composites at GSI
Ion irradiation: C – U
Energies: 70 MeV – 1 GeV
Fluence: up to 1x1014 i/cm2
Structural characterization:
XRD, Raman spectroscopy, SEM
Functional properties degradation:
thermal ,mechanical, electrical
Material optimization

## Slide 10: Beam induced structural changes in Mo-Gr
Structural characterization:
pristine
1e12 Au ions/cm2
In-plane crystallite size reduction – SEM, Raman spectroscopy:
Swelling → Stress → Deformation → Cracks in the matrix
In situ SEM during irradiation
pristine
3e113 Au ions/cm2

## Slide 11: Radiation damage effect on properties degradation
Irradiation induced hardening
– dynamic harness:
Increase of electrical resistivity
- online measurements during irradiation
Defect accumulation results in gradual resistivity increase
Presence of carbon fibers reduce material’s resistivity degradation
Hardness and Young’s modulus increased with accumulated dose.
Samples annealed at higher temperatures show less degradation

## Slide 12: Irradiation induced deformation and mitigation
Macroscopic bending was observed around 5×1012 Au ions/cm²
Optimization of the material to avoid swelling and deformation

## Slide 13: Irradiation induced hardening- latest measurements
MoGr - less hardening than isotropic graphite and CFC

## Slide 14: Irradiation induced hardening- latest measurements
MoGr - less increase of elastic modulus than isotropic graphite and CFC

## Slide 15: Irradiation induced hardening- MoGr-long fibers- MG6530
Many pop-ins - Amount increasing with fluence
pristine:
1e13:

## Slide 16: Dynamic hardness- impact nanoindentation
Irradiated MoGr - less increase of dynamic hardness than isotropic graphite and CFC

## Slide 17: Damping constant of irradiated MoGr- impact nanoindentation
MoGr - less decrease of damping constant than isotropic graphite and CFC

## Slide 18: FLUKA for GSI
Beam
FLUKA: General purpose particle physics MonteCarlo code used for machine protection, design studies, R2E, activation, collimation -> simulates particle interaction with matter
3 different heavy Ions, 2 different energies and 3 different MoGr grades simulated
1cm^2 beam size impacting on 1 cm^2 target
No significant differences between grades

## Slide 19: Irradiation induced hardening hardness and elastic modulus for Au 4.8 MeV/u DPA dependence

## Slide 20: Irradiation induced hardening impact response for Au 4.8 MeV/u DPA dependence

## Slide 21: Beam-induced bending of MG6400Ua transversal comparison Au 4,8 MeV/u Ca4,8 MeV/u

## Slide 22: Online study of electrical resistivity degradation for isotropic graphite –light ions
relative change of average resistivity for the whole ion range ~ 35 µm)
MG6530 (long fibers, no Ti) < MG6541 (short fibers, Ti) < MG6400 (no fibers, no Ti)
Ca ions to simulate damage induced by secondary particles and recoil atoms in collimator jaw
Degradation of electrical resistivity and thermal conductivity due to beam-induced in-plane size reduction of crystallites
DPA: 10-4
Notes: Graphite resistivity decreases with temperature up to ~600 C.
Experiments with lighter ions are also aiming at determining the dependence of property degradation on the ion stopping power. This dependence is necessary for scaling of ion induced defects for lower stopping powers at high energy and for determining the energy-loss threshold for property degradation.

## Slide 23: Conclusions
Synergistic activity on optimization of MoGr composition as respect to radiation hardness: CERN, GSI, Brevetti Bizz, BNL
  Outcome:
        MoGr with better radiation hardness
        less deformation in GSI experiments
        no failure in BNL irradiation
        Ti addition leads to more stable carbide phases
        Higher temperature treatment- helps
          My personal favorite MG6541
DPA calculations combined with experimental investigations- swift lighter ions (C-Xe) can be used to acquire accelerated damage for radiation hardness characterization
Transmutations effects not addressed by experiments at GSI and simulations at CERN- to be developed in ARIES

## Slide 24: Thank you!
Questions ?