## Slide 1: RD51 – “Precision timing Workshop”
Our experience in the use of
CsI in gaseous detectors
Fulvio Tessarotto
INFN – Trieste
On behalf of the COMPASS RICH team

## Slide 2: OUTLINE
CsI photoconversion
RD26 MWPCs with CsI Photocathodes
COMPASS MWPCs with CsI
The winter accident and CsI memory
The long term CsI quantum efficiency variation
The Hybrid THGEM+MM PDs
CsI deposit on THGEMs
COMPASS upgraded PDs

## Slide 3
OMEGA
DELPHI
TMAE(Tetrakis-Dimethylamine-Ethylene)
SLD - CRID
TEA (Tri-Ethyl-Amine)
CLEO III
E605
Before CsI, photoconverting vapours
in large RICHs with gaseous PD’s
Cherenkov photon
photoelectron
E
Townsend
avalanche
anode wires cathode pads
QE,
NIMA 323 (1992) 351
CERN, 21/02/2017, RD51 Miniweek - Precision timing Workshop - CsI in gaseous detectors - Fulvio Tessarotto

## Slide 4: Thin CsI film provides UV photoconversion
1956:
CsI layer has large
QE for photons
with hν > 6 eV
(Philipp and Taft)
vacuum operated photocathodes
were developed for space astronomy:
G.R.Carruthers,
Appl. Opt. 8 (1969) 633
Appl. Opt. 12 (1973) 2501
Appl. Opt. 14 (1975) 1667
The first position sensitive gas detectors with CsI photocathodes were developed at the end of the 80s:
G.Charpak et al., Proceedings of Symposium on Particle Identification at
High Luminosity Hadron Colliders, Fermilab, Batavia, IL, 1989, p. 295.
J.Séguinot et al., Nucl. Instr. and Meth. A 297 (1990), p. 133

## Slide 5
Thin film photo cathodes
Semitransparent photocathode:
Light absorption
e- propagation
e- escape
e-
g
PC
vacuum
(1)
(2)
(3)
x
0
xmax
a = 0.1 nm-1
b = 0.05 nm-1
Reflective photocathode:
g
PC
substrate
e-
e-
window
CERN, 21/02/2017, RD51 Miniweek - Precision timing Workshop - CsI in gaseous detectors - Fulvio Tessarotto

## Slide 6
J.Séguinot et al., Nucl. Instr. and Meth. A 371 (1996), p. 64.
Cherenkov
photon
Townsend
avalanche
thin layer (300 - 500 nm) of
CsI on a cathode pad plane
CsI is highly reactive
with moisture:
it took many years to
develop appropriate
substrate preparation,
deposition method,
handling technology
for high QE gaseous PDs
This technique was pioneered by T. Ypsilantis and
J. Séguinot, who built an extraordinary prototype
and correctly concluded the technology was not
adequate for the extreme time performance they needed
Reflective CsI photocathodes

## Slide 7
RD26: the technology of MWPCs + CsI
François Piuz
1992, F. Piuz et al. Development of large area advanced fast-RICH detector for particle identification at LHC operated with heavy ions
  TO ACHIEVE HIGH CsI QE:
  Substrate preparation:
  Cu clad PCB coated by Ni (7 µm) and Au(0.5 µm), surface cleaning in ultrasonic bath, outgassing at 60 oC for 1 day
  Slow deposition of 300 nm CsI film:
  1 nm/s (by thermal evaporation or e--gun) at a vacuum
  of ~ 10-7 mbar, monitoring of residual gas composition
  Thermal treatment:
  after deposition at 60 oC for 8 h
  Careful Handling:
  measurement of PC response, encapsulation under dry Ar, mounting by glove-box.
The best fused silica cuts here
A. Di Mauro, NIM A 525 (2004) 173.
Schematic structure of the COMPASS Photon Detector:

## Slide 8: Photoelectron extraction from CsI in gas
Photoelectron extraction from a CsI film, the role of gas and E
M. Alexeev et al., NIM A 623 (2010) 129
C. D. R. Azevedo et al., 2010 JINST 5 P01002
Breskin et al.,
NIM A 367 (1995) 342
VACUUM

## Slide 9: CsI robustness
  CsI is the most robust solid-state photoconverting material among the typical ones, thanks to a higher work function (PC stability under ion bombardment)
CsI exhibits a relative chemical robustness against oxygen and water, as compared to other photoconverters:
Accelerated ageing test, H. Hoedlmoser et al., NIM A 574 (2007) 28.
1 mC/cm2
0.2 mC/cm2

## Slide 10
MWPCs with solid state photocathode (the RD26 effort)
TIC, NA44
COMPASS RICH-1 2002 CsI > 5 m2
JLAB-HALL A
ALICE-HMPID
2009
CsI > 10 m2
STAR
HADES 1999
CsI > 1 m2
RICH with large area gaseous PD’s
2 nd generation: MWPC’s + CsI

## Slide 11: ALICE HMPID
RADIATOR: 15 mm liquid C6F14, n ~ 1.2989 @ 175nm, βth = 0.77
PHOTON CONVERTER: Reflective layer of CsI (QE ~ 25% @ 175 nm)
PHOTOELECTRON DETECTOR: MWPC with CH4 at atmospheric pressure (4 mm gap) HV = 2050 V.
- Analogue pad readout
7 modules, each ~1.5 x 1.5 m2

## Slide 12: Charge dose on the ALICE CsI photocathodes
PC with Npe dropping
Charge dose threshold (Qth red line) for possible CsI QE loss: 0.2 mC/cm2;
Still far during Run2;

## Slide 13
COMPASS RICH-1 MWPC’s with CsI

## Slide 14
photocathodes

## Slide 15
Pictures of RICH PDs in 2002
“lunette” photon interceptor was inserted to protect the PDs from high illumination

## Slide 16: Beam halo ring from data
Beam time: 27/5 – 10/9 ~ 100 days
Duty factor: ~0.25 x ~100 days = ~2 x106 s
PD 5 at 2000 V, anode current in spill: ~ 130 nA
Total charge generated in PD 5: ~ 0.26 C
Number of highly illuminated pads: ~ 50 - 100
Charge on single highly illuminated pad: ~ 1 - 3 mC

## Slide 17
Accidental exposure to air of a
photocathode during winter shut-down

## Slide 18: The whole halo region

## Slide 19: Few months after the end of the first run
highest photon flux region
accumulated charge:~ 1 mC/pad
wires

## Slide 20: CsI surface at microscope (x 1000)
10 mm
“white strip”
normal

## Slide 21
6 consecutive years of COMPASS data taking
up to 15 days of data taking per sample
identical cuts applied to the reconstructed particle trajectories (track quality)
Study of long term CsI QE variations
    Principle:
    Extract the mean number of detected photons per particle from the data collected during six years of COMPASS data taking
RATES IN THE EXTERNAL DETECTORS during SPS spills:
Photoelectrons < 10 Hz / cm2
MIPs < 10 Hz / cm2
 Integrated charge over 6 years < 10 mC/cm2
MAPMTs
M. Alexeev et al, 2014 JINST 9 P01006

## Slide 22
only identified p’s
only rings fully contained in a single cathode
count Nph (detected photons) of each ring
(background cannot be disentangled at this stage)
1 mrad wide qCh bins  N = < Nph >
Cherenkov photons : Poisson distribution
 detected photons : Poisson distribution
at least 1 detected photon
measured N is biased, corrected
measured: m’
m solving numerically the equation
FIT THE DISTRIBUTION:
Data selection, correction and fit
corrected
Frank and Tamm distribution
Background (flat distribution assumed)

## Slide 23
distributions
and fits (>25 mrad)
2006 data
c2 theoretical
NDF = 18
Fit results stable versus:
fit range variations
different ring selection:
at least 2, 3 photons
estimated systematic error: 0.7 x sstat
use N(qCh = 55.2 mrad)
for extrapolation
Fit quality, consistency and stability

## Slide 24
N(qCh = 55.2 mrad)
vs year
(statistical errors)
Frank and Tamm
background
Too few photons:
not used in the following
MEAN OVER 11 CATHODES
(statistical & systematic errors)
results

## Slide 25
<N> vs year is compatible
with no CsI QE variation
max CsI QE variation
rate : 2.3 % / year
[1 “COMPASS year” :
~6 months of data taking]
For the 3 most critical cathodes:
max CsI QE variation rate : 5.2 % / year
Estimated systematic error of the measurement: 2 % /year
Errors enlarged to get 50% probability for the linear fit
<N> corrected for
lower HV (-20V)
CsI photocathodes can preserve QE over years
The CsI QE decrease is modest

## Slide 26
MWPCs with CsI have good performance
photons / ring (b ≈ 1, complete ring in acceptance) : 14
sq-ph (b ≈ 1) : 1.2 mrad
sring (b ≈ 1) : 0.6 mrad
2s p - K separation @ 43 GeV/c
PID efficiency ~ 95% for q Ch > 30 mrad
except for the very forward region
After a long fight for increasing electrical stability at high m.i.p. rates and systematic studies at the CERN GIF we came to the same conclusion as Ypsilantis and Seguinot:
J. Seguinot et al., NIM A 371 (1996), 64:
CsI-MWPC with 0.5 mm gap to minimize ion collection time, fast front-end electronics (20 ns int. time):
stable operation is not possible at 105 gain because of photon feedback, space charge and sparks

## Slide 27: THGEM + CsI R&D for RICHes
ALICE VHPID
THGEM &
HYBRID
beam
Č photon
V.Peskov et al., NIMA 695 (2012) 154
COMPASS, RICH-1 upgrade by Triple THGEM detectors

## Slide 28
radiator:
C4F10
5 m
6 m
3 m
UV mirror
wall
radiator gas: C4F10
Photon detectors system now:
              12 MWPC + CsI 600 x 600 mm2
              4 MAPMT 600 x 600 mm2 (2006)
… in 2016
MWPC + CsI
MAPMT
4 New 600 x 600 mm2 MPGD based PDs
will be installed for a total sensitive surface of ̴ 1.1 m2
Photon Detectors
COMPASS RICH-1 UPGRADE IN 2016
Hybrid Detector (2 THGEM + MM)

## Slide 29: The Hybrid detector concept and the building blocks
    One 300 mm x 600 mm Bulk Micromegas detector
    Two layers of THGEMs (300 mm x 600 mm) in staggered configuration
Signal read out via capacitive coupling pad readout and APV25 F/E boards
Multi-Pad Anode 8mm X 8mm pad size
To simplify the construction requirements a modular architecture has been adopted where one “module” consists of:
THGEM 1
THGEM 2
Two modules are put side by side to build a 600 mm x 600 mm detector

## Slide 30: exploded view of the new COMPASS PD
CERN, 21/02/2017, RD51 Miniweek - Precision timing Workshop - CsI in gaseous detectors - Fulvio Tessarotto

## Slide 31: The THGEMs design: specifics
12 sectors on both top and bottom, 0.7 mm separation
24 fixation points to guarantee THGEMs flatness
Thickness: 0.4 mm, hole diameter: 0.4 mm, pitch: 0.8 mm
border holes diam.: 0.5 mm
pillars in PEEK
THGEM pcb size = 620 mm x 320 mm,
active area = 581 mm x 287 mm

## Slide 32: THGEM production @ ELTOS and the surface treatment in Trieste
  stripping dry-film
  development
  etching
  image transfer
  multi-spindle drilling
  mounting
A post production specific surface treating and cleaning procedure developed in Trieste is applied:
Surface Polishing.
High pressure water cleaning.
Ultrasonic Bath with Sonica PCB solution (PH11), distilled water rinsing and oven @ 160 ºC
  drilling

## Slide 33: THGEM storage, transport and gold coating
  etching
  THGEM ready for CsI coating

## Slide 34: The CERN CsI evaporation system
CERN, 21/02/2017, RD51 Miniweek - Precision timing Workshop - CsI in gaseous detectors - Fulvio Tessarotto

## Slide 35: THGEM CsI coating
Turbopump
THGEM
THGEM box
4 evaporators
piston
evaporators
QE measurement

## Slide 36: COMPASS THGEM CsI coating
  etching
  THGEM number evaporation date at 60 degrees at 25 degrees
19 CsI evaporations performed in 2015 - 2016
on 15 pieces: 13 THGEMs, 1 dummy THGEM,
and 1 reference piece (from ALICE coatings)
11 coated THGEMs available, 8 used + 3 spares
Thick GEM 319 |  |  | 1/18/2016 | 2.36 | 2.44
Thick GEM 307 |  |  | 1/25/2016 | 2.65 | 2.47
Thick GEM 407 |  |  | 2/2/2016 | 2.14 | 2.47
Thick GEM 418 |  |  | 2/8/2016 | 2.79 | 2.98
Thick GEM 410 |  |  | 2/15/2016 | 2.86 | 3.14
Thick GEM 429 |  |  | 2/22/2016 | 2.75 | 2.74
Thick GEM 334 |  |  | 2/29/2016 | 2.77 | 3.00
Thick GEM 421 re-coating |  |  | 3/10/2016 | 2.61 | 2.83
QE measurements indicate an average THGEM QE = 0.73 x Ref. piece QE, in agreement with expectations (THGEM optical transparency = 0.76)
  Reference piece 7/4/2016 3.98 3.76
We are grateful to Thomas Schnider and Miranda Van Stenis for their excellent
professsionality and dedication: working with them is both effective and a pleasure

## Slide 37: glovebox for CsI THGEM mounting
CERN, 21/02/2017, RD51 Miniweek - Precision timing Workshop - CsI in gaseous detectors - Fulvio Tessarotto

## Slide 38: the challenge of the integration in the existing environment
30 mm x 30 mm
“Photon” view
External view
CERN, 21/02/2017, RD51 Miniweek - Precision timing Workshop - CsI in gaseous detectors - Fulvio Tessarotto

## Slide 39: larger glovebox for CsI mounting on RICH

## Slide 40: A preliminary estimate of the number of photons
from the same data, the number of “signal hits” on Hybrids is larger than on MWPCs
Active surface of the detector (HV) 50%
Comparing the number of detected photons in the present status:

## Slide 41: THANK YOU