## Slide 2
FCC beam screen
  Beam screen functions and concept
  Beam screen prototype manufacturing
  Status
New deformable RF finger module
LHC cold/warm transition
Cold vacuum system

## Slide 3
LHC beam screen and cold bore
Cold bore: separation UHV/ superfluid helium
Cold mass
Beam screen
Coils

## Slide 4
Photon distribution
Handling of high synchrotron radiation load of protons @ 50 TeV:
~30 W/m/beam (@16 T) (LHC <0.2W/m)
5 MW total in arcs
New beam screen with ante-chamber
absorption of synchrotron radiation at 50 K to reduce cryogenic power
avoids photo-electrons, helps vacuum
Synchrotron radiation/beam screen

## Slide 5
Cooling channels
Copper layer, 0.3 mm for impedance
Screen
Deflector
Ribs:
Mechanical strength
Photon stopper
Copper strips for heat transfer
Pumping holes
Beam screen concept
Magnet cold bore

## Slide 6
Design – Main dimensions
Cold bore diameter: 44/47 mm
Beam screen wall:
  1.25 mm P506 (high-Mn high-N st. steel)
  0.3 mm copper
Nominal aperture:
  H:~ 29.6 mm
  V:~26.4 mm
Slit height: ~ 3/5 mm
Cooling channel:
  Thickness 1 mm
  Internal 53.58 mm2
  Hydraulic diameter: 5.61 mm
Copper for heat transfer: 0.3 mm

## Slide 7
Prototypes
Series vs first prototypes
Cooling channel:
316L,
3D printed + machined
Cooling channel:
P506 stainless steel
Extruded
Reflector:
P506 stainless steel
Extruded + finishing
Beam screen wall:
P506, 1.25 mm
copper colamination, 0.3 mm
Ribs:
P506
punching
Beam screen wall:
304L, 1. 5 mm
copper electrodeposition, 0.05 mm
Sub-component manufacturing:
Ribs:
304L
Laser cutting
Reflector:
304,
Machined + forming + finishing
Series
1st prototype

## Slide 8
Short (30 cm) prototype manufacturing
Assembly and welding
Cold sprayed copper (0.3 mm)
30 cm long prototypes

## Slide 9
Status
First 2m long prototype being manufactured and to be tested at ANKA.
Next steps:
New prototypes with updated design
Beam screen interconnection
2 m long prototype
Updated design

## Slide 10
HL-LHC cold vacuum system layout principle
IP
side
Cryostat vacuum vessel
Cold mass
Cold bore
Beam screen
Fixed point Cold mass/ vacuum vessel
BPM
BPM
Fixed point of the beam screen on the IP side
Bellows between beam screen and cold bore on the other side
Shielded bellows between the two magnets (PIM)
Connection beam screen/cold bore
Bellows

## Slide 11
Copper Beryllium deformable RF fingers:
Compact and robust design
C17410
0.1 mm thick, 3 mm width, gap: 1.4 mm
RF finger design in triplet area
Beam vacuum interconnection (BPM not integrated)
Titanium spring (total prestress: ~370 N)
Static RF fingers
Copper insert
131

## Slide 12
Status
First prototypes have been manufactured.
Mechanical and RF tests have been successfully carried out.
Prototype for RF measurements
Prototype assembly
Plug-in modules with deformable RF fingers are now the baseline for the HL-LHC interconnections in the triplet areas.
The design is being updated.
New prototypes will have to be produced and tested before the series production.

## Slide 13
Cold/Warm transition for the collimator by-pass
Vacuum system for the collimator by-pass
New C/W transition with vacuum port integrated
The design is being completed (2D detailed drawings ongoing).
Manufacturing of two pre-series units (straight after) and then the series.

## Slide 15
Beam screen concept - Principle
Photons are channelled in the antechamber and stopped onto the ribs.
Photondesorpted gas is channelled in the antechamber and pumped through pumping holes.
Synchrotron radiation power is deposited mainly on the deflector tip and the ribs and is transferred to the cooling circuit by the external copper.