## Slide 1: New Magnetic Phase in the Nickelate Perovskite TlNiO3
Lukas Korosec
ETH Zürich, Department of Physics
Joint Annual Meeting of SPS and ÖPG 2017

## Slide 3: Outline
Why are RNiO3 perovskites interesting?
Investigations via NMR and µSR
Two magnetic phase transitions in TlNiO3
Conclusions

## Slide 4: RNiO3: introduction
Phase diagram of RNiO3
Korosec et al., PRB 95, 060411(R) (2017).
Notes: Simultaneous MIT and structural transition
Transition temperature depend continuously on bond angle (features of crystal structure)

## Slide 5: RNiO3: introduction
Large
Small
Insulating phase: structure
Phase diagram of RNiO3
Kim et al., Chem. Mater. 14, 4926 (2002).
Korosec et al., PRB 95, 060411(R) (2017).
Notes: Insulating phase: Large and small octahedra alternate (rocksalt pattern) -> “charge disproportionation”? “site-selective Mott?”
Same distortion found in TlNiO3

## Slide 6: RNiO3: magnetic structure
Possible magnetic structures
Phase diagram of RNiO3
Giovannetti et al., PRL 103, 156401 (2009).
Korosec et al., PRB 95, 060411(R) (2017).
Notes: Propagation vector known from neutron powder diffraction (4 Ni / period), multiple structures give same powder pattern
Collinear or non-collinear, equal or unequal moments? TlNiO3: TN = 104 K
Breaking of inversion symmetry -> electric polarization (not yet detected)?

## Slide 7: Experimental techniques
Nucleus | γ / 2π
205Tl | 24.56 MHz/T
203Tl | 24.32 MHz/T
µ | 135.5 MHz/T
NMR + µSR:
Zeeman Hamiltonian
Notes: Use spin ½ to probe electronic system-> Zeeman Hamiltonian
If spin not parallel to B, precession, frequency measures of B-field at nucleus

## Slide 8: Experimental techniques
Nucleus | γ / 2π
205Tl | 24.56 MHz/T
203Tl | 24.32 MHz/T
µ | 135.5 MHz/T
Spin-echo + T2 decay
NMR + µSR:
Zeeman Hamiltonian
From Wikipedia
Notes: Spin echo: refocus spins with slightly different frequencies
T2 = dephasing time (fluctuations or nuclear-spin – nuclear-spin interactions)

## Slide 9: Experimental techniques
Nucleus | γ / 2π
205Tl | 24.56 MHz/T
203Tl | 24.32 MHz/T
µ | 135.5 MHz/T
NMR + µSR:
Zeeman Hamiltonian
From Wikipedia
Spin-echo + T2 decay
Notes: Spin echo: refocus spins with slightly different frequencies
T2 = dephasing time (fluctuations or nuclear-spin – nuclear-spin interactions)

## Slide 10: Experimental techniques
Nucleus | γ / 2π
205Tl | 24.56 MHz/T
203Tl | 24.32 MHz/T
µ | 135.5 MHz/T
NMR + µSR:
Zeeman Hamiltonian
Yamada and Sakata, JPSJ 55, 1751 (1986).
NMR on AFM powders
Notes: H = internal field of antiferromagnet, HA = applied field. Powder pattern has edges at HA +/- H

## Slide 11: Why TlNiO3?
Same RT insulating phase as rare-earth nickelates [1]
Same low-T magnetic propagation vector [1]
Tl3+ is diamagnetic
205Tl and 203Tl are good nuclei for NMR
TlNiO3 is an ideal system for NMR on RNiO3!
[1]: Kim et al., Chem. Mater. 14, 4926 (2002).
Notes: For NMR, Tl better than all rare-earths
Ni, O: rare isotope with S > ½ -> quadrupole

## Slide 12: Tl-NMR spectra
NMR in applied field
PM phase: Narrow line
AFM phase: Two wide patterns
Korosec et al., PRB 95, 060411(R) (2017).
Notes: PM phase: expect narrow line for each isotope;
AF phase: expect broad pattern, edges at shift corresponding to internal field

## Slide 13: Tl-NMR spectra
NMR in applied field
PM phase: Narrow line
AFM phase: Two wide patterns
Broad ZF signals
Magnetic order up to ~200 K!
Korosec et al., PRB 95, 060411(R) (2017).
Zero-field NMR frequencies
Notes: ZF: Resonances at expected frequencies (but broad), one vanishes at 200 K! (No NMR near transition for technical reasons)

## Slide 14: Zero-field µSR
Frequencies vs T
Rapid signal decay: broad spectrum
Two magnetic transitions!
TN = 104 K, TN* = 202 K
Time-domain asymmetries
Korosec et al., PRB 95, 060411(R) (2017).
Notes: T > 105 K: single damped cosine; T < 105 K: Multiple damped cosines
Four resonances at low temperatures -> different stopping sites. Strange temperature-dependences presumably because of combination of two magnetic orders.

## Slide 15: Magnetic susceptibility
Visible transition at TN = 104 K, but not at TN* = 202 K.
Korosec et al., PRB 95, 060411(R) (2017).
Notes: Phase transition does not occur in applied fields? Not seen in SQUID magnetometry!

## Slide 16: NMR T2 relaxation
B0 = 3.5 T
Hysteresis of single T2 between TN = 104 K and TN* = 202 K
=> Entire sample is affected by TN*
Activated behavior at low T with Δ = 82 ± 5 K
=> gap in magnetic excitation spectrum?
Korosec et al., PRB 95, 060411(R) (2017).
Notes: In a few Tesla, transition at TN* does not occur
T2 relaxation shows that the entire sample knows about both phases

## Slide 17: Conclusions
NMR and µSR offer new insights into RNiO3
TlNiO3 admits two magnetically ordered phases
New phase is easily suppressed by magnetic fields
New phase has not been found in rare-earth nickelates