## Slide 1: Laser Update
Carlos Vergel-Infante
May 17th, 2017

## Slide 2: Size and Max. Height of flaws (Stave #4)

## Slide 3
Considering only the flaws found in the honeycomb structure (all minus the smallest red one), and ignoring all the flaws with the foam.
Measuring two variables in 5 psi – 0 psi plots:
  Max Height: Pixel with maximum height in the area where a flaw is
  Size: Number of pixels above 3 sigma in the area where the flaw is

## Slide 4
Chart: 
| 6.0 | 7.0 | 17.0 | 8.0 | 7.0 | 7.0 | 12.0 | 4.0 | 13.0 | 7.0 | 7.0 | 7.0 | 4.0 | 14.0 | 7.0 | 7.0 | 4.0 | 10.0 | 17.0 | 6.0 | 10.0
Height | 156 | 126 | 359 | 184 | 64 | 151 | 170 | 81 | 232 | 133 | 122 | 115 | 60 | 324 | 149 | 187 | 90 | 85 | 433 | 73 | 253
Chart: 
| 6.0 | 7.0 | 17.0 | 8.0 | 7.0 | 7.0 | 12.0 | 4.0 | 13.0 | 7.0 | 7.0 | 7.0 | 4.0 | 14.0 | 7.0 | 7.0 | 4.0 | 10.0 | 17.0 | 6.0 | 10.0
Size | 173 | 313 | 1164 | 449 | 135 | 396 | 425 | 148 | 679 | 279 | 254 | 209 | 47 | 1202 | 382 | 460 | 232 | 380 | 1657 | 119 | 696

## Slide 5
Chart: 
| 6.0 | 7.0 | 17.0 | 8.0 | 7.0 | 7.0 | 12.0 | 4.0 | 13.0 | 7.0 | 7.0 | 7.0 | 4.0 | 14.0 | 7.0 | 7.0 | 4.0 | 6.0 | 10.0
Height | 156 | 126 | 359 | 184 | 64 | 151 | 170 | 81 | 232 | 133 | 122 | 115 | 60 | 324 | 149 | 187 | 90 | 73 | 253
Chart: 
| 6.0 | 7.0 | 17.0 | 8.0 | 7.0 | 7.0 | 12.0 | 4.0 | 13.0 | 7.0 | 7.0 | 7.0 | 4.0 | 14.0 | 7.0 | 7.0 | 4.0 | 6.0 | 10.0
Size | 173 | 313 | 1164 | 449 | 135 | 396 | 425 | 148 | 679 | 279 | 254 | 209 | 47 | 1202 | 382 | 460 | 232 | 119 | 696
Trend for both variables after removing the two flaws indicated in red arrows

## Slide 6
Analyzing only flaws with 7 honeycombs structures with this shape (yellow and red ones).
Chart: 
| 271.0 | 391.0 | 52.0 | 496.0 | 933.0 | 1068.0 | 1068.0
Height | 149 | 187 | 126 | 151 | 133 | 122 | 116
Chart: 
| 391.0 | 52.0 | 496.0 | 933.0 | 1068.0
Height | 187 | 126 | 151 | 133 | 122
Only flaws between pipes (middle region)
Chart: 
| 271.0 | 391.0 | 52.0 | 496.0 | 933.0 | 1068.0 | 1068.0
Size | 382 | 460 | 313 | 396 | 279 | 254 | 209
Chart: 
| 391.0 | 52.0 | 496.0 | 933.0 | 1068.0
Size | 460 | 313 | 396 | 279 | 254
Same x position for two same intended flaws
122 and 116
254 and 209

## Slide 7
Analyzing only flaws with 4 honeycombs structures with this shape (yellow and red ones).
Chart: 
| 470.0 | 764.0 | 1237.0
Height | 90 | 81 | 60
Chart: 
| 470.0 | 764.0 | 1237.0
Size | 232 | 148 | 47

## Slide 8: Summary
There is a correlation between the number of honeycomb structures of a flaw with its height, and also with its size (>3 sigma=36 um).
The correlation between distance from the pressure pipe and the size of the flaw does not seem to be linear, but has a maximum around 40 cm from the pipes.