## Slide 1: New stave no5
William Heidorn, Jie Yu
Iowa State University
ISU group meeting, August.09.2017

## Slide 2: set up and data taking
Stave (no 5 ?) no intended flaws.
  Stave connectors affect our L side setup. Temporary solution managed.
  A small pop up area on the stave (J side).
  measurements of L and J side @-55 and +50 C.

## Slide 3: J side
@ —55 C
@ +50 C
J side
L side
glass edge cover.

## Slide 4: T profile J side
Liquid inlet
Liquid outlet
@ —55 C
@ +50 C
edge effect due to end of stave card.
Rather smooth after background subtraction.
Edge glass effect.

## Slide 5: T profile L side
Liquid inlet
Liquid outlet
@ —55 C
@ +50 C
edge effect due to end of stave card.
Maybe larger fluctuations @-55C, but don't look like flaws.

## Slide 6: Stave #4 flaws for comparison
(A): 5–8 cm
(B): 2-3 cm
(B): <=2cm
J side
10
20
30
40
50
60
70
80
90
100
110
120
130
2cm
8cm
J side
(A): Pipe-foam glue missing (partial).
(B): Foam-facing glue missing (full)
  detected: 2cm. undetected: 1 cm.
(C): Foam-facing glue missing (partial).
  seen, but not clearly.
X
?
X
(X)
X
one sided?
3.5cm
2cm
4cm

## Slide 7: Summary
Very first look at the stave #5, no intended flaws.
  No obvious flaws are detected using either high or low temperature data.
  Some edge effect due to end of stave card and supporting glass as expected.
  T profile is smoother @+50 C as seen before.

## Slide 8
backup

## Slide 9: Stave #4 comparison, matching
L side
(A): 5–8 cm
(B): 2–3 cm
L side
10
20
30
40
50
60
70
80
90
100
110
120
130
1cm
8cm
?
??
?
3cm
X
X
X
Undetected
2
1
L side
(A): Pipe-foam glue missing (partial) undetected 1.
(B): Foam-facing glue missing (full) all found (?!).
  1 cm can also be seen. Not so clearly.
(C): Foam-facing glue missing (partial) undetected 2.
  3 and 4.5 cm, closer to liquid in/out.
3.5cm
4.5 cm
2 cm
Total
8
3
2cm

## Slide 10: Stave #4 comparison, matching
(A): 5–8 cm
(B): 2-3 cm
(B): <=2cm
J side
10
20
30
40
50
60
70
80
90
100
110
120
130
2cm
8cm
Undetected
1.5
2
J side
(A): Pipe-foam glue missing (partial) undetected 2.
(B): Foam-facing glue missing (full) undetected 1.
  very close to liquid in/out edge!
(C): Foam-facing glue missing (partial) undetected 0.5
  seen, but not clearly.
X
?
?
X
(X)
Total
5
3 ?
X
one sided?
3.5cm
2cm
4cm

## Slide 11: Delamination type from stave #2
Conclusions below depend on how accurately the delaminations are implemented.
(A): Pipe-foam glue missing (full pipe ring or partially??).
  1 (nice peak) out of the 3 seen on both sides, the other two seen on one side.
  2.5 cm one is hardly seen. 8cm one doesn’t form nice peak. Might due to some other kind of delamitation on a larger scale.
(B): Foam-facing glue missing (full).
  Mostly form a nice peak ~1 C height.
  3cm is clear, 2cm can also be found.
  Effect seen also on the other side’s T distribution.
(C): Foam-facing glue missing (partial).
  Cannot form nice peaks. A wider T deficit seen.
  2cm is hardly seen. 2.5cm is found.
might be one of the two peaks.
4cm
3.5cm
(A)
(B)
(C)
can be fluctuation.