## Slide 1: Modelling radiation damage in TCAD D. Passeri(1,2), F. Moscatelli(2), A. Morozzi(1,2)
(1) Dipartimento di Ingegneria - Università di Perugia, Italy (2) Istituto Nazionale Fisica Nucleare - Sezione di Perugia, Italy

## Slide 2: Outline
Motivations and background.
TCAD radiation damage modelling: discussion.
Simulation results and comparison with experimental data:
  - DC (steady-state) -> Diodes / Gate Controlled Diodes.
  - AC (small-signals) -> MOS Capacitors.
  - Time (transient) -> Multi-strip structures.
Conclusions.

## Slide 3: Outline
Motivations and background.
TCAD radiation damage modelling: discussion.
Simulation results and comparison with experimental data:
  - DC (steady-state) -> Diodes / Gate Controlled Diodes.
  - AC (small-signals) -> MOS Capacitors.
  - Time (transient) -> Multi-strip structures.
Conclusions.

## Slide 4: Motivations
Modern TCAD tools(1) offer a wide variety of approaches, characterized by different combinations among physical accuracy and comprehensiveness, application versatility and computational demand -> mixed-mode approaches can be efficiently followed.
A number of different physical damage mechanisms actually may interact in a non-trivial way. Deep understanding of physical device behavior therefore has the utmost importance, and device analysis tools may help to this purpose.
Bulk and surface radiation damage have been taken into account by means of the introduction of deep level radiation induced traps whose parameters are physically meaningful and whose experimental characterization is feasible.
Within a hierarchical approach, increasingly complex models have been considered, aiming at balancing complexity and comprehensiveness.
(1) Sentaurus Device

## Slide 5: Once upon a time... (1996)
Numerical analysis and physical modelling of semiconductor devices -> application in High Energy Physics domain…
Modelling of the interaction between ionizing particle / silicon substrate compatible with Box Integration Method simulation scheme.
Grad can be distributed in time and space according to the numerical spatial and time discretization algorithms.
TCAD applications in HEP in 1996…

## Slide 6: Radiation damage modelling
Continuity equation for both free and trapped carriers:
Numerical modelling of radiation damage effects in semiconductor devices.
Deep-level recombination centres / traps radiation induced.
Explicit contribution of the trapped charges to the charge density (modified Poisson equation):

## Slide 7: “University of Perugia” model
[1] D. Passeri, P. Ciampolini, G.M. Bilei, and F. Moscatelli, Comprehensive Modeling of Bulk-Damage Effects in Silicon Radiation Detectors, IEEE Trans. on Nuclear Science, vol. 48, no. 5, October 2001.
[2] M. Petasecca, F. Moscatelli, D. Passeri, and G. U. Pignatel, Numerical Simulation of Radiation Damage Effects in p- Type and n-Type FZ Silicon Detectors, IEEE Trans. on Nuclear Science, vol. 53, no. 5, October 2006.
More than 20 specific journal papers on TCAD radiation damage modelling
…

## Slide 8: LHC CMS Si Tracker design
Choice of the Si-Strip detector substrate resistivity.
Strip geometry optimization (w/p, metal overhang).
Electron concentration at the surface
Critical Electric Fields (within Si) reduction

## Slide 9: Outline
Motivations and background.
TCAD radiation damage modelling: discussion.
Simulation results and comparison with experimental data:
  - DC (steady-state) -> Diodes / Gate Controlled Diodes.
  - AC (small-signals) -> MOS Capacitors.
  - Time (transient) -> Multi-strip structures.
Conclusions.

## Slide 10: TCAD radiation damage models
Pennicard et al., Simulations of radiation-damaged 3D detectors for the Super-LHC, NIM A 592 (2008) 16–25 .
- 3 levels, increased capture cross-sections n, p.
E. Verbitskaya et al., Operational voltage of silicon heavily irradiated strip detectors utilizing avalanche multiplication effect, JINST 7 C02061, 2012.
- 2 levels, avalanche multiplication, 1D “analytical” approach.
Delhi University (R. Dalal et al., Vertex - 2014, 23rd RD50 CERN, Nov. 2013)
- 5 levels + QF / 2 levels + QF + Qit.
RD50 Collaboration (T. Peltola PSD2014 / RESMDD2014)
  - defect models tuned by R. Eber from V. Eremin et al., Avalanche effect in Si heavily irradiated detectors: Physical model and perspectives for application, NIM A 658 (2011) for Φeq=1.01014 - 1.51015 cm-2 at fixed T=253 K;
  - 3-level model within 2 μm of device surface + proton model in bulk.
Hamburg model J. Schwandt, R. Klanner – Global parameter optimization (27th RD50 Workshop, December 2-4, 2015).

## Slide 11: New “University of Perugia” model
Extend the predictive capabilities to HL-LHC radiation damage levels (e.g. fluences > 2.0×1016 cm-2 1 MeV neutrons).
Keep low the number of traps (e.g. fitting parameters).
New effects (e.g. charge multiplication <- avalanche effects).
Physically grounded approach.
No over-specific modelling (one model fits all…).
Predictive capabilities @, @T, @Vbias, …

## Slide 12: New “University of Perugia” model
TEST STRUCTURE MEASUREMENTS
DETECTOR OPTIMIZATION
Modelling the effects of the radiation damage.
Predictive insight of the behaviour of detectors, aiming at their performance optimization.
MODEL
PARAMETERS EXTRACTION
MODEL VALIDATION
CHARGE COLLECTION

## Slide 13: Radiation damage effects

## Slide 14: Radiation damage effects (2)
Ionization -> SURFACE damage
  - build-up of trapped charge in the oxide;
  - increase in the number of bulk oxide traps.
  - increase in the number of interface traps;
  - QOX, NIT
Atomic Displacement -> BULK damage
  - silicon lattice defect generations;
  - point and cluster defects;
  - increase of deep-level trap states;
  - NT
T. R. Oldham, F. B. McLean, Total Ionizing Dose Effects in MOS Oxides and Devices, IEEE Trans. on Nuclear Science, vol. 50, no. 3, June 2003

## Slide 15: Traps characteristics
Traps provide allowed energy states within the band-gap, affecting the device behavior to many respects, e.g. by altering the effective doping, by enhancing recombination, by increasing leakage…
Several models, e.g. Shockley–Read–Hall recombination, depend on traps implicitly
Traps can be specified in terms of:
  Type (Acceptor, Donor)
  Energy Distribution (Level, Gaussian, Uniform, …)
  Capture cross-sections (electrons, holes)
  Concentration / Spatial distributions

## Slide 16: Traps type
Acceptor traps are uncharged when unoccupied (empty) / negatively charged when occupied (they carry the charge of one electron when fully occupied).
Donor traps are uncharged when unoccupied (empty) /positively charged when occupied (they carry the charge of one hole when fully occupied).
neutral if above ()
charged (-) if below ()
charged (+) if above ()
neutral if below ()
Acceptor
Donor

## Slide 17: Traps energy distribution
Traps energetic parametrization.
FromMidBandGap
EnergyMid=0

## Slide 18: The space discretization issue
Mesh (grid) definition is crucial for simulation accuracy.
Global Refinement & Interface

## Slide 19: The space discretization issue (2)
Mesh (grid) definition is a crucial for simulation accuracy / simulation convergence.
G. Giugliarelli et al., “TCAD simulations of breakdown voltage and isolation properties of 3D sensors”, 12th “Trento” Workshop on Advanced Silicon Radiation Detectors.

## Slide 20: The time discretization issue
MIP DISCRETIZATION

## Slide 21: The time discretization issue (2)
Time discretization of the charge generation…
Numerical issues in charge generation -> charge collection evaluation.
Poor time discretization
Proper time discretization
Good Landau shape
“Extra” time discretization
Pure Gaussian shape

## Slide 22: Outline
Motivations and background.
TCAD radiation damage modelling: discussion.
Simulation results and comparison with experimental data:
  - DC (steady-state) -> Diodes / Gate Controlled Diodes.
  - AC (small-signals) -> MOS Capacitors.
  - Time (transient) -> Multi-strip structures.
Conclusions.

## Slide 23: Diode simulation: leakage current
Effect of the capture cross-sections variation combined with impact ionization (simplified n-on-p single strip structure).
Relatively low effect
Significant effect of the impact ionization at high fluences

## Slide 24: Gate Controlled Diode
Non-irradiated structures.
Ld/2 = 20 µm
Lg/2 = 20 µm
psub
n+
SiO2
  100 µm active depth
  n+ = 1×1019 cm-3
  psub = 3×1012 cm-3

## Slide 25: Sensitivity analysis: QOX + NIT
Combined effect of fixed charge (QOX) and interface trap states/trapped charge (NIT) increase.

## Slide 26: Effect of Interface Trap type
NITA acceptor type traps, NITD donor type traps.
NitA > NitD
NitA >> NitD
NitA << NitD
NitA < NitD
NitA = NitD

## Slide 27: Outline
Motivations and background.
TCAD radiation damage modelling: discussion.
Simulation results and comparison with experimental data:
  - DC (steady-state) -> Diodes / Gate Controlled Diodes.
  - AC (small-signals) -> MOS Capacitors.
  - Time (transient) -> Multi-strip structures.
Conclusions.

## Slide 28: MOS Capacitor measurements
QOX and NIT evaluation (from CHF - CQS measurements).
NIT evaluation from p-type substrate (MOS C, GD) and pMOSFET.
Following the method proposed in P. J. McWhorter and P. S. Winokur
in Applied Physics Letters 48, 133 (1986), it is possible to separate the two contributions of QOX and NIT.
Q

## Slide 29: Interface Trap density measurements
NIT/DIT evaluation (from CHF - CQS measurements).
Acceptor interface trap states
from -type substrates
Donor interface trap states
from -type substrates
Non negligible interface trap state density
Relatively low interface trap state density region

## Slide 30: MOS Capacitor simulations
Non-Irradiated structures.
Measurements
Simulations
CHF
CQS

## Slide 31: MOS Capacitor simulations
Sensitivity analysis: effect of QOX and DIT.
Increase of DITA
Increase of QOX

## Slide 32: MOS Capacitor simulations
Irradiated structures.
Measurements
Simulations

## Slide 33: Outline
Motivations and background.
TCAD radiation damage modelling: discussion.
Simulation results and comparison with experimental data:
  - DC (steady-state) -> Diodes / Gate Controlled Diodes.
  - AC (small-signals) -> MOS Capacitors.
  - Time (transient) -> Multi-strip structures.
Conclusions.

## Slide 34
MultiStrips simulation: MIP response
Current responses to different impact locations.
MIP
MIP

## Slide 35
Transient analysis: Charge Collection
Measurements from Affolder et al., “Collected charge of planar silicon detectors …” NIM A, Vol. 623 (2010), pp. 177-179.
Charge collection: simulations vs. measurements at different biasing voltages (T = 248 K)

## Slide 36: Outline
Motivations and background.
TCAD radiation damage modelling: discussion.
Simulation results and comparison with experimental data:
  - DC (steady-state) -> Diodes / Gate Controlled Diodes.
  - AC (small-signals) -> MOS Capacitors.
  - Time (transient) -> Multi-strip structures.
Conclusions.

## Slide 37: The model
Surface damage (+ QOX)
Bulk damage
(1.61016 ÷ 2.21016 n/cm2)
(7.01015 ÷ 1.51016 n/cm2)
(up to 7.01015 n/cm2)
From DIT measurements
EC
EV
DITD
DITA
F. Moscatelli; D. Passeri; A. Morozzi; S. Mattiazzo; G. -F. Dalla Betta; M. Dragicevic; G. M. Bilei, Effects of Interface Donor Trap States on Isolation Properties of Detectors Operating at High-Luminosity LHC, IEEE Transactions on Nuclear Science, 2017, Vol. 64, Issue: 8, 2259 - 2267

## Slide 38: Conclusions
Modelling radiation damage effects is a hard task!
Radiation damage modelling scheme (bulk + surface), suitable for commercial TCAD tools (e.g. Synopsys Sentaurus).
Predictive capabilities extended to HL-LHC radiation damage levels (e.g. fluences > 2.0×1016 cm-2 1 MeV neutrons).
Further validation with experimental data comparisons -> model refinement.
Application to the optimization of (pixel) detectors (3D detectors, 2D planar detectors, …).