## Slide 1: Scintillators - Applications
Paul Lecoq
CERN, Geneva

## Slide 2: Outlook
Lecture 1: Scintillator fundamentals
  Organic scintillators
  Inorganic scintillators
    Scintillation mechanisms
    Limits to the light yield and decay time
    Energy resolution and non-proportionality
Lecture 2: Scintillator applications
  Crystal growth techniques
  High energy physics and dark matter searches
  Space borne missions
  Medical applications
  Geophysical exploration
  Homeland security

## Slide 3: What drives sthe devlopment of new scintillators

## Slide 4: HEP and PET use the largest volume of scintillators

## Slide 5: Various appelications of scintillators

## Slide 6: Back to Creation
Possible use of crystals
Notes: The goal of LHC is to understand the origin of the universe
As I am a partcle physicist I will start withan exemple of application of scintillators in particule physics
But at he end of my talk I will also show that scintillators are also used to understand the universe as it is today with space missions

## Slide 7: Limits of scintillator properties

## Slide 8: Most frequently used crystal growth technologies

## Slide 9: From principles to practice

## Slide 10: Continuous crystal growth

## Slide 11: Continuous crystal growth

## Slide 12: Continuous crystal growth

## Slide 13: Continuous crystal growth

## Slide 14: Preparation of large size plates for SPECT cameras
After growth the NaI:Tl crystal is cut and pressed at high temperature to prepare large area plates for SPECT cameras
Institute of Single Crystals
Kharkhov, Ukraine
NaI:Tl single crystal
520 mm,
mass > 550 kg

## Slide 15: NaI cylindrical detectors

## Slide 16: Micro-pulling-down crystal fiber growth
BGO
YAG:Ce
LYSO:Ce
YAP:Ce
F=400mm
F=1mm
F=2mm
F=2mm
Courtesy Fibercryst, Lyon
Notes: Production cost of small cross-section crystal pixel m,ay become prohibitive with standard production technologies. In particular the cost of surface treatment may become a dominant cost driver
Hole at the bottom of crucible, with a capillary. When the first drop of melt reaches the seed, the fiber is pulled down at an impressive speed several cm/mn compared to a few mm/hour

## Slide 17: Ceramics

## Slide 18: Crystal Calorimetry: a Powerful Tool for Particles Spectroscopy
50cm diameter spherical ball of NaI(Tl) crystals
672 crystals 42cm long, PMT readout
Very good resolution allowed precise spectroscopic study of charmonium states
Charmonium spectroscopy – Crystal Ball - SLAC

## Slide 19: CERN in Geneva area

## Slide 20: The Large Hadron Collider LHC
Lake of Geneva
Large Hadron Collider
27 km circumference
CMS
ATLAS
LHCb
ALICE
Mt Blanc

## Slide 21: Compact Muon Solenoid
4 T magnetic field
For a light Higgs (as suggested by present data)
Hγγ best channel. Narrow width, irreducible background:
ECAL resolution crucial !
Main CMS goal:
search for Higgs
and new physics
Length ~ 22 m
Diameter ~ 15 m
Weight ~ 14500 t

## Slide 22: Some popular crystals in HEP
Notes: Through the study and development of these crystals we have learned a lot
1- about fundamental mechanisms fro cross luminescent crystals, necessarily:
UV emitting
fast
low light yield
2- about Ce3+ as one of the most promising activator for fast scintillators
3- about mechanisms of energy relaxation in crystals (scintillation efficiency)
4- about the role of impurity and defects on:
scintillation efficiency
decay time (quenching and slow components)
Radiation hardness

## Slide 23: ECAL layout
barrel
Super Module
(1700 crystals)
endcap
supercystals
(5x5 crystals)
Pb/Si preshower
barrel cystals
EndCap “Dee”
3662 crystals
Barrel: || < 1.48
36 Super Modules
61200 crystals (2x2x23cm3)
EndCaps: 1.48 < || < 3.0
4 Dees
14648 crystals (3x3x22cm3)
PWO: PbWO4
about 10 m3, 90 t

## Slide 24: Production facilities in Bogoroditsk
159 Lazurit 3M growth ovens
12 low gradient annealing ovens

## Slide 25: Some important steps in radiation hardness progress
1994: Nb doping
  Suppress stable di-hole centres
  Suppress induced 620nm band
    MRS Proceedings Vol348 p99
    NIM A 365(1995) p291
1996: Y doping
  Suppress stable e- centre on Vo
  Suppress induced bands in visible
  1318: best crystal in test beam
    CMS LHCC 1996-146
1997: Stoechiometry tuning
  Suppress Vc and Vo centres
    CMS Note 1997/55
    Rad. Measurements Vol29, p27
1318

## Slide 26: Some important steps in radiation hardness progress
1997: More trivalent doping
  La, Lu, Y, Al
  Improves transmission and decay
  Improves Rad. hardness (see Y)
    Kobayashi for La: KEK 1997-12
    CMS Note 97/54, NIM A 402(1998) p75
1998: New raw material optimization +La codoping
  Factor 2 better than Nb or La
  No sign of drawback seen with La
    NIM letter to editor, snbmitted Sept 98
Front irradiation : 60Co 0.15Gy/h
Dose (Gy)

## Slide 27: PWO growth of large ingots
Replace 120mm Pt crucible by new 170mmcomposite Pt crucibles
Upgrade the Rf power cycle for heating, smelting, pulling and cooling
Optimization of procedure for crystal ingot extraction from crystallization unit
Notes: We wanted to grow larger size ingots (endcaps and higher productivity) but we had only 700kg Pt available

## Slide 28: Square end cut 85mm

## Slide 29: CMS Barrel

## Slide 30: CMS Endcaps
16 years of effort

## Slide 31: First results
π0 invariant mass
Events/15 MeV/c2
m(γγ) [GeV/c2]
Cosmics event

## Slide 32: And finally!!
H ➝ gg

## Slide 33: A different detector concept for precise jet calorimetry
A conventional approach is limited to about 60% - 70%/ √E
ALEPH resolution
New approaches have been proposed
Particule Flow for a 3D imaging calorimeter
  Each particle in a jet measured individually
  Requires very high granularity
  Limitations
    Complex Integration due to huge number of channels
    Identification of individual particles in a jet challenging at very high energy
Dual readout method
  Measure event by event the electromagnetic fraction of the hadronic shower by separating Cerenkov and scintillation light
ILC goal

## Slide 34
UV excitation
Some crystal fibers
YAG and LuAG up to 2m
BGO ( : from 0.6 mm to 3 mm ; Length up to 30 cm)
LYSO:Ce ( : from 0.6 mm to 3 mm ; Length up to 20 cm)

## Slide 35
Dual readout based on Metamaterials
Select a non-intrinsic scintillating material (unlike BGO or PWO) with high bandgap for low UV absorption
The undoped host will behave as an efficient Cerenkov: heavy material, high refraction index n, high UV transmission
Cerium or Praesodinum doped host will act as an efficient and fast scintillator
  ≈ 60ns decay for Ce
  ≈ 20ns decay for Pr
SiPMTs
MOEMS diffractive optics
light concentrator
MOEMS diffractive optics
light concentrator
SiPMTs
LuAG is an excellent candidate
Ce doped LuAG
undoped LuAG
30cm
Ø 2mm
Fibercryst
Energy Resolution
12%
Scintillating fibers bundle
undoped fibers bundle
Decay time

## Slide 36
Evidence of Dark Matter
Rotation curve of spiral galaxies
Direct detection - elastic scattering off nuclei
Features:
1. Low energy → Low energy threshold (~10 keV)
2. Expected event rate < 0.1/kg day
L.Bergstrom Rep.Progr.Phys.63 (2000) 793
V=(GM/r)1/2
M~0.3 X~0.7
Detector mass 1kg-100 kg
High radiopurity of detector
and construction materials
Underground location
Background rejection
WIMP-Dark matter searches

## Slide 37: Why cryogenic scintillator? CREST detector
Sensitivity + Selectivity
high-energy resolution of cryogenic phonon detector + discrimination of events with low detection threshold (≤10 keV)
WIMP
W-thermometer (phonon detector)
light detector
Reflector
Crystal
Phonons
Light
P.Meunier et al, Appl.Phys.Let 75 (1999) 1335
b+g
neutrons

## Slide 38
high light yield at low temperatures
  low threshold,
  good energy resolution
Radiopurity (ex Lu, Rb, K, U, Th)
Suitable thermodynamics characteristics
Possible candidates
  CaWO4 – satisfactory choice, currently in use, large ongoing effort to improve the material
  ZnWO4 – scintillator under development for cryogenic application
  CaMoO4 and CdMoO4– material under investigation
Scintillator requirements

## Slide 39
Scintillation Detectors on
Space Missions

## Slide 40
Important Projects for Gamma Astrophysics
Parameter | EGRET | GLAST (Minimum Spec.)
Energy Range | 20 MeV - 30 GeV | 20 MeV – 300 GeV
Peak Effective Area1 | 1500 cm2 | >8000 cm2
Field of View | 0.5 sr | >2 sr
Angular. Resolution2 | 5.8° (100 MeV) | <3.5° (100 MeV) <0.15° (>10 GeV)
Energy Resolution1 | 10% | <10%
Deadtime per Event | 100 ms | <100 s
Source Location Determination4 | 15' | <0.5'
Point Source Sensitivity5 | -І x 10–7cm–2 s–1 | <6 x 10–9 cm–2 s–1
EGRET – Energetic Gamma Ray Experiment Telescope
GLAST – Gamma Ray Large Area Space Telescope

## Slide 41
EGRET on Compton GRO (1991-2000)
GLAST Large Area Telescope (2006-2015)
EGRET versus GLAST
NaI
CsI

## Slide 42
The BepiColombo Mercury mission

## Slide 43
History- LaBr3 development program

## Slide 44: Scintillators in nuclear medicine
High detection efficiency for different type of radiations, particularly -rays
Good energy resolution
Very good timing
High counting rate capability
Great variety in size and composition

## Slide 45: SPECT principle Spatial resolution

## Slide 46: SPECT requires large size crystals

## Slide 47
PET data acquisition
e+
Positron range (r)
Acolinearity
(α D)
e+
e-
e+
Neutron-deficient
isotope
p
p
p
p
p
p
n
n
n
n
p
n
Parallel projections
Projection
f
s
PET data (sinograms)
s
z
f
f
18FDG
injection
PET images
z
x
Reconstruction
2t
Coincidences
n
(6p; 5n)➔(5p; 6n)
PET Principles
Notes: Neutron defficient isdotope, for instance 18F, attached to a molecule involved in some metabolic process we want to study. Very often this is FDG, easily fixed in cancer cells and inflamatory areas.
PET is a fantastic tool to see organs at work.

## Slide 48: Scintillators for PET
Density (g/cm3)
Atomic number
Photofraction
Decay time (ns)
Light output (h/MeV)
Peak emission (nm)
Refraction index
7.13
75
0.35
300
8200
480
2.15
7.40
66
0.32
35-45
27000
420
1.82
NaI BGO GSO:Ce LSO:Ce LuAP:Ce LaBr3:Ce LuAG:Ce
3.67
51
0.17
230
43000
415
1.85
6.71
59
0.25
30-60
12500
430
1.85
8.34
65
0.30
17
11400
365
1.97
6.73
63
0.30
60
>25000
535
1.84
5.29
47
0.13
18
70000
356
1.88
Scintillators for PET
1962
1977
1995
1999
2001
2007
2003
Notes: Better timing requires faster crystals with high LY

## Slide 49
incorrect LOR
Depth-of-interaction
(DOI) information is
needed to maintain good resolution at off-centre positions
Spatial Resolution -
Depth-of-interaction
DOI
Parallax error in PET

## Slide 50
Lu2SiO5:Ce
LuAlO3:Ce
LuAlO3:Ce
Lu2SiO5:Ce
APD array
or
multi-anode PMT
columns
Phoswich configuration in PET
Different response
time and/or
wavelength
DOI

## Slide 51: The AXPET concept
2.5 to 4mm FWHM position resolution for 10cm long crystals
Depending on surface state and wrapping conditions

## Slide 52
Detector B
Detector A
e-
e+
Patient
tA
tB
Dt = tA – tB = [(d+d1) – (d-d1)]/c
d1 = c Dt/2
d
d1
Time of Flight PET
dt (ps)
10
100
300
500
dx (cm)
SNR*
0.15
1.5
4.5
7.5
16
5.2
3.0
2.3
* SNR gain for 40 cm phantom
SNRTOF = √(2D/cDt) · SNRconv
10ps TOF resolution
dx = 1.5mm
SNRTOF/SNRCONV= 16!
State-of-the-art
Notes: But there is also a request for good timing resolution for another important application of scintillating crystals. PET scanners.

## Slide 53
Scintillators for Geophysical Exploration

## Slide 54
Oil Well Logging
Neutron/Gamma
generator
Shielding
Near detector
Far detector

## Slide 55
Nuclear Tools

## Slide 56
Desirable Scintillator Properties
LuAP ?

## Slide 57
Homeland security

## Slide 58
Passive instrumentation

## Slide 59
Active Instrumentation

## Slide 60
Border control

## Slide 61: Conclusion 1
Scintillators are widely used in a large number of scientific and industrial domains
The ideal scintillator does not exist and research should continue on new materials and new production technologies (micro-pulling down)
Structuring at the nanoscale gives access to quantum confinment phenomena and increases the range of optical electric and magnetic properties that can be engineered
Metamaterials based on quantum dots, photonic crystals and photonic crystal fibers can open the way to new detection paradigms with huge design flexibility

## Slide 62: Conclusion 2
A number of good scintillators have been discovered that have proved difficult to manufacture – e.g. LuPO4:Ce
An alternative approach is to start with materials of known manufacturability, and improve the scintillation properties – e.g. PWO, YAG, GGG
“One of the continuing scandals in the physical sciences is that it remains in general impossible to predict the structure of even the simplest crystalline solids from a knowledge of their chemical composition.” John Maddox, editor of Nature (1988)
Not true anymore!!!

## Slide 63: PWO: The Problem to be solved
Historical background
  Lead Tungstate (PbWO4) first time introduced as material for HEP in 92 at CRYSTAL 2000 Chamonix conference by Nagornaya (Kharkhov) and Katchanov (IHEP)
  Crystal Clear collaboration at CERN initiated a worldwide R&D effort since 92
  First growth technology developed by INP Minsk and Kharkhov and transferred to Bogoroditsk at the end of 92
  PbWO4 chosen as ECAL baseline by CMS in Oct 94
Challenging problem: How to
  technically develop
  Install production infrastructure
  Mass produce 76’000 crystals (11 m3, 90 tons)
in about 10 years
at an affordable price for European tax payers

## Slide 64: PWO: The solution to the problem
Take advantage of the large effort made in the field of crystallography during the cold war in former Soviet Union, which resulted in
  Availability of many highly skilled people
    Academic experts in all the fields related to crystallography
    Excellent technologists
  Impressive crystal growth infrastructure installed in several plants, to produce large quantities of crystals for military applications
Once this situation has been understood and correctly evaluated, we have
  Selected the Bogoroditsk Techno-Chemical Plant after an audit of several companies
  Started a fruitful collaboration with ISTC

## Slide 65: PWO: The 4 phases of the project (1 & 2)
Technology development phase- CERN-ISTC
Project #354b from July 99 to July 2000
1.3M$ CERN + 1.3M$ ISTC
Implement a production technology to mass produce PbWO4 crystals with a consistent
quality at an affordable price
6000 preproduction crystals
R&D phase- CERN-ISTC
Project #354 from July 96 to July 98
350K$ CERN + 350K$ ISTC
Demonstrate that PbWO4 crystals could
reach the level of performance imposed
by the very challenging requirements of our experiment

## Slide 66: PWO: The 4 phases of the project (3 & 4)
Implementation of a modern industrial culture
CERN-ISTC Partnership #1718: 8.7M$ CERN
30’000 barrel crystals from Aug. 2000 to end 2004
On the basis of a sizable fraction of CMS needs
    organize a modern managerial structure
    implement a Quality Assurance policy
    install modern communication tools
    develop a Marketing strategy
Towards commercial contracts
Implementation of a new technology for large ingots
Allows endcap crystals (larger) to be grown
Allows higher productivity for barrel and endcaps
CERN-ETHZ contract for 26’000 barrel crystals and 16’000 endcap crystals
Last crystal delivered in February 2008

## Slide 67
Monolithic scintillation detectors
GEANT4 Monte Carlo simulation of an LSO block read out by two APD arrays.
A small fraction of the optical photons produced by the absorption of a 511 keV annihilation photon is shown.
APD arrays
LSO
511 keV gamma photon
DOI by light distribution

## Slide 68: BrainPET insert detectors
4 rings (ø=40 cm, H= 4x18.6 mm) with 52 detector modules each
Dual layer of trapezoidal LSO blocks and two APDs per block
Dedicated ASIC summing preamplifier (64 inputs, 16 summed outputs, 1 total energy sum, < 1000 e- rms noise per sum channel)
Complete MRI compatibility is not the main goal but it gives us some first experience in designing MR compatible PET technology for future version.
Current CCC project (Jülich, Ciemat, VUB)

## Slide 69: From EGRET to GLAST
Telescope resolution is a core to identify the sources
ERGET (Phases 1-5)
GLAST Sky Survey

## Slide 70
ClearPET®, small animal PET Crystal Clear Collaboration
8cm
20cm
phoswich with 2 crystals LYSO and LuYAP
each crystal is 2 x 2 x 10mm
80 PM with 64 photocathodes each
Spatial resolution 1.5 mm at centre