## Slide 1: SEY measurements of the arc 1-2 removed-magnet beam screen
Valentine Petit 05.04.2017

## Slide 2: Outline
Global configuration and aim of the study
Characterisation techniques
Analysed components
Results
Conclusions and perspectives
LHC Machine Committee 05.04.2017

## Slide 3: Global configuration and aim of the study
Dipole A31L2
V1
V2
04.01.17
  Nitrogen venting
  Filtered air (RF ball)
10.01.17
  Dipole extraction
Dipole
Quadrupole
Investigate surface modifications due to exposure to the e-cloud in the machine
Secondary Electron Yield reduction (conditioning)
Surface chemistry modification
Air exposure : deconditioning

## Slide 4: Characterisation techniques
SEY measurements
+
Dose received by the sample during a measurement : 10-7 C/mm² (no conditioning effect)
Reproducibility (twice the same point) : ± 0.02
Reproducibility (day by day) : ± 0.05

## Slide 5: Characterisation techniques
Conditioning in laboratory
Irradiation by electrons
Ep = 250 eV
SEY measurement
Follow up of maximum SEY versus irradiation dose
Chart: LHC Beam screen, Top side
| 82 | 132 | 182 | 232 | 282 | 332 | 382 | 432 | 482 | 532 | 582 | 632 | 682 | 732 | 782 | 832 | 882 | 932 | 982 | 1032 | 1082 | 1132 | 1182 | 1232 | 1282 | 1332 | 1382 | 1432 | 1482 | 1532 | 1582 | 1632 | 1682 | 1732
Extracted from the LHC | 1.3433 | 1.5538 | 1.6347 | 1.6627 | 1.6632 | 1.6457 | 1.6177 | 1.5836 | 1.5457 | 1.5078 | 1.4715 | 1.4364 | 1.4051 | 1.3767 | 1.3503 | 1.3229 | 1.3002 | 1.2809 | 1.2633 | 1.2467 | 1.2302 | 1.2138 | 1.1974 | 1.1812 | 1.1655 | 1.1506 | 1.1376 | 1.1253 | 1.1143 | 1.1034 | 1.0926 | 1.0817 | 1.0712 | 1.0611
Fully conditioned in laboratory | 0.76447 | 0.91758 | 0.99832 | 1.0403 | 1.06 | 1.0673 | 1.0648 | 1.0577 | 1.0469 | 1.0348 | 1.0214 | 1.0082 | 0.99491 | 0.98188 | 0.96897 | 0.95676 | 0.94437 | 0.93162 | 0.91872 | 0.90573 | 0.89307 | 0.88073 | 0.86897 | 0.85793 | 0.84784 | 0.83833 | 0.83003 | 0.82288 | 0.81642 | 0.81029 | 0.80381 | 0.7969 | 0.78966 | 0.78169

## Slide 6: Characterisation techniques
Chart: XPS Spectra, Al Kα (1486.6 eV)
chemical environment
specific for each element
X-Ray photoelectron spectroscopy
Analysis of surface chemical composition
  Probed thickness : few nm
Irradiation with photons E = 1486.6 eV
Emission of photoelectrons
Cu 2p
O 1s
O KLL
Cu LMM
C 1s
Cu 3s
Cu 3p
C KVV
N KLL
N 1s

## Slide 7: Analysed components
Beam screen
Pumping slot shield
Transition tube (Dipole – Quadrupole)
Transition tube (copper)
  magnetic field free region
Beam screen (colaminated copper on stainless steel)
  Looking for SEY differences due to electron confinement and synchrotron radiations
Pumping slot shield (copper – beryllium alloy)
  Looking for SEY differences due to masking by beam screen
Sawtooth side
Top side
Bottom
Welding side

## Slide 8: Transition tube
Chart: Maximum SEY versus azimuthal position
| -25.5 | -15.3 | -5.0999999999999996 | 5.0999999999999996 | 15.3 | 25.5 | 64.5 | 73 | 81.5 | 90 | 98.5 | 107 | 115.5 | -64.5 | -73 | -81.5 | -90 | -98.5 | -107 | -115.5 | -154.5 | -163 | -171.5 | 180 | 171.5 | 163 | 154.5
 | 2.0167 | 1.9807 | 2.0288 | 2.0481 | 1.9896 | 1.9941 | 1.9914 | 2.0767 | 2.3663 | 2.1699 | 2.15 | 1.9683 | 1.9196 | 1.9267 | 1.9445 | 1.9333 | 1.92 | 1.9977 | 1.9212 | 1.9027 | 2.0174 | 1.9576 | 2.0383 | 1.9648 | 2.1111 | 2.2059 | 2.3354
-90°
0
90°
±180°
No difference between 0°/180° and ±90° positions
Fully conditioned + 3 weeks air exposed sample: lowest possible limit

## Slide 9: Beam Screen : A31L2 magnet
No difference between flat sides / welding side in spite of dipole field
Distance from beam screen extremity
Chart: Azimuthal position (degree)
| 33 | 29.6 | 25.9 | 22 | 18 | 13.7 | 9.1999999999999993 | 4.5999999999999996 | 0 | -4.5999999999999996 | -9.1999999999999993 | -13.7 | -18 | -22 | -25.9 | -29.6 | -33 | -36 | 141 | 130 | 118.3 | 107.5 | 95.7 | 84.3 | 73 | 61.7 | 50.4 | 39.1 | -147 | -150 | -154.1 | -158 | -162 | -166.3 | -170.8 | -175.4 | 180 | 175.4 | 170.8 | 166.3 | 162 | 158 | 154.1 | 150.4 | 147 | 144 | -38.9 | -48.2 | -57.5 | -66.75 | -76.099999999999994 | -85.3 | -94.7 | -104 | -113.3 | -122.6 | -132 | -141.19999999999999
3.5 cm | 1.739 | 1.794 | 1.8174 | 1.7935 | 1.7971 | 1.8079 | 1.8159 | 1.8194 | 1.7988 | 1.837 | 1.849 | 1.8356 | 1.84 | 1.8358 | 1.825 | 1.8322 | 1.8557 | 1.8228 | 1.9652 | 2.0298 | 1.7844 | 1.7347 | 1.8023 | 1.8409 | 1.7446 | 1.7969 | 1.8117 | 1.7808 | 1.6727 | 1.7324 | 1.7944 | 1.8473 | 1.8331 | 1.8395 | 1.8382 | 1.807 | 1.8029 | 1.7948 | 1.814 | 1.8227 | 1.7967 | 1.8147 | 1.8077 | 1.9082 | 1.8547 | 1.8151 | 1.7261 | 1.7446 | 1.7236 | 1.7037 | 1.6921 | 1.7765 | 1.684 | 1.6573 | 1.7587 | 1.7701 | 1.7407 | 1.7401
15 cm | 1.6776 | 1.6987 | 1.6952 | 1.6823 | 1.6928 | 1.6862 | 1.6864 | 1.6681 | 1.6425 | 1.679 | 1.755 | 1.6935 | 1.7017 | 1.6737 | 1.7037 | 1.7104 | 1.6896 | 1.6977 | 1.6674 | 1.6745 | 1.6791 | 1.6635 | 1.7464 | 1.7219 | 1.6499 | 1.7437 | 1.7152 | 1.6689 | 1.7731 | 1.7769 | 1.7392 | 1.7485 | 1.7571 | 1.7481 | 1.8096 | 1.7599 | 1.7054 | 1.7127 | 1.6966 | 1.7257 | 1.7145 | 1.71 | 1.7055 | 1.7006 | 1.6931 | 1.6508 | 1.6942 | 1.7369 | 1.7305 | 1.7278 | 1.6969 | 1.6189 | 1.6125 | 1.6565 | 1.7058 | 1.7066 | 1.7046 | 1.7243
215 cm | 1.5794 | 1.5597 | 1.5652 | 1.5766 | 1.5827 | 1.5958 | 1.588 | 1.5856 | 1.5894 | 1.6478 | 1.7305 | 1.5722 | 1.6608 | 1.6985 | 1.6776 | 1.6344 | 1.6287 | 1.673 | 1.6569 | 1.6112 | 1.6598 | 1.8256 | 1.6634 | 1.6171 | 1.6666 | 1.6107 | 1.6285 | 1.6191 | 1.6055 | 1.5816 | 1.6526 | 1.6391 | 1.6485 | 1.6302 | 1.6316 | 1.6483 | 1.7172 | 1.6755 | 1.6391 | 1.622 | 1.6202 | 1.6045 | 1.5982
230 cm | 1.6905 | 1.6796 | 1.6773 | 1.6757 | 1.6988 | 1.6725 | 1.7088 | 1.7059 | 1.7054 | 1.7381 | 1.822 | 1.6765 | 1.7463 | 1.7573 | 1.7969 | 1.7586 | 1.725 | 1.714 | 1.7101 | 1.6992 | 1.7197 | 1.6603 | 1.7379 | 1.7425 | 1.7169 | 1.729 | 1.6635 | 1.698 | 1.9989 | 2.0118 | 1.8705 | 1.7707 | 1.6874 | 1.709 | 1.6837 | 1.6842 | 1.6735 | 1.6598 | 1.6689 | 1.7095 | 1.7213 | 1.6626 | 1.6578 | 1.6521 | 1.6372 | 1.6396 | 1.7939 | 1.6801 | 1.6439 | 1.6366 | 1.5393 | 1.5751 | 1.5644 | 1.5154 | 1.6267 | 1.6287 | 1.6147 | 1.7274
Top side
Sawtooth side
Welding side
Bottom
Side
NB : ranking of SEY of samples does not correspond to chronology of measurements

## Slide 10: Beam Screen : A31L2 magnet
Maximum SEY below « not installed » beam screen
Distance from beam screen extremity
Chart: Azimuthal position (degree)
| 33 | 29.6 | 25.9 | 22 | 18 | 13.7 | 9.1999999999999993 | 4.5999999999999996 | 0 | -4.5999999999999996 | -9.1999999999999993 | -13.7 | -18 | -22 | -25.9 | -29.6 | -33 | -36 | 141 | 130 | 118.3 | 107.5 | 95.7 | 84.3 | 73 | 61.7 | 50.4 | 39.1 | -147 | -150 | -154.1 | -158 | -162 | -166.3 | -170.8 | -175.4 | 180 | 175.4 | 170.8 | 166.3 | 162 | 158 | 154.1 | 150.4 | 147 | 144 | -38.9 | -48.2 | -57.5 | -66.75 | -76.099999999999994 | -85.3 | -94.7 | -104 | -113.3 | -122.6 | -132 | -141.19999999999999
3.5 cm | 1.739 | 1.794 | 1.8174 | 1.7935 | 1.7971 | 1.8079 | 1.8159 | 1.8194 | 1.7988 | 1.837 | 1.849 | 1.8356 | 1.84 | 1.8358 | 1.825 | 1.8322 | 1.8557 | 1.8228 | 1.9652 | 2.0298 | 1.7844 | 1.7347 | 1.8023 | 1.8409 | 1.7446 | 1.7969 | 1.8117 | 1.7808 | 1.6727 | 1.7324 | 1.7944 | 1.8473 | 1.8331 | 1.8395 | 1.8382 | 1.807 | 1.8029 | 1.7948 | 1.814 | 1.8227 | 1.7967 | 1.8147 | 1.8077 | 1.9082 | 1.8547 | 1.8151 | 1.7261 | 1.7446 | 1.7236 | 1.7037 | 1.6921 | 1.7765 | 1.684 | 1.6573 | 1.7587 | 1.7701 | 1.7407 | 1.7401
15 cm | 1.6776 | 1.6987 | 1.6952 | 1.6823 | 1.6928 | 1.6862 | 1.6864 | 1.6681 | 1.6425 | 1.679 | 1.755 | 1.6935 | 1.7017 | 1.6737 | 1.7037 | 1.7104 | 1.6896 | 1.6977 | 1.6674 | 1.6745 | 1.6791 | 1.6635 | 1.7464 | 1.7219 | 1.6499 | 1.7437 | 1.7152 | 1.6689 | 1.7731 | 1.7769 | 1.7392 | 1.7485 | 1.7571 | 1.7481 | 1.8096 | 1.7599 | 1.7054 | 1.7127 | 1.6966 | 1.7257 | 1.7145 | 1.71 | 1.7055 | 1.7006 | 1.6931 | 1.6508 | 1.6942 | 1.7369 | 1.7305 | 1.7278 | 1.6969 | 1.6189 | 1.6125 | 1.6565 | 1.7058 | 1.7066 | 1.7046 | 1.7243
215 cm | 1.5794 | 1.5597 | 1.5652 | 1.5766 | 1.5827 | 1.5958 | 1.588 | 1.5856 | 1.5894 | 1.6478 | 1.7305 | 1.5722 | 1.6608 | 1.6985 | 1.6776 | 1.6344 | 1.6287 | 1.673 | 1.6569 | 1.6112 | 1.6598 | 1.8256 | 1.6634 | 1.6171 | 1.6666 | 1.6107 | 1.6285 | 1.6191 | 1.6055 | 1.5816 | 1.6526 | 1.6391 | 1.6485 | 1.6302 | 1.6316 | 1.6483 | 1.7172 | 1.6755 | 1.6391 | 1.622 | 1.6202 | 1.6045 | 1.5982
230 cm | 1.6905 | 1.6796 | 1.6773 | 1.6757 | 1.6988 | 1.6725 | 1.7088 | 1.7059 | 1.7054 | 1.7381 | 1.822 | 1.6765 | 1.7463 | 1.7573 | 1.7969 | 1.7586 | 1.725 | 1.714 | 1.7101 | 1.6992 | 1.7197 | 1.6603 | 1.7379 | 1.7425 | 1.7169 | 1.729 | 1.6635 | 1.698 | 1.9989 | 2.0118 | 1.8705 | 1.7707 | 1.6874 | 1.709 | 1.6837 | 1.6842 | 1.6735 | 1.6598 | 1.6689 | 1.7095 | 1.7213 | 1.6626 | 1.6578 | 1.6521 | 1.6372 | 1.6396 | 1.7939 | 1.6801 | 1.6439 | 1.6366 | 1.5393 | 1.5751 | 1.5644 | 1.5154 | 1.6267 | 1.6287 | 1.6147 | 1.7274
Top side
Sawtooth side
Welding side
Bottom
Side
Not installed beam screen

## Slide 11: Beam Screen : comparison LHC A31L2 and “not installed”
Conditioning at Ep = 250 eV
Room temperature
Base pressure P = 2.10-9 mbar
Error bars : dispersion over 4 measurement points
LHC beam screen samples
  Identical conditioning path for both samples
  Ultimate limit δmax = 1.05
LHC versus «not installed » beam screen
  extracted LHC beam screen needs a lower dose to reach δmax =1.35 (threshold for e-cloud in dipole) than « not installed » one
Chart: Conditioning
| 9.9999999999999995E-8 | 9.6466431095406345E-6 | 3.8586572438162538E-5 | 9.6466431095406356E-5 | 1.9293286219081271E-4 | 6.7526501766784449E-4 | 9.6466431095406345E-4 | 2.8939929328621905E-3 | 9.6466431095406351E-3 | 3.4911660777385153E-2 | 8.2911660777385154E-2
LHC_BeamScreen_A | 1.6662 | 1.4693 | 1.323 | 1.2353 | 1.1517 | 1.0906 | 1.0857 | 1.0761 | 1.0666 | 1.0625 | 1.0627
LHC_BeamScreen_B | 1.7197 | 1.525 | 1.3692 | 1.2641 | 1.1812 | 1.0849 | 1.0809 | 1.0644 | 1.0537 | 1.0487 | 1.0522 | 1.0485 | 1.046
Not installed beam screen | 1.8912 | 1.6351 | 1.4937 | 1.367 | 1.2363 | 1.1154 | 1.099 | 1.0626 | 1.051 | 1.0547 | 1.0656 | 1.0768 | 1.0782 | 1.0789
9 days air exposed

## Slide 12: Beam Screen : comparison LHC A31L2 and “not installed”
Chart: XPS : Cu 2p peak
Cu(OH)2
Cu/Cu2O
LHC beam screen : intermediate Cu 2p peak shape between « not installed » and deconditioned beam screen

## Slide 13: Pumping Slot Shield
Dark traces
    Low SEY regions
Out of dark traces
    High SEY regions
Dark traces corresponding to pumping slot shield shape and spacing
10 mm
As received
10 mm
26h at 120°C
Baked to enhance colour contrast
Chart: Maximum SEY versus longitudinal position
| 0 | 1.5 | 3 | 4.5 | 6 | 7.5 | 9 | 10.5 | 12 | 13.5 | 15 | 16.5 | 18 | 19.5 | 21 | 22.5 | 24 | 25.5 | 27 | 28.5 | 30 | 31.5 | 33 | 34.5 | 36
 | 1.9901 | 2.076 | 1.9331 | 1.889 | 1.8623 | 1.9069 | 1.9775 | 1.9692 | 1.9762 | 1.9844 | 2.0113 | 1.9145 | 1.7823 | 1.7871 | 1.8901 | 1.8629 | 1.9762 | 1.9668 | 1.9622 | 1.9462 | 1.8786 | 1.8183 | 1.8163 | 1.8137 | 1.9142

## Slide 14: Pumping Slot Shield
Chart: Maximum SEY versus longitudinal position
| 0 | 1.5 | 3 | 4.5 | 6 | 7.5 | 9 | 10.5 | 12 | 13.5 | 15 | 16.5 | 18 | 19.5 | 21 | 22.5 | 24 | 25.5 | 27 | 28.5 | 30 | 31.5 | 33 | 34.5 | 36
 | 1.9901 | 2.076 | 1.9331 | 1.889 | 1.8623 | 1.9069 | 1.9775 | 1.9692 | 1.9762 | 1.9844 | 2.0113 | 1.9145 | 1.7823 | 1.7871 | 1.8901 | 1.8629 | 1.9762 | 1.9668 | 1.9622 | 1.9462 | 1.8786 | 1.8183 | 1.8163 | 1.8137 | 1.9142
Dark traces
  Low SEY regions
  Compatible with “deconditioned” state
Out of dark traces
  High SEY regions
  same δmax as “clean” material
Cleaned
Cleaned + cond. + air exposed 1 week
Dark traces corresponding to pumping slot shield shape and spacing
10 mm
As received
10 mm
26h at 120°C
Baked to enhance colour contrast

## Slide 15: Pumping Slot Shield
Chart: XPS : Cu 2p peak
Cu(OH)2
Cu/Cu2O
Chart: Maximum SEY versus normalized intensity of Cu2p at 934.8 eV
| 0.55287801852785012 | 0.90404043830783354 | 0.50000305842197668 | 0.99650937030968145 | 0.98216879672694835 | 0.65929295591029491 | 0.49093403316235235 | 0.85147871508238937 | 0.49169831085504773 | 0.46451899343808334 | 0.40761233994608242
 | 1.7823 | 1.9622 | 1.8163 | 1.9762 | 1.9775 | 2.0113 | 1.8901 | 1.9762 | 1.8786 | 1.8623 | 1.9331
In dark traces
  SEY measurements
  Cu 2p peak
  Parts exposed to e-cloud : conditioned
δmax : low SEY regions versus high SEY regions
Cu 2p peak : high Cu(OH)2 versus low Cu(OH)2 peak
  Parts exposed to e-cloud : conditioned

## Slide 16: Conclusions
Transition tube
  Uniform SEY in azimuth
Beam screen :
  Uniform SEY in azimuth
  Maximum SEY globally lower than “not installed” beam screen
      → compatible with a partial conditioning state in the machine
Pumping slot shield
  zones presenting the memory of conditioning

## Slide 17: Perspectives
  Influence of the conditioning level reached on the SEY value observed after air exposure (deconditioning)
  Analysis of V2 beam screen
  More statistics on the sawtooth extracted from the A31L2 magnet
  Long-term : conditioning at low temperature

## Slide 18: Acknowledgments
M. Taborelli, E. Garcia-Tabares, H. Neupert, P. Garritty, H. Kos, N. Kos, H. Rambeau, G. Bregliozzi, P. Maurin, V. Baglin, P. Chiggiato

## Slide 19
Thank you

## Slide 20: Spares

## Slide 21: Transition tube
Plug-In Module
As received : δmax = 1.84
Fully conditioned : δmax = 1.09
Deconditioned 3 weeks : δmax = 1.58
Fully reconditioned : δmax = 1.09
Chart: Conditioning
| 9.9999999999999995E-8 | 9.6466431095406345E-6 | 3.8586572438162538E-5 | 9.6466431095406356E-5 | 1.9293286219081271E-4 | 6.7526501766784449E-4 | 9.6466431095406345E-4 | 2.8939929328621905E-3 | 9.6466431095406351E-3 | 3.4911660777385153E-2 | 5.8500000000000003E-2 | 7.6200000000000004E-2 | 0.20619999999999999 | 0.2747
Conditioning | 1.8361 | 1.6334 | 1.4435 | 1.2662 | 1.2233 | 1.191 | 1.1844 | 1.1568 | 1.1249 | 1.1043 | 1.0961 | 1.0913 | 1.092 | 1.088
Reconditioning | 1.5808 | 1.3627 | 1.2613 | 1.1752 | 1.144 | 1.117 | 1.1197 | 1.1075 | 1.096 | 1.0875 | 1.0895
Conditioning at Ep = 250 eV
Base pressure P = 2.10-9 mbar
Error bars : dispersion over 4 measurement points

## Slide 22: Transition tube
Plug-In Module
Conditioning :
Shift to lower binding energy
Remove bump at 288.5 eV

## Slide 23: Beam Screen : A31L2 magnet
Chart: Average maximum SEY
| 33 | 29.6 | 25.9 | 22 | 18 | 13.7 | 9.1999999999999993 | 4.5999999999999996 | 0 | -4.5999999999999996 | -9.1999999999999993 | -13.7 | -18 | -22 | -25.9 | -29.6 | -33 | -36 | 141 | 130 | 118.3 | 107.5 | 95.7 | 84.3 | 73 | 61.7 | 50.4 | 39.1 | -147 | -150 | -154.1 | -158 | -162 | -166.3 | -170.8 | -175.4 | 180 | 175.4 | 170.8 | 166.3 | 162 | 158 | 154.1 | 150.4 | 147 | 144 | -38.9 | -48.2 | -57.5 | -66.75 | -76.099999999999994 | -85.3 | -94.7 | -104 | -113.3 | -122.6 | -132 | -141.19999999999999
 | 1.6716 | 1.683 | 1.6888 | 1.682 | 1.6928 | 1.6906 | 1.6998 | 1.6947 | 1.684 | 1.7255 | 1.7892 | 1.6945 | 1.7372 | 1.7413 | 1.7508 | 1.7339 | 1.7247 | 1.7269 | 1.7809 | 1.8012 | 1.71 | 1.6674 | 1.7366 | 1.7827 | 1.6937 | 1.7217 | 1.7142 | 1.7159 | 1.7638 | 1.7874 | 1.7558 | 1.743 | 1.7148 | 1.7373 | 1.7427 | 1.7249 | 1.703 | 1.6997 | 1.707 | 1.7438 | 1.727 | 1.7066 | 1.6982 | 1.7203 | 1.6974 | 1.6759 | 1.7381 | 1.7206 | 1.6993 | 1.6893 | 1.6428 | 1.6568 | 1.6203 | 1.6098 | 1.6971 | 1.7018 | 1.6866 | 1.7306

## Slide 24: Beam Screen : A31L2 magnet
Chart: Carbon relative concentration
| 33 | 29.6 | 25.9 | 22 | 18 | 13.7 | 9.1999999999999993 | 4.5999999999999996 | 0 | -4.5999999999999996 | -9.1999999999999993 | -13.7 | -18 | -22 | -25.9 | -29.6 | -33 | -36 | 141 | 130 | 118.3 | 107.5 | 95.7 | 84.3 | 73 | 61.7 | 50.4 | 39.1 | -147 | -150 | -154.1 | -158 | -162 | -166.3 | -170.8 | -175.4 | 180 | 175.4 | 170.8 | 166.3 | 162 | 158 | 154.1 | 150.4 | 147 | 144 | -38.9 | -48.2 | -57.5 | -66.75 | -76.099999999999994 | -85.3 | -94.7 | -104 | -113.3 | -122.6 | -132 | -141.19999999999999
3.5 cm | 25.9997 | 26.9347 | 28.5662 | 23.21 | 24.6162 | 24.686 | 29.0123 | 36.4897 | 32.2365 | 28.2715 | 25.8614 | 26.2004 | 30.4962 | 26.1362 | 27.8349 | 30.4313 | 33.8862 | 31.4958 | 31.9203 | 32.4757 | 27.1771 | 31.6042 | 36.8685 | 38.3455 | 33.2515 | 28.294
15 cm | 30.0959 | 31.1146 | 31.7666 | 27.0578 | 27.8202 | 28.4201 | 35.6322 | 29.8249 | 30.254 | 25.4995 | 26.2058 | 28.748 | 27.3983 | 31.8778 | 30.8118 | 29.6562 | 34.6799 | 34.141 | 33.9218 | 33.0344 | 30.8233 | 36.2687 | 48.6313 | 38.3691 | 30.2031 | 34.3315
215 cm | 32.7075 | 31.4607 | 30.4434 | 26.1839 | 22.9305 | 26.7972 | 20.8138 | 24.9368 | 25.8155 | 22.8566 | 35.4667 | 30.3516 | 28.6158 | 26.8839 | 28.2962 | 30.0346 | 32.1477
230 cm | 31.0242 | 36.919 | 28.3251 | 23.0282 | 27.8927 | 26.7982 | 32.4142 | 26.879 | 26.5272 | 21.865 | 24.9602 | 32.2684 | 43.1453 | 35.4565 | 28.0268 | 30.2189 | 34.6015 | 30.9095 | 33.2952 | 50.2832 | 45.8395 | 35.1531 | 44.405

## Slide 25: Heat load
G.Iadarola

## Slide 26: Magnetic field
Chart: z [mm]
magnetic length starts | -200 | 200
magnetic length ends | -200 | 200
Yoke starts | -200 | 200
Yoke ends | -200 | 200
Pad starts | -200 | 200
Pad ends | -200 | 200
Conductors starts | -200 | 200
Conductor ends | -200 | 200
Magnetic Yoke
Magnetic Length
Coil Length
Total Yoke Length
250 mm non magnetic
(43 laminations)
150 mm non magnetic
(26 laminations)
S. Izquierdo Bermudez