## Slide 1: 2D Sensitivity Study and Critical Tolerances of CD1 Magnet
G. Montenero1 , B. Auchmann1,2 , and G. Rolando2
1) Paul Scherrer Institut
2) CERN
26 June 2017

## Slide 2: Summary
2D Mechanical modelling of CD1 dipole with ANSYS
Design’s objectives
Baseline Design (+ excursus on CD2)
Nominal Design vs. Material Properties
Mechanical tolerances
Parametric Study
Conclusions

## Slide 3: Summary
2D Mechanical modelling of CD1 dipole with ANSYS
Design’s objectives
Baseline Design (+ excursus on CD2)
Nominal Design vs. Material Properties
Mechanical tolerances
Parametric Study
Conclusions

## Slide 4: 2D Mechanical modelling Setup of the numerical simulations (ANSYS)
  The simulation is divided in 5 load steps:
    Vertical bladders inflation (max 40 MPa pressure) and vertical keys insertion
    Vertical bladders deflation and horizontal bladder inflation (max 40 MPa pressure) with horizontal keys insertion
    Horizontal bladders deflation-> assembly at room temperature
    Cool down of the assembly to 1.9 K
    Operation->Lorenz forces acting on the conductor according to short sample limit (1.9 K, 12 T)
Horizontal and vertical keys
horizontal and vertical bladders
1
2
Al Shell
Iron Yoke
Steel Pads
Coil Pack

## Slide 5: Summary
2D Mechanical modelling of CD1 dipole with ANSYS
Design’s objectives
Baseline Design (+ excursus on CD2)
Nominal Design vs. Material Properties
Mechanical tolerances
Parametric Study
Conclusions

## Slide 6: Design’s Objectives
What we care the most
  Limit the maximum stress on the conductor
  Keep the maximum stress of the mandrel below 0.2% yield stress
  Guarantee:
    pad/pad contact interface
    Extra margins for steel pads configuration (using in the simulations Lorenz force maps associated to ultimate load (12 T, Iss=20 kA at 1.9 K))
For the other materials of the assembly
  Aluminum for external and coil assembly shells (Al 7075)
  Ferromagnetic Iron yoke
  Steel for the pads (316LN)
Notes: Table for objectives

## Slide 7
2D Mechanical modelling of CD1 dipole with ANSYS
Design’s objectives
Baseline Design (+ excursus on CD2)
The Design vs. Material Properties
Mechanical tolerances
Parametric Study
Conclusions

## Slide 8: The Magnet
Assembly - room temp.
Room temp. steps
Cool down 1.9 K
Operation at short sample limit (1.9 K, 12 T)
Vert. bladder operation
Hor. bladder operation
1.9 K steps

## Slide 9: The Coil
Assembly - room temp.
Room temp. steps
(σθ - Azimuthal)
Cool down 1.9 K
Operation at short sample limit (1.9 K, 12 T)
Cable σθ = [- 46.4, 25.7] MPa
Cable σθ = [-55.7, 57.7] MPa
Cable σθ = [-87.1, 94.6] MPa
Vert. bladder operation
Hor. bladder operation
Cool down
and
operation steps
(σθ - Azimuthal)
Cable σθ = [-12.1, 1.1] MPa
Cable σθ = [-21.5, 10.5] MPa
Cable σνmax = 45.6 MPa
Cable σνmax = 11.6 MPa
Cable σνmax = 19.8 MPa
Cable σνmax = 66.4.5 MPa
Cable σνmax = 101 MPa

## Slide 10: The Former
Assembly - room temp.
Room temp. steps
(σθ - Azimuthal)
Cool down 1.9 K
Operation at short sample limit (1.9 K, 12 T)
Former σνmax = 110.6 MPa
Former σνmax = 184.8 MPa
Former σνmax = 271.6 MPa
Vert. bladder operation
Hor. bladder operation
Former σνmax = 53.4 MPa
Former σνmax = 65.9 MPa
Former σθ= [-110.6, 105.0] MPa
Former σθ = [-185.2, 108]MPa
Former σθ = [-224.0, 273.0]MPa
Former σθ = [- 53.4, 3.0] MPa
Former σθ = [-66.2, 13.7] MPa
Cool down
and
operation steps
(σθ - Azimuthal)

## Slide 11: The Protective Coil Pack Shell
Assembly - room temp.
Cool down 1.9 K
Operation at short sample limit (1.9 K, 12 T)
Vert. bladder operation
Hor. bladder operation
Prot. Shell σνmax = 27.4 MPa
Prot. Shell σνmax = 91.0 MPa
Prot. Shell σνmax = 133.5 MPa
Prot. Shell σνmax = 14.6 MPa
Prot. Shell σνmax = 16.0 MPa
Room temp. steps
Cool down
and
operation steps

## Slide 12: The Steel Pads
Assembly - room temp.
Room temp. steps
Cool down 1.9 K
Operation at short sample limit (1.9 K, 12 T)
Vert. bladder operation
Hor. bladder operation
Cool down
and
operation steps
Pads IR σνmax = 165.5 MPa
Pads IR σνmax = 316.3 MPa
Pads IR σνmax = 161.0 MPa
Pads IR σνmax = 48.0 MPa
Pads IR σνmax = 80.6 MPa

## Slide 13: The Iron Yoke
Assembly - room temp.
Room temp. steps
Cool down 1.9 K
Operation at short sample limit (1.9 K, 12 T)
Vert. bladder operation
Hor. bladder operation
Cool down
and
operation steps
Yoke σνmax > 180 MPa
Yoke σνmax = 355.0 MPa
Yoke σνmax = 389.0 MPa
Yoke σνmax = 54.5 MPa
Yoke σνmax = 105.0 MPa

## Slide 14: The Support Shell
Assembly - room temp.
Room temp. steps
Cool down 1.9 K
Operation at short sample limit (1.9 K, 12 T)
Vert. bladder operation
Hor. bladder operation
Cool down
and
operation steps
Shell σνmax = 23.9 MPa
Shell σνmax = 179.0 MPa
Shell σνmax = 208.0 MPa
Shell σνmax = 116.3 MPa
Shell σνmax = 69.8 MPa

## Slide 15: Former Displacement
Radial displacement difference of the former between
cool down and short sample load steps
The arrow indicates the radial movement direction from cool down to operation on X and Y axes
Along Y axes the coil pack squeeze of roughly of 180 m
Along X axes the coil pack expand of roughly of ~ 140 m

## Slide 16
2D Mechanical modelling of CD1 dipole with ANSYS
Design’s objectives
Baseline Design (+Excursus on CD2)
The Design vs. Material Properties
Mechanical tolerances
Parametric Study
Conclusions

## Slide 17: CD2 mechanical structure
  The CD2 design:
    Same Layer-2 OD =122 mm of CD1
    Inclined cable channels
    Same Bladder and Key structure of CD1
    2D Simulations -> 5 steps (as for CD1)and same B&K config.
      Operation->Lorenz forces acting on the conductor according to test condition (4.2 K, 10.5 T) , limited by the test station Imax=22 kA
Horizontal and vertical keys
horizontal and vertical bladders
1
2
Al Shell
Iron Yoke
Steel Pads
Coil Pack
CD2

## Slide 18: CD2- The Coil
Assembly - room temp.
Room temp. steps
(σθ - Azimuthal)
Cool down 1.9 K
Operation at short sample limit (1.9 K, 12 T)
Cable σθ = [- 45.2, 22.3] MPa
Cable σθ = [-109.0, 50.3] MPa
Cable σθ = [-70.5, 44.9] MPa
Vert. bladder operation
Hor. bladder operation
Cool down
and
operation steps
(σθ - Azimuthal)
Cable σθ = [-21.1, 11.1] MPa
Cable σθ = [-33.8, 9.8] MPa
Cable σνmax = 46.2 MPa
Cable σνmax = 20.8 MPa
Cable σνmax = 33.0 MPa
Cable σνmax = 102.0 MPa
Cable σνmax = 72.4 MPa

## Slide 19: CD2-The Former
Assembly - room temp.
Room temp. steps
(σθ - Azimuthal)
Cool down 1.9 K
Operation at short sample limit (1.9 K, 12 T)
Former σνmax = 185 MPa
Former σνmax = 340 MPa
Former σνmax = 175.0 MPa
Vert. bladder operation
Hor. bladder operation
Former σνmax = 100 MPa
Former σνmax = 158 MPa
Former σθ= [-185.0, 52.5] MPa
Former σθ = [-355.0, 248.0]MPa
Former σθ = [-174.0, 167.0]MPa
Former σθ = [- 107.0, 12.5] MPa
Former σθ = [-164.0, 50.5] MPa
Cool down
and
operation steps
(σθ - Azimuthal)

## Slide 20
2D Mechanical modelling of CD1 dipole with ANSYS
Design’s objectives
Baseline Design
Nominal Design vs. Material Properties
Mechanical tolerances
Parametric Study
Conclusions

## Slide 21: Pads: Steel vs. Iron
--- cable limit
---room temp. limit
… cold (1.9 K) limit
Why steel instead of iron
Thermal contraction of steel higher than iron
Thermal contraction of steel much closer to the one for the coil pack
For the iron pads, after cool down the differential thermal contraction gives a smaller value of pre-stress leading to higher maximum stress at operating conditions
Von Mises (σν) maximum stresses
cable and former for the 5 load steps
23 MPa
104 MPa

## Slide 22: Conductor’s Mechanical Properties
--- cable limit
---room temp. limit
… cold (1.9 K) limit
Mechanical Properties for comparison
Von Mises (σν) maximum stresses
cable and former for the 5 load steps
Used for simulations
The only remarkable differences are
7.7 MPa higher peak stress for Cond. Prop.2 on the cable at short sample operating condition
85 MPa higher peak stress for Cond. Prop.3 on the former at short sample operating condition

## Slide 23
2D Mechanical modelling of CD1 dipole with ANSYS
Design’s objectives
Baseline Design
The Design vs. Material Properties
Mechanical tolerances
Parametric Study
Conclusions

## Slide 24: Mechanical Tolerances
Coil pack
Tolerances of interest:
Mismatch between radii of coil and pads assemblies (OR1-IR2) ≠ 0 (coil/pad radial)
Horizontal key tolerance (hor. key)
Vertical key tolerance (vert. key)
Pad/pad interface contact (pad/pad cont.)
Use ANSYS contact technology
(coil/pad radial) < 0 → gap
(coil/pad radial) > 0 → compression
(hor. or vert. key) < 0 → undersize key
(hor. or vert. key) > 0 → oversize key
(pad/pad cont.) < 0 → undersize pads
(pad/pad cont.) > 0 → oversize pads
Horizontal and vertical keys
horizontal and vertical bladders
1
2
pad/pad cont.
vert. key
hor. key
OR1
IR1

## Slide 25
2D Mechanical modelling of CD1 dipole with ANSYS
Design’s objectives
Baseline Design
The Design vs. Material Properties
Mechanical tolerances
Parametric Study
Conclusions

## Slide 26: Parametric study and design’s objective
For any combination of the parameters tolerances:
Maximum stress on the conductor below 130 MPa
Maximum stress on the former below 250 MPa at room temp and 400 MPa. at 1.9 K
The pad/pad interface has to be in contact during all the operating conditions.
If any of the maximum allowed stresses on the conductor and on the former are exceeded, the parameters combination is considered to be harmful for the magnet operation
A pad/pad interface not in contact during all the steps
Use a ± 100 µm tolerance on the parameters of interest with a 50 µm step (five values for each parameter, reasonable computation time 5x5x5x5 simulations)
Nominal values of the parameters
  coil/pad radial gap equals to 0.0 mm
  hor. key interference of 0.3 mm
  vert. key interference of 0.0 mm
  pad/pad contact gap equal to 0.0 mm

## Slide 27: Sensitivity to Parameters One-factor-at-the-time
One-factor-at-the-time (quick check of important parameters)
Average the stress values over all the simulations runs for a given param. value and load step
Display the average as a function of the load step and param. value
Color map identify the spread on the results
Coil/pad radial mismatch has the larger influence on maximum stresses
Horizontal and vertical keys tolerances have a minor influence
Pad/pad contact tolerance can play a rule
We can restrict ourselves to the interactions between two parameters

## Slide 28
Sensitivity to Parameters
Two Parameters Analysis
FIRST ROW
  ± 100 µm tolerance on the coil/pad radial mismatch can not be accepted (required below 50 µm);
  A ± 50 µm tolerance on the hor. and vert. key must be considered
  Better to leave a small gap between coil and pad (≤ 50 µm)
2nd, 3rd and 4th ROWS
  Any combination of the other parameters gives a safe scenario
  Using tighter tolerances help to guarantee pad/pad contact
Varying two parameters while keeping the others at their nominal value:
All good
Pad/pad interface
Stresses values exceeded

## Slide 29
Defining Tolerances
  Target tolerances (according to the procurement of mechanical parts)
  coil/pad radial → [-40, 0] µm
  hor. key → ± 50 µm
  vert. key → ± 50 µm
  pad/pad contact → ± 25 µm
  4 simulations runs above limit -by a small amount- out of 625 simulations (5 values per tolerance):
Results from parametric study
with target tolerances
  THIS IS NOT GOING TO BE A PROBLEM: WE HAVE EXTRA MARGINS!

## Slide 30
2D Mechanical modelling of CD1 dipole with ANSYS
Design’s objectives
Baseline Design
The Design vs. Material Properties
Mechanical tolerances
Parametric Study
Conclusions

## Slide 31: Conclusions
A parametric study on the 2D model of CD1 magnet is carried out
Critical tolerances a parameter sensitivity is investigated
Tolerances for technical design are defined
Numerical Results from 2D simulations show the feasibility of the CD1 design

## Slide 32: CD1 - The Coil Radial Stress
Assembly - room temp.
Room temp. steps
(σr - Radial)
Cool down 1.9 K
Operation at short sample limit (1.9 K, 12 T)
Cable σr = [- 46.6, 29.0] MPa
Cable σr = [-63.7, 54.6] MPa
Cable σr = [-104.0, 36.2] MPa
Vert. bladder operation
Hor. bladder operation
Cool down
and
operation steps
(σr - Radial)
Cable σr = [-10.7, 16.6] MPa
Cable σr = [-21.1, 5.3] MPa

## Slide 33: CD1 - The Former Radial Stress
Assembly - room temp.
Room temp. steps
(σr - Radial)
Cool down 1.9 K
Operation at short sample limit (1.9 K, 12 T)
Vert. bladder operation
Hor. bladder operation
Former σr= [-50.2, 102.0] MPa
Former σr = [-86.4, 78.7]MPa
Former σr = [-204.0, 174.0]MPa
Former σr = [- 20.2, 30.6] MPa
Former σr = [-16.9, 28.8] MPa
Cool down
and
operation steps
(σr - Radial)

## Slide 34: CD2 - The Coil Radial Stress
Assembly - room temp.
Room temp. steps
(σr - Radial)
Cool down 4.2 K
Operation at short sample limit (4.2 K, 10.5 T)
Cable σr = [-26.5, 24.7] MPa
Cable σr = [-76.5, 43.6] MPa
Cable σr = [-79.0, 47.3] MPa
Vert. bladder operation
Hor. bladder operation
Cool down
and
operation steps
(σr - Radial)
Cable σr = [- 20.5, 10.2] MPa
Cable σr = [-22.2, 8.7] MPa

## Slide 35: CD2 - The Former Radial Stress
Assembly - room temp.
Room temp. steps
(σr - Radial)
Cool down 4.2 K
Operation at short sample limit (4.2 K, 10.5 T)
Vert. bladder operation
Hor. bladder operation
Cool down
and
operation steps
(σr - Radial)
Cable σr = [-57.7, 66.0] MPa
Cable σr = [-95.9, 143.0] MPa
Cable σr = [-169.0, 62.6] MPa
Cable σr = [- 36.3, 40.8] MPa
Cable σr = [-32.2, 44.6] MPa