## Slide 1
LGAD Simulations with Ga doping:
An Exploration
F.R. Palomo1, S.Hidalgo2
fpalomo@us.es
1Dept. Ingeniería Electrónica, Escuela Superior de Ingenieros
Universidad de Sevilla, Spain
2CNM-IMB Barcelona, Spain

## Slide 2
Introduction
Development of several LGAD models to test gain variation with bias and n+/pwell doping
Previous results (29th RD50 workshop, Nov 2016@CERN)
Analisis of radiation effects in LGAD Ga doped (a tentative): 300 um device
Analisis of radiation effects in LGAD Ga doped (a tentative): 50 um device

## Slide 3
Sentaurus TCAD Simulation SetUp
P-Stop
Collector
Ring
C-Stop
Low Gain Avalanche Detector (LGAD)
cross-section
Doping profiles under confidenciality rules
Simulation
Setup
x
y
z
Simulation Setup:
Red Pulsed Laser: 670 nm, 10 mm spot, 50W/cm2, 200 ps,
BackIllumination at Device Center
2D detector model: 1 mm in Z direction, 5 mm in X direction,
300 mm in Y direction)

## Slide 4
From 29th RD50: Radiation Damage Models
Simulation of Silicon Devices for the CMS Phase II Tracker Upgrade CMS Note 250887
CMS Proton Model
CMS Neutron Model
Four damage models
Pennicard Model f =1e12 up to 1e14 neq/cm2
CMS Proton and Neutron model f = 1e14-1e15 neq/cm2
Two Level Model Proton f = 1e14-1e15 neq/cm2
New Perugia Model f =1e12 up to 2e16 neq/cm2
Combined effect of bulk and Surface damage on strip insulation properties of proton irradiated n+-p silicon strip sensors, R.Dalal et al. JINST 2014 9 P04007
*The origin of double peak electric field distribution in heavily irradiated silicon
detectors, V.Eremin, E.Verbitskaya, Z.Li, NIMA 476 (2002) 556-564
Eremin et al two level model*
N(cm-3)=gint x f
Pennicard Model
Simulations of radiation-damaged 3D detectors for the Super-LHC, D.Pennicard et al. NIMA 592(1-2), 2008, pp16-25
N(cm-3)=hint x f
New Perugia
Modeling of radiation damage effects in silicon detectors at high fluences
HL-LHC with Sentaurus TCAD, D.Passeri et al, NIMA 824 (2016), 443-445

## Slide 5
From 29th RD50 LGAD:
All Models show a similar panorama, for example:
CMS Model
Electric Field along Y axis
At 1e15 a double junction appears at P+ volumen (device back side)
Electric Field Profiling
Back side detail
Front side detail
1e15
1e15
Back side
Front side

## Slide 6
From 29th RD50: Acceptor Removal+Trap Model (New Perugia)
253K
293K
Radiation effects in Low Gain Avalanche Detectors after hadron irradiations, G.Kramberger et al., JINST 2015 10 P07006
c=10e-16 cm-2
Boron Doping
Beyond 1e15 neq/cm2 there is no p mult.layer for all practical purposes,

## Slide 7
Wafer Data (from Mar Carulla @ Trento Meeting)
 | Dopant | Doping(cm-3) | CA (cm2)
Wafer9 (Mar) | Ga | 2,25E+16 | 6,90E-16
Kramb. Paper(2015) | B | 5,00E+16 | 9,10E-16
Wafer10 (Mar) | Ga | 1,00E+17 | 1,00E-16
Wafer11 (Mar) | Ga | 2,30E+17 | 3,30E-16
Wafer14 (Mar) | B | 3,00E+18 | 2,00E-17
Explanation for carrier removal and type conversión in irradiated silicon solar cells, T.Yamaguchi et al. Applied Physics Letters 72(10), 1998
A detailed model to improve the radiation resistance of Si space solar cells, T.Yamaguchi et al. IEEE Trans on Electron Devices,46(10), 1999
Strategies for improving radiation tolerance of Si space solar cells, A.Kahn et al. Solar Energy Materials & Solar Cells, 75, 271-276, 2003
Defects in Semiconductors, L.Romano, V.Priviera, C.Jagadish, 2015 AP Elsevier publishers
Radiation effects in Low Gain Avalanche Detectors after hadron irradiations, G.Kramberger et al., JINST 2015 10 P07006
Last measurements and developments on LGAD detectors, Mar Carulla et al., 12th “Trento” Workshop February 2017
We consider the acceptor removal model from literature (Watkins’ removal mechanism)
From Mar Carulla we extrapolate CA=4e-16 cm2 for a Kramberger’s Paper type Gallium LGAD device, no T dependence as a first approach (also 2003 Kahn)
We consider also the trap model (new Perugia)
Simulation of Red Laser Back Transient
Maximum fluence damage 2e15 neq/cm2 compatible with CMS ETL (Endcap Timing Layer) see Cartiglia’s talk
;
;
(1999 Yamaguchi)
(1998 Yamaguchi)
Notes: Resultados de Mar, mecanismo de Watkins

## Slide 8
We define a new LGAD with higher doping in the p multiplication layer
NO Ga physics card in Sentaurus so:
  We suppose that as a dopant, Ga behaves like B
  We use the acceptor removal coefficients from the Mar Carulla analysis of the Ga doped wafers
Tested several hypothetical devices, too high doping and the device goes to avalanche too soon
The LGAD doping profile is a narrow Street
From Mar Carulla wafer results, the acceptor removal coefficient goes down quickly
We extrapolate the value cA=4e-16 for the simulations, no T dependence (~worst case)
  Probably the cA value will be even lower if we consider the carbon interstitials effect (for the future)
For sure, we need more experimental data
First, we analyze the 300 um new LGAD device
Second, we analyze a posible 50 um LGAD device
Exploration of different damage fluences, trap & acceptor removal models, 293 & 253K, even variable bias
Everything ready to inject new data from experiments and the T dependence of cA
LGAD-Ga analysis, a tentative one
Notes: Mecanismo de Watkins, mejoras en el dispositivo

## Slide 9
Fluence n/cm2 | Charge LGAD (C) | Charge PIN (C) | Gain Qlgad/Qpin
NoIrrad | 7,42e-15 | 2,01e-15 | 3,689
1e13 | 7,19e-15 | 2,01e-15 | 3,581
1e14 | 5,6e-15 | 1,99e-15 | 2,818
1e15 | 1,86e-15 | 1,19e-15 | 1,563
2e15 | 1,28e-15 | 9,98e-16 | 1,284
LGAD300um
Red Laser Back
400V Bias 293K
1e13-2e15 neq/cm2
c=4x10e-16 cm-2
New Perugia Trap Model
Acceptor Removal+Trap Model (New Perugia)
detector LGAD7859_Gallium_RedLaserBack_400V
detector PINLGAD7859_Gallium_RedLaserBack_400V
Notes: LGAD300um293K

## Slide 10
Fluence n/cm2 | Charge LGAD (C) | Charge PIN (C) | Gain Qlgad/Qpin
NoIrrad | 9,86e-15 | 2,01e-15 | 4,91
1e13 | 9,46e-15 | 2,00e-15 | 4,72
1e14 | 6,77e-15 | 1,95e-15 | 3,46
1e15 | 1,74e-15 | 1,22e-15 | 1,42
2e15 | 1,28e-15 | 1,19e-15 | 1,08
LGAD300um
Red Laser Back
400V Bias 253K
1e13-2e15 neq/cm2
c=4x10e-16 cm-2
New Perugia Trap Model
Acceptor Removal+Trap Model (New Perugia)
detector LGAD7859_Gallium_RedLaserBack_400V
detector PINLGAD7859_Gallium_RedLaserBack_400V
Notes: LGAD300um253K

## Slide 11
Fluence n/cm2 | Charge LGAD (C) | Charge PIN (C) | Gain Qlgad/Qpin
NoIrrad | 9,86e-15 | 2,01e-15 | 4,91
1e15(400V) | 1,74e-15 | 1,22e-15 | 1,42
1e15(600V) | 1,86e-15 | 1,22e-15 | 1,53
2e15(400V) | 1,28e-15 | 1,19e-15 | 1,08
2e15(600V) | 1,30e-15 | 1,19e-15 | 1,09
2e15(800V) | 1,34e-15 | 1,19e-15 | 1,13
LGAD 300um
Red Laser Back
Variable Bias,253K
1e15-2e15 neq/cm2
c=4x10e-16 cm-2
New Perugia Trap Model
detector LGAD7859_Gallium_RedLaserBack_Variable Bias
detector LGAD7859_Gallium_RedLaserBack_400V
detector PINLGAD7859_Gallium_RedLaserBack_400V
Notes: LGAD300um253K Variable bias

## Slide 12
Fluence n/cm2 | Charge LGAD (C) | Charge PIN (C) | Gain Qlgad/Qpin
NoIrrad | 9,52e-15 | 2,02e-15 | 4,72
1e13 | 9,27e-15 | 2,02e-15 | 4,60
1e14 | 7,49e-15 | 2,02e-15 | 3,71
1e15 | 2,72e-15 | 1,92e-15 | 1,42
2e15 | 1,98e-15 | 1,84e-15 | 1,08
LGAD50um
Red Laser Back
150V Bias 293K
1e13-2e15 neq/cm2
c=4x10e-16 cm-2
New Perugia Trap Model
detector PINLGAD7859_Gallium_RedLaserBack_150V
detector LGAD7859_Gallium_RedLaserBack_150V
Notes: LGAD50um293K

## Slide 13
Fluence n/cm2 | Charge LGAD (C) | Charge PIN (C) | Gain Qlgad/Qpin
NoIrrad | 1,37e-14 | 2,02e-15 | 6,78
1e13 | 1,32e-14 | 2,01e-15 | 6,54
1e14 | 9,94e-15 | 2,01e-15 | 4,96
1e15 | 2,84e-15 | 1,93e-15 | 1,47
2e15 | 1,98e-15 | 1,87e-15 | 1,05
LGAD50um
Red Laser Back
150V Bias 253K
1e13-2e15 neq/cm2
c=4x10e-16 cm-2
New Perugia Trap Model
detector LGAD7859_Gallium_RedLaserBack_150V
detector PINLGAD7859_Gallium_RedLaserBack_150V
Notes: LGAD50um253K

## Slide 14
Fluence n/cm2 | Charge LGAD (C) | Charge PIN (C) | Gain Qlgad/Qpin
NoIrrad | 1,37e-14 | 2,02e-15 | 6,78
1e15(150V) | 2,84e-15 | 1,93e-15 | 1,47
1e15(250V) | 3,4e-15 | 1,93e-15 | 1,77
2e15(150V) | 1,98e-15 | 1,87e-15 | 1,05
2e15(250V) | 2,11e-15 | 1,87e-15 | 1,13
2e15(350V) | 2,31e-15 | 1,87e-15 | 1,23
PIN50um
LGAD50um
LGAD 50um
Red Laser Back
Variable Bias,253K
1e15-2e15 neq/cm2
c=4x10e-16 cm-2
New Perugia Trap Model
detector LGAD7859_Gallium_RedLaserBack_Variable Bias
detector PINLGAD7859_Gallium_RedLaserBack_150V
detector LGAD7859_Gallium_RedLaserBack_150V
Notes: LGAD50um253K Variable bias

## Slide 15
Conclusions
New experimental data are desperately needed
Ga and C doping could be the solution up to 2e15 neq/cm2 damage (ELT@CMS)
The simulation models are ready for the new data

## Slide 16
Thanks for your attention
fpalomo@us.es