## Slide 2: CHARM Dose Gradient Assessment
Melanie Krawina
EN – STI FDA
SMA Connector Test

## Slide 3: Outline
Experiment
FLUKA
Plots
Comparison with RPL
Gradient

## Slide 4: Shape Memory Alloy (SMA)
SMA Components
Connection device for vacuum chambers
Change their shape according to the temperature
Future use in the HL – LHC
Tested at CHARM to analyze the effects of strong radiation on them

## Slide 5: Experimental Set up
Experiment
For each sample two RPL dosimeters
In front and behind the SMAs
Placed on test position T0
Irradiated for 90 days to get a dose around 100 kGy

## Slide 6: FLUKA Set up
6
Primary
We used 50.000.000 primaries on target
USRBIN
We scored for the dose and the 1MeV Neutron on the table
Simplified Geometry
Due to the close distance to the target we did not simulate the whole CHARM geometry because some effects are not significant or negligible

## Slide 7: Geometry
Layout 1
Layout 2
24 GeV
24 GeV

## Slide 8: FLUKA
LAYOUT 1
 1kGy/d
 1kGy/d
TARGET HEIGHT
Regular Cartesian mesh
0.5 cm x 0.5cm x 0.5cm
[Gy/d]

## Slide 9: FLUKA
Layout 1
Layout 2
24 GeV
24 GeV
3
2
1
3
2
1
[Gy]
X
Z
X
Z

## Slide 10: Plot Z Axis
Beam
Three samples distributed on the z Axis
Simulated with Air and Samples
Air1 and Layout 1 are on the same height, v.v

## Slide 11: Plot X Axis : Dose
X

## Slide 12: Comparison with RPL : Layout 1
RPL [kGy] |  | FLUKA [kGy] | FLUKA/RPL
1B | 55 | 52.1 | 0.94
1F | 100 | 163 | 1.63
2B | 75 | 102 | 1.36
2F | 150 | 321 | 2.14
3B | 90 | 152 | 1.69
3F | 140 | 418 | 2.98
3
2
1
24 GeV

## Slide 13: Comparison with RPL : Layout 2
RPL [kGy] |  | FLUKA [kGy] | FLUKA/RPL
1B | 55 | 63.7 | 1.16
1F | 100 | 175 | 1.75
2B | 75 | 115 | 1.53
2F | 150 | 354 | 2.36
3B | 90 | 172 | 1.91
3F | 140 | 465 | 3.32
3
2
1
24 GeV

## Slide 14: Gradient
Gradient effects due to height differences
Height difference of 2 cm
Stronger gradient with increasing Z value
We want to quantify these effect for three different positions
Results between 0.2 and 15 % according to the position

## Slide 15
Comparison of the Gradient in Z Axis
Start Table
Middle Table
End Table
0 [cm]
1.28E+02 [kGy]
1.27E+02 [kGy]
15.25 [cm]
2.18E+02 [kGy]
3.04E+02 [kGy]
30.5 [cm]
3.42E+02 [kGy]
3.75E+02 [kGy]
9.60 %
0.95 %
8.19 %

## Slide 16
Comparison of the Gradient in X Axis : Sample 1
Start Table
Middle Table
End Table
0 [cm]
8.52E+01 [kGy]
8.05E+01 [kGy]
7.75 [cm]
1.24E+02 [kGy]
1.32E+02 [kGy]
15.5 [cm]
1.71E+02 [kGy]
1.83E+02 [kGy]
6.81 %
5.5 %
6.62 %

## Slide 17
Start Table
Middle Table
End Table
0 [cm]
1.37E+02 [kGy]
1.31E+02 [kGy]
7.75 [cm]
2.08E+02 [kGy]
2.21E+02 [kGy]
15.5 [cm]
3.28E+02 [kGy]
3.72E+02 [kGy]
13.56 %
4.26 %
6.04 %
Comparison of the Gradient in X Axis : Sample 2

## Slide 18
Start Table
Middle Table
End Table
0 [cm]
1.50E+02 [kGy]
1.58E+02 [kGy]
7.75 [cm]
2.64E+02 [kGy]
2.89E+02 [kGy]
15.5 [cm]
4.01E+02 [kGy]
4.44E+02 [kGy]
10.68 %
5.84 %
9.41 %
Comparison of the Gradient in X Axis : Sample 3

## Slide 19: Gradient at the Table
Gradient effects due to height differences
3
2
1
X
Z
We see an increasing gradient in positive Z axis
The strongest gradient in X axis for the middle of the table/Sample 2
In fact we have an angular distribution of the gradient

## Slide 20: FLUKA vs. RPL?
Do we trust the FLUKA values ?
If we know the exact position of the RPLs

## Slide 21: Comparison with RPL (Joao)
RPL [Gy] |  | FLUKA [Gy] | FLUKA/RPL
1 | 644.7 | 571.0 | 8.86E-01
2 | 674.2 |  | 8.47E-01
3 | 579.0 | 465.0 | 8.03E-01
4 | 547.8 |  | 8.49E-01
5 | 371.1 | 282.2 | 7.61E-01
6 | 416.7 |  | 6.77E-01
3
2
1
4
5
6

## Slide 22: Comparison with RadFET (Joao)
RF [Gy] |  | FLUKA [Gy] | FLUKA/RF
1 | 525 | 631.4 | 1.20E+00
2 | 441 | 440.7 | 9.99E-01
3 | 307 | 271.7 | 8.85E-01
4 | 1326 | 2056.0 | 1.55E+00
5 | 1172 | 1700.9 | 1.45E+00
6 | 684 | 828.4 | 1.21E+00
3
2
1
4
5
6

## Slide 23: Conclusion
Dose Gradient
We see indeed a strong dose gradient on the table
Exact Position
To compare the values from the dosimeters with the FLUKA Simulation we need to know the exact positions
Future Experiments
We have to quantify the gradient effect for the test positions to ensure the dose for future CHARM users

## Slide 24
Melanie Krawina
Tech. Student @ CERN - EN/STI - FDA
R2E Project
melanie.krawina@cern.ch

## Slide 25: Appendix

## Slide 26: Plot Z Axis
Beam

## Slide 27: Plot X Axis : 1MeVN

## Slide 28: Comparison Data 2016
RPL [kGy] |  | FLUKA [kGy] | FLUKA/RPL
1B | 55 | 58.8 | 1.07
1F | 100 | 145 | 1.45
2B | 75 | 107 | 1.42
2F | 150 | 282 | 1.88
3B | 90 | 156 | 1.73
3F | 140 | 350 | 2.50
3
2
1

## Slide 29
Comparison of the Gradient in Z Axis
Start Table
Middle Table
End Table
Center S1
Center S3
Center S2
0 [cm]
1.28E+02 [kGy]
1.27E+02 [kGy]
15.25 [cm]
2.69E+02 [kGy]
3.00E+02 [kGy]
30.5 [cm]
3.42E+02 [kGy]
3.75E+02 [kGy]
3.1 [cm]
1.59E+02 [kGy]
1.60E+02 [kGy]
15.25 [cm]
2.69E+02 [kGy]
3.00E+02 [kGy]
27.4 [cm]
3.46E+02 [kGy]
3.82E+02 [kGy]
0.95 %
11.42 %
9.60 %
0.23 %
11.42 %
10.30 %

## Slide 30
Comparison of the Gradient in X Axis : Sample 1
Start Table
Middle Table
End Table
Before S1
After S1
Center S1
0 [cm]
8.52E+01 [kGy]
8.05E+01 [kGy]
7.75 [cm]
1.24E+02 [kGy]
1.32E+02 [kGy]
15.5 [cm]
1.71E+02 [kGy]
1.83E+02 [kGy]
15.5 [cm]
1.71E+02 [kGy]
1.83E+02 [kGy]
12.4 [cm]
1.52E+02 [kGy]
1.64E+02 [kGy]
9 [cm]
1.25E+02 [kGy]
1.32E+02 [kGy]
5.5 %
6.62 %
6.81 %
6.81 %
7.63 %
5.68 %

## Slide 31
Comparison of the Gradient in X Axis : Sample 2
Start Table
Middle Table
End Table
Before S2
After S2
Center S2
0 [cm]
1.37E+02 [kGy]
1.31E+02 [kGy]
7.75 [cm]
2.08E+02 [kGy]
2.21E+02 [kGy]
15.5 [cm]
3.28E+02 [kGy]
3.72E+02 [kGy]
15.5 [cm]
3.28E+02 [kGy]
3.72E+02 [kGy]
12.4 [cm]
2.67E+02 [kGy]
2.95E+02 [kGy]
9 [cm]
2.21E+02 [kGy]
2.48E+02 [kGy]
4.26 %
6.04 %
13.56 %
13.56 %
10.21 %
12.34 %

## Slide 32
Comparison of the Gradient in X Axis : Sample 3
Start Table
Middle Table
End Table
Before S3
After S3
Center S3
0 [cm]
1.50E+02 [kGy]
1.58E+02 [kGy]
7.75 [cm]
2.64E+02 [kGy]
2.89E+02 [kGy]
15.5 [cm]
4.01E+02 [kGy]
4.44E+02 [kGy]
15.5 [cm]
4.01E+02 [kGy]
4.44E+02 [kGy]
12.4 [cm]
3.54E+02 [kGy]
3.78E+02 [kGy]
9 [cm]
2.80E+02 [kGy]
3.04E+02 [kGy]
5.84 %
9.41 %
10.68 %
10.68 %
6.73 %
8.79 %