## Slide 1
Thin films and surfaces treatments in accelerator technology
S. Calatroni / G. Rosaz
On behalf of TE-VSC
9/4/2015

## Slide 2: Outline
Surface treatment
Thin film activities – general
SRF Thin films
Visit

## Slide 3: Surface Treatment

## Slide 4
Stainless steel 316LN
Cleaning UHV components and monitoring cleanliness :
XPS
Wavenumber [cm-1]
CH3 asymmetric deform. of Si-CH3
CH3 symmetric deform. of Si-CH3
Si-O-Si stretching
Si-C stretching and CH3 rocking
CH stretching of CH3
Transmittance [%]
S.Ilie, C.Petitjean, C.Dias-Soares
FTIR
Through elution with C6H14
Precision cleaning is important to reduce outgassing and achieve UHV (standard up to 7m length)

## Slide 5
Plug-in Modules with RF Fingers
RF bridge (fingers) to interconnect superconducting magnets (~ 1 700 PIM)
Au/CuBe and Rh/Cu plating: different metals to avoid cold welding under vacuum and soft-on-hard contact to have sufficiently low resistivity (< 0.1 mOhm contact resistance)
RF bellows
Copper transition tube
Upstream flange
Downstream flange
Plug-in module transition tube
RF-contact Gold coating 5 m
RF-contact strips
coating 5 m
Indium brazed
RF-contact strips
coating 5 m
Indium brazed
RF-contact transition flange
Rhodium coating 3 m
Screw & Spring washer
Screw & Spring washer
Room temperature position
Working position at cryogenic temperature
Courtesy R. Veness
cooling
Au
Rh

## Slide 6
Electrolytic deposition: on stainless steel, copper and aluminum
Copper electroplating
Cover of DTL LINAC 4
Rhodium electroplating
RF transition LHCVSR
Gold electroplating
LINAC3 test chamber
Silver electroplating
RF fingers TDI shield
Ag plating on Al stripline contact AD
Cu plating on DTL tank of Linac 4

## Slide 7
7
Wet surface treatments: Cu plating of DTL tank of LINAC4
Final assembly with the electrodes for the accelerator
Difficult to obtain uniform plating
and plating in the ports

## Slide 8: Thin Films for Accelerators

## Slide 9
Why?...
LEP dipole vacuum chamber
NEG
coating
Thin film of Non-Evaporable-Getter as vacuum pump
In accelerators at ultra-high-vacuum (<10-10 mbar) the trend is to bring the pump closer to the outgassing source and distribute the pumping speed evenly.
 transform the entire vacuum chamber in a pump by coating it with a getter thin film: ~2μm of TiZrV deposited by DC magnetron; activated with a standard vacuum bake-out at 180°C-230°C (24h), operates at RT
Pump space hindrance and conductance vs pressure profile!
Pumps (chemisorption) H2, CO, CO2, …..
Does not pump CHx and noble gases
Characterised by XRD, EDX, SEM, XPS…
pump
pump
pump
pump

## Slide 10
Activation process: Monitoring by surface analysis (XPS)
Heating stepwise for 1h at each T
Surface Oxygen decrease
Diffusion of O into the bulk
Reduction of the surface oxides of all the metals: the surface is metallic and reactive
Ti
Zr
V
ox
ox
ox
met
met
met

## Slide 11
The NEG thin film is obtained by ion bombarding a target
made of inter twisted wires of titanium, zirconium and vanadium. The atoms of the target are then sputtered and deposited on the beam pipe walls.
3mm wires of Ti, Zr and V
Before coating
after coating
Kr+
beam pipe
wall
Ti, Zr, V
Kr+
Kr+
Kr+
Kr+
Kr+
Kr+
Kr+
Kr+
Kr+
Kr+
Kr+
Kr+
Kr+
Kr+
Kr+
Kr+
Kr+
Kr+
Kr+
Kr+
Kr+
Kr+
Kr+
Kr+
-U
B

## Slide 12: NEG coatings for LHC LSS & experiments
Large scale production for the LHC and experiments by DC Cylinder Magnetron sputtering (DCCM) from a target of Ti, Zr and V wires (more than 1300 chambers)
3mm wires of Ti, Zr and V
8 meter solenoid
Notes: Appropriate situation with the CERN logotype
Mixture of different logotypes
All of them are circulating
All CERN clubs were also very creatives

## Slide 13
Electron cloud and SEY
+
+
+
+
Proton bunch (charge +)
Electron (charge -)
 Perturbation of the beam (emittance growth), thermal load on cryogenics, noise on beam instrumentation; the problem is more important for high beam currents (beam potential) and short bunch spacing
To reduce the effect one must reduce the secondary electron yield (SEY) of the walls or attract the generated electrons by other means
Gas molecule

## Slide 14
The possible solution : carbon a-C coatings
-Carbon (graphitic) coating on copper deposited by magnetron sputtering
-SEY does not change for thicknesses above 50 nm
-development started in 2008 for an upgrade of SPS
a-C(Ne9)
Dose below
10-6 Clb/mm2
as received

## Slide 15
Cathode:
graphite targets
(cells)
Cathode in the SPS MBB dipole
LIU-SPS: Carbon coating of the SPS vacuum chambers
`
Project of coating of the Super Proton Synchrotron dipoles with carbon to mitigate electron cloud (744 dipoles x 6.5 m each, 18 t)
hollow cathode coating (cannot apply axial B-field for magnetron in the yokes)
successful on short section, tested with beam in SPS (section ~200 m)
development ongoing to do the coating in the tunnel in 2018
6.5 m
6.5 meter

## Slide 16
Carbon coating of triplet magnets of LHC in situ during LS2
ARC types, ≥Q7 (c.bore inner diam. 50 mm)
LSS types, Q1–Q6 (cold bore inner diameters 50, 53, 63, 69 and 74 mm)
In order to cope with the thermal load on cryogenics provoked by e-cloud
Close to interaction points
Coating 35 m of beamscreen without dismounting the cryogenic magnets
35 m

## Slide 17
electron gun
Ip = Is + Ic
d = Ic / (Is + Ic)
Sample
Ip
Ic
A
Is
A
Ic
XPS
SEY
measurement
Measurement of SEY
Coatings

## Slide 18
Effect of hydrogen
0 0.05 0.10 0.15 0.20 0.25 0.30 0.35
H2% in Ar gas
1.6
1.5
1.4
1.3
1.2
1.1
1.0
0.9
0.8
SEY
Effect of hydrogen content in the sputtering gas
Hydrogen is the most important residual gas in a baked vacuum system (outgassing), therefore a special care must be taken to have a «clean» coating system
Remark: it is very difficult to measure the H content in a carbon coating!

## Slide 19: Superconducting Radio Frequency (SRF) Thin Films activities at CERN

## Slide 20: Thin Film SRF at CERN
Thin Film SRF projects at CERN
LEP2 4-cells cavity
Past:
x288 Nb/Cu 350 MHz 4-cells cavities for LEP2 (90’s)
x16 Nb/Cu 400 MHz single cell cavities for LHC (2008)
Current:
x25 Nb/Cu 100 MHz cavities for HIE-ISOLDE
x8 Nb/Cu spare 400 MHz cavities for LHC
HIE-ISOLDE cavity
LHC cavity
FCC study
Future: FCC (Future Circular Collider) study
  400 MHz elliptical single cell, quantities ~ 300
  400/800 MHz elliptical multi-cells, quantities > 1000
  400 MHz Wide Open Waveguide for “crabbing”

## Slide 21: SRF Cavities production
7 W
10 W
13 W
Superconducting booster for ISOLDE radioactive ion beam facility at CERN 39 MV needed to reach 10 MeV/u
for A/q = 4.5 (highest possible at ISOLDE)
25 Quarter Wave Resonators cavities
 cavities production for phase 2 completed,
 4th cryomodule under commissioning,
 + 3 spare cavities produced out of 5
1. HIE-ISOLDE QWR Nb/Cu cavities
First 2 seamless (no weld) cavity coated
 Best RF performance of all the production!
Beam direction
300 mm
950 mm
Frequency | 101.28 MHz
Specification | 6 MV/m @ Q0 = 4.7x108
@ 4.5K

## Slide 22: SRF Cavities production
1. HIE-ISOLDE QWR cavities – Nb coating hardware and process
  Cavity in UHV chamber
  (10-8 mbar base vacuum)
  Cu cavity substrate, biased at -80 V
  Nb cylindrical cathode used on both sides, not cooled
  Anode grids on both sides of cathode, grounded
   DC-bias diode sputtering, 8 kW, 0.2 mbar Ar
  Cavity bake-out to 650°C (IR lamps) prior to coating
  Coating at high temperature (300  620°C)
  15 runs of 25’ each, net coating duration = 6h
  Multi-layers due to coating run/cool-down cycles
  Nb layer thickness ranging from 1.5 mm to 12 mm

## Slide 23: SRF Cavities production
2. LHC spare cavities – Nb coating hardware and process
Cathode
Magnet
Coating apparatus schematic
  Cavity as UHV chamber
  (10-8 mbar base vacuum)
  Cavity = anode, grounded
  Nb cylindrical cathodes tubes
  movable electromagnet inside, liquid cooled
   DC-magnetron sputtering, 6.4 kW, 6.10-4 mbar Kr
  Cavity bake-out (bake-out tent) to 180°C
  Coating 7 steps for the 7 different electromagnet positions
  Duration = 1h 20’ at low temperature (150°C)
  Nb layer thickness ~ 2 mm

## Slide 24: SRF Cavities production
 8 Spare cavities to be manufactured, Nb coated and dressed with He-tank
2. LHC spare Nb/Cu cavities
Practice cavities (PC): 3 coatings
PC01 recoated: substrate structural defect
PC05: coated, RF test pending
PC02 recoated:
Cavity at specs (Q0 = 2.2.109 at 6 MV/m)
Coating recipe and assembly flow validated
Ability to recover a heavily damaged cavity by surface machining
1 m
1 m
Frequency | 400.8 MHz
Specification | 5 MV/m @ Q0 = 2x109
@ 4.5K

## Slide 25: R&D: HiPIMS coatings for SRF cavities
Mitigate the high field Q-slope in Nb/Cu cavity
Low surface resistance (<10 nW, 1.3 GHz, 2K) with Nb layer
High Power Impulse Magnetron Sputtering
Layer densification
GOALS AND MOTIVATION
From this
To this
GOALS AND MOTIVATION
Very encouraging results on 1.3 GHz cavities: 20 nW residual resistance
Target: 5 nW.
Q-slope among the best for sputtered cavities
Bias effect: lower values induce lower surface resistance
Substrates affected by surface defects  collaboration with Jlab for surface finishing (centrifugal barrel polishing)
Coating on b = 0.65 704 MHz cavities enabled by tuning magnetic configuration : Best candidate to evaluate the Q-slope dependence to layer density
Ions Energy Analysis  bias delayed to mitigate working gas incorporation

## Slide 26: R&D: A15 Materials for SRF cavities
Switch from Nb/Cu to A15/Cu
Higher Tc ,Higher efficiency
Low surface resistance RBCS ~ 0.25 nΩ @ 4.2K / 400MHz (Nb ~ 60 nΩ)
Toward leptonic machine compatible thin film on copper
GOALS AND MOTIVATION
Synthesize A15 crystalline phase
Obtain theoretical Tc (18.3K for Nb3Sn) on copper substrate
Manage stress in the film
CHALLENGES
RESULTS
Best Tc obtained on Cu: 16.5K
Substrate plays a major role in the layer final properties
FCC cubic phase synthesized on Cu
Impact of layer microstrain on superconducting properties
XRD
SRF properties to be characterized in 2018

## Slide 27
Chart: J profile - β-1-SPL - optimised
Bulk Nb superconducting cavities: Optimization of the Electropolishing
5-cell cavity
Simulation with smooth electrode (red) and optimized electrode (blue) to get more uniform current and polishing
Electrode and current density map
COMSOL
software

## Slide 28
Future Circular Collider Study
Beam Screen Impedance

## Slide 29: FCC-hh: pushing the energy frontier
The name of the game of a hadron collider is energy reach
Compared to the LHC:
Factor ~6 in energy  Ecms 100 TeV pp
Factor ~3 in radius  bending 100 km
Factor ~2 in field  Bdipole 16 T
Factor ~144 in synchrotron radiation power  E4-2

## Slide 30: Synchrotron radiation/beam screen
High synchrotron radiation load (SR) of protons @ 50 TeV:
~30 W/m/beam (@16 T)
5 MW total in arcs (LHC <0.2W/m)
New type of ante-chamber
absorption of synchrotron radiation
avoids photo-electrons, helps vacuum
Courtesy: C. Garion
Taking into account vacuum requirements, overall cryogenic efficiency and power consumption of the accelerator, the synchrotron radiation has to be absorbed at 50 K
Copper coating for impedance as in the LHC…
…might not be good enough for the FCC-hh

## Slide 31: Impedance basics
Image charges flow on the surface of the beampipe and produce wakefields
The wakefields potential is proportional to surface impedance
Power dissipation from wakes is where is a summation of over the bunch frequency spectrum
Wakefields have an effect on beam stability, in particular the transverse plane: the Transverse Coupled-Bunch Instability (TCBI)
Risetime of resistive-wall instability depends on the surface impedance
with at the frequency of the unstable mode
Transverse mode-coupled impedance (TMCI) limits the maximum
bunch intensity, also linked to the surface impedance

## Slide 32: HTS films requirements for beam screen
Bunches of 1011 protons, 8 cm long
Beam screen of ~30mm diameter.
Assuming a film thickness / skin depth of 1 µm the HTS material should have a critical current density
Jc of about 25 kA/cm2 (2.5x108 A/m2) at 50 K and 16T
Beam instantaneous image current
Frequency spectrum for various bunch shapes

## Slide 33: Material choices
Data from:
Nature 414, 368-377 (15 November 2001)
High-Tc superconducting materials for electric power applications
David Larbalestier, Alex Gurevich, D. Matthew Feldmann & Anatoly Polyanskii
Superconductor Science and Technology, Volume 11, Number 8
Synthesis and properties of fluorine-doped Tl(1223): bulk materials and Ag-sheathed tapes
E Bellingeri, R E Gladyshevskii, F Marti, M Dhallé and R Flükiger
Courtesy: E. Bellingeri

## Slide 34: Challenges for HTS coatings
YBCO and Tl-based HTS are the only possible candidates
How to obtain good quality HTS inside tube geometry
  Considerable experience exists in coated tape production for YBCO, scalability to tubes is extremely challenging: develop forming techniques.
  Tl-based HTS has characteristics similar to YBCO, and should allow full scalability to tubes thanks to electrodeposition on silver (coated) substrates: develop this (old) new material

## Slide 35: Surface impedance basics
The surface impedance depends strongly on the depinning frequency

## Slide 36: HTS films projected performance: YBCO relative to Cu at 50 K and 16 T
Surface resistance of superconductors in the presence of a dc magnetic field: frequency and field intensity limits, S. Calatroni and R. Vaglio
IEEE Trans. Appl. Supercond. 27-5 (2017) 3500506

## Slide 37: HTS films projected performance: Tl-1223 relative to Cu at 50 K and 1.06 T / 16 T
Thallium-based high-temperature superconductors for beam impedance mitigation in the Future Circular Collider, Calatroni, S.; Bellingeri, E.; Ferdeghini, C.; Putti, M.; Vaglio, R.; Baumgartner, T.; Eisterer, M.,
Superconductor Science and Technology, Volume 30, Issue 7, article id. 075002 (2017).

## Slide 38
Re(Z) [Ohm/m]

## Slide 39
Im(Z) [Ohm/m]

## Slide 40
THANK YOU!