## Slide 1: RMM – Magnetic study
E. Rochepault, S. Izquierdo Bermudez – 21/07/2015

## Slide 2: Design constraints
Bo = 16 T at 4.2 K with 10 % margin
Strand available or easy to procure
  Winding should start January 2017 (cable should be ready for insulation two months before)
“Accelerator size”
  Coil w~70 mm
  Outer magnet diameter < 800 mm
Field Quality: bn due to saturation < 300 units
Can be protected without dump? Not clear requirements set in terms of protection.
Remark: Very difficult to satisfy all of them at the same time, we will need to set priorities!

## Slide 3: Strand and cable parameters
All the designs (unless otherwise specified), consider the following parameters:
Strand diameter = 1 mm
Jc(12T,4.2K,wo self-field) = 3000 A/mm2
Bc2(12T,4.2K) = 25 T
Cu2Sc ratio = 1.0-2.0
Cable packing factor ~ 80 %
Cable degradation = 5 %

## Slide 4: Summary of the designs
Remarks:
When to numbers are displayed: High Field/Low Field
Orange = risk associated as strand procurement needed and/or coil technology to develop
Red = Do not fulfil initial requirements
Quench protection without dump might not be possible, but it is set as a lower priority
HF/LF
 | Strand |  | Grading? | Coil size | Field quality | Operating Parameters |  |  | Margins
 | D (mm) | Cu2Sc | -- | (mm) | b3 sat | Inom (kA) | Bo (T) | Bp (T) | %
Design 0 | 1 | 1.3 | no | >120 | <10 |  |  |  | 
Design 1 | 1 | 1 | no | 120 | <10 | 9.8 | 16.1 | 16.3 | 10
Design 2 | 1 | 1 | no | 105 | <150 | 11.1 | 16 | 16.2 | 10
Design 3 | 1 | 1 | no | 96 | <150 | 11.1 | 15.9 | 15.9 | 10
Design 4 | 1 | 1/1.5 | yes | 69 | <150 | 10.9 | 16 | 16/12.7 | 10/14
Design 5 | 1/0.7 | 1/1.2 | yes | 69 | <150 | 8 | 16 | 16/12.7 | 10/22

## Slide 5: Design options using a RMM prototype cable
40 strands
1 mm diameter strands
1:1 Cu:Sc ratio
78% packing factor
5% cabling degradation

## Slide 6: Design 1
RMM prototype cable
10 mm bore tube
2 double pancakes
210 turns
9.8 kA
16.0 T bore field
10 % margin
18.2 T short sample field at 4.2K

## Slide 7: Design 1 - eRMC
RMM prototype cable
10 mm bore tube
1 double pancakes
110 turns
13.9 kA short sample current at 4.2 K
17.4 T short sample field at 4.2 K

## Slide 8: Design 2
RMM prototype cable
10 mm bore tube
2 double pancakes
170 turns
11.1 kA
16.0 T bore field
9 % margin
17.8 T short sample limit at 4.2K
 20 % gain in the # turns with an iron pole

## Slide 9: Design 2 - eRMC
RMM prototype cable
10 mm bore tube
1 double pancakes
90 turns
13.4 kA short sample current at 4.2 K
17.2 T short sample field at 4.2 K

## Slide 10: Design 3
RMM prototype cable
10 mm bore tube
3 pancakes
150 turns
11.0 kA
16 T bore field
10 % margin
17.8 T short sample limit at 4.2K

## Slide 11: Load-lines comparison
Chart: Bpeak [T]
| 21 | 20.5 | 20 | 19.5 | 19 | 18.5 | 18 | 17.5 | 17 | 16.5 | 16 | 15.5 | 15 | 14.5 | 14 | 13.5 | 13 | 12.5 | 12 | 11.5 | 11 | 10.5 | 10
Ic RRP 1.9K | 8.4571 | 9.9463 | 11.5791 | 13.3618 | 15.3011 | 17.4044 | 19.6796 | 22.1353 | 24.7811 | 27.6273 | 30.6853 | 33.9678 | 37.4884 | 41.2628 | 45.3081 | 49.6435 | 54.2905 | 59.2736 | 64.6204 | 70.3624 | 76.5357 | 83.1823 | 90.3506
Ic RRP 4.2K | 3.538 | 4.5294 | 5.6587 | 6.9316 | 8.3544 | 9.9338 | 11.677 | 13.5922 | 15.688 | 17.9738 | 20.4602 | 23.1587 | 26.0819 | 29.244 | 32.6606 | 36.3492 | 40.3297 | 44.624 | 49.2574 | 54.2586 | 59.6603 | 65.5005 | 71.8233
RMC | 17.5 | 19.5
FRESCA2 | 10.82 | 12.78 | 14 | 15.2
Design 1 | 10.1 | 0 | 9.8006 | 11.0467 | 12.1467
eRMC 1 | 12 | 0 | 12.5 | 13.9386 | 15.3421
Design 2 | 11.4 | 0 | 11.1074 | 12.3861 | 13.6383
eRMC 2 | 0 | 13 | 15.1424 | 16.6249 | 22
Design 3 | 0 | 10.5 | 11.8881 | 13.1194
10% margin

## Slide 12: Design options using grading
High Field (HF) cable:
40 strands
1 mm diameter strands
Width = 21.32 mm
1:1 Cu:Sc ratio
78% packing factor
5% cabling degradation
Low Field (HF) cable:
19 strands
1 mm diameter strands
Width = 10.13 mm = 21.26/2
1:1.5 Cu:Sc ratio
78% packing factor
5% cabling degradation

## Slide 13: Design 4
grading
10 mm bore tube
2 double pancakes in the HF region + 2 4-pancakes in the LF region
34+128=162 turns
10.9 kA
16.0 T bore field
Margins: 10% (HF) – 14% (LF)
short sample limits at 4.2K: 17.8 T (HF) – 15.0 T (LF)

## Slide 14: Load lines
Chart: Bpeak [T]
| 21 | 20.5 | 20 | 19.5 | 19 | 18.5 | 18 | 17.5 | 17 | 16.5 | 16 | 15.5 | 15 | 14.5 | 14 | 13.5 | 13 | 12.5 | 12 | 11.5 | 11 | 10.5 | 10
Ic HF 4.2K | 3.538 | 4.5294 | 5.6587 | 6.9316 | 8.3544 | 9.9338 | 11.677 | 13.5922 | 15.688 | 17.9738 | 20.4602 | 23.1587 | 26.0819 | 29.244 | 32.6606 | 36.3492 | 40.3297 | 44.624 | 49.2574 | 54.2586 | 59.6603 | 65.5005 | 71.8233
Ic LF 4.2K | 9.9111 | 11.1127 | 12.411 | 13.8127 | 15.3253 | 16.9571 | 18.7178 | 20.6183 | 22.6709 | 24.8902 | 27.2928
Ic HF 1.9K | 8.4571 | 9.9463 | 11.5791 | 13.3618 | 15.3011 | 17.4044 | 19.6796 | 22.1353 | 24.7811 | 27.6273 | 30.6853 | 33.9678 | 37.4884 | 41.2628 | 45.3081 | 49.6435 | 54.2905 | 59.2736 | 64.6204 | 70.3624 | 76.5357 | 83.1823 | 90.3506
Ic LF 1.9K | 11.6604 | 12.9077 | 14.2456 | 15.6799 | 17.2171 | 18.8645 | 20.6304 | 22.524 | 24.5557 | 26.7377 | 29.0836 | 31.6093 | 34.3332
Design 4 | 0 | 12 | 12.3934 | 13.7049 | 11 | 0 | 12 | 12.8687 | 14.0808 | 11
10% margin
15% margin
LF load-line
HF load-line

## Slide 15: Design options using grading
High Field (HF) cable:
29 strands
1 mm diameter strands
Width = 14.85 mm
1:1 Cu:Sc ratio
78% packing factor
5% cabling degradation
Low Field (LF) cable:
40 strands
0.7 mm diameter strands
Width = 14.85
1:1.2 Cu:Sc ratio
78% packing factor
5% cabling degradation

## Slide 16: Design 5
grading
5mm bore tube
2 double
19+68 = 87 turns
8 kA
16.0 T bore field
Margins: 10% (HF) – 22% (LF)
short sample limits at 4.2K: 17.4 T (HF) – 15.7 T (LF)

## Slide 17: Load Line
Chart: Bapplied (T)
| 19 | 18.5 | 18 | 17.5 | 17 | 16.5 | 16 | 15.5 | 15 | 14.5 | 14 | 13.5 | 13 | 12.5 | 12 | 11.5 | 11 | 10.5 | 10
LF, 4.2 K | 3.9664 | 4.7009 | 5.507 | 6.3875 | 7.345 | 8.3825 | 9.5033 | 10.7107 | 12.0085 | 13.4006 | 14.8913 | 16.4853 | 18.1876 | 20.0037 | 21.9397 | 24.0019 | 26.1976 | 28.5345 | 31.0212
HF, 4.2 K | 5.3352 | 6.323 | 7.4074 | 8.5917 | 9.8796 | 11.2752 | 12.7827 | 14.4068 | 16.1524 | 18.0249 | 20.03 | 22.1741 | 24.4638 | 26.9067 | 29.5107 | 32.2846 | 35.238 | 38.3813 | 41.7261
Design 5 (iron pole) | 8 | 10 | 12
Design 5 (iron pole) | 8 | 10 | 12
LF, 4.2 K | 3.9664 | 4.7009 | 5.507 | 6.3875 | 7.345 | 8.3825 | 9.5033 | 10.7107 | 12.0085 | 13.4006 | 14.8913 | 16.4853 | 18.1876 | 20.0037 | 21.9397 | 24.0019 | 26.1976 | 28.5345 | 31.0212
HF, 4.2 K | 5.3352 | 6.323 | 7.4074 | 8.5917 | 9.8796 | 11.2752 | 12.7827 | 14.4068 | 16.1524 | 18.0249 | 20.03 | 22.1741 | 24.4638 | 26.9067 | 29.5107 | 32.2846 | 35.238 | 38.3813 | 41.7261
Design 5 (iron pole) | 8 | 10 | 12
Design 5 (iron pole) | 8 | 10 | 12

## Slide 18: Protection

## Slide 19: Protection
Protection very challenging!
What are the requirements for RMM?
Protection with quench heaters and/or CLIQ + dump?
Design 4
If we want to protect only with a dump:
 |  | Design 3 | Design 4 | Design 5
MIITs to reach 300K | -- | 58 | 58/17 | 28/16
Max. Voltage | (kV) | 1 |  | 
Rdump for Vmax | (kJ/m) | 91 | 92 | 125
Time for detection + validation + dump effective | (MJ/m3) | 25 |  | 
MIITs discharge if "only dump" for 1 m length magnet | (A/mm2) | 59 | 55 | 35
 |  | Design 3 | Design 4 | Design 5
cu2sc | -- | 1 | 1/1.5 | 1/0.7
Ld | (mH/m) | 42 | 40 | 64
E | (kJ/m) | 2699 | 2500 | 2600
Ed | (MJ/m3) | 90.5 | 146 | 152
Jcu | (A/mm2) | 700 | 694/1217 | 702/953
Jeng | (A/mm2) | 350 | 347/730 | 351/520

## Slide 20: Protection
 | LHC MB dipole | DS-11T dipole | MQXF quadrupole
Field (T) /Gradient (T/m) | 8.3 | 11.2 | 132.5
Peak field in the conductor at Inom (Bp), T | 8.6 | 11.6 | 11.4
Engineering current density (Jeng), A/mm2 | 500 | 790 | 730
Stored energy at Inom, MJ/m3 | 60 | 130 | 110
Differential inductance at Inom, mH/m | 6.9 | 11.7 | 8.21
Magnetic length, m | 14.3 | 2 x 5.3 | 4x4.2/2x7.15
Temperature margin, K | 1.8-6.5 | 4.5-14.5 | 5.0-14.0
 |  | Design 3 | Design 4 | Design 5
cu2sc | -- | 1 | 1/1.5 | 1/0.7
Ld | (mH/m) | 42 | 40 | 64
E | (kJ/m) | 2699 | 2500 | 2600
Ed | (MJ/m3) | 90.5 | 146 | 152
Jcu | (A/mm2) | 700 | 694/1217 | 702/953
Jeng | (A/mm2) | 350 | 347/730 | 351/520

## Slide 21: Where are we?
[E. Todesco]
 |  | Design 3 | Design 4 | Design 5
w | (mm) | 96 | 69 | 69
B | (T) | 16 | 16 | 16

## Slide 22: Where are we?
[E. Todesco]
 |  | Design 3 | Design 4 | Design 5
w | (mm) | 96 | 69 | 69
Joverall | (A/mm2) | 221 | 254/497 | 254/352

## Slide 23: Where are we?
 |  | Design 3 | Design 4 | Design 5
Ed | (J/mm3) | 0.090 | 0.146 | 0.152
Joverall | (A/mm2) | 221 | 254/497 | 254/352
[E. Todesco]

## Slide 24: Summary
The “iron pole” solution is preferable, as the coil size can be reduced (for the case of no-grading by 20 %) keeping b3 saturation < 150 units.
Important decisions to be taken:
  Do we go for grading and “accelerator size” coil or known technology but big coil?
    If we go for grading:
      quench protection is a real issue! It will be difficult with the available strands to find a combination that provides enough margin in the load line and in terms of quench protection.
      3D magnetic analysis to start soon as it can have an impact on the 2D.
Next step:
  First iteration on mechanics for “Design 3” to define
    Minimum wall thickness of the bore
    Minimum outer magnet radius

## Slide 25: Additional slides

## Slide 26: Protection – Reference for comparison
 | LHC MB dipole | DS-11T dipole | MQXF quadrupole
Field (T) /Gradient (T/m) | 8.3 | 11.2 | 132.5
Peak field in the conductor at Inom (Bp), T | 8.6 | 11.6 | 11.4
Engineering current density (Jeng), A/mm2 | 500 | 790 | 730
Stored energy at Inom, MJ/m3 | 60 | 130 | 110
Differential inductance at Inom, mH/m | 6.9 | 11.7 | 8.21
Magnetic length, m | 14.3 | 2 x 5.3 | 4x4.2/2x7.15
Temperature margin, K | 1.8-6.5 | 4.5-14.5 | 5.0-14.0
Comparing to the Main Bending LHC dipoles:
High stored energy density
(compact winding for cost reduction)
Low stabilizer fraction
(to achieve the desired margins)
Large temperature margin
(use Nb3Sn as superconductor)
Main parameters for the high-field Nb3Sn magnets for the LHC luminosity upgrade.

## Slide 27: MIITs vs Tmax (Design 4)

## Slide 28: Longitudinal block position
Bp/Bo=1.09
Bp/Bo=1.03
Bp/Bo=0.957
Bp/Bo=0.997