## Slide 1
Review of peak power limits for high-luminosity IR triplet magnets
Daniel Schoerling
23rd of June 2017

## Slide 2
High luminosity IRs
 | MQXA | MQXB | MQXC | D1 | D2
Number of units | 8 | 16 | 8 | 12 | 12
G, B | 115 T/m | 94 T/m | 94 T/m | 1.97 T | 1.97 T
L | 15 m | 13.2 m | 15 m | 12.5 m | 12.5 m
Aperture | 190 mm | 240 mm | 240 mm | ~200 mm | ~70 mm
For the design of the 2 IRs (* = 0.3 m, L* = 45 m) a table with the quadrupole strength limit vs aperture has been established [1]
The separation and recombination dipoles D1 and D2 can be normal-conducting (an alternative design with 4-5 T dipole magnets to be evaluated)
Nested H/V orbit correctors with a field of 3 T, length 1.3 m, are proposed
Radiation and heat load limits:
  Peak power limit: 5 mW/cm3 (compare [2] and [3])
  Radiation limit: 30 MGy (baseline) and 250 MGy (ultimate)
  Displacement-Per-Atom (DPA) limit: 3.5  10-3 (Ti-doped, limit under discussion)
  55 mm tungsten shielding (baseline) and 15 mm (ultimate) fulfil the limits (cooling, DPA, aperture, activation to be confirmed, see simulations [4])
Reduction of aperture for thin shielding to be evaluated
Alternative IR design under study (baseline to be decided)
[1] E. Todesco in CAS-CERN Accelerator School, Erice, Italy, 24 April – 4 May 2013, CERN–2014–005 (CERN, Geneva, 2014); here was assumed: Nb3Sn , 25% NCu in the coil cross-section, 20% load line margin, 15% below the maximum achievable gradient
[2] M. La China and D. Tommasini, Phys Rev STAB 11, 082401 (2008)
[3] P.P. Granieri, IEEE Trans. Appl. Supercond., Vol. 24, No. 3, June 2014;
[4] M.I. Besana, 28. April 2017, FCC-hh magnet-beam dynamics coordination meeting 02
Aperture | G
(mm) | (T/m)
72 | 249
100 | 193
120 | 166
140 | 149
160 | 133
180 | 120
200 | 110
220 | 102
240 | 94
260 | 88

## Slide 3
Introduction
Porous (typically for Nb-Ti windings) and non-pourous insulation feature very different heat transfer
[1] M. China and D. Tommasini, Phys. Rev ST Accel. Beams 11, 082401 (2008), pdf

## Slide 4
Heat transfer curves
In non-permeable insulations, in fact, the maximum drainable heat is directly related to temperature margin. In permeable insulations, instead, a relatively big heat transfer can be reached with small temperature margin, as revealed by the steep initial slope of the permeable insulation curves (LHC and enhanced)
In Nb3Sn coils the only thermal path available is through the insulation material. The underlying assumptions are:
  longitudinal heat transfer is negligible;
  heat is evacuated through the cable small face;
  thermal boundary resistance at the strand-epoxy interface is negligible;
  strand and external bath are isothermal.
[1] M. China and D. Tommasini, Phys. Rev ST Accel. Beams 11, 082401 (2008)

## Slide 5
Temperature margin in HL-IR triplets
Temperature margin for triplets is around T = (6.4-1.9) K = 4.5 K
Chart: B in T
Load line | 0 | 1710.0617 | 2137.5771
 | MQXA | MQXB | MQXC | D1 | D2
Number of units | 8 | 16 | 8 | 12 | 12
G, B | 115 T/m | 94 T/m | 94 T/m | 1.97 T | 1.97 T
L | 15 m | 13.2 m | 15 m | 12.5 m | 12.5 m
Aperture | 190 mm | 240 mm | 240 mm | ~200 mm | ~70 mm

## Slide 6
Temperature I/III
In [1], Tab. IV, last column, 26 mW/cm2, assuming that one side of the coil (double-layer) is cooled and the cable height is 1.5 cm one finds 26/1.5 mW/cm3 = 17.3 mW/cm3 for a T = 1.52 K
If we allow us to use a budget of T = 0.5 K, we find a maximum average allowed heat deposition of ~5.7 mW/cm3 (this is the average heat deposition over the cable assuming that the heat transfer between the strands of the cables is good)
We assume that the heat transfer inside the cable is good: seems justified; see next slide
[1] M. China and D. Tommasini, Phys. Rev ST Accel. Beams 11, 082401 (2008), pdf

## Slide 7
Temperature II/III
For CTD101 (baseline impregnation for FCC-hh), we find under the same assumptions as before: 0.25 W/(14 cm * 1.51 cm * 0.19 cm) = 60 mW/cm3, T = 3.2 K. However, this sample was cooled from two sides, so 60 mW/cm3 /(2 * 3.2 K) = 9.4 mW/(cm3.K) for one side cooling. So we would find a value of ~5 mW/cm3 for an allowed temperature increase of T = 0.5 K. Here, we assumed that no heat transfer through the adjacent cables took place.
[1] P.P. Granieri, L. Hincapié, R. van Weelderen, IEEE Trans. Appl. Supercond., Vol. 24, No. 3, June 2014, pdf
Sample instrumented before impregnation
Measured temperature difference between cable and bath as a function of the power generated in the central conductor, in a He bath at 1.9 K. The temperature sensors were installed before impregnation, in the cable center and edge. The lines are a guide to the eye [2].

## Slide 8
Temperature III/III
A thermal analysis and its experimental verification for the present and future IR triplets (HL-LHC) has been performed by A.V. Zlobin [1]
Temperature margin 6.6 K (Tc0 = 18 K in EuroCirCol Tc0 = 16 K) at 17% loadline margin: 40 mW/cm3/6.6 K= 6 mW/K.cm3  0.5 K limit: 3 mW/cm3
[1] A. Zlobin, Thermal analysis and its experimental verification for the present and future IR triplets, Workshop on beam generated heat deposition and quench levels for LHC magnets, 3-4 March, 2005, CERN, Switzerland
Chart: Iop/Ic
| 0.75 | 0.8 | 0.85 | 0.9 | 0.95
MQXB_NbTi | 13.152 | 11.3687 | 10.0312 | 8.2479 | 6.4646
IRQ90_Nb3Sn | 44.0171 | 41.453 | 39.3162 | 36.3248 | 33.3333 | 30.3419 | 26.9231
Calculated quench limit for Nb3Sn IRQ and NbTi MQXB (inner-layer mid-plane turns) wrt the radiation heat depositions vs. the critical current margin at Top=1.9 K.

## Slide 9
Conclusion
Allowing to use a temperature budget of 0.5 K out of ~4.5 K one finds a maximum allowed average power density of ~3-5 mW/cm3
The final value depends on the insulation thickness and material, the cooling method, the number of layers (inter-layer cooling?) and the distribution of the energy deposition.
A detailed study shall be performed once a design is available
If the temperature budget of 0.5 K is used, the load line margin is reduced from 20% to 18.8%, the current margin is reduced from 0.56 to 0.54
Chart: B in T
Load line | 0 | 1710.0617 | 2137.5771