## Slide 1: First Experimental Results on Damage Limits of Superconducting Accelerator Magnet Components due to Instantaneous Beam Impact
V. Raginel, M. Bonura, D. Kleiven, K. Kulesz, M. Mentink, R. Schmidt, C. Senatore, A. Siemko, A. Verweij, A. Will, and D. Wollmann
7th HL-LHC Collaboration Meeting, 13.-16.11. 2017, CIEMAT Madrid

## Slide 2: Motivation of the study – HL-LHC ultra-fast failure
Injection kicker magnet
Injection absorber
Superconducting magnet
particle shower
Quench ! Damage ?
One such event per year in today’s LHC. No damage.
For HL-LHC beam, peak energy deposition of 100 Jcm-3 in the D1 magnet without mask [1] – similar in Q5 in case of asynchronous beam dump [2].
Will the magnets survive?
What are the damage mechanisms and limits of superconducting magnets ?
LHC BEAM
Injection Failure LHC
[1] A. Lechner et all, Protection of superconducting magnets in case of accidental beam losses during HL-LHC injection, In Proceedings of IPAC15
[2] B. Auchmann et all, Quench and Damage Levels for Q4 and Q5 Magnets near Point 6, CERN EDMS 1355063, 2014
Notes: Will the magnet survive? = Will it be still operational after beam impact?

## Slide 3: Beam – matter interaction
Damage experiment on solid copper
Burkart, F., et al. Journal of Applied Physics 118.5 (2015): 055902.
The fast (μs) interaction of an high energy beam with matter leads to:
  Temperature rise Ieading in the worst cases to phase transition (melting, vaporization, plasma ….).
  Dynamic stresses that can lead to extended mechanical damage - deformations, cracks.

## Slide 4
Reduction of the Jc induced by:
  High temperature
  Mechanical stress, deformation and cracks
Magnets most sensitive parts
Nb3Sn RRP type (HL-LHC triplet)
Nb-Ti strands (LHC dipole)
200 μm
200 μm
Decomposition of the polyimide when expose to high temperature
  Reduction of the dielectric strength
Nb-Ti and Nb3Sn superconducting cables
Fessia, P., et al. IEEE Transactions on Applied Superconductivity 20.3 (2010): 1622-1625.
Polyimide insultation

## Slide 5
Polyimide insulation degradation due to heating over hours [1]
  Cable stacks heated over hours in furnace between ~460 K and ~860 K.
  Polyimide dielectric strength measured with high voltage.
Jc degradation of Nb-Ti and Nb3Sn due to heating over seconds [2]
  Nb-Ti and Nb3Sn single strands heated up between ~640 K and ~1250 K using a capacitive discharge.
  Strand were in air at room temperature.
  Jc degradation measured via magnetization measurements
  Identification of degradation mechanisms via microscopic analysis
Degradation of polyimide insulation and of Nb-Ti & Nb3Sn critical current density induced by impact of a 440 GeV proton beam
Experimental Road Map
[1] V. Raginel, et al, “Degradation of the insulation of the LHC main dipole cable when exposed to high temperatures”, IPAC’16
[2] V. Raginel, et al, “Change of critical current density in Nb-Ti and Nb3Sn strands after millisecond heating”, IPAC’17

## Slide 6: Beam Experiment: Samples
At CERN HiRadMat facility sending 440 GeV proton beam pulses on:
Samples at room temperature within an inert atmosphere (Argon).
30 Nb-Ti cables
~ 5 cm
Nb-Ti & Nb3Sn strands

## Slide 7: Experimental setup
Second Picture with the tank open
Nb-Ti cable stacks
in steels moulds
Nb-Ti and Nb3Sn strands fixed on a steel plate

## Slide 8: Experimental setup
Second Picture with the tank open
6x1011 p+
2.6x1012 p+
1.3x1012 p+
p+
933 K 1026 K
1035 K
823 K
445 K
706 K
882 K
960 K
V. Raginel, D. Wollmann

## Slide 9: Polyimide insulation degradation
Degradation due to chemical decomposition as function of temperature and exposure time.
No degradation measured after beam impact – temperature up to ~1050 K (2.5 kJ cm-3) for few ~ms
  Weakening of the insulation at the point of the beam impact was observed for T > 850 K (1.9 kJ cm-3).
beam impact
Side view of a Nb-Ti cable stack after beam impact

## Slide 10: Jc degradation of Nb-Ti
ΔM ∝ Jc x df
Fp = Jc x B
b = B / Bc2(T)
@ 6 K
@ 6 K
@ 6 K
@ 6 K
Capacitive discharge
Beam impact
Capacitive discharge, ΔM degradation (∝ Jc) above 651 K
After beam impact, ΔM degradation above 878 K (2.2 kJ cm-3)
Fp decrease and Fpmax shifts toward lower b.
Change of pinning behaviour
Decrease of Bc2(T) for T ≥ 916 K in discharge case. No decrease for beam case.
Variation of Ti content in filaments

## Slide 11: Jc degradation of Nb-Ti
* C. Scheuerlein et all., Journal of Physics: Conference Series, vol. 234, no. 2. IOP Publishing, 2010
*
@ 4 K and 5 T
At T=1157 K (discharge case), filament merging is observed
Jc decreases with increasing exposure time
Diffusion process & change of pinning behaviour
Degradation of Jc caused by variations of α-Ti precipitates size and spacing
If higher temperature or longer exposure time, Ti diffuses outside filaments to form Cu-Ti compound => Bc2(T) reduction, filament merging
Ref
1157 K
Nb-Ti

## Slide 12: Jc degradation of Nb3Sn
Capacitive discharge, Jc degradation for T > 823 K
All samples degraded after beam impact, T ≥ 699 K (1.4 kJ cm-3)
Fp decrease and no shift of Fpmax
No change of pinning behaviour
No grain growth observed (SEM analysis)
Decrease of Bc2(T) not observed, however Tin content measurements are planned
Capacitive discharge
Beam impact
@ 15 K
@ 15 K
@ 15 K
@ 15 K
Ref.
1264 K

## Slide 13: Jc degradation of Nb3Sn
@ 4 K and 5 T
Contrary to Nb-Ti, Jc decreases with decreasing exposure time
Indication degradation due to beam impact is dominated by stresses and potentially cracks caused by fast heating and high thermal gradients
Further investigations to identify the origin

## Slide 14: Conclusions and Outlook
Polyimide insulation
  No degradation induced by beam up to 1050 K, however observation of a weakening for T > 850 K (1.9 kJ cm-3)
  Chemical decomposition due to exposure to high temperature
Nb-Ti strands
  Jc degradation for peak temperatures above 900 K (2.2 kJ cm-3) in case of (single) beam impact
  Degradation dominated by diffusion processes
Nb3Sn strands
  Jc degradation due to beam impact observed in all samples – lowest peak temperature 700 K (1.4 kJ cm-3)
  Grain growth is excluded. Further investigations to identify degradation mechanism
  Probably caused by stresses and cracks induced by the fast heating and high thermal gradients
Experimental validation of results with beam at liquid Helium temperature scheduled for mid-2018

## Slide 15: Acknowledgements
TE/MPE: R. Denz, F. Boisier, F. Rodrigues-Mateos, J. Mourao, M. Favre, M.J. Bednarek, B. Auchmann, M. Valette
TE/MSC : C. Scheuerlein, A. Ballarino, D. Richter, A. Bonasia, S. Luzieux, G. De Rijk, N. Bourcey, D. Tommasini, R. Lopez, P. Fessia
TE/VSC: G. Bregliozzi, J. Finelle
BE/RF: G. Mcmonagle, G. Ravida
HiRadMat team: A. Fabich, A. Bouvard, V. Clerc
EN/MME: M. Guinchard, O. Sacristan Frutos, M. Meyer, S. Sgobba
EN/STI: D. Grenier, A. Lechner

## Slide 16
Thank you for your attention!
Questions?

## Slide 17
Spare slides

## Slide 18: Insulation degradation due to hours heating
~7 hours
Insulated cable stacks heated over hours in furnace between 461 K and 864 K in inert atmosphere (Argon).
Dielectric strength is measured via cable-to-cable breakdown voltage measurement after heat treatment.
Vivien Raginel
Stack of 6 Nb-Ti cables
25 cm