## Slide 1: High Order Correctors status
Marco Statera
on behalf of the LASA team
INFN Milano - LASA
7th HL-LHC Collaboration Meeting
CIEMAT, Madrid – 15 November 2017

## Slide 2: OUTLINE
Introduction
Status of work progress
  MCOXFP1 construction and test
  MCDXFP1 construction and test
  next prototypes design and production status
Integration
MgB2 demonstrator status
Test cryostat for next prototypes and for series production
Conclusions and next steps

## Slide 3: SCOPE
The INFN-LASA follows the design, construction and test of the 5 prototypes of the High Order (HO) corrector magnets for the HL interaction regions of HL-LHC
This activity is founded by INFN (Magix “activity”), and with an agreement CERN contributes for about 50%
The INFN-LASA will follow the series production of the HO corrector magnets for the HL interaction regions of HL-LHC

## Slide 4: THE LOW BETA SECTION AND THE HIGH ORDER CORRECTORS
a2
73.6 m
IP
by P. Fessia
b6
a6
b5
a5
b4
a4
b3
a3

## Slide 5: HO CORRECTOR MAGNETS ZOO
MCDXFP1
a2
a3
b3
a4
b4
a5
b5
a6
b6
MCTXFP1
MCOXFP1
MCSXFP1
MQSXFP1
MgB2
round coil
Tested 2016
OD460
From 6-pole to 12-pole magnets exist in both normal and skew form
NbTi superconducting coils
superferric design
60% margin @ 1.9 K
existing power supplies
no energy extraction (but 4P)
OD320
Tested 2017
Tested 2017
Tested 2016

## Slide 6: MCOXFP1 - THE OCTUPOLE
MCDXFP1
a2
a3
b3
a4
b4
a5
b5
a6
b6
MCTXFP1
MCOXFP1
MCSXFP1
MQSXFP1
MgB2
round coil

## Slide 7: MCOXFP1
 | nominal | design
length | 160 mm | 183 mm
integrated field @ Iop @ r50 mm | 46 Tmm | 46 Tmm
magnetic length | 87 mm | 99 mm
energy @Iop | 1.4 kJ | 1.07 kJ
harmonics |  | B12=11.6 B20=-3.0
DURATRON
PEI U2300 coils
electrical connections redesigned
183 mm
OD 320 mm

## Slide 8: MCOXFP1 ASSEMBLY 1
assembly procedure
same as 6pole
new electrical connections
spacers
fixed longitudinally
wedges in position
the wedges are fixed
two printed circuit boards
coils’ connections
signals
Copper 2 mm wide
0.035 mm thick
lamination
alignment frame
CuBe rods

## Slide 9: MCOXFP1 ASSEMBLY 2

## Slide 10: MCOXFP1 COILS
single coil’s cold test:
2 training quenches
reached short sample sample 247 A
nominal current
s.s.l.
B1 | M08-01
B2 | M08-08
B3 | M08-07
B4 | M08-06
B5 | M08-09
B6 | M08-10
B7 | M08-11
B8 | M08-12
heigth
inner long
outer long
inner short
outer long
12 coils produced
coils’ assessment
Geometry
6pole average s 0.09 mm
8pole average s 0.13 mm
Resistance
number of turns
HV insulation
all coils above 1.8 TW at 5 kV
HCMCOXFC01-I1000001

## Slide 11: HEATERS
Two heaters are installed
DURATRON thickness reduced by hand in coil B5
A Φ 2 mm Aluminum nitride (AlN) ceramic insert in one hole of coil B6
quench induced at 4.2 K, I= 73 A
AlN
1 mm thick
By INTELLION S.a.r.l.
4.4 J
10.1 J

## Slide 12: MCOXFP1 GROUND INSULATION
10 uA limit
MCOXFP1 as assembled

## Slide 13: 8POLE TEST
qualification @ 4.2 K
qualification 1h @ 108% @2.17 K
training @4.2 K
working condition test
w/o energy extraction
thermal cycle
qualification @ 4.2 K

## Slide 14: 8POLE COLD TEST RESULTS
stable at ultimate current (108% Inom) and at 150% Inom
26 quenches – Imax= 207 A (89.2 % s.s.l.)

## Slide 15: QUENCH SEQUENCE
Not all coils had training
Single tested coil (B1) has training I> 150% Inom
No evidence of induced quench effect
B1
7
4
4
3
7
3
5
7
4
1
7
3
8
3
3
1
1
1
3
1
7
8
7
8
8
7
B2
B3
B4
B5
B6
B7
B8
H
H

## Slide 16: 8POLE COLD TEST RESULTS - 2
He II test: 2.17 K
1h @ 108% Inom (114 A)
1h @ 150% Inom (158 A)
no quenches occurred
qualification
1h@ 108% In
1h@ 150% In
tests @ 4.2 K
full training: Imax 89% of s.s.l.
working condition test
qualification @4.2 K after a thermal cycle

## Slide 17: QUENCH PROTECTION IN LHC
Protection in LHC
  Existing power supplies
  Measuring current
  Time range 60-180 ms
  Max current: ultimate current (114 A)
Protection at LASA
  Total voltage and differential voltage (half magnet)
  Quench induced by heater (and AlN insert)

## Slide 18: QUENCH PROTECTION (no ENERGY EXTRACTION)
200 ms
training
no dump
tuning of the simulation by QLASA
  inductance
  current decay
  voltages
time
  Quech induced by heater (and AlN insert)
  threshold up to 5.0 V
  total time before relay opening: 145 ms
  DI = 8 A @ 145 ms PS dependent

## Slide 19: PRELIMINARY FIELD MEASUREMENT
preliminary measurement of the field
single point
in front of a pole
radius of 50±1 mm (correction applied)
reproducible
5 mT
saturation 30 A
complete measurement at CERN (2017?)

## Slide 20: MCDXFP1 THE DECAPOLE
MCDXFP1
a2
a3
b3
a4
b4
a5
b5
a6
b6
MCTXFP1
MCOXFP1
MCSXFP1
MQSXFP1
MgB2
round coil

## Slide 21: MCDXFP1 10POLE
COILS
  Updated BTS2 Arisawa design
  Hybrid BTS2/DURATRON
Improved electrical connection design, pcbs supporting and integration with connection box
 | nominal | design
length | 172 mm | 183 mm
integrated field @ Iop @ r50 mm | 25 Tmm | 26 Tmm
magnetic length | 95 mm | 97 mm
harmonics |  | B15=11.6 B25=-0.7
5 coils BTS2
5 coils hybrid
M. Todero and D. Pedrini
183 mm

## Slide 22: MCDXFP1 COILS’ ASSESSMENT
Geometry
8pole average s 0.13 mm
10pole average s 0.11 mm
Resistance
number of turns
HV insulation
(Al wrap) all coils above 36 GW at 2.5 kV
current [A]
100
200
300
event number
1
3
5
provoked
Inom
Iult
s.s.l.
98% of coils’ s.s.l.
Single coil test
B1 | M10-05
B2 | M10-08
B3 | M10-09
B4 | M10-11
B5 | M10-13
B6 | M10-06
B7 | M10-10
B8 | M10-12
B9 | M10-14
B10 | M10-15
BTS2
DURATRON
16 coils produced
4 batches
1st batch single coil test
and LHe cooldown
2nd batch LN2 cooldown

## Slide 23: MCDXFP1 GROUND INSULATION
10 mA limit
MCDXFP1 as assembled

## Slide 24: THERMAL CYCLES
temperature
Cooldown in about 1 day
  Nitrogen heat exchanger
Warmup in about 1 week
  Standard warming speed below 10 k/h
  Using heaters 30-40 K/h (temperature range 20 K -60 K )
hours
hours

## Slide 25: MCDXFP1 TEST
Week 1
  4.2 K 1h @ Iult , 121 A (115% Iop)
  2.17 K 1h @ Iult , 121 A
Week 2
  4.2 K 1h @ Iult , 121 A (115% Iop)
  no energy extraction quench test
  (operating conditions simulation)
  training

## Slide 26: MCDXFP1 QUENCH SEQUENCE
One provoked
One 98 A quench
Ultimate 114 A -1 h test (4.2 K and 2.17 K)
Reached 100% S.S.L at 4.2 K
event number
B3-B4
B3-B4
B7-B8
B9-B10
B3-B4
B3-B4

## Slide 27: QUENCH vs COILS TECHNOLOGY
Quench detection detects 2 coils
Quench heater on coil B3 (3 provoked)
4 quenches on B3-B4
1 quench on B7-B8
1 quench on B9-B10
B1 | M10-05
B2 | M10-08
B3 | M10-09
B4 | M10-11
B5 | M10-13
B6 | M10-06
B7 | M10-10
B8 | M10-12
B9 | M10-14
B10 | M10-15
BTS2
DURATRON
4
1
1
No sensitive difference between coils’ technology

## Slide 28: SINGLE POINT MAGNETIC FIELD
Single Hall probe
rref= 50 mm
Errors not shown
4.2 K and 2.17 K
4.2 K after thermal cycle
O simulations
Good reproducibility
Harmonic measurements
at CERN (2017?)

## Slide 29: QUENCH PROTECTION SYSTEM UPGRADE
2 IGBTS working in parallel
Same components as 10 kA switch (by A. Paccalini and M. Quadrio)
<1 ms
15 ms
trigger

## Slide 30: QUENCH PROTECTION (no ENERGY EXTRACTION)
Protection in LHC
  Measuring current
  Time range 60-180 ms
  Max current: ultimate current (114 A)
Protection at LASA
  Quech induced by heater (and AlN insert)
  Increase validation time
  Reached 120 ms and 140 ms at ultimate current
MCDXFP1 survived

## Slide 31: AFTER THERMAL CYCLE
Detailed inspection on one side
One defect on coil M10-14
No detached wedges

## Slide 32: NEXT STEPS: MCTXFP1 AND MCQSXFP1
MCDXFP1
a2
a3
b3
a4
b4
a5
b5
a6
b6
MCTXFP1
MCOXFP1
MCSXFP1
MQSXFP1
MgB2
round coil

## Slide 33: DODECAPOLE MCTXFP1
Normal (Skew) | nominal | simulation
length plate to plate | 514 mm (166 mm) | 575 mm (200 mm)
integrated field @ Iop @ r50 mm | 0.086 Tm (0.017 Tm) | 0.086 Tm (0.017 Tm)
magnetic length | 430 mm | 471 mm
energy @Iop | 4.35 kJ | 7,78 kJ
harmonics @Iop |  | B18= -6.2 B30= -3.5
connections
at LASA
connections
box
at CERN
PCB boards
OD320
575 mm
coils
432 windings
F 0.5 mm NbTi
500 mm long
Full BTS2 technology

## Slide 34: SKEW QUADRUPOLE MCQSXFP1
Iop=182 A - f 0.7 mm NbTi
protection: 1.5 W dump
50% energy extracted
 | nominal | simulation
length plate to plate | 903 | 814
integrated field @ Iop @ r50 mm | 1.0 Tm | 1.016 Tm
magnetic length | 807 mm | 671 mm
energy @Iop | 24 kJ | 36 kJ
The poles are modified hyperbolas
B(@z=0,r=50 mm) = 1.5 T
Transfer Function
8.86 Tm/kA ÷ 5.58 Tm/kA
saturation at ~0.3 I/Inom
harmonics
B6= -30 U at low current
B6= 30 U at Iop
B10= -8 U ÷ -12 U
754 windings
f 0.7 mm NbTi
OD 460 mm
Modified holes for Heat Exchanger

## Slide 35: DELIVERY AND TEST
Tender approved by INFN
contract sent to company – arrived 4 weeks later
Start end of October (T0)
Updated schedule
  4/6/2018 MCTXFP1 delivered to LASA
  (T0 + 7 months)
  4/9/2018 MCQSXFP delivered to LASA
  (T0 + 10 Months)
Test at LASA 2 months

## Slide 36: INTEGRATION
Cold mass
Magnet length vs magnetic design
Position in the cold mass
Alignment
Electrical connections (box definition and position)
Fix threads and nuts by resin (CTD 101K) and anti vibration washers
Position and diameter for the Heat Exchanger (MCQSXFP)
Power supply and protection
Reduction of nominal current 134 A -> 105 A
  But MCQSXFP1 (4P)
  MCSXFP1 (6P) to be updated (no major changes)
Quench protection w/o energy extraction in LHC
Documentation
All produced magnets are in MTF/EDMS
Test reports and test summaries
Acceptance procedures
Workflow
MIPs in preparation

## Slide 37: QUENCH PROTECTION
No dump | Quadrupole | Sextupole Inom=134 A | Octupole | Decapole | Dodecapole
Peak voltage to ground | 633 V | 135 V | 70 V | 36 V | 251 V
Hot spot temperature | 132 K | 164 K | 131 K | 122 K | 147 K
4P | Ground at magnet end | Ground at half dump | Ground at half magnet
0 Ω | 633 V | 633 V | 422 V
0.5 Ω | 474 V | 447 V | 316 V
1 Ω | 407 V | 357 V | 271 V
1.5 Ω | 358 V | 287 V | 238 V
QLASA simulations by V. Marinozzi
Room Temperature test
Vtest=(2 x Vmx + 500) x2
HO correctors tested
Vtest 1.5 kV at RT
But 4P
6p to be reviewed

## Slide 38: GROUND INSULATION
10 mA limit
MCDXFP1
MCSXFP1
MCSXFP1 20 months
MCOXFP1

## Slide 39: ROUND COIL MAGNET
Demonstrator
Mechanics design ongoing
Winding machine done
mould construction done
First batch of insulated MgB2 wire delivered at LASA
demonstrator
Fe
Fe
coil
100 mm
f 380
C. Uva
M. Todero and D. Pedrini

## Slide 40: ROUND COIL MAGNET II
SCHEDULE
Winding MgB2 wire in 2017
Impregnation in 2017
Cold test of the coil 1Q2017
Magnet assembly 2Q 2018
Test Cu coil
M. Quadrio and A. Paccalini

## Slide 41: NEW CRYOSTAT
Cryostat for testing MCTXFP1 (12P), MCQSXFP1 (4P) and series magnets
520 mm inner diameter
About 3 m cold volume (with top flange insulation)
Up to 4 magnets (3 possible configurations)
Flange modification, thermal insulation, magnet support, room temperature connections.
Ordered end 2017
HE inlet
Mag.meas.
Safety
Valve and disk
Connections X3
CL
2+4

## Slide 42: TEST CONFIGURATIONS
Prototypes
Single magnet test
Series production
3 batches
  18 magnets
  2X12P 2X4P
  5 cooldowns
600
2350
12P
4P

## Slide 43: TEST STATION UPGRADE
New cryostat all components ordered
New main switch for power supply (fast solid state switch, Dt<1 ms) DONE
New power supply for magnet test (200 A, 50 V)
ORDER ONGOING
New acquisition system for test monitoring
ORDER ONGOING
Installation of system for magnetic measurement at low/room temperature (supplied by CERN)

## Slide 44: CONCLUSIONS
magnet |  | assembly | Cold test | Field measurement
MCSXFP1 | 6P | 2015 | 2016 | 2016
MCOXFP1 | 8P | 2016 | 2017 | 2017?
MCDXFP1 | 10P | 2017 | 2017 | 2017?
MCTXFP1 | 12P | 2018 | 2018 | 2018
MCQSXFP1 | 4P | 2018 | 2018 | 2018

## Slide 45: CONCLUSIONS AND NEXT STEPS
MCOXFP1
  Tested
MCDXFP1
  Assembled
  First cooldown and thermal cycle results
MCQSXFP1 and MCTXFP1: 2018
MgB2 RCSM
  Winding end 2017
  Test 2018
New cryostat (MAGIX)
  Flange and magnet support 1Q 2018

## Slide 46
THANK YOU
LASA team
F. Alessandria, G. Bellomo, F. Broggi, S. Mariotto, A. Paccalini, D. Pedrini, A. Leone, V. Marinozzi, M. Quadrio, M. Sorbi, M. Statera, M. Todero, C. Uva

## Slide 47
SPARE

## Slide 48: MCOXFP1 COILS - spares
4 parts
machined from bulk
0.15 mm BTS2
1.05 mm BTS2
1.3÷1.5 mm DURATRON
>1 mm BTS2 – new design
machined from bulk