## Slide 1: Coating studies on 6 GHz seamless cavities
FCC Week 2018, Amsterdam, 12th April 2018
Cristian Pira Giovanni Caldarola, Eduard Chyhyrynets,
Vincenzo Palmieri, Fabrizio Stivanello, Ruggero Vaglio
In the framework of CERN-INFN-STFC Agreement N. KE2722/BE/FCC

## Slide 2: Outline
Q-slope problem and LNL approach
Deposition Set Up
Process Parameters
Results

## Slide 3: Q-slope problem

## Slide 4: LNL Approach
High temperature
Thick films

## Slide 5: Thick film motivation
Q-slope is related to local enhancement of the thermal boundary resistance at the Nb/Cu interface, due to poor thermal contact between film and substrate
Theoretical model from Vaglio and Palmieri
V. Palmieri and R. Vaglio, Supercond. Sci. Technol., vol. 29, no. 1, p. 015004, Jan. 2016
Copper cavity
Nb thin film

## Slide 6: Thick film motivation
Q-slope is related to local enhancement of the thermal boundary resistance at the Nb/Cu interface, due to poor thermal contact between film and substrate
Theoretical model from Vaglio and Palmieri
V. Palmieri and R. Vaglio, Supercond. Sci. Technol., vol. 29, no. 1, p. 015004, Jan. 2016
Copper cavity
Copper cavity
Nb thin film
Nb thick film

## Slide 7: Thick films increase grain dimensions and RRR
EBSD Micrograph of cavity #4,
courtesy of Reza Valizadeh (STFC)
Grain dimension ≈1μm
RRR > 60
20μm
Cu
Nb

## Slide 8: High Temperature Deposition Motivation
Thorton SZ Diagram J.A. Thornton and D.W. Hoffman, Thin Solid Films, vol. 171, no. 1, pp. 5–31, 1989
CERN (550 °C) C. Benvenuti et al., Physica B 197 (1994) 72-83
LNL Alpi Linac (300-500 °C) Stark et al., Proceedings of SRF1997
Hie-Isolde (650 °C) Sublet et al., Proceedings of SRF2013

## Slide 9: 6 GHz cavity coating protocol (2 weeks per cavity)
Spinning
Degreasing
Mechanical Grinding
EP + SUBU
HP Rinsing
Cleanroom Vacuum Assembling
48 h Baking 600 °C
7 h PVD process
HP Rinsing
Cleanroom RF Assembly
4,2 K RF Test
1,8 K RF Test

## Slide 10: Deposition Set Up
6 GHz cavity
IR Lamp
Nb Post Magnetron Target
Quartz sample
Thermocouple

## Slide 11: Process parameters
Temperature = 550 °C (baking 600 °C)
Base pressure < 2 • 10-9 mbar (room T)
Ar Pressure = from 7 • 10-3 to 5 • 10-2 mbar
Current = 1 A (0,017 A/cm2)
Magnetic Field = 830 Gauss
Deposition Rate = 2,5 - 3 nm/s
Bending of the flange at 650 °C

## Slide 12: Deposition parameters optimization
Pressure
Multilayer

## Slide 13: Pressure
7 · 10-3 mbar
9 · 10-3 mbar
2 · 10-2 mbar
5 · 10-2 mbar
300 °C
Test on kapton foil
Bending as a function of a pressure

## Slide 14: Pressure
7 · 10-3 mbar
9 · 10-3 mbar
2 · 10-2 mbar
5 · 10-2 mbar
300 °C
Test on kapton foil
Bending as a function of a pressure

## Slide 15: Multilayer
DC ON
DC OFF
30 %
Time = 9 - 10 h
70 %
Deposition Rate = 3 nm/s
Total Thickness (on the cell) = 70 µm
Single Layer Thickness = 100, 300, 400, 500 nm

## Slide 16: Pressure
5 • 10-2 mbar
7 • 10-3 mbar
Zero stress pressure helps to increase accelerating gradient
6 GHz @ 4,2 K
6 GHz @ 1,8 K

## Slide 17: Multilayer
One shot deposition
Multilayer
Deposition
Multilayer process helps to increase accelerating gradient
6 GHz @ 4,2 K
6 GHz @ 1,8 K

## Slide 18: Results interpretation
Sputtering pressure and multilayer deposition reduce film stress
Film stress reduction reduces film peeling and voids dimension at the interface
How to explain low reproducibility?

## Slide 19: Cavity surface after spinning

## Slide 20: After Mechanical Finishing (grinding)
With mechanical grinding some areas of the cell are difficult to access

## Slide 21
Surface defects after chemistry

## Slide 22: Thick films help on Q-slope problem?

## Slide 23: Q-slope remains in many cavities…

## Slide 24: …but not in all ones!

## Slide 25: Conclusions and future actions
We explored the thick films deposition on Nb/Cu cavities
Strong Q-slope mitigation on 3 cavities
The technique is very promising but not mature
Improvements on cavity preparation process is mandatory
Film characterization from STFC

## Slide 26: Enzo Palmieri

## Slide 27: 8th International Workshop on Thin Films and New Ideas for Pushing the Limits of RF Superconductivity
October 8–10, 2018
Legnaro National Laboratories INFN
Legnaro (Padua) - Italy