## Slide 1
Results on the FCC-hh Beam Screen prototype at the KArlsruhe Research Accelerator (KARA)
Luis Gonzalez
LNF-INFN/CERN TE-VSC
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring
Task4.6: Measurements on cryogenic
beam vacuum system prototype
1
2
3
4
5
L.A. Gonzalez,1, 2
M. Gil Costa,3, 2 P. Chiggiato,2 V. Baglin,2 C. Garion,2 R.Kersevan,2 S. Casalbuoni,4 E. Huttel,4 I. Bellafont2,5 and F. Perez5

## Slide 2: Motivation of Experiment
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Validation of Simulation Techniques
used for the real machine
PSD
Reflectivity
Heat Load
Photoelectron Generation
CERN February 20th 2018
 | LHC - 0.58A 7TeV | FCC-hh - 0.5A 50TeV
SR power [W/m] | 0,2 | 35,2
Flux* ph/m/s | 4,2·1016 | 1,5·1017
Critical Energy | 44,2eV | 4,3 KeV
R.Kersevan; Beam Dynamics meets Vacuum, Collimations, and Surfaces Workshop. KIT, Karlsruhe. March 2017
*Photon energy above 4eV
1
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring

## Slide 3: Samples: FCC-hh Beam Screen Prototypes
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Prototype #1 July- Oct ‘17
Prototype #2 Jan- May ‘18
Prototype #3 June-Aug‘18
#1: Validation of temperature profile and validity of photon reflector
#2: #1 + Electrode for photoelectron current measurements
#3: Surface treatments as for baseline. Updated internal screen and pumping slots. Substitution Reflector for Sawtooth
CERN February 20th 2018
2
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring

## Slide 4: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
KARA
(KArlsruhe Research Accelerator)
Simulations performed with Synrad; M. Ady, R. Kersevan, M.Grabski, IPAC15. http://test-molflow.web.cern.ch/node/107
Ec FCC-hh = 4.2 KeV
Ec KARA = 6.2KeV
KARA reasonably resembles FCC-hh’s spectrum and linear power, and even at nominal beam energy (2.5 GeV) ANKA’s spectrum is a close match of that of FCC-hh.
CERN February 20th 2018
3
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring

## Slide 5: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
The Setup
Beam
BEam Screen Testbench EXperiment
BESTEX (Installation May 2017)
CERN February 20th 2018
6
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring

## Slide 6: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Irradiated length 1.8m
2m
KARA e-Beam
D-horizontal
D-vertical
2m FCC-hh Protoype
θ
CERN February 20th 2018
4
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring

## Slide 7: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
After collimation :
83% of Photon Flux Cropped
69% of Photon Power Cropped
 | KARA | FCC-hh
SR Flux | 8.7E+16ph/s | 1.5E+17ph/s
SR Power | 32W/m | 32W/m
Angle of Incidence | 18mrad | <2 mrad
Ec | 6.2KeV | 4.2KeV
CERN February 20th 2018
Beam Direction
5
1.8m
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring

## Slide 8: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Experimental Configurations
Ph Flux = 8.73E+16 Ph/s
Ph Flux = 1.44E+17 Ph/s
Geometry #1
Geometry #2
Geometry #4
Geometry #3
Ph Flux = 8.73E+16 Ph/s
Ph Flux = 1.44E+17 Ph/s
Injection @ FCC-hh
Normal operation of FCC-hh
Injection @ FCC-hh
Misalignment @ FCC-hh
CERN February 20th 2018
Power
Flux
7
Power
Flux
Power
Flux
Power
Flux
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring

## Slide 9: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
PSD Studies
Chimney Connection
Middle
BAG + RGA
Back End BAG
Front End BAG
Beam
CERN February 20th 2018
8
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring

## Slide 10: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Middle
Front
Back
CERN February 20th 2018
PSD Studies
Experimental Results Prototype #1
9
#1
#2
#3
#4
During Irradiation of Geom #1 Dynamic pressure decreases due to conditioning as photon dose increases
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring
Middle
Front
Back

## Slide 11: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Middle
Front
Back
CERN February 20th 2018
PSD Studies
Experimental Results Prototype #1
10
#1
#2
#3
#4
Middle
Front
Back
Levenberg-Marquardt Algorithm
X=-0.54 ± 0.01
X=-0.41 ± 0.01
X=-0.55 ± 0.01
During Irradiation of Geom #1 Dynamic pressure decreases due to conditioning as photon dose increases
For doses higher than 1x1022 ph/m the normalized pressures decrease linearly

## Slide 12: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
 | 2.5GeV/130mA |  |  |  |  | 
 | 3Ah |  |  | 9.5Ah |  | 
 | Experiment | Calculations | Rel Discrepancy % | Experiment | Calculations | Rel Discrepancy %
Middle (mbar) | 5.7E-09 ± 15% | 6.3E-9 | 9% | 3.0E-09 ± 15% | 3.3E-9 | 13.2%
Front (mbar) | 2.9E-09 ± 15% | 2.9E-9 | 1% | 2.0E-09 ± 15% | 1.6E-9 | 15%
Back (mbar) | 2.0E-09 ± 15% | 2.8E-9 | 29% | 1.0E-09 ± 15% | 1.4E-9 | 25%
PSD Studies
Experimental Results – Comparison with Calculations
Important aspects to take
into account for a realistic model
Not leak tight Chimney
Rounded reflector
…
11
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring

## Slide 13: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
PSD Studies
Experimental Results Prototype #1
12
#1
#2
#3
#1
#1
#2
#3
#4
At Geom #2 photon dose increases irradiating new areas away from the effect of the reflector - Normalized pressure increases
At Geom #3 normalized pressure continue the decreasing rate observed at #2 – Preconditioning of the inner chamber due to reflected photons
Back to Geom #1 the normalized pressure recovers the original decreasing trend
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring
Middle

## Slide 14: Experiment at KARA
At Geom #4, the pressure evolution indicates preconditioning of the inner chamber due to reflected photons during previous geometries
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
PSD Studies
Experimental Results Prototype #1
14
#1
#2
#3
#4
#4
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring
Middle

## Slide 15: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
PSD Studies
Experimental Results Prototype #2
15
#1
#2
#3
#1
#1
#2
#3
#1
#1
#2
#3
#4
At low doses, normalized pressure is about 100 times higher than for Proto#1 - Effect ascribed to the cold sprayed Cu and ceramics
The pressure increase at Geoms #2 and #3 is negligible
The effect of a large amount of photons reflected into the main chamber is now visible due to the presence of clearing electrode and ceramics
Back to Geom #1 the normalized pressure recovers the original decreasing trend
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring
Middle Prototype #2
Middle Prototype #1

## Slide 16: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
PSD Studies
Experimental Results Prototype #2
16
#1
#2
#3
#4
At low doses, normalized pressure is about 100 times higher than for Proto#1 - Effect ascribed to the cold sprayed Cu and ceramics
The pressure increase at Geoms #2 and #3 is negligible
The effect of a large amount of photons reflected into the main chamber is now visible due to the presence of clearing electrode and ceramics
Back to Geom #1 the normalized pressure recovers the original decreasing trend
Sample#1
Sample#2
Levenberg-Marquardt Algorithm
X=-0.54 ± 0.01
X=-0.98 ± 0.01
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring
Middle Prototype #2
Middle Prototype #1

## Slide 17: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Beam
CERN February 20th 2018
Reflectivity Studies
Experimental Equipment
RI=
17
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring
#1
#2
#3
#4

## Slide 18: Experiment at KARA
Photoelectron current measured at electrode
Comparison:
Straight vs Reflection
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
Reflectivity Studies
Experimental Results Prototype #1
RI=
18
2.4%
0.5%
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring
#1
#2
#3
#4

## Slide 19: Experiment at KARA
Photoelectron current measured at electrode
Comparison:
Straight vs Reflection
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
Reflectivity Studies
Experimental Results Prototype #1
RI=
The surface roughness and their aspect ratios were measured at different parts of the sample
18
Electrodeposited Cu
AR ~ 0.5
Stainless Steel
AR ~ 0.06
2.4%
0.5%
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring
#1
#2
#3
#4

## Slide 20: Experiment at KARA
Calculation* of photons reaching photon cup
Comparison:
Straight vs Reflection
Photoelectron current measured at electrode
Comparison:
Straight vs Reflection
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
Reflectivity Studies
Experimental Results Prototype #1
RI=
The surface roughness and their aspect ratios were measured at different parts of the sample
18
Electrodeposited Cu
AR ~ 0.5
Stainless Steel
AR ~ 0.06
2.4%
0.5%
Geom #1
Geom #2 and #3
Geom#4
=1.3%
=1.2%
=0.3%
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring
#1
#2
#3
#4

## Slide 21: Experiment at KARA
Calculation* of photons reaching photon cup
Comparison:
Straight vs Reflection
Photoelectron current measured at electrode
Comparison:
Straight vs Reflection
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
Reflectivity Studies
Experimental Results Prototype #1
RI=
The surface roughness and their aspect ratios were measured at different parts of the sample
18
Electrodeposited Cu
AR ~ 0.5
Stainless Steel
AR ~ 0.06
2.4%
0.5%
Geom #1
Geom #2 and #3
Geom#4
=1.3%
=1.2%
=0.3%
Experimental results are in good correlation with Calculations
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring
·
·
#1
#2
#3
#4

## Slide 22: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Beam
CERN February 20th 2018
Heat Load Studies
Experimental Equipment
PT100
PT100
19
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring

## Slide 23: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Calculation
C
CERN February 20th 2018
Heat Load Studies
Experimental Results Prototype #2
A
B
J
20
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring
I
0
500
1000
1500
2000
1.2
0

## Slide 24: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
Photoelectron Generation Studies
Experimental Equipment
A
+
-
SR
e-
Cold Sprayed Isolated Electrode
21
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring

## Slide 25: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Photoelectrons
23.7% Increase
Photon Flux
75.4% Increase
CERN February 20th 2018
Photoelectron Generation Studies
Experimental Results – Prototype #2
A
+
-
SR
e-
#1
#2
22
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring

## Slide 26: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Effect of the surface conditioning is visible
CERN February 20th 2018
Photoelectron Generation Studies
Experimental Results – Prototype #2
A
+
-
SR
e-
#1
#2
23
100V
40V
#1
#2
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring

## Slide 27: Summary and Conclusions
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
After installation of BESTEX at KARA, experimental data has been obtained for the first two prototypes.
Experiments have been carried out in different irradiation configurations, in order to mimic the different scenarios at FCC-hh
Sample #1 shows a satisfactory behavior under SR in terms of vacuum
Sample #2 shows a large amount of photoelectrons reflected towards the BS’s main chamber
Reflectivity measurements show an unforeseen decrease of the amount of reflected photons for the misalignment case. Effect ascribed to the roughness of electrodeposited Cu at the BS´s main chamber.
Calculations were compared to experimental results :
  PSD calculations were compared to experimental results and tuned by using more realistic models. Discrepancies remain below 30% in all cases.
  Temperature distribution calculations are in good agreement with experiment.
  Experimental reflectivity results are in good correlation with calculations
Measurements on Photoelctron generation inside the BS have been peformed.
Instation of Sample #3 (Sawtooth profile) and test to be carried out from June 2018
24
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring

## Slide 28
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
Thank You
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring

## Slide 29: Fluorescent Screen Information
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring

## Slide 30: Fluorescent Screen Information
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring

## Slide 31: Fluorescent Screen Information
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring

## Slide 32: Alignment
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring

## Slide 33: Alignment
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring

## Slide 34: Alignment
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring

## Slide 35: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Middle
Front
Back
Levenberg-Marquardt Algorithm
X=-0.16 ± 0.01
X=-0.02 ± 0.01
X=-0.23 ± 0.01
CERN February 20th 2018
PSD Studies
Experimental Results
Power
Flux
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring

## Slide 36: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
PSD Studies
Experimental Results
Lower starting point lower conditioning rate.
Indicates pre-conditioning of the Geometry #4 region due to scattered photons
Middle
Front
Back
Levenberg-Marquardt Algorithm
X=-0.16 ± 0.01
X=-0.02 ± 0.01
X=-0.23 ± 0.01
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring

## Slide 37: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Geometry #1
Geometry #2
Geometry #3
2.4%
0.5%
1.3%
1.2%
0.3%
Geometry #4
CERN February 20th 2018
Reflectivity Studies
Experimental Results
Photoelectron Currents Ratio
Straight Irradiation
Irradiation after Reflection
Straight Irradiation
Irradiation after Reflection
Straight Irradiation
Irradiation after Reflection
Geometry
#1
Geometry
#2 & #3
Geometry
#4
.
.
2.4%
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring

## Slide 38
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
ANKA Parameters |  | 
Energy | 2.5 | GeV
Emittance | 50 | nm
Circumference | 110.4 | m
Current | 200 | mA
Optics | 4x2 | DBA
DP-Field | 1.5 | T
DP SR Power | 18 | W/mrad
DP SR Photon Flux | 6 1019 | Ph/(s mrad)
Ecritic | 6.2 | KeV
FCC Parameters |  | 
DP SR Power | 32 | W/m*
DP SR Photon Flux | 1x1017 | Ph/(s m*)
BESTEX Parameters (at ANKA after collimation) |  | 
DP SR Power | 32 | W/m*
DP SR Photon Flux | 5 1016 | Ph/(s m*)
Incident angle | 18 | mrad
*m: irradiated length |  | 
FCC Week 2018 April 10th
Results on the FCC-hh Beam Screen prototype at the KIT electron storage ring