## Slide 2
Cold Spray Additive Manufacturing
Outline
Cold spray technology:
Principle
Advantage
Possible applications in accelerators:
Local coating
Additive manufacturing
New materials
Applications of cold spray to UHV systems
Thermal outgassing
Leak tightness
Conclusion
C. Garion

## Slide 3
The gas dynamic cold spray coating is based on the projection of solid powder at high velocity.
Compressed gas
Powder feeder
Substrate
De Laval Nozzle
Principle of Cold Spray
A compressed gas is heated before entering in a DeLaval Nozzle.
The gas is accelerated in the nozzle.
Powder is injected in the gas stream and accelerated as well.
The powder reaches velocity up to 1200 m/s.
The powder is plastically deformed and the coating is building up.

## Slide 4
Principle of Cold Spray
1D isentropic flow equations:
De Laval Nozzle
P0, v0, T0
P1, v1, T1,
A1
g=5/3 (1.67) for monoatomic perfect gas
g=7/5 (1.4) for diatomic perfect gas and
g=1,33 for polyatomic perfect gas
Rs is the specific gas constant given by R/Mmolar
A*
Nitrogen is commonly used. Helium is used to reach higher velocity.
Notes: P0 ~30 – 50 bars
T0 : 300 C

## Slide 5
Cold Spray Advantages and Limitations
Advantages:
No powder melting.
  No phase change.
  No grain growth.
  Low heating of the substrate.
No significant impact on the oxide content w.r.t. initial material.
Powder mixture possible.
Compressive residual stress (fatigue life increase).
Nozzle geometry can be tuned for a given jet size.
Thick coating.
High deposition rate.
Limitations:
One constituent has to be ductile.
Accessibility to the surface to be coated.

## Slide 6
Possible Applications in Accelerators
Local coating:
Electrode:
Measurement of electrons for the FCC-hh beam screen prototype experiment at ANKA.
Clearing electrode (optimisation of ceramic layer required for non-baked system).
Copper and aluminium cold spray coating on ceramic insulated copper coated stainless steel sheet
Heat transfer:
Copper trips on FCC-hh beam screen prototype.

## Slide 7
Connectors
Titanium heating track
Copper pipe
Ceramic insulation layer
Copper plate with plasma sprayed ceramic and 0.2 mm thick cold sprayed titanium heating track
Heating element for bake out in or outside vacuum
Measurement of the temperature field
Possible Applications in Accelerators
Local coating:
267
284
Expected temperature profile on a copper tube, ID 80 mm
A prototype of a copper tube with permanent radiation tolerant bake out system is in fabrication.
A study will be carried out for heating system in a vacuum vessel (low outgassing of ceramic coating).

## Slide 8
Additive manufacturing for:
Joining of dissimilar materials
New feature
Repair
Local reinforcement of thin walled structure
Titanium on glassy carbon
New Manufacturing Process
J. Villafuerte, ADVANCED MATERIALS & PROCESSES, 2014
FCC-ee quadrupole chamber with BPM

## Slide 9
Metallization of polymer
Shuo Yin, Barry Aldwell and Rocco Lupoi, Advanced diamond-reinforced copper composite coatings via cold spray and material characterization, Trinity College Dublin
New Materials
Composite material:
Example of diamond copper composite
D. Giraud, Etude des composantes mécanique et métallurgique dans la liaison revêtement-substrat par projection dynamique pas gaz froid pour les systèmes aluminium/Polyamide6,6 et titane/TA6V, Mines ParisTech, 2014
Could it be a candidate for experimental vacuum chamber?
Could it be a candidate for collimator material?

## Slide 10
Requirements for UHV applications:
Outside vacuum chamber: not relevant.
In vacuum applications: low outgassing rate.
Vacuum barrier:
  Low outgassing rate.
  Leak tightness.
Ceramic plasma spray underlayer might be applied for some applications. Same requirements apply.
Application of Cold Spray for UHV system

## Slide 11
Vacuum Performance
Thermal outgassing
Measurements by accumulation method:
Samples:
Substrate: 3 stainless steel tubes, vacuum fired
Titanium coating, grade 2, 0.5 mm thick
Copper, 99.95%, 0.5 mm thick
Titanium coated samples
Copper coated samples
Substrates
Set-up principle for thermal outgassing measurement by accumulation

## Slide 12
Vacuum Performance
 | Total Outgassing [mbar·l·s-1] | Specific Outgassing (H2) [mbar·l·s-1·cm-2]
Background | 3.9e-11 | 
Stainless steel substrate | 6.37e-11 | 4.5e-14
Copper | 6.24e-11 | 3.9e-14
Titanium #1 | 1.73e-11 | 
Outgassing of H2 for copper is similar to bulk material.
Titanium outgassing is surprisingly low. Measurement to be redone.
Inert gas used during the powder fabrication may have a significant impact (high outgassing of N2 and Ar observed, for copper).
RGA scan for copper samples
Typical current (pressure) curves accumulation time and valve opening
Thermal outgassing

## Slide 13
Vacuum Performance
Present study program on aluminium coatings (in collaboration with Mines ParisTech):
Powder :
  Morphology, metallurgical characteristics, mechanical properties.
  Pre-treatment.
Processing parameters:
  Cold spray: gas pressure and temperature.
  Post-treatment.
Coating microstructure.
Vacuum performance.
Mechanical testing.
Modeling and numerical simulations.
Courtesy S. Weiller, F. Delloro (Mines ParisTech)
Leak tightness
Powder morphology
Aluminium Coating with “closed” porosities

## Slide 14
Conclusions
Gas dynamic cold spray is a coating method based on supersonic jet of powders, heavily plastically deformed during the impact.
Ductile materials are well suitable for this manufacturing process.
Cold sprayed copper coating has been successfully been applied on a first FCC-hh beam screen prototype.
A study is carried out at CERN to assess the vacuum performance of cold sprayed materials.
Other applications have been identified in different field of high energy particle accelerators. First tests are ongoing.

## Slide 16
Copper on copper
Assadi et al., Bonding mechanism in cold gas spraying, Acta Materialia, 51, 4379-4394, 2003
T. Schmidt et al., From Particle Acceleration to Impact and Bonding in Cold Spraying, Journal of Thermal Spray Technology, 18, 5-6, 794-808, 2009
Bounding mechanism
Rebound zone
Material jet
Typical surface around the critical velocity
A1050 powder on 2024-T3 substrate
Q. Blochet, Influence of substrate surface roughness on cold-sprayed coating-substrate bond strength in aluminum-based systems, PhD Thesis, Mines ParisTech, 2015
Notes: Adiabatic shear instability

## Slide 17
After Jeandin et al., Coating properties in Modern cold spray, Ed. J. Villafuerte, Springer, 2015
Electrical conductivity
Bounding strength
Coating strength
 Material properties are affected by the cold spray process but they can significantly be recovered by dedicated post treatment.
Some properties: example of copper
T. Stoltenhoff et al., Microstructures and key properties of cold-prayed and thermally sprayed copper coatings, Surface & coatings Technology, 200, 2006
With helium
With nitrogen
C.H. Boyle, Mechanical performance of integrally bounded copper coatings for the long term disposal of used nuclear fuel, Nuclear Engineering and design, 293, 2015
F. Gärtner, Mechanical properties of cold-sprayed and thermally sprayed copper coatings, Surface & Coatings Technology 200, 2006
N2
He

## Slide 18
Application to FCC
Colaminated copper- stainless steel internal screen
Cooling channel
Pumping holes
Copper strip for heat transfer
Requirements:
Copper material (thermal conductivity)
Stainless steel substrate
Discountinuous (longitudinally  reduced Lorentz forces during a magnet quench)
Continuous as close as possible to the cooling channel (better cooling and temperature control)
Done after beam screen assembly (welds)
No spray or coating contamination inside the beam screen
Industrial process
FCC-hh beam screen

## Slide 19
Application to FCC beam screen
Cold sprayed copper on austenitic stainless steel.
Surface preparation by blasting (Al2O3)
Possible improvements:
Surface preparation: laser treatment
Nozzle geometry: correct width
Process parameters