0
 Thermal runaway of metal nano-tips during intense electron emission
A. Kyritsakis, M. Veske, K. Eimre,
V. Zadin, F. Djurabekova
Mini MeVArc 2017
Tartu 17.10.2017

---
Outline
  - Motivation
  - Methods:
    - Molecular Dynamics – Electrodynamics
    - Electron emission
    - Heat diffusion
  - Results:
    - Thermal runaway in intensively emitting Cu nanotips
    - Evaporation rate – connection to plasma onset simulations
  - Open questions - future plans
  - Conclusions

---
Motivation
  - Electron emission is known to initiate vacuum arcs. However, the exact mechanism is still unclear.
  - Reveal and understand the mechanisms leading from intense electron emission to plasma formation
  - Plasma PIC simulations [1]: plasma can ignite from a Cu field emitter assuming:
    - Intense field electron emission up to mA
    - Evaporation of Cu neutral atoms to a rate of 0.015 atoms/emitted e.
  - What is the origin of those neutrals?
  - What mechanisms lead to their evaporation?
[1]: H. Timko et. al., Contrib. Plasma. Phys. 4 , p229 (2015)

---
Need for multi-physics simulations
- Existing hypothesis:
  - Intense electron emission → heating → thermal-field-assisted evaporation
  - Is this evaporation enough??
- A simulation of this process must include:
  - Material deformations: Molecular Dynamics
  - Electric field effects: Finite Element Method
  - Electron emission: GETELEC
  - Heat diffusion: Finite Difference Method
All the above processes have to be calculated concurrently and self-consistently

---
Concurrent MD-ED
h = 93nm, r=3nm, sa = 3o
Atomistic data (MD)
Surface extraction
Coulomb and Lorentz forces F
(Boundary conditions, Φ=0)
nabla ^2 %PHI = 0
widevec {F} = q widevec{E} + q sum from{i=neighb} {{q_i} over {4 %pi %epsilon_0 r_{i}} }
Electric potential Φ and field
widevec {E} = - nabla %PHI
Gauss Law
Charges q on atoms

---
Electron emission in the space-charge limited regime
Electric potential Φ and field
widevec {E} = - nabla %PHI
GETELEC code
Current density J and
Nottingham heat PN distributions
Modified 1D SC model
Space-Charge Field suppression factor
Modified 1-D model: multiply the total voltage by ω<1, use representative values for E, J distributions
Fitting to full 3D simulation data by Uimanov [1]
Good agreement: The 1D SC model is sufficient
[1] I. Uimanov, IEEE Trans. Dielectr. Electr. Insul. 18, 924 (2011)

---
Heating: Joule and Nottingham
GETELEC
Current density J and
Nottingham heat PN distributions
C_V{partial T} over {partial t} = nabla (%sigma(T) L T nabla T) + P_N + J^2/%sigma
Temperature
distribution T(z)
Conductivity σ(Τ)
Berendsen velocities scaling

---
The whole simulation model
Atomistic data (MD)
Coulomb and Lorentz forces F
Surface extraction
(Boundary conditions, Φ=0)
Berendsen velocities scaling
widevec {F} = q widevec{E} + q sum from{i=neighb} {{q_i} over {4 %pi %epsilon_0 r_{i}} }
nabla ^2 %PHI = 0
Electric potential Φ and field
Gauss Law
Charges q on atoms
widevec {E} = - nabla %PHI
Temperature
distribution T(z)
GETELEC code
Space-Charge Field suppression
Conductivity σ(Τ)
Current density J and
Nottingham heat PN distributions
C_V{partial T} over {partial t} = nabla (%sigma(T) L T nabla T) + P_N + J^2/%sigma

---
Results: Thermal runaway-evaporation
Simulating for Eappl=0.8GV/m, Vappl=3kV DC
Thermal runaway:
↑ resistivities
↑ Temperature
↑atom mobility
↑sharpness
↑local field
↑induced stresses
↑electron emission
Evaporation of large parts of the tip in forms of atoms and nanoclusters
Eventually the tip has not enough length and it cools down gradually.

---
Evaporation analysis
Tested for two different Cu inter-atomic potentials
7 independent runs for each potential with different seeds
The same qualitative behaviour for all (the numbers might deviate)
Mean evaporation rate between first and last evaporation events: RCu= 75±11 atoms/ps
Mean current I = 2807±153 e/ps
RCu/e= 0.025±0.003 atoms/e
Exceeds the minimum 0.015 found in the ArcPIC simulations!!!

---
Conditions to runaway
Prerequisites for the thermal runaway process to be initiated:
Heating enough to cause melting of a significant area at the apex region. T reach ~1400-1500K
Current densities that cause this high heating are of the order 1012 A/m2 (agreement with experiments)
Local field at the top (after SC lowering) must be more than ~10GV/m to “pull” the tip upwards
Tips of 20-100nm height must be present to initiate this process

---
Open questions - Future plans
Still open questions:
What happens with the evaporated atoms and clusters?
How do they affect the electrostatics?
What is the transient effect of the space charge?
Further development:
Develop full 3D simulation for the space charge
Simulate the impact of the nanoclusters on the anode
Include the evaporated atoms in the electrostatic simulation
Integrate PIC simulations in the vacuum region and track all evaporated particles until plasma ignition.

---
Conclusions
The mechanism leading from intense field emission to vacuum arc has still a lot of questions to be answered
The integrated multi-physics simulations can reveal and give an insight in several processes
A thermal runaway process leads to evaporation of large parts of a nanotip in the form of both atoms and nanoclusters
The number of evaporated atoms matches well the minimum number required in plasma simulations to initiate plasma
Further investigation of the behaviour of the vapour is needed to understand the behaviour of mechanisms and fully connect to the plasma calculations.

---
Acknowledgements

---
Thank you!!!!