## Slide 1: Ion beam analysis of materials with MeV beams at the Ruhr University Bochum
Ruhr-Uni-Bochum
Contribution to the ISOLDE workshop, Dec, 4th 2017, Hans-Werner Becker

## Slide 2
Accelerators in Bochum
Ion Beams from a few keV up to some 20 MeV

## Slide 3: Depth profiling with Nuclear Resonance Reaction Analysis
Motivation:
Detection of light elements (in particular Hydrogen)
isotopic tracing
Example:
Hydrogen depth profiling
with an 15N beam

## Slide 4: Nukleare Reaktions Analyse (NRA) am Beispiel 15N(p,a g)12C
E = ER
E > ER
Probe
Detektor
E = ER
E > ER
Strahlenergie [MeV]
Wirkungsquerschnitt [rel.]
Wasserstoff in Silizium
Ringversuch Bundesanstalt für Materialforschung

## Slide 5
sample
beam
Depth resolution: a few nm

## Slide 6
The set-up in Bochum
p = 2x10-9 mbar

## Slide 7: Rutherford Backscattering Spectroscopy
Probability
for scattering:
energy scale 
mass scale 
depth scale 
ZrO2 auf Si, Ea = 2,0 MeV,
AG Fischer / Devi, RUB
Zr
Si
O
Ei
Ef = k Ei
sample
Scattering angle (u)
Detector
Energy of scattered particle:

## Slide 8
Study of Diffusion in Minerals – why?
Diffusion is observed in samples
e.g. from subduction zones or meteorites…
…and one can learn something about
processes in the interior of the Earth or during the origin of the solar system
when diffusion parameters are known!
(time- temperature- and pressure scales)
1.

## Slide 9
Study of Diffusion in Minerals – why?
There is a close connection between diffusion and creep
mechanical properties
and it all depends on defects in crystals !
2.
microscopic properties

## Slide 10
100 mm
100000 years
B
A
AB
Experiment
Nature
B
A
AB
~ 8 days
10 nm
Measurement of diffusion processes in the laboratory
Timescale
Temperature scale
Q = activation energy

## Slide 11: RBS-profile of a diffusion anneal 900 °C 67 hours fO2 = 1.e-15 bar
before annealing
after annealing
- simulation
Olivine:
(Fex,Mg1-x)2SiO4
Fayalite
Fe2SiO4
Forsterite
Mg2SiO4
Example: Fe-Mg diffusion in olivine:
Olivin
Olivin
Fe
Si
Mg
O
Energy [keV]
Yield [counts]

## Slide 12: It would be very interesting for the understanding of diffusion studies to know more about amount and type of defects
PAC ?
There is only very little literature about PAC studies in minerals
e.g. Miami University Oxford, Ohio 2005
H. Jaeger, M. P. Rambo, R. E. Klueg, S. McBride…
Our first challenge is now
to understand what we can learn from PAC results
„finding a common language between geoscientists and PAC people“

## Slide 13
e.g. the investigations of zircon (ZrSiO4)
Thesis McBride 2005
Measurement fitted with the perturbation function…
(asymmetry parameter)
νQ (quadrupole frequency)
δ (damping parameter)
…to deduce
the EFG parameters:

## Slide 14
= 0 no radiation damage
> 0 radiation damage
and impurities ?
Change in slope of temperature dependence
> displacive phase transition ?
The EFG parameters
what to learn from
the damping parameter
Thesis S. P. McBride 2005

## Slide 15
Main question: What is the physical picture, in terms of structure and defects, that we can learn from these and other PAC results?
For example, can we answer questions such as:
What is the concentration of a certain kind of defect at a given condition e.g. T, P,…
What is the geometry of the atoms around the defect site?
How much energy is required to form a certain kind of defect?
What are the different kinds of defects that are present in a crystal, and in what concentrations?
etc. etc.
from the geoscientist

## Slide 16
… is needed