Shielding magnetic fields of several Tesla: the FCC SuShi project
http://cern.ch/sushi-septum-project
Kristóf Brunner, Dániel Barna
Wigner Research Centre for Physics, Budapest, Hungary
Miro Atanasov, Alejandro Sanz-Ull
CERN

---
The Future Circular Collider
Baseline:
- 50+50 TeV
  proton-proton collider
- 100 km ring
- Using existing CERN infrastructure as injector
Targeted problem: extraction of the 50 TeV beam towards the beam dump

---
Extraction scheme
Beam is dumped when:
Something misbehaves
At the end of the cycle

---
Doing it at the LHC: the Lambertson septa
S. Bidon, et al: Steel septum magnets for the LHC beam injection and extraction, Proc EPAC 2002
Coils
B < 1.2 T
Mu-metal layer on vacuum chamber
Circulating & extracted beams
Iron yoke

---
Doing it at the LHC: the Lambertson septa
Using μr ≫ 1
to „suck out” the field lines
from the circulating beam
Can't go above ~1.5 T due to saturation of iron
S. Bidon, et al: Steel septum magnets for the LHC beam injection and extraction, Proc EPAC 2002
Coils
B < 1.2 T
Iron yoke
Mu-metal layer on vacuum chamber
Circulating & extracted beams

---
FCC parameters for extraction
At top energy (most difficult):
}
Septum integrated field	190	T m
Available space for septum	120	m
Need ≥ 2 T field
(to accomodate gate
valves, pumps, etc)
(Space would be even more tight in the „high-energy LHC” - LHC tunnel with FCC technology)
- B > 2 T (target: 3 Tesla)
  - Not easy with normal-conducting devices
  - need superconductors?
- Must follow the ring energy to be ready for beam-abort at any time (quasi-DC mode)
- Field homogeneity: ~1%
- Leakage field at circulating beam: < 10-4 relative

---
Doing it at the FCC: the SuShi idea
- If cooled down in 0 field,
  a superconductor can shield
  the outside field
- Persistent currents
- Concept is similar to eddy current septum,
  but can work in DC mode, (because the
  eddy currents are persistent)
Homogeneous high field
~5-7 cm

---
Doing it at the FCC: the SuShi idea
- If cooled down in 0 field,
  a superconductor can shield
  the outside field
- Persistent currents
- Concept is similar to eddy current septum,
  but can work in DC mode, (because the
  eddy currents are persistent)
Homogeneous high field
~5-7 cm
Using μr ≪ 1 material
to expel the field lines

---
Pros & cons
Pros
Cons
- Shielding currents arranged by nature (high precision zero field)
- Continuous 2D current distribution (unlike a winded magnet) → perfect shielding
- Bulk shield, better mechanical, and thermal stability
- Highest possible current density(critical state model) →thinnest shield
- Superconductor in high rad zone (quench)
- Hysteretic behavior, always have to start from virgin state
- To erase ‘memory’ of shield, temperature has to be increased

---
Combining μr≫1 and μr≪1
The „magnetic cloak”
Ferromagnet absorbs the induction lines expelled by the superconductor
Seems a natural choice, since it does not distort the external field
%mu_{ r } = { R_{2}^{2} + R_{1}^{2} } over { R_{2}^2-R_{1}^{2} }
R1
R2
Does not work for FCC with realistic geometrical parameters:
field in ferromagnet would be too high: ~13-18 T
μr=0

---
Challenges
- Max. physical septum width: 25 mm
  (including vacuum pipe walls etc!)
- Go against „common practice” of superconductors (very fine filaments to avoid flux jumps – thermomagnetic instability)
  - Want to exclude B from a large area
  - Need special measures to ensure stability
- Care about the excluded field's quality (homogeneity)
- „Reset cycle” (warm-up and zero-field-cool) to be on the „virgin curve” of magnetization

---
Homogeneity at various field strengths
At injection
Flat wall → homogeneity despite significantly different penetration depths
pos. winding
neg.
     winding
≤0.5 T
At top energy
3 T

---
CERN Bubble chambers
- In the '70ies: superconducting tube to shield high magnetic field
- To introduce low-momentum
  particles into the high field of
  the bubble chamber
- Different materials, and
  techniques could bring the
  shielded field strength from
  2 T up to 5.9 T
Superconductor tube
M.Firth, et.al.: Performance of the superconducting field shielding tube for the CERN 2m hydrogen bubble chamber
M.Firth, L.Krempasky, F.Schmeissner: Preliminary work on field-free particle beam paths from hollow superconducting shielding tubes – Proc. 3rd. Int. Conf. Magn. Tech. (1970) 1178
http://www.iaea.org/inis/collection/NCLCollectionStore/_Public/46/027/46027030.pdf

---
SLAC
B
F.Martin, S.J.St.Lorant, W.T.Toner: A four-meter long superconducting magnetic flux exclusion tube for particle physics experiments – NIM 103 (1972) 50

---
MgB2
Produced by the Reactive Liquid Magnesium Infiltration (RLI) process
(G. Giunchi, Int.J.Mod.Phys.B17,453)
Extra large boron grainsize (160 μm) to be stable against flux jumps
(G.Giunchi et al,IEEE Trans. Appl. Supercond. 26, 8801005)
450 mm
8.5 mm
50 mm

---
Testing of prototypes at SM18
LHC corrector magnet MCBY
Shield
Long aluminium support tube
Hall sensors
Transverse alignments

---
MgB2 magnetization cycle
Field outside the shield
Field inside the shield

---
MgB2 magnetization cycle
2 minute plateaus for relaxation measurement
Ramp rate: 0.1 A/s →5 mT/s on external sensors
(realistic for FCC: 3 T/10 minute)

---
MgB2 magnetization cycle
Smooth penetration at 2.6 T
Complete shieldig below 2.6 T

---
MgB2 magnetization cycle
No flux jump on the virgin curve up to the highest field
Flux jumps at low fields, after the shield has been exposed to high fields
Smooth penetration at 2.6 T

---
MgB2 magnetization cycle

---
MgB2: field penetration
2.6 T plateau
(full shielding)
OUTSIDE
Significant creep
on the plateaus
(smooth, not an
avalanche-like jump!)
INSIDE
64 A magnet current

---
MgB2: field penetration
2.6 T plateau
(full shielding)
OUTSIDE
Significant creep
on the plateaus
(smooth, not an
avalanche-like jump!)
INSIDE
Full shielding (<0.1 mT)
deeper inside
88 mm from
shield's end
Field penetration at
open end of the tube
INSIDE

---
MgB2: linearity
Measured external magnetic field is non-linear as a function of magnet current!

---
MgB2: linearity
COMSOL simulation in precise model of MCBY magnet
Increasing field → more penetration
Effective shielding surface drifts away from Hall sensor
Less field concentration at sensor
realistic MgB2
Jc(B) = J0∙ exp( – γ B)
Hall sensor

---
MgB2: linearity
COMSOL simulation in precise model of MCBY magnet
J0 and γ are strongly correlated
realistic MgB2
Jc(B) = J0∙ exp( – γ B)
Hall sensor

---
MgB2: linearity
COMSOL simulation in precise model of MCBY magnet
J0 and γ are strongly correlated
realistic MgB2
Jc(B) = J0∙ exp( – γ B)
Hall sensor

---
MgB2: linearity
COMSOL simulation in precise model of MCBY magnet
J0 and γ are strongly correlated
realistic MgB2
Jc(B) = J0∙ exp( – γ B)
Hall sensor

---
MgB2: linearity
From observed nonlinearity one can get some info on Jc(B)
At 64 A different parameters give B penetration profiles with same, almost
full depth
64A
B profiles
60A
50A
40A
30A
20A
10A
Shielding current profiles
shield
outer surface
shield
inner surface
     1.5 mm

---
HTS tape covered tube
Layers overlapping
Superposition
Little current loops
Copper support tube
25 layers of helically wrapped
SuperOx 2G HTS tape, soft-soldered
450 mm
Ø46.5 mm

---
HTS: Shielding performance
No flux jumps!
Smooth, full penetration
above 0.25 T
Due to limited Jc?
Shielding up to 0.25 T
(not perfect, as we will see!)

---
HTS: penetration at low field!
Continuous penetration from zero field!
Attenuation is about 10-3 here
Due to geometry?
(non-continuous geometry,
small gaps between tape layers, small current loops)

---
NbTi/Nb/Cu multilayer shield
- Consists of multilayer sheets of ~0.8mm, containing 30 layers of 9 µm NbTi
- From previous tests it seems
  possible to shield 2.5T field
  with 3 sheets (~2.4mm)
- A 4-sheet shield will be
  tested in the beginning of
  next year
I.Itoh, K.Fujisawa, H.Otsuka: NbTi/Nb/Cu Multilayer Composite Materials for
Superconducting Magnetic Shielding,
Nippon Steel Technical Report No. 85, January 2002

---
Shielding performance
Exponential Jc(B)=J0·exp(-γB)
leads to exponential increase of required thickness:
d = d0·exp(γB)
with d0 = 1/γμ0J0
For MgB2: roughly x3 increase for +1 T
NbTi/Nb/Cu multilayer sheet (various conditions) [1]
Large-grain MgB2
(estimates from our tests, using simulation)
[1] I.Itoh, T.Sasaki, Cryogenics 35 (1995) 403

---
Shielding performance
MgB2 cheaper
Exponential Jc(B)=J0·exp(-γB)
leads to exponential increase of required thickness:
d = d0·exp(γB)
with d0 = 1/γμ0J0
For MgB2: roughly x3 increase for +1 T
NbTi/Nb/Cu multilayer sheet (various conditions) [1]
Large-grain MgB2
(estimates from our tests, using simulation)
[1] I.Itoh, T.Sasaki, Cryogenics 35 (1995) 403
NbTi more performant

---
Outlook
- Passive superconductors:
  - Perfect shielding if thickness is sufficient
  - Up to very high fields
  - DC and AC mode
  - Very attractive if space is tight
  - Very versatile:
    - MgB2: large bulk, complex shapes, EDM machining, cheap
    - NbTi multilayer: ductile, robust, formable
- Future plans:
  - Measurement of third prototype
  - Construct a full demonstrator

---
Thank you for your attention!
Acknowledgements
- FCC Study group
- CERN SM18 (M. Bajko, H. Bajas, M. Strychalski)
- CERN TE-MSC-MM (C. Petrone, M. Buzio)
- CERN TE-ABT (B. Goddard, J. Borburgh, M. Atanasov, A. Sanz-Ull)
- G. Giunchi (MgB2)
- A. Molodyk (SuperOx)
- European Commission (FP7/EUCARD-2, grant agreement no. 312453)
- Hungarian Academy of Sciences
- Wigner Research Centre for Physics, Budapest

---
Additional slides

---
Measurement possibilities
Rotating coil to measure field quality (during tests only)
Shield thick enough to ensure perfect shielding safely...
Most important: detect flux-jumps (very quickly and reliably) →beam abort
Hall sensors close
to the shield (off the mid-plane)
(tests & real app. ?)
Hall sensor to measure the „zero field”
(during tests only)
Do not need to be high precision
Pick-up coil to detect flux-jump (tests & real app.)

---
MgB2: long-term relaxation
If external field at a safe level below full penetration...
...relaxation is small, can be compensated by the excitation current
0.25%