## Slide 1
Comparison between a THGEM made of ARLON and a traditional THGEM made of FR4
INFN, Trieste - ICTP, Trieste
Jinky Agarwala

## Slide 2
ARLON and FR4 THGEMs
Set up and conditions of the measurements
Comparison of results
Effect of x-ray illumination
Previous characterization of a THGEM made of Permaglass
Conclusions
Outlines

## Slide 3: ARLON and FR4 THGEMs
Area: (300 x 300) sq. mm Thickness of the piece: 0.4 mm
Pitch: 0.8 mm Hole diameter: 0.4 mm No Rim
ARLON 25 FR
Dielectric constant: 3.58
Ceramic-filled fiberglass material
Fiberglass FR4
Dielectric constant: 4.7
Woven fiberglass and epoxy resin
Both produced by ELTOS

## Slide 4
The Readout Pads (Anode):
24 x 24 matrix
Divided into 18 regions
Each region has 32 (4 x 8) pads read together
Gas Used:
Ar:CO2= 70:30
HVPS: CAEN N1471H
Software for HVPS: GECO 2020
PreAmplifier: CREMAT 110
Amplifier: Ortec 672
MCA: AMPTEK 8000A
Source: 55Fe (5.9 keV)
Rate: 5 kHz
Multi-Pad Anode (12mm X 12mm)
Thickness: 0.4 mm
KAPTON
Drift
17.5 mm
2.5 mm

## Slide 5
Chart: ARLON: Drift_SCAN
| 0.5714285714285714 | 0.2857142857142857 | 0.31428571428571428 | 0.34285714285714286 | 0.37142857142857144 | 0.4 | 0.42857142857142855 | 0.45714285714285713 | 0.48571428571428571 | 0.51428571428571423 | 0.54285714285714282 | 0.5714285714285714 | 0.6 | 0.62857142857142856 | 0.65714285714285714 | 0.68571428571428572 | 0.7142857142857143 | 0.74285714285714288 | 0.77142857142857146 | 0.8 | 0.82857142857142863 | 0.8571428571428571 | 0.88571428571428568 | 0.91428571428571426 | 0.94285714285714284 | 0.97142857142857142 | 1 | 0.5714285714285714
 | 143.7253 | 132.7897 | 135.9142 | 137.4764 | 139.0387 | 140.6009 | 140.6009 | 142.1631 | 142.1631 | 143.7253 | 143.7253 | 145.2876 | 145.2876 | 145.2876 | 146.8498 | 146.8498 | 146.8498 | 146.8498 | 146.8498 | 146.8498 | 146.8498 | 146.8498 | 145.2876 | 146.8498 | 146.8498 | 146.8498 | 146.8498 | 140.6009
Chart: FR4: Drift_Scan
| 0.24571428571428583 | 0.30285714285714288 | 0.3600000000000001 | 0.41714285714285737 | 0.47428571428571431 | 0.53142857142857181 | 0.58857142857142852 | 0.61714285714285733 | 0.64571428571428569 | 0.67428571428571471 | 0.70285714285714262 | 0.73142857142857176 | 0.76000000000000023 | 0.7885714285714287 | 0.81714285714285739 | 0.84571428571428553 | 0.87428571428571455 | 0.90285714285714258 | 0.93142857142857172 | 0.96000000000000019 | 0.98857142857142855 | 0.81714285714285739
 | 137.3011 | 145.6859 | 149.8783 | 154.0707 | 157.215 | 159.3112 | 161.4074 | 161.4074 | 162.4555 | 163.5036 | 164.5517 | 165.5998 | 165.5998 | 165.5998 | 165.5998 | 165.5998 | 165.5998 | 165.5998 | 165.5998 | 165.5998 | 164.5517 | 158.2631
Chart: FR4: Induction_Scan
| 2 | 0.4 | 0.8 | 1.2 | 1.6 | 2 | 2.4 | 2.8 | 3.2 | 3.6 | 4 | 2
 | 159.3112 | 55.5493 | 92.2328 | 123.6758 | 142.5416 | 157.215 | 168.7441 | 180.2732 | 188.658 | 194.9466 | 205.4276 | 156.1669
Chart: ARLON: Induction_SCAN
| 2 | 0.4 | 0.8 | 1.2 | 1.6 | 2 | 2.4 | 2.8 | 3.2 | 3.6 | 4 | 2
 | 148.412 | 51.5537 | 90.6095 | 118.7296 | 137.4764 | 149.9743 | 160.9099 | 171.8455 | 181.2189 | 187.4678 | 193.7168 | 151.5365
Measurements: Drift Scans and Induction Scans
Similar responses

## Slide 6
Effective Gain
Very similar effective gains
Vc | 889 V
¦Ec¦ | 22.2 kV/cm
ΔV10 | 178 V
¦ΔE10¦ | 4.45 kV/cm
Vc | 902 V
¦Ec¦ | 22.6 kV/cm
ΔV10 | 192 V
¦ΔE10¦ | 4.8 kV/cm
ARLON
FR4
E_Ind= 2kV/cm, E_D= 0.8 kV/cm
Chart: Effective Gain Vs ΔV
| 1250 | 1260 | 1270 | 1280 | 1290 | 1300 | 1250 | 1240 | 1230 | 1220 | 1210
ARLON | 126.684 | 139.196 | 162.656 | 178.296 | 211.14 | 237.728 | 125.12 | 109.48 | 98.532 | 86.02 | 76.636
FR4 | 51.3569 | 60.7898 | 68.1265 | 77.5594 | 88.0404 | 99.5695 | 113.1948 | 129.9644 | 146.734 | 167.696 | 190.7542 | 216.9567 | 250.4959 | 281.9389 | 322.8148 | 162.4555

## Slide 7
Energy Resolution
Calibration factor:1.048228
231 electrons per channel,
27 channels/fC
Energy Resolution: 11.9 %
ARLON
FR4
Energy Resolution: 12.2 %
They have the same Energy Resolution

## Slide 8
Effective gain variation with time
ARLON
FR4
8 h
60 h
Gain variations with time for the two pieces are not the same

## Slide 9
Correlation between effective gain and P/T
Correction Factor (C): 1+0.00151X{(P/T)-(P_0/T_0)}
Correction is applied if: 0.01 < |1-C| < 0.001
This recipe is used by COMPASS RICH-1 hybrid detectors
Labview HV control program with P, T corrections
HV bias modified to compensate for P and T variations

## Slide 10
Chart: Gain Curve with the Program for Correction ON
Gain stabilization with HV corrections
Variation within +(-) 2.5%

## Slide 11
Gain Uniformity
ARLON
FR4
σ= 9.1 %
σ= 16.1 %

## Slide 12
Effect of illumination by 55Fe source
Chart: Variation of eff. gain at each region
| A1 | A2 | A3 | A4 | A5 | A6 | B1 | B2 | B3 | B4 | B5 | B6 | C1 | C2 | C3 | C4 | C5 | C6
 | 273.576 | 256.547 | 260.508 | 262.01 | 222.974 | 156.35 | 206.553 | 225.95 | 223.403 | 222.117 | 197.728 | 208.895 | 211.568 | 216.495 | 221.523 | 211.718 | 212.956 | 200.316
Chart: Variation of resolution at each region
| A1 | A2 | A3 | A4 | A5 | A6 | B1 | B2 | B3 | B4 | B5 | B6 | C1 | C2 | C3 | C4 | C5 | C6
 | 0.3484 | 0.30221 | 0.27348 | 0.26934 | 0.32005 | 0.40175 | 0.36298 | 0.27896 | 0.29617 | 0.28945 | 0.30018 | 0.30637 | 0.28361 | 0.28402 | 0.28065 | 0.27727 | 0.27889 | 0.30716
Broadening of the spectra
Uniformity scan performed after A6 was illuminated for 5 hours
Chart: Eff. Gain
| A1 | A2 | A3 | A4 | A5 | A6 | B1 | B2 | B3 | B4 | B5 | B6 | C1 | C2 | C3 | C4 | C5 | C6
 | 282.261 | 262.927 | 269.779 | 113.025 | 220.472 | 212.81 | 199.105 | 225.19 | 219.216 | 216.453 | 196.472 | 201.849 | 208.331 | 210.018 | 208.896 | 210.812 | 208.375 | 200.316
Chart: Resolution
| A1 | A2 | A3 | A4 | A5 | A6 | B1 | B2 | B3 | B4 | B5 | B6 | C1 | C2 | C3 | C4 | C5 | C6
 | 0.38404 | 0.30446 | 0.29473 | 0.44621 | 0.43968 | 0.41016 | 0.41117 | 0.30876 | 0.3401 | 0.33529 | 0.35571 | 0.37571 | 0.35007 | 0.32366 | 0.32275 | 0.30535 | 0.31711 | 0.30716
Uniformity scan performed after A4 was illuminated for 67 hours

## Slide 13
Long term persistence of the illumination effect on ARLON and FR4
08-Sept 11-Sept 13-Sept 15-Sept 18-Sept
10 DAYS
26-Jun 21-July 24-July 01-Aug 09-Aug 06-Sept 08-Sept
70 DAYS
ARLON
FR4
Chart: Effect of illumination
A3 | 1.1722 | 1.2395 | 0.5099 | 0.54592 | 1.0163
A4 | 1.1817 | 0.51037 | 0.94234 | 0.97122 | 1.124
A6 | 0.70044 | 0.94783 | 0.96816 | 0.98392 | 1.0223
C4 | 0.95775 | 0.96241 | 0.9488 | 0.96488 | 0.99841
Chart: Effect of illumination
A6 | 1.0406 | 1.0229 | 0.77158 | 0.5912 | 0.53691 | 0.50353 | 0.50883
C3 | 0.72491 | 0.79108 | 0.80775 | 0.80431 | 0.83893 | 0.86793 | 0.88522
C6 | 1.1452 | 0.91819 | 0.97075 | 1.0174 | 1.0604 | 1.0799 | 1.0874
A1 | 1.0108 | 1.0095 | 1.0179 | 1.0312 | 1.0134 | 1.0203 | 1.0037

## Slide 14
The responses of identical THGEMs made of ARLON and FR4 have been compared
The gain and the energy resolution are the same
The charging up is faster in FR4
The recovery from the illumination effect is much slower in ARLON
The ARLON material is not suitable for high rate THGEM application
Conclusions

## Slide 15
About PERMAGLAS
Permaglas ME730 by RESARM Engineering Plastics SA
  Epoxy glass fibre material, amorphous, machinable
  The plate planarity is obtained by machining
    Purchased by us:

## Slide 16: THICKNESS UNIFORMITY
Raw material characterization
Nominal thickness 0.7 mm
  /D/ < 4%; s < 2%
Nominal thickness 1 mm
  /D/ < 2%; s < 1%
 Very good thickness uniformity!
Cu layers glued at CERN by Rui de Oliveira
Drilling performed by ELTOS

## Slide 17: ELECTROSTATIC PROPERTIES
PASCHEN test for 1mm thick piece
90% PASCHEN limit

## Slide 18: RESULTS
UNIFORMITY SCAN:
  s: 13%
ENERGY RESOLUTION:
  20 %
GAIN PERFORMANCE:
  A robust device
Gas:
Ar:CO2= 70:30
Source: 55Fe

## Slide 19: TIME DEPENDENT EFFECTS
CHARGING UP STUDIES
Effect of the ion motion in the material

## Slide 20: CONCLUSIONS about PERMAGLAS THGEM
Robust material with good uniformity performance
Difficult to get good quality thin foils
Limited gain dependence on rate (charging up) and time (ion displacement in the bulk dielectric)

## Slide 21
Thank You