## Slide 1: UHV characterization of advanced materials and their coatings Carlotta Accettura EN/MME, with many contributions of TE/VSC 1st Workshop of ARIES PowerMat (WP17) Turin- 27 November 2017

## Slide 2: Outline
Introduction: the LHC and the UHV
Outgassing of collimator materials:
  Graphite, CFC and MoGr
  MoGr investigation – bulk material
  MoGr investigation – coating
  CuCD
Conclusions and outlook

## Slide 3: The UHV requirements
In all the particle accelerators an high or ultra-high vacuum is required: beam stability and lifetime (beam-gas scattering)
LHC vacuum acceptance limits for collimators:
  Low outgassing rate (1·10-7 mbar·l/s)
  No NEG saturation (N2, CO, CO2,..)
  Low SEY (ESD, electron cloud)

## Slide 4: Collimation system upgrade
MoGr
MoGr with Mo coating
CuCD

## Slide 5: Graphite outgassing – Air content
CH4
H2
N2
CO
Ar
CO2
2D Carbon-Fibre-reinforced Carbon (CFC)
Graphite
Avoid high T treatment with inert gas

## Slide 6: Molybdenum-Carbide Graphite
Material | Qs [ mbar∙l/ s∙cm2]
MoGr | 1.9∙10-10
Graphite | 1.3∙10-11
CFC | 1.9∙10-11
CH4
N2
CO
Ar
CO2
H2
Bulk porosities
Surface damage

## Slide 7: MoGr treatment
CO2 blasting:
Qafter/Qbefore= 50
CO2 adsorption
Air content (N2, Ar) increased
Surface peak
Bulk peak
CO2

## Slide 8: US cleaning-last grade
US cleaning:
Qafter/Qbefore= 3
Solvent contamination
Completely recovered after 48h firing

## Slide 9: MoGr treatment
N2
CO
CO2
N
Ar
H2
Diamond paste polishing (particle size 1μm):
Qjaws= 5.4∙10-7 mbar∙l/s 
Air still dominant
Surface damage seems removed
The surface plays a role (CO2 blasting), but there should be also a bulk contribution to air trapping

## Slide 10: Solution 1: Higher T process
Higher temperature during production process:
Qjaws= 3.1∙10-8 mbar∙l/s 
H2 dominated
Similar surface damaged (FIB)
Lower density: similar void fraction, lower carbide content (3D FIB)
 | Compliant sample | Non-compliant sample
%vol carbide | 4.5 | 7.8
%vol void | 5.1 | 5.7
25x70x6 mm

## Slide 11: Solution 2: Different compaction
Material | Qs [ mbar∙l/ s∙cm2]
As received | 4.7∙10-11
48h firing | 3.5∙10-12

## Slide 12: Mo coating on MoGr – TDS
CH4
CO2
CO2 blasted MoGr with Mo coating
The coating:
  reduces the outgassing up to 200-250°C (oxide layer?)
  increases the outgassing above these T (CO2 blasting) with a proper preparation should be compliant

## Slide 13: Mo coating on MoGr – SEM
Need to verify possible air trapping within the Mo layer
CO2 BLASTING
US CLEANING

## Slide 14: Copper-Diamond
Robustness against accident situation: W alloy CuCD
US cleaning before the test→ impossible to pump-down
After 48+24 h of bake-out at 250°C
Material | Qs [ mbar∙l/ s∙cm2] | Qjaws [ mbar∙l/ s]
CuCD + cladding | 7.4∙10-12 | 2.9∙10-8 

## Slide 15: Secondary Electron Yield
MoGr
CuCD
SEY max collimator~ 1.4
Graphite
Copper
Courtesy of D. Zanin (TE/VSC)
Courtesy of V. Baglin

## Slide 16: Conclusions and outlook
A complete characterization (outgassing, TDS, microscopy, knowledge of the production process,..) is required to understand the phenomena
Air content in MoGr has to be reduced during the production:
  higher T (Reproducible? Why?)
  under vacuum compaction
  longer annealing
CuCD: promising material, air exposure to be checked
Coating characterization:
  surface preparations effect on outgassing ✔
  coating effect on outgassing (ongoing)
  adhesion

## Slide 17
Thank you for the attention!

## Slide 18: TDS-MoGr

## Slide 19: MoGr- 48h firing
48 h, 950°C vacuum firing:
Qbefore/Qafter= 7, but still out of the limits (~2.5 for 2h firing)
H2 decreased
N2 decreased, Ar not

## Slide 20: CFC- 48h firing
Ar
N2
H2
Treatment | Total outgassing [mbar*l/s] | Internal leak [mbar*l/s]
None | 7.5·10-8  | 8.3·10-9 
2h firing, 950°C | 1.1·10-8  | 5.7·10-9 
48h firing, 950°C | 6.9·10-9  | 3.5·10-10 

## Slide 21: US cleaning-first supplier
US cleaning + 48 h firing:
Qbefore/Qafter= 16
N2 decreased, Ar constant (normalized graph)
→ result similar to just 48 h vacuum firing

## Slide 22: US cleaning-last grade

## Slide 23: Outgassing and thermal treatment
Grade | Thermal treatment | Total outgassing jaws [mbar*l/s] | Internal leak [mbar*l/s] | Gas analysis
Nd-7301Cb | VF 950°C 48h, Ar venting | 1·10-8  |  | 
Nd-7301Cb | VF 950°C 48h, Ne venting | 2.5·10-9  | 2.2·10-9  | 
Nw-8301Ed | None | 1.8·10-7  | 9.3·10-9  | 
Nw-8301Ed | VF 950°C 48h, air venting | 1.4·10-8  | 5.3·10-9  | 
Reduction~10
Reduction~1.8
Nd-7301Cb
Nw-8301Ed

## Slide 24: Gas venting after firing 48h
H2 dominated
Adsorption of venting gas
H2 dominated
CH4 reduction
Low outgassing
H2 dominated spectra
Low internal leak
Compliant after 48h firing
+
+
Ar
N2
Ne
Ar
N2

## Slide 25: Mo coating machine

## Slide 26: Secondary Electron Yield
Graphite 
MoGr as received 
MoGr air exposure 
SEY max collimator~ 1.4