## Slide 1: Results from recent investigations and characterizations at GSI
Philipp Bolz
Roberto Colina-Ruiz, Fabian Jäger, Daniel Schmitt, Pascal Simon, Marilena Tomut

## Slide 2: Table of content
Motivation
Materials
Structural characterization
  Raman spectroscopy
  Infrared thermography
  Functional characterization
  Indentation
  3-point bending test
  Laser flash analysis
  Conclusion and outlook

## Slide 3: Motivation
Properties of graphite:
Low density
High thermal conductivity
Low coefficient of thermal expansion
High service temperature
Graphite materials are used for:
Target wheel and beam catchers in Super Fragment Separator
Beam dumps in experimental caves
Collimators
Super-FRS working group, 2008

## Slide 4: Investigated materials
Polycrystalline graphite (PG)
Carbon fibre reinforced carbon (CFC)
2 dimensional fibre orientation
Fibre plane parallel or perpendicular to surface
CFC
PG
Material | Particle size [µm]
R6300 | 20
R6500 | 10
R6550 | 10
R6650 | 7
POCO ZEE | 1
Transversal 
In plane ‖

## Slide 5: Structural characterization Raman spectroscopy
Main peaks for graphite:
  D-peak ≈ 1380 cm-1
  G-peak ≈ 1580 cm-1
  2nd D-peak ≈ 2700 cm-1
Ratio of ID/IG allows determination of defect concentration and lattice parameters
Bands included for Raman spectra deconvolution:
D1-D3: Lorentzians
D2: Gaussian
G: Lorentzian
G‘2D-G‘3DA-G‘3DB: Lorentzians
P7: Splitlorentzian
P9: Lorentzian
N. Larouche, B.L. Stansfield, Carbon N. Y. 48 pp. 620–629, 2009

## Slide 6: Raman results of isotropic polycrystalline graphite grades
Particle size: 1 µm
Porosity: 20%
Pore size: 0.3 µm
Density: 1.77 g/cm3
SGL R6650
Particle size: 7 µm
Porosity: 10%
Pore size: 1.1 µm
Density: 1.84 g/cm3
ID/IG = 0.455
ID/IG = 0.288
POCO ZEE

## Slide 7: Infrared thermography
Infrared thermography acquires and processes thermal information from non-contact measurement devices
Experimental setup
heat
heat source
sample
Infrared camera
Control unit

## Slide 8: Infrared thermography
SGL Mechanical
2D-CFC
Fibre plane normal to surface
POCO FOAM
Graphitic Foam
Fibre plane parallel to surface
Normal
Parallel

## Slide 9: Functional characterization Microindentation
Area function A:
Hardness H:
Reduced modulus Er:
Young’s modulus E:
Oliver and Pharr, J. Mater. Res., vol. 7, no. 6, pp. 1564-1583, 1992
β = Geometrical correction factor
ϑ = Poisson’s ratio

## Slide 10: Microindentation of investigated materials
Young’s modulus
Hardness
Transversal 
In plane ‖
Material | Particle size [µm]
R6300 | 20
R6500 | 10
R6550 | 10
R6650 | 7
POCO ZEE | 1

## Slide 11: Dynamic indentation
Indenter is accelerated with constant force towards the sample
Resulting bouncing of the indenter on the surface of the sample is measured
Dynamic hardness DH:
Damping constant k:

## Slide 12: Dynamic indentation results of polycrystalline graphite and carbon fibre reinforced carbon grades
Transversal 
In plane ‖
Dynamic hardness
Damping constant

## Slide 13: Multiple Impulse indentation
Indenter is accelerated with constant force towards the sample
Indenter is moved back to the initial position and accelerated again
Allows measurement of fatigue
Polycrystalline graphite:
SGL R6550
Carbon fibre reinforced carbon:
SGL Premium in plane

## Slide 14: Multiple impulse results of polycrystalline graphite grades
Material | Particle size [µm]
R6300 | 20
R6500 | 10
R6550 | 10
R6650 | 7
POCO ZEE | 1

## Slide 15: 3-point bending test
l = 20 mm
In plane ‖
A = 4x4 mm²
Transversal 
Stress (MPa)

## Slide 16: Flexural strength
Transversal 
In plane ‖

## Slide 17: Laser flash analysis
https://www.netzsch-thermal-analysis.com/de/produkte-loesungen/waerme-und-temperatur-leitfaehigkeitsbestimmung/lfa-427/ (23.11.2017)
-200
0
200
400
Time (ms)
1
2
3
4
5
6
Voltage (V)

## Slide 18: Laser flash analysis results
Transversal 
In plane ‖
Thermal diffusivity [mm²/s]

## Slide 19: Empirical relation between ID/IG and thermal diffusivity
HOPG was used as reference (Ideal case has ID zero)
The relation shows an exponential behavior
Lower ID /IG implies larger thermal diffusivity

## Slide 20: Conclusion and outlook
Properties of polycrystalline graphite depend on the grain size
Carbon fibre reinforced carbon and graphite foams properties depend on orientation with a strong and a weak direction
The thermal diffusivity is decaying exponentially with increasing defect concentration
Results allow calculation of figures of merit and improved simulations to predict the behaviour during irradiation
Experiments at HiRadMat and at GSI will allow evaluation of beam induced effects and property changes of the different irradiated graphitic materials

## Slide 21: Acknowledgment
Thank you for your attention
Thanks to Roberto Colina-Ruiz, Fabian Jäger, Daniel Schmitt, Pascal Simon and Marilena Tomut for providing data
This project has received funding from the European Union’s Horizon 2020 Research and Innovation programme under Grant Agreement No 730871