## Slide 1: Requirements for radiation damage simulations regarding FAIR targets, beam dumps / catchers and previous experiments at GSI
M. Tomut
With input from P. Katrik, H. Weick et al.
PowerMat

## Slide 2: Radiation damage in beam dumps and beam catchers
Radiation damage in the carbon part of the beam dump is caused by three mechanisms:
Elastic collisions of the primary beam, fragments or neutrons with the carbon atoms
For high linear energy deposition the heating by the electronic energy loss can cause microscopic material transformation and track formation. This happens in graphite above a threshold of dE/dx = 18 keV/nm and will therefore occur only in the Bragg peak close to the end of the range
• Spallation of the nuclides and creation of other chemical elements

## Slide 3: Super-FRS Target and Beam Catcher
Beam Catchers (graphite + iron)
Production
Target (graphite)
Driver beams:
12C to 238U up to
1.5 GeV/u

## Slide 4: Super-FRS Beam Catcher
graphite
copper
linear drive
460 mm
.
graphite
Be/Cu
Courtesy H. Weick
Thermal simulation shows cooling problem with radiation damaged graphite, l = 70-40 W/(m K) --> 15 W/(m K),
Beam energy: 750 MeV/u.

## Slide 5
PHITS simulation of DPAs from elastic collision, all values stay below 1 DPA for the whole lifetime of the device even with full uranium beam intensity over 15 years with 77 days continuous operation in each year . The peak in carbon represents the end of the range near the maximum of nuclear stopping power.
Courtesy H. Weick

## Slide 6: DPA calculation for the Super-FRS graphite target
Graphite wheel cooled only by radiation
5 concentric graphite rings, 16 mm wide
thicknesses of 1, 2.5, 4, 6 and 8 g/cm2
beam parameters:
1. Slow extraction mode:
  extraction time ~1s; 1012 ions/cycle
  beam energies: 1 GeV/u.
  beam spot: two-dimensional Gaussian with σx = 1 mm and σy = 2 mm
  ions fluence per year: 1017 ions/cm2 (assuming an annual accumulation of 107 pulses )
  The temperature distribution for the worst case (1012 ions/spill, 1 GeV/u 238U on the 4 g/cm2 ring) The target layer is heated to a maximum temperature of 750 ºC
2. Fast extraction mode:
  1012 ions extracted within 50 ns

## Slide 7: DPA calculation for the Super-FRS graphite target
max DPA/source~ 4x10-19
DPA/ year ~ 4 x 10-3
H prod ~ 50 appm/year (diffuses out)
He prod ~ 5 appm/year
(high enthalpy of solution, can reach very high concentration in material - accumulates in bubbles)

## Slide 8: Radiation Damage Estimate with Neutrons
Radiation Damage and Life-time Evaluation of RBMK Graphite Stack, XA9642904,
P.A.Platonov, O.K.Chugunov, V.N.Manevsky, V.I.Karpukhin, Russian Research Center Kurchatov Institute
10
20
DPA

## Slide 9: How long will the Super-FRS graphite target last: low extraction
M.Tomut, GSI
1013 tracks/cm2 is a critical density of ion tracks:
        high values of swelling and induced stresses which are relaxed through crack formation
Fluence/puls = 1012 / A ring =1.11*1010 i/ cm2
Fluence /year = 107pulses/year x fluence/puls ~ 1017 i/cm2

## Slide 10: Heavy ion track yield at Super-FRS energies of primary beam and target temperatures
M.Tomut, GSI
Track yield is highly reduced at high ion energy and target temperature (Liu et al, PRB 64 (2001) 184115)
10-3 efficiency of track formation at Super-FRS energies
10-3 efficiency of track formation at temperatures above 800 K
(J.Liu et al./ NIM B 245 (2006) 126-129)
estimation of the track density/ year in the Super-FRS target:
10 11 tracks/cm2
750 ºC
B. Achenbach,
ANSYS workbench
1012 238U/s
4 g/cm2 C target
12 kW power
Gaussian vertical profile,
σy = 2 mm
5 steps (1 – 8 g/cm2)

## Slide 12
He implantation experiments

## Slide 13: Morphology evolution with He+ fluence
Virgin
1∙1015
1 ∙ 1016
5 ∙ 1016
1 ∙ 1017

## Slide 14: Raman spectra of graphite irradiated with 100keV He+-ions
Fluence: 1∙1015
Fluence: 1∙1016
Fluence: 5∙1016
Fluence: 1∙1017
G-peak shifts first to higher then to lower wavenumbers
Increase of D-peak to G-peak ratio followed by decrease of this ratio

## Slide 15
Ion: C, Ca, Sm, Au and U
Energy : 4.8 MeV/u
Material:
graphite 1.8 g/cm3
MoGr 2.6 g/cm3
dpa/ primary
as a function of depth
Experiments at GSI
for dpa calculations
Sample
Damage evolution with depth
197Au, 11.1 MeV/u